## Slide 1
Main Results of Instrumentation Development and Scientific Research in the Field of Condensed Matter at the IBR-2 Reactor in 2019
D.P. Kozlenko
Frank Laboratory of Neutron Physics, Joint Institute for Nuclear Research, 141980 Dubna, Russia

## Slide 2
IBR-2M Spectrometers Complex
Diffractometers:
HRFD, DN-6, RTD, DN-12, FSD, SKAT/Epsilon, FSS
Small Angle Scattering Spectrometer: YuMO
Reflectometers:
REMUR, REFLEX, GRAINS
Inelastic Neutron Scattering Spectrometers:
NERA, DIN-2PI
New Instruments:
DN-6, GRAINS, NRT, FSS
Reconstruction:
REFLEX – SESANS
2011:
11 instruments in operation
Now:
15 instruments in operation
Radiography and Tomography: NRT

## Slide 3
The priority directions of fundamental research :
Nanoscale physics
Physics and Chemistry of Functional Materials
Physics and Chemistry of
Complex Liquids and Polymers
Physics of Soft Condensed Matter

## Slide 4
The priority directions of applied research:
Structural characterization of functional
materials used in different (nano)technologies
Non-destructive control of residual
stresses and internal organization of bulk
materials and products
Texture analysis of geomaterials
and constructional materials
Stainless steel
Zr based alloy

## Slide 5
Diffractometer DN-6 for studies of microsamples under extreme conditions
DAC
Neutron diffraction patterns of Cr2O3 sample measured in DAC up to 35 GPa
90-deg. circular detector of DN-6, consisting of 96 separate 3Не counters
Sample volume: 0.01-0.05 mm3
DN-6 diffractometer
Intensity gain: 12 times (compared to DN-12)
Pressure range: 30-50 GPa
Temperature range: 4– 300 K
Neutron diffraction patterns of Cr2O3 sample measured in sapphire anvil cell up to 4.6 GPa

## Slide 6
The averaged incident neutron flux gain is ~ 6 times.
Multiplication factor compared to DN-12: 35 times
Further Development of DN-6: Installation of Neutron Parabolic Focusing Device (7 m length)
Neutron flux at sample position: 3107 n/cm2/s (with focusing device)
Resolution at d = 2 Å, 2 =900: d/d = 0.025
D-spacing range: 0.8 - 12 Å
Pressure range: 0 – 50 GPa
Temperature range: 4 – 300 K
Top level among relevant class of instruments, achievable pressure range comparable with SNAP (SNS)

## Slide 7
Upgrade of the Curved Part of the Neutron Guide
Mechanical layout
Final model
Replacement part –
curved neutron guide based on natural Ni coating mirrors (coating: m=1)
Calculations
The replacement of the curved part of the mirror neutron guide (17 m) from m = 1 to m = 3 will provide gain factor ~ 2 times for 2<<5 Å and >5 for <2 Å
Swissneutronics, completion of fabrication – first half of 2020

## Slide 8
Development of new circular detector for scattering angle 45 deg
Neutron diffraction patterns of 1mm3 La(11B)6 for 2θ region 40-48 deg.
Model of 45 degrees 96 He3+
neutron counters based ring detector
One of 16 detector modules
Test experiment setup
Dhkl range | Up to 14Å
Solid angle | Up to 0,63 sr
2θ angle range | 32°-54°
d/d | 0.025 for =2Å

## Slide 9
Magnetic and electronic properties of magnetite across the high pressure anomaly
Ferri-magnetic, TN = 850 K at 0 GPa
Post-spinel orthorhombic Bbmm
Inverse spinel cubic Fd-3m
Ferri-magnetic, TN = 420 K at 33 GPa
P
Neutron diffraction patterns of magnetite measured at ultrahigh pressures up to 35 GPa at RT
P-T phase diagram of magnetite
D.P.Kozlenko et al., Scientific Reports 9, 4464 (2019)
Magnetite Fe3O4 demonstrates pressure-induced anomalous behavior of magnetic and electronic properties in vicinity of the structural phase transition, occurring at P ~ 25-30 GPa
Synchrotron Moessbauer spectra of 57Fe-enriched magnetite measured at 33 GPa and different T
Notes: The magnetite Fe3O4, being anciently known magnetic material to human kind and remaining in leading positions for development of advanced technologies presently, demonstrates a number of puzzling physical phenomena, remaining at focus of extensive research for more than century. Recently the pressure-induced anomalous behavior of physical properties of magnetite in vicinity of the structural phase transition, occurring at P ~ 25-30 GPa, has attracted particular attention, and its nature remains unclear. Here we study the magnetic and electronic properties of magnetite across high pressure anomaly and in the pressure-induced phase by means of neutron diffraction and 57Fe synchrotron Moessbauer spectroscopy over pressure 0-40 GPa and temperature 10-290 K ranges. In the high pressure phase the long range ferrimagnetic order formation below TNP ~ 420 K was observed and spin arrangement symmetry was deduced. The structural, magnetic and electronic phase diagram of magnetite in the discussed pressure range is established.
Минерал магнетит Fe3O4 является одним из первых магнитных материалов, использующихся человечеством с древних времен, в настоящее время он также находит широкое применение в развитии современных технологий. Магнетит демонстрирует ряд необычных физических явлений, которые активно исследуются но протяжении более ста лет. Недавно было обнаружено аномальное поведение физических свойств магнетита при высоких давлениях в области структурного фазового перехода, происходящего при Р ~ 20-25 ГПа. Для выяснения природы этого явления проведено исследование магнитных и электронных свойств магнетита с помощью дифракции нейтронов и синхротронной Мессбауэровской спектроскопии на изотопе железа 57Fe в диапазоне давлений 0 – 40 ГПа и температур 10 – 300 К. В фазе высокого давления обнаружено ферримагнитное упорядочение, возникающее при температуре TNP ~ 420 K и установлена его симметрия. Определена структурная, магнитная и электронная диаграмма магнетита в исследуемом диапазоне термодинамических параметров.

## Slide 10
High Resolution Fourier Diffractometer
t0f = 15 s
I(ω, t) ~ ∫ σ(τ)·R[(τ - t), ω] dτ
0
t
New Fourier chopper and neutron guide with vertical parabolic focusing. The intensity gain factor ~2.5.

## Slide 11
The isothermal phase transitions in Fe3Ga-type compounds
A.M. Balagurov et al., Acta Cryst. B 75, 1024 (2019)
Giant magnetostriction effects
Notes: Проведены исследования изотермических фазовых переходов в функциональных сплавах F3Ga. Возможности установки ФДВР использовались максимально полно: состояния перед нагревом и после исследовались в режиме высокого разрешения. Переходы исследовались в режиме высокой интенсивности, время экспозиции в таких in situ экспериментов составляло 1 минута. Примеры дифрактограмм показаны.
Слева показаны изменения во времени интенсивностей основных (D03, 400 и L12, 200) и сверхструктурных (D03, 111 и L12, 100) дифракционных пиков в ходе быстрого нагрева и последующей изотермической выдержке при температурах 405, 435 и 470 ºС (левая шкала). Исчезновение пика (D03, 111) означает переход D03 → A2. Появление пика (L12, 100) означает переход А1 → L12. Вертикальными линиями обозначены интервалы времен, в которых структура находится в неупорядоченном состоянии. Начало шкалы времени соответствует началу подъема температуры.
Определено, что переход между D03 → L12. проходит через атомно неупорядоченные фазы сплавов.
Иллюстрация перехода показана внизу слайда.
D03 → L12 есть переход первого рода с большим (~1%) скачком атомного объема, требующим значительной перестройки кристаллической решетки. При переходах типа разупорядочения (D03 → A2) и упорядочения (A1 → L12) деформация решетки однородна и очень мала (ε ≤ 0.001), тогда как при переходе 1-го рода А2 → A1 линейные деформации различны и составляют εc ≈ 0.266, εab ≈ -0.117.

## Slide 12
Beam profiles:
analytical calculations and Monte Carlo simulation
Gauge volume of 1.8 mm
Fourier Stress Diffractometer Upgrade
Loading machine LM-20
Development of the 90-deg scintillation detector ASTRA
Development of new Fourier Chopper

## Slide 13
Pawley refinement results (sample TD): lattice parameters a and c
Diffraction patterns evolution vs. applied load
FSD: Lattice strain evolution in AZ31 magnesium alloy under applied load
Microstrain vs. applied load

## Slide 14
Installation of Fourier Stress Spectrometer (FSS) Components at 13 beamline of IBR-2
The neutron guide, Fourier chopper and detector system of the FSS spectrometer (left). The high resolution spectrum of the iron sample and resolution function (right).
The replacement of the mirror neutron guide with a new one (m = 2, linear convergence), is completed.

## Slide 15
New neutron guide (m=2) at FSS diffractometer (beamline 13)
FSS: spectra measured with old and new neutron guides
FSS: comparison of spectral distributions measured with old and new neutron guides
Resolution function of FSS at max. F-chopper speed Ωmax = 2000 rpm
FSS: new neutron guide
FSS spectrum fitted by Rietveld method
List-mode DAQ unit MPD-32

## Slide 16
Modernization of channel 10, IBR-2
GRAINS (10b)

## Slide 17
‘beam from bottom’
configuration
PEEK case
Single crystal block Si
Counter electrode
Seal groove
RE connector
WE/CE connectors
Pressing plates (Al)
Electrolyte filling
Modified neutron reflectometry cell for studies of electrochemical interfaces

## Slide 18
Studies of electrochemical interfaces for lithium ion batteries by neutron reflectometry
Neutron Reflectometry
Electrochemical measurements (deposition mass)
M.V.Avdeev, A.A.Rulev, E.E.Ushakova, Ye.N.Kosiachkin, V.I.Petrenko, I.V.Gapon, E.Yu.Kataev, V.A.Matveev, L.V.Yashina, D.M.Itkis. Appl. Surf. Sci. 486 (2019) 287
A.A.Rulev, A.V.Sergeev, L.V.Yashina, T.Jacob, D.M.Itkis, ChemElectroChem 6 (2019) 1324

## Slide 19
M.V.Avdeev, R.A.Eremin, V.I.Bodnarchuk, I.V.Gapon, V.I.Petrenko, R. Erhan, A.V. Churakov, D.P.Kozlenko, J. Surf. Investigation. (2018)
32 m
Development of new small angle scattering and imaging spectrometer at 10-A channel of IBR-2
ССD camera based detector
Beam size | 5050 мм2
Neutron wavelength range: | 0.5 – 10 Å
q-range: | 0.003 – 0.5 Å-1
Angular resolution | 5 - 20 %
Maximum sample size | 205050 мм2
Incident neutron flux at the sample | 1.0106 см-2 c-1
Detector system | PSD, 3He, 100100 см2, resolution 55 мм2
Expected parameters
T = 300 K
Before bender
(detector overload)
After bender
TOF
T = 30 K
Before bender
(strong detector overload)
After bender
TOF
Beamline 10A
Beam splitter – completed, installed, 2019, (Mirrotron)
Bender – completed, 2017 (Mirrotron)
Neutron transport system - to be completed and installed in 2020 (Mirrotron)
Detector vacuum tube – fabrication in progress, completion in 2021 (Mirrotron)
PSD detector – conclusion of the contract is planned in 2020

## Slide 20: Isotope Identifying Reflectometry at REMUR spectrometer: Created the channels of secondary radiation: spin-flipped neutrons, charged particles and gamma-quants

## Slide 21
Spin rotator coil upgrade
Cooling system development
SESANS Instrument Development at 9 channel of IBR-2
Testing the experimental concept

## Slide 22
YuMO Small Angle Scattering Spectrometer
1 – two reflectors;
2 – zone of reactor with moderator;
3 – chopper;
4 – first collimator;
5 – vacuum tube;
6 – second collimator;
7 – thermostate;
8 – samples table;
9 – goniometer;
10-11 – Vn-standard;
12 – ring-wire detector;
13 – position-sensitve edetector "Volga";
14 – direct beam detector.
L1 =17.8 m, L2 =13.2 m
Neutron flux at sample position: 4107 n/cm2/s
Q-range: 710-3 - 0.5 Å-1
Q-resolution: 5-20 %
Typical measurement time: 10 m
Unique dynamic Q-range Qmax/Qmin ~ 90
Fast measurements
Development of new incident beam collimator, modernization of detector system, sample environment

## Slide 23
Structural organization of the iron oxide nanoparticles in SBA-15 nanoporous silica
A.Zeleňáková, et al., Scientific Reports 9, 1 (2019)
SANS curve and structural organization modeling

## Slide 24
Development of the neutron guide system of the NERA spectrometer
Elements of the supermirror neutron guide with vertical focusing (m = 5)
Spectral distribution of the incident neutron beam at the sample position measured with the vanadium sample
The end part sections of the mirror neutron guide (m = 1) at the NERA spectrometer of 25 m length have been replaced by the supermirror sections ( m = 5) with vertical focusing, fabricated by SwissNeutronics. The average gain factor of 1.5 times has been achieved.

## Slide 25
Spectrometer for Neutron Radiography and Tomography
Upgrade of the Two Mirror CCD-based detector

## Slide 26
Neutron imaging and diffraction study of Chelyabinsk meteorite
S.E.Kichanov, D.P.Kozlenko et al., Springer Nature Applied Sciences (2019)
Photo of the studied meteorite fragment
Neutron diffraction pattern of the fragment, analyzed by the profile matching method
Parts of the 3D model of structural organization of the studied fragment, obtained by neutron tomography. The pink regions correspond to metallic inclusions

## Slide 27
Thank You for Your Attention!