## Slide 1
TEM examination of ceramics irradiated with heavy ions of fission fragment energies
V.A. Skuratov
Flerov Laboratory of Nuclear Reactions, Joint Institute for Nuclear Research, Dubna, Russia

## Slide 2
Collaborators:
Centre for HRTEM, Nelson Mandela University
Port Elizabeth, South Africa
Eurasian National University
Institute of Nuclear Physics
Nur-Sultan, Kazakhstan
Belarusian State University, Minsk, Belarus

## Slide 3
The overall intention of this work is to yield sufficient basic data to determine and compare the radiation tolerance of ceramics against against swift heavy ion (SHI) irradiation simulating fission fragment impact.
Examination of the dense ionization effect in ceramics and oxides irradiated with heavy ions of fission fragments energy:
Evaluation of latent track parameters in Al2O3, Si3N4, YAP, YAG as function of electron stopping power and irradiation temperature;
Structural consequences of latent track interference in Al2O3 and Si3N4;
Surface effects of dense ionization in dielectrics and surface nanoscale radiation damage formation.
Transmission electron microscopy (TEM) is the only direct experimental technique for observation of SHI-induced latent tracks in solids

## Slide 4
167 MeV xenon ion induced tracks in Al2O3
Al2O3
V.A.Skuratov et al., Nucl. Instr. Meth.B 327 (2014) 89

## Slide 5
- Al
- O
Y
Z
X
Y
Z
X
~1.8 nm
9.8 nm
TEM and MD simulated 167 MeV Xenon ion induced tracks in Al2O3
R. A. Rymzhanov et al. J. Phys. D. 50 (2017) 475301

## Slide 6
167 MeV Xenon ion induced tracks in Al2O3
J. H. O’Connell et al., Nucl. Instr. Meth.B 374 (2016) 97

## Slide 7
J. H. O’Connell et al., Nucl. Instr. Meth.B 374 (2016) 97
  The number of ion tracks saturates at fluence of ~ 1.1 x 1012 cm-2
167 MeV Xenon ion induced tracks in Al2O3

## Slide 8
Passage of a second ion causes annealing of defects created by the first one
Passage of the ion at longer distances from older tracks causes partial annealing of the defects
Effective radius of recovery is ~6.5 nm (experimental ~5.4 nm) and corresponds to track density of ~2.7×1012 см-2
6.5 nm
Overlapping SHI tracks
Xe 167 MeV
R.A. Rymzhanov et al.,
Nucl.Instr.Meth. B 435 (2018) 121

## Slide 9
  TEM insets
MgO - only point defects were created around the ion trajectory
Al2O3 - crystalline discontinuous track with the diameter about 2 nm
YAG - continuous amorphous track of ~6.5 nm in diameter
Recrystallization during track formation propcess

## Slide 10
Track size in YAG vs electronic stopping power
39.7 keV/nm
23.0 keV/nm
17.0 keV/nm
11.5 keV/nm
Y3Al5O12

## Slide 11: p-Si3N4 + Xe 220 МэВ
5x1011 см-2
1x1013 см-2
2x1014 см-2

## Slide 12
Si3N4 +Bi, 700 MeV
Amorphous tracks in crystalline matrix
Amorphous tracks in amorphous matrix
Ion fluence for latent track overlapping Фoverlap. ×πR2 = 1cm2
R=1.65 nm Фoverlap. = 1.2×1013 cm2

## Slide 13: a-Si3N4 и n-Si3N4 + Bi 710 МэВ
n-Si3N4
a-Si3N4

## Slide 14: a-Si3N4 + Bi 710 МэВ, 5x1010 см-2
х, нм
Radial density of Si3N4

## Slide 15
3D AFM image of of MgAl2O4 surface irradiated with 710 MeV Bi ions.
Ion fluence 5x1010 cm-2.
Surface effects of dense ionization in ceramics and oxides

## Slide 16
Surface effects of dense ionization in ceramics and oxides
167 MeV Xenon ion induced hillocks and latent tracks in TiO2

## Slide 17
Xe (167 MeV)+TiO2

## Slide 18
Surface effects of dense ionization in ceramics and oxides
Xe (220 MeV) + TiO2: Hillock size vs irradiation temperature

## Slide 19
Al2O3
Y3Al5O12
ZrO2:Y
Surface effects of dense ionization in ceramics and oxides

## Slide 20
Amorphous hillocks in YAG
Bi 700 MeV ion
YAG demonstrates almost no damage recovery:
amorphous cylindrical track and amorphous hillock
R.A. Rymzhanov et al., J.App.Phys. 2020, 127(1) 015901

## Slide 21
Summary
Latent track formation processes are governed by recrystallization of ion track region
Final defect structure of swift heavy ion irradiated ceramics is defined by interference of isolated latent track regions

## Slide 22
Thank you for your attention!