## Slide 1
Study of the scintillation properties of pure and yttrium-doped BaF2 crystals
Ilya Vasilyev, Yuri Davydov, Vladimir Baranov
Dzhelepov Laboratory of Nuclear Problems, JINR, Dubna
The XXIV International Scientific Conference of Young Scientists and Specialists
(AYSS-2020)
November 9-13, 2020

## Slide 2
What is Mu2e?
A search for neutrino less conversion of a muon into an electron in the field of a nucleus Charged-Lepton Flavor Violation via
Will use current Fermilab accelerator complex to reach a sensitivity 10 000 better than current world’s best
Introduction
2
The 0.5 ns scintillation in BaF2 promises a ultrafast crystal calorimeter to face the challenge of high event rate expected by Mu2e-II
 | CsI | BaF2
Density (g/cm3 ) | 4,51 | 4,89
Radiation length (cm) | 1,86 | 2,03
Z value | 54 | 51,6
dE/dX (MeV/cm) | 5,56 | 6,52
Emission peak (nm) | 310 | 300 (slow) 220 (fast)
Refractive index | 1,95 | 1,5
Decay time (ns) | 30(slow) 6(fast) | 650(slow) 0,5(fast)
Undoped CsI crystal used for the Mu2e calorimeter has a fast scintillation at 310 nm with 30 ns decay time and survives an ionization dose up to 100 krad.
BaF2 crystal has an ultrafast scintillation at 220 nm with 0,5 ns decay time and a similar intensity as CsI, and may survive 100 Mrad. Its slow scintillation at 300 nm with 650 ns decay time, however, causes pileup in a high rate environment.
m- N  e- N

## Slide 3: Approaches to solve the problem of the BaF2 slow component
1) Develop a SiPM that is sensitive only to the fast component
D. Hitlin et al. An APD for the Detection of the Fast Scintillation Component of BaF2, IEEE Trans.Nucl.Sci 63(2016) no. 2, p.513.
2) Use of a thin multilayer filter on the quartz glass substrate between the crystal and the photodetector to suppress luminescence in the range 250-400 nm
A.M. Artikov et al., Suppression of the slow component of BaF2 crystal luminescence with a thin multilayer filter, J.Phys.Conf.Ser. 1162(2019) 1, 012028. DOI: 10.1088/1742-6596/1162/1/012028
3) Use of a solar-blind photomultiplier with an aluminum-gallium nitride (AlGaN) photocathode
N. Atanov et al., A Photomultiplier With an AlGaN Photocathode and Microchannel Plates for BaF2 Scintillator Detectors in Particle Physics, IEEE Trans.Nucl.Sci 67(2020) no. 7, p.1760.
4) Suppress the BaF2 slow component by Y doping
J. Chen et al., Slow Scintillation Suppression in Yttrium Doped BaF2 Crystals, IEEE TNS 65(2018), no. 8, p. 2147.

## Slide 4
Crystal samples
4
We have samples from both SICCAS and BGRI (China):
BaF2 pure crystal, 10x10x10 mm
BaF2 crystal doped with Y (1at.%), 10x10x10 mm
BaF2 crystal doped with Y (3at.%), 10x10x10 mm
BaF2 crystal doped with Y (5at.%), 10x10x10 mm
and
BaF2 pure crystal, 30x30x200 mm
BaF2 crystal doped with Y (3at.%), 30x30x200 mm
We also expect to receive more samples from Incrom (Russia)

## Slide 5
Irradiation facility at IBR-2M
5
Crystal samples were irradiated at the irradiation facility of the IBR-2M pulsed reactor at the Frank Laboratory of Neutron Physics, JINR (Dubna, Russia).
Typical reactor run continues 12-14 days. The reactor operates with a pulse frequency of 5 Hz with 200-300 microseconds pulse duration.
Thermal neutron flux density immediately after the water moderator is ~1016 n/cm2∙s per pulse or ~1013 n/cm2∙s on average over time. For 2 weeks of operation, it is possible to obtain a neutron fluence from ~1011 n/cm2 on the end of channel #3 up to ~1018 n/cm2 next to the water moderator.
4 samples from SICCAS of 10x10x10mm were taken: pure BaF2, BaF2:Y(1 at.%), BaF2:Y (3 at.%) and BaF2:Y (5 at.%)
The samples were placed about 5 m from the water moderator. A nickel wire placed along with the samples was used to measure the fluence of the fast neutrons.
During the irradiation run, ~2.3×1014 n/cm2 (E>1MeV) were passed through the samples

## Slide 6: Transmittance measurements
The transmittance of the samples was measured before irradiation and 4 month later after irradiation using the SHIMADZU SolidSpec-3700 DUV spectrophotometer

## Slide 7
Light output measurements
7
Light outputs were measured by a Hamamatsu R2059 PMT with 22Na gamma source with a coincidence trigger (E=511 keV)
Samples were wrapped with Teflon tape (2x100 micron)
No optical grease was used between samples and PMT
The total signal was integrated within 2 microseconds, while the fast component was taken within first 20 ns and the slow component – after 20 ns
The calibration was performed using a single-photoelectron peak from PMT

## Slide 8: Results and discussion
Total spectra (0-2μs)
Slow component (20ns-2μs)
Fast component (0-20ns)
 | Y doping | 0% | 1at.% | 3at.% | 5at.%
Before irradiation | Total | 583±28 | 205±19 | 129±15 | 122±14
 | Slow | 526±27 | 146±16 | 71±12 | 67±11
 | Fast | 57±10 | 57±10 | 56±9 | 53±9
After irradiation | Total | 543±28 | 175±16 | 109±13 | 105±13
 | Slow | 490±26 | 125±14 | 60±11 | 58±10
 | Fast | 53±9 | 48±9 | 47±9 | 44±9
Light output (ph.e./MeV)
Light output (ph.e./MeV)

## Slide 9
Results and discussion
9
Light output loss after irradiation (%)
The light output loss after neutron irradiation is more than twice as high for yttrium doped samples as compared to the pure BaF2 sample
Y doping | 0% (pure) | 1at.% | 3at.% | 5at.%
Fast | 7.6% | 16.1% | 16.8% | 16.3%
Slow | 6.8% | 14.4% | 15.5% | 13.4%
Total | 6.9% | 14.7% | 15.3% | 14.0%

## Slide 10
Conclusion
10
Light outputs of a pure BaF2 crystal and three samples doped with yttrium in a proportion of 1at.%, 3at.% and 5at.% were measured before and after irradiation in a neutron beam.
The light output losses after neutron irradiation are almost two times higher for the yttrium doped samples compared to the losses in the pure BaF2 sample
The light output loss of the fast component after neutron irradiation is higher compared with the slow component on all samples
Obviously, more study is required in a wider range of radiation doses.

## Slide 11
Acknowledgments
This work was partially supported by a grant from the Russian Foundation for Basic Research No. 18-52-05021
The authors are grateful to the IBR-2M staff of the Frank Laboratory of Neutron Physics for their help in irradiating the samples
11

## Slide 12: Thank you for your attention!