## Slide 1: Swift Heavy Ion Irradiation-Induced Changes in Mechanical Properties of Si3N4
2020
The XXIV International Scientific Conference of Young Scientists and Specialists
A.D. Ibrayeva, E. Korneeva, J. Arno Vuuren, L.Kurpaska, M. Clozel, N.Kirilkin, V.A. Skuratov, J.Neethling, M.V. Zdorovets

## Slide 2: Si3N4 as a candidate material for inert matrices
The small absorption cross section for thermal neutrons
The resistance at irradiation with neutrons, α particles, and fission fragments.
Good thermal properties
Si3N4 is the ONLY nitride ceramic where latent tracks have been registered

## Slide 3
There is almost no data about Si3N4 mechanical characteristics changes induced by swift heavy ion irradiation despite the actuality for its use inert matrix fuel hosts.
Change in microhardness of Si3N4 depending on the fluence of 0.5 MeV Si+ ions. Circles correspond to T = 450 K, triangles-T=100 K
[Bolse W., Peteves S.D. (1992). NIM B 68(1-4), 331-341]

## Slide 4: The purpose of the work
is to study the radiation-induced changes in mechanical properties of Si3N4 under the irradiation with swift heavy ions

## Slide 5: Experimental
Incident ion | Energy, MeV | Fluence, cm-2
Ar | 46 | 4×1013
Kr | 107 | 2×1013, 3×1013, 1×1014, 2×1014
Xe | 167 | 5×1012, 1×1013, 5×1013, 5×1014
 | 220 | 6×1011, 1×1013, 2×1014
Bi | 710 | 1×1012, 5×1012, 1×1013, 2×1013
All samples were irradiated at accelerators in FLNR JINR (Dubna, Russia) and Institute of Nuclear Physics (Nur-Sultan, Kazakhstan)
TEM research was conducted in HR TEM Center of Nelson Mandela University (Port-Elizabeth, South Africa)
Mechanical hardness was measured in National Center for Nuclear Research (Sverk, Poland) and Nazarbayev University (Nur-Sultan, Kazakhstan).

## Slide 6: TEM images and SAD of p-Si3N4+220 MeV Xe
5x1011 cm-2
1x1013 cm-2
2x1014 cm-2

## Slide 7: TEM images of p-Si3N4+710 MeV Bi
Fluence, cm-2
Crystalline matrix
Matrix amorphizied under irradiation

## Slide 8
Nanoindentation curves of p-Si3N4

## Slide 9
Nanoindentation curves of p-Si3N4

## Slide 10
Dependence of relative nanohardness of ion-irradiated p-Si3N4 on fluence

## Slide 11
Maximal studied fluencies of Xe and Bi lead to a decrease in the material hardness by ~23 % and ~15%, respectively. However, at slightly lower fluence values of 1×1013 cm-2 for 167 MeV Xe and 5×1012 cm-2 for 710 MeV Bi, the sample hardness growth by ~23-25% is observed.
The hardness of initial samples was 23±2.3 GPa, which corresponds to the literature data for a given load value. The hardness of the irradiated p-Si3N4 is close to the value of the hardness for the unirradiated ones, which is observed up to a fluence of 1 × 1014 cm-2. For a sample irradiated with a fluence of 2×1014 cm-2, the hardness decreases by 15% compared to the initial sample, and is equal to 17.1±3 GPa
Nanohardness of ion-irradiated p-Si3N4 vs fluence

## Slide 12: Conclusion
The dependence of the radiation-stimulated change in the mechanical properties of silicon nitride on the fluence of high-energy ions of krypton, xenon, and bismuth has been studied by the nanoindentation method. It was found that irradiation to fluences corresponding to radiation damage doses of ~3×10-3 dpa leads to a decrease in material hardness by ~20%.
Hardening was observed for all other SHI-irradiated samples up to a critical fluence which is related to the onset of complete amorphisation, which then results in a decrease in the hardness.
The obtained values of radiation-stimulated changes in material hardness and their non-monotonic character are consistent with the literature data (devoted to silicon nitride irradiated with Si ions with energies of 0.5–1 MeV). Based on both these results it could be suggested that amorphization of the material plays a significant role in changing the mechanical characteristics of nitride ceramics under the irradiation conditions

## Slide 13: Thank you for your attention!