## Slide 1: POLARIZED NEUTRON REFLECTOMETRY WITH SECONDARY RADIATION REGISTRATION
Zhaketov Vladimir
Participants of work: V.D. Zhaketov, A.V. Petrenko, Yu.M. Gledenov, Yu.N. Kopach A.N. Gundorin, Yu.V. Nikitenko, V.L. Aksenov
Frank Laboratory of Neutron Physics
Joint Institute for Nuclear Research, Dubna, Russia
The XXIV International Scientific Conference of Young Scientists and Specialists (AYSS-2020), 9-13 November 2020

## Slide 2
Spin-triplet superconductivity,
including of a long-range proximity
2. Inverse proximity effect 
magnetization of superconductor
3. Cryptoferromagnetic state in ferromagnet 
antiferr. ordered domains with size 1-100 nm
4. Paramagnetic Meissner effect -
- Positive magnetic moment at cooling in magnetic field
5. Spontaneous vortex phase
at zero external field in superconducting ferromagnetic
Motivation
Proximity effects at the superconducting / ferromagnetic
heterostructures
1/16
S/F system
Spin-triplet pairing
Inverse proximity effect

## Slide 3
Motivation
Diffusion of elements at interface
2/16
Ta(20nm)
V(150nm)
Fe0.7V0.3(1nm)
V(1.2nm)
Nb(150nm)
Si(0.5mm)
Fe0.7V0.3(1nm)
Nb(70nm)
Ni(65%)Cu(35%)(4nm)
Substrate (Si, 1 mm)
9 month after manufacturing
15 month after manufacturing
Cu→Nb
2 layers

## Slide 4
Task 2
Correspondence of magnetic profile to element profile
Task 1
Definition at interface the spatial profiles of elements
Motivation
Tasks to the experimental method
3/16
To determine magnetic profile – only polarized neutron reflectometry (PNR)
Use different methods for spatial profile:
  poor fit and correspondence of experimental data
  samples change
  disadvantages of the other methods
Question: how improve PNR to get spatial profile of separate element or its isotope ?

## Slide 5
Conventional neutron reflectometry
4/16
At interface of two and more isotopes:
i – isotope
j – type of secondary radiation
Geometry of experiment
Initial beam

## Slide 6
1 – interface vacuum/Al
2 – structure vacuum/(Al+10B)(1nm)//Al
3 – structure vacuum/Al(20nm)/(Al+10B)(1nm)//Al
Yu.V.Nikitenko et al. Isotope-Identifying Neutron Reflectometry
// Crystallography reports, 2017, vol.60, No.4, pp. 466-479
Neutron reflectometry gives information only about integral distribution of the coherence length density for all elements and their isotopes.
In the case of low absorption in the system (several % or less), classical reflectometry does not allow determining the neutron absorption coefficient
Absorption coefficient
for 2 and 3 cases
Neutron reflectometry disadvantages
5/16

## Slide 7
charged particles (n, α); (n, t); (n, p)
gamma quanta (n, γ)
fission fragments (n, f)
coherent spin-flip neutrons because of passage through magnetically non-collinear medium
incoherently scattered neutrons on atomic nuclei
inelastically scattered neutrons by atoms and the medium
diffusely scattered neutrons at interfaces and inhomogeneities in the structure layers
Secondary radiation
6/16
Initial beam

## Slide 8
Standing wave mode
7/16
Total reflection
Standing waves
Enhanced standing waves
Secondary radiation
i – isotope
j – type of secondary radiation
6

## Slide 9: Interface profile through absorption through secondary radiation
Model calculations
8/16

## Slide 10
Measurements scheme
1 – ionization chamber
2 – goniometer
Perspective: possibility for detection of charged particles with simultaneous application of magnetic field
Charged particle detection channel at the REMUR
9/16

## Slide 11
Charged particles 2d-map
1 – tritons
2 – alpha-particles
Atmosphere of Ar + 3% CO2 at pressure 1.5 bar – effective for triton registration with energy 2.73 MeV.
Charged particle detection channel at the REMUR
10/16
Normed spectra
Secondary radiation coefficient
Substrate (Si)
Substrate (Si)
V (5nm)
6LiF (5nm)
CoFe (5nm)
V (20nm)
V (15nm)
V (10nm)
6LiF (5nm)
CoFe (5nm)
Sample №1
Sample №2
Substrate (Si)
Substrate (Si)
6LiF (5nm)
CoFe (5nm)
6LiF (5nm)
CoFe (5nm)
Cu (10nm)
Cu (10nm)
V (65nm)
V (5nm)
V (15nm)
V (55nm)
Sample №3
Sample №4
Sample №4
1 - sample №1
2 - sample №2
1 - sample №3
2 - sample №4
1 - neutron reflectivity
2 - secondary radiation

## Slide 12
Spin-flipper
Wide-aperture analyzer
polarization
Electromagnet
Background protection for PSD-detector and polarization analyzer
Polarizer:
Spin-flippers: radio-frequent with steady gradient magnetic field
Polarization analyzer: focused multichannel with 125 m2-supermirrors and cross-section 20cm·20cm (5 m from sample position)
Polarized neutrons detection channel at the REMUR
11/16
)

## Slide 13
Substrate (Si)
Substrate (Si)
V (5nm)
6LiF (5nm)
CoFe (5nm)
V (20nm)
V (15nm)
V (10nm)
6LiF (5nm)
CoFe (5nm)
Sample №1
Sample №2
1, 2 – absorption
3, 4 – spin-flip
12/16
Polarized neutrons detection channel at the REMUR
Sample 1

## Slide 14
REMUR
Gamma-detector
Gamma detector and sample position
Anti-compton detector scattering
Gamma detector and sample position
13/16
Gamma quanta registration channel at the REMUR

## Slide 15
Standing waves mode
Gamma quanta spectra
Enhanced standing waves mode
Angle dependence
SNMS data
14/16
Gamma quanta registration channel at the REMUR

## Slide 16
Channel of gamma quanta: min = 0.3 barn
  0.3 barn (  100 isotopes ):
Cl, 36Ar, 39K, 43Ca, 45Sc, Ti, V(5.4K), Cr, 53,55Mn, Fe, 59Co, Ni, Cu, 67Zn, 75As, Se, Br, Kr, 87Sr, Mo(0.915 K), 99Tc(7.8 K), Ru, 103Rh, La(4.9 ,6.0 K), Pd, Nb (9.25K), Ag, Cd(0.52K), Dy, Gd, Tb, Ho, Er, Tm, In(3.41K), Sn(3.72K), Re(1.7K), Ta(4.47K), Os,192,195Pt, 197Au, Hg, 226Ra,227Ac, 228-230Th(1.4K), 231Pa(1.4K), W(1.5K), Re, Os(0.66K), 192,195Pt, 197Au, Hg(4.15, 3.95K), 203,204Tl, 207Pb(7.2K), 226Ra, 227Ac, 228-230Th, 231Pa, 231-235U, 203,204Tl(2.38K), 237Np, 238-242Pu, 241-243Am, 243-245,247Cm, 249-252Cf
Estimation of element minimal cross-section from a measurement time
15/16
Channel of charged particles: min = 0.025 barn
  0.025 barn (22 isotopes):
3He, 6Li, 7Be, 10B, 14N, 17O, 21Ne, 22Na, 26Al(1.18K), 33S, 35Cl, 36Cl, 37Ar, 40K, 41Ca, 59Ni, 65Zn(0.85K), 76Br, 84Rb, 109Cd(0.52K), 203Tl, 143Nd, 149Sm
Red color – Superconductor elements, Green – Magnetic
Channel of polarized neutrons
For magnetic layer of 5 nm thickness minimal perpendicular component magnetization is of order 1 Gs
Fe, Co, Ni, Gd, Dy, Tb, Ho, Er, Tm, (9 elements )

## Slide 17
Simultaneous registration of reflected (refracted) neutrons and secondary radiation allows to define the spatial profiles of isotopes
Further improvements are connected with possible decreasing of background (5÷10 times), increasing of neuron intensity (5÷10 times) and increasing of detector solid angle for gamma channel (4 times)  1 mbarn at 5 nm layer thickness or  1 Å layer thickness at =50 mbarn
With supermirror reflector in SW regime can be achieved spatial resolution 1 Å
Realization of modes: cryostat + gamma-detection, electromagnet + gamma-detection, electromagnet + charged particles
Further application of the method
Conclusion
16/16

## Slide 18
Thank you for your attention !