## Slide 1
Spectroscopic Analysis of P2O5–ZnO–Na2O Doped Glass
The XXIV International Scientific Conference of Young Scientists and Specialists
(AYSS-2020)
Shymaa Moslem
MTI – University
In collaboration with
Cairo University
Egypt
Research Group members
Prof. Hussam Hassan – Dr. Yehia El-bashar- Dr. Diaa Al-rayan

## Slide 2: Contents
1
Introduction
2
Experimental Technique
3
Results and Discussions
4
Conclusion
NiO
Concentration

## Slide 3
Physical States of Matter
Solids can be classified into two main groups according to their atomic arrangement:
Crystalline solids
Amorphous solids
The glassy state
Glass is an amorphous (non-crystalline) solid material. Usually produced when a suitably viscous molten material cools very rapidly thereby not giving enough time for regular crystal lattice to form.
The XXIV International Scientific Conference of Young Scientists and Specialists
(AYSS-2020)

## Slide 4
Experimental Technique
The XXIV International Scientific Conference of Young Scientists and Specialists
(AYSS-2020)

## Slide 5
Each composition was taken in an open porcelain crucible and melted in an electric furnace.
Temp. rang 1000 °C for 1 hour.
Finally, the melted samples are then quickly quenched by infuse them on a stainless-steel plate and cover them with another one plate. This casting happens in a heated furnace at 250 oC.
We let the samples inside it for 2 hours, then the furnace is turn off. The glass samples are allowed to cool down inside the furnace for 24 hours.
The mixture of chemicals is well-grounded after carefully weighted the calculated ratios.
The XXIV International Scientific Conference of Young Scientists and Specialists
(AYSS-2020)
Preparation of the Samples
melt-quenching technique

## Slide 6
The glass system under investigation has the general formula:
42P2O5– 40ZnO–(18-x) Na2O–xNiO
with X=1, 2, 3, 4, 5 and 6 mol. %
P2O5 : Good Glass Former.
ZnO: Residual Stresses.
Transparence.
Na2O : Melting Point.
NiO : optical filtering element.
The XXIV International Scientific Conference of Young Scientists and Specialists
(AYSS-2020)
Glass System & prepared samples
NiO= 1 mol.%
NiO= 2 mol.%
NiO= 3 mol.%
NiO= 4 mol.%
NiO= 5 mol.%
NiO= 6 mol.%

## Slide 7
Results
&
Discussions
The XXIV International Scientific Conference of Young Scientists and Specialists
(AYSS-2020)

## Slide 8
The XXIV International Scientific Conference of Young Scientists and Specialists
(AYSS-2020)
XRD spectra doesn’t exhibit any sharp peak.
This pattern confirms the amorphous structure of prepared glass .
X-ray diffraction
Phosphorus, Sulfur, and Silicon and the Related Elements, Y.H. Elbashar, S.S. Moslem, et. al.
DOI: https://doi.org/10.1080/10426507.2020.1800703

## Slide 9
Physical property | NiO=1 mol.% | NiO=2 mol.% | NiO=3 mol.% | NiO=4 mol.% | NiO=5 mol.% | NiO=6 mol.%
Density (gm/cm3) | 3.029 | 3.073 | 3.062 | 3.096 | 3.098 | 3.160
Molar Volume (cm3/mol) | 34.154 | 33.702 | 33.865 | 33.536 | 33.562 | 32.937
(Å) | 3.842 | 3.036 | 2.656 | 2.406 | 2.234 | 2.089
(Å) | 1.548 | 1.223 | 1.070 | 0.969 | 0.900 | 0.843
Physical property | NiO=1 mol.% | NiO=2 mol.% | NiO=3 mol.% | NiO=4 mol.% | NiO=5 mol.% | NiO=6 mol.%
Density (gm/cm3) | 3.029 | 3.073 | 3.062 | 3.096 | 3.098 | 3.160
Molar Volume (cm3/mol) | 34.154 | 33.702 | 33.865 | 33.536 | 33.562 | 32.937
 | 3.842 | 3.036 | 2.656 | 2.406 | 2.234 | 2.089
 | 1.548 | 1.223 | 1.070 | 0.969 | 0.900 | 0.843
Physical Parameters of the Nickel Doped Zinc Sodium Phosphate Glasses
The XXIV International Scientific Conference of Young Scientists and Specialists
(AYSS-2020)
        The density increased due to substitution of light sodium ions by heavier nickel ions.
        The molar volume increased, expected that the glass structure become more compact.
Phosphorus, Sulfur, and Silicon and the Related Elements, Y.H. Elbashar, S.S. Moslem, et. al.
DOI: https://doi.org/10.1080/10426507.2020.1800703
Inter-ionic distance (ri), polaron radius (rp) decreases, suggests that the reduction in free space inside glass network.

## Slide 10
The XXIV International Scientific Conference of Young Scientists and Specialists
(AYSS-2020)
Fourier transform Infrared (FTIR)
        The deconvolution of the FTIR absorption spectrum of the sample containing 6 mol.% of NiO.
        FTIR absorbance spectra.
Phosphorus, Sulfur, and Silicon and the Related Elements, Y.H. Elbashar, S.S. Moslem, et. al.
DOI: https://doi.org/10.1080/10426507.2020.1800703

## Slide 11
Wavenumber (cm-1) | Assignment
1474-2000 | bending vibrations of water bonds (H2O) .
1256-1338 | asymmetric stretching vibration of the PO2− or (P=O) groups (Q2 ).
1110-1156 | asymmetric stretch of the PO2 or (O-P-O) groups (Q1 ).
915-1036 | asymmetric stretching vibrational mode of groups.
633-762 | symmetric stretching vibrations P-O-P or (P2O).
≈544 | stretching vibrations of Zn–O.
423-496 | stretching vibrations of octahedral NiO6 group in Ni–O–Ni bond .
Wavenumber (cm-1) | Assignment
1474-2000 | bending vibrations of water bonds (H2O) .
1256-1338 | asymmetric stretching vibration of the PO2− or (P=O) groups (Q2 ).
1110-1156 | asymmetric stretch of the PO2 or (O-P-O) groups (Q1 ).
915-1036 | 
633-762 | symmetric stretching vibrations P-O-P or (P2O).
≈544 | stretching vibrations of Zn–O.
423-496 | stretching vibrations of octahedral NiO6 group in Ni–O–Ni bond .
The XXIV International Scientific Conference of Young Scientists and Specialists
(AYSS-2020)
Summary of FTIR Spectral Band Positions of the Investigated Glasses.

## Slide 12
Transitions Band positions (nm) |  |  |  |  |  | 
(Octahedral transitions) | NiO=1mol.% | NiO=2mol.% | NiO=3mol.% | NiO=4mol.% | NiO=5mol.% | NiO=6mol.%
3A2g(F) 3T1g(P) | 444 | 438 | 438 | 438 | 416 | 428
3A2g (F) 1T2g(D) | - | - | - | - | - | 452
3A2g(F)3T1g(F) | 818 | 816 | 814 | 800 | 800 | 800
3A2g(F)3T2g(F) | 1358 | 1356 | 1360 | 1360 | 1366 | 1366
(Tetrahedral transitions) |  |  |  |  |  | 
3T1(F)3T1(P) | - | - | 682 | 682 | 682 | 684
Transitions Band positions (nm) |  |  |  |  |  | 
(Octahedral transitions) | NiO=1mol.% | NiO=2mol.% | NiO=3mol.% | NiO=4mol.% | NiO=5mol.% | NiO=6mol.%
 | 444 | 438 | 438 | 438 | 416 | 428
 | - | - | - | - | - | 452
 | 818 | 816 | 814 | 800 | 800 | 800
 | 1358 | 1356 | 1360 | 1360 | 1366 | 1366
(Tetrahedral transitions) |  |  |  |  |  | 
 | - | - | 682 | 682 | 682 | 684
Assignment of the observed optical absorption bands in the studied glasses.
The XXIV International Scientific Conference of Young Scientists and Specialists
(AYSS-2020)
Optical Absorbance Spectra

## Slide 13
The XXIV International Scientific Conference of Young Scientists and Specialists
(AYSS-2020)
Energy Gap Eg and Urbach Energy ΔE of the Studied Samples.
NiO mol. % | Eg (eV) | ∆E (eV)
1 | 4.87 | 0.36
2 | 4.68 | 0.37
3 | 4.19 | 0.63
4 | 3.88 | 0.68
5 | 3.74 | 0.98
6 | 3.65 | 1.25
Phosphorus, Sulfur, and Silicon and the Related Elements, Y.H. Elbashar, S.S. Moslem, et. al.
DOI: https://doi.org/10.1080/10426507.2020.1800703

## Slide 14
NiO mol. % | Λth | (Å3)
1 | 0.54 | 1.48
2 | 0.55 | 1.49
3 | 0.56 | 1.5
4 | 0.57 | 1.52
5 | 0.58 | 1.53
6 | 0.59 | 1.54
NiO mol. % | Λth | 
1 | 0.54 | 1.48
2 | 0.55 | 1.49
3 | 0.56 | 1.5
4 | 0.57 | 1.52
5 | 0.58 | 1.53
6 | 0.59 | 1.54
The values of theoretical optical basicity (Λth) and oxide ions polarizability ().
The XXIV International Scientific Conference of Young Scientists and Specialists
(AYSS-2020)
        The values of Λth and increase with the increase of NiO concentration.
        This means that, the prepared glass are more base and the bond between Ni2+ ions and ligands is ionic bond.
This ionic property supports the production of the NBO in the glass network.
Phosphorus, Sulfur, and Silicon and the Related Elements, Y.H. Elbashar, S.S. Moslem, et. al.
DOI: https://doi.org/10.1080/10426507.2020.1800703

## Slide 15
It is observed that the density (ρ) increases and the molar volume (M.V) decreases with increasing NiO content. This result mean the glass network becomes more compact.
FTIR spectra shows that the network structure is based mainly on Q1 and Q2 units. This refers to the increase in the amount of NBO and disorder of glass network due to presence of nickel ions as a modifier.
The optical band gap energy (Eg) decreases with increasing of NiO content. This may be attributed to the formation of non-bridging oxygen (NBO).
The theoretical calculation of optical polarizability (α02-) and the optical basicity (Λ) enhancing the ionic bond forming between Ni2+ ions and ligands. This is in agreement with the experimental results.
conclusion
The XXIV International Scientific Conference of Young Scientists and Specialists
(AYSS-2020)

## Slide 16
The XXIV International Scientific Conference of Young Scientists and Specialists
(AYSS-2020)
References
Limkitjaroenporn, P.; Kaewkhao, J.; Limsuwan, P.; Chewpraditkul, W. Physical, Optical, Structural and Gamma-Ray Shielding Properties of Lead Sodium Borate Glasses. J. Phys. Chem. Solids. 2011, 72, 245-251.
Çelikbilek, M.; Ersundu, A.E.; Aydin, S. Preparation and Characterization of TeO2–WO3–Li2O Glasses. J. Non-Cryst. Solids. 2013, 378, 247-253.
Gedam, R.S.; Ramteke, D.D. Electrical, Dielectric and Optical Properties of La2O3 Doped Lithium Borate Glasses. J. Phys. Chem. Solids. 2013, 74, 1039–1044.
Rao, P.V.; Satyanarayana, T.; Reddy, M.S.; Gandhi, Y.; Veeraiah, N. Nickel Ion as a Structure Probe in PbO-Bi2O3-B2O3 Glass System by Means of Spectroscopic and Dielectric Studies. Physica B, 2008, 403, 3751-3759.
Dimitrov, V.; Komatsu, T., An Interpretation of Optical Properties of Oxides and Oxide Glasses in Terms of The Electronic Ion Polarizability and Average Single Bond Strength. J. Univ. Chem. Technol. Metall. 2010, 45, 219-50.
Halimah, M.K.; Daud, W.M.; Sidek, H.A.A.; Zaidan, A.W.; Zainal, A.S. Optical Properties of Ternary Tellurite Glasses. Mater Sci-Poland. 2010, 28, 173-180.

## Slide 17
The XXIV International Scientific Conference of Young Scientists and Specialists
(AYSS-2020)