## Slide 1
Condensed matter research at IBR-2: overview of main scientific results and instrumentation developments achieved in 2016
D.P. Kozlenko
Frank Laboratory of Neutron Physics, Joint Institute for Nuclear Research, 141980 Dubna, Russia

## Slide 2
The priority directions of scientific research :
Physics and chemistry of novel functional materials;
Physics of nanosystems and nanoscale phenomena;
Physics and Chemistry of Complex Liquids and Polymers;
Molecular Biology and Pharmacology;
Materials and Engineering Sciences.

## Slide 3
Novel type of the charge ordering state in iron oxide Fe4O5 involving competing dimer and trimer formation
Crystal structure of Fe4O5 (a), neutron diffraction patterns, measured at different temperatures and processed by the Rietveld method (b), magnetic structures at Т = 150 К (c), and Т = 10 К (d).
Formation mechanism of the dimeric and trimeric states
S.V.Ovsyannikov,.., D.P.Kozlenko, et al., Nature Chemistry (2016)
Previously known: Fe3O4, Fe2O3, FeO
A new one: Fe4O5

## Slide 4
Structural and Magnetic Properties of Magnetoelectric BaMn1-xTixO3
Neutron diffraction patterns of BaMn1-xTixO3, x = 0, 0.05, 0.1, 0.15, 0.2 and 0.25, measured at 290 and 10 K and refined by the Rietveld method.
Structural models of possible polytypes of BaMn1-xTixO3 (0 < x <0.5
D.P.Kozlenko et al., J. Alloys and Compounds (2016)
X =0
X =0.05
0.1< X <0.25
BaTiO3 – large ferroelectric polarization (TC = 410 K, no magnetic order)
BaMnO3 – magnetic order, magnetoelectric effect, no FE polarization (TN = 230 K)

## Slide 5
A Structural Study of the Fe-Al phase diagram
Neutron diffraction patterns of Fe-26.6Al alloy measured on heating with a rate of 1 deg/min.
An example of high resolution ND patterns and W2 on d2 dependences in Fe26.5 and Fe-27Al.
A.M.Balagurov et al., JETP Letters (2016)

## Slide 6
Structure and stability of ferrofluids in bulk and at interface
(FLNP JINR - IEP - KNU - CFATR - NIPNE - MPI SSR- IGIC NAS)
Impact of synthesis method on FFs bulk structure
FFs structure at interface (Neutron Reflectometry)
MNPs reorganization at the PEG polymer addition
microemulsion method
cryogenic way of synthesis
in diethylene glycol environment
Nagornyi A.V., Petrenko V.I., et al. JMMM, 2016, in press.
Kubovcikova M., Gapon I.V., et al. JMMM, 2016, in press.

## Slide 7
ζ = -22 mV C60
ζ = +45 mV C60+Dox.
ζ = 0 mV Dox
ζ = -22 mV C60;
ζ = -17,6 mV C60+Cis
S.Prylutska, et al. Nano Res. (2017) accepted.
Yu.I.Prylutskyy, et al. RSC Adv. (2016).
Fullerenes complexation with antitumor drugs
(FLNP JINR – Biological and Physics Department KNU)
Doxorubicin
Cisplatin
Landomycin
NaCl crystals
C60+Cis
ζ = -22 mV C60
ζ =-10 mV C60+LA
SAXS
UV-Vis
SAXS
SANS
AFM
SEM
Mutagenic activity in Salmonella typhimurium
Biological tests

## Slide 8
A study of structural organization of organogels
SANS curves for 7OPhOLCA in DMSO-d6 for concentrations C = 0.005, 0.010, 0.015, 0.020 и 0.025g/ml at T = 10ºC after one cycle of heating-cooling.
4-heptyloxyphenylolithocholic acid (7OPhOLCA)
Phase diagram of the gel – sol transition on heating (top) and cooling (bottom).
M.Ordon, Yu. Gorshkova et al. Thermochimica Acta (2016)

## Slide 9
Low-Q phononic gap
No phonon propagation
at Q < Qgap
The cut-off value Qgap
(at which gap occurs)
Characteristic length-scale
dgap = 2π/Qgap of a local “order”
(no phonons at smaller Q  more disorder on long scale! )
Qgap
The Mechanism of Passive Transport in Lipid Bilayers
We observe:
nm-scaled short-lived molecular clusters  local chain ordering, or density fluctuations
Increased disorder beyond the cluster size  indication of the transient voids formation
Size and the life time of the clusters agrees well with the theory prediction
Low-Q phononic gap
NO phononic gap
Phonon-mediated nm-scale clustering
the cluster size dgap = 2π/Qgap is ~ 1.1-1.6 nm
Lifetime: ~1 ps (agrees well with common
assumptions – a few ps)
M.Zhernenkov, .., D.Soloviov, et al. Nat. Commun. (2016)

## Slide 10
Monitoring of electrochemical processes at the interface metal electrode/liquid electrolyte by neutron reflectometry (FLNP JINR – Dep. Chem. MSU)
M.V.Avdeev, et al. Appl. Surf. Sci. (2016) submitted.
Electrochemical cell for NR experiments
Working electrode (WE)
Counter electrode (CE)
Reference electrode (RE)
Electrochemical interface with a metal electrode and lithium-containing liquid electrolyte
SLD profiles
Experimental NR curves and fitting results

## Slide 11
Observation of cryptoferromagnetic domain state in layered structure V(150nm)/Fe(7%)+V+Nb)(20nm)/Nb(150nm)
Scattering at 10K, 2. Scattering at 1.5K, 3. Decreasing of scattering in range 1.5K-150K,
4. Transformation of cluster structure from 8K to 1.5 K at H=0
5. Structure at T=1.5K and H=1 kOe – Clusters and Domains (cryptoferromagnetism)

## Slide 12
A study of structure and dynamics of lovastatine
Molecular (left) and crystal (right) structures of lovastatine (LOV; (1S,3R,7S,8S,8aR)-8-{2-[(2R,4R)-4-Hydroxy-6-oxooxan-2-yl]ethyl}-3,7-dimethyl-1,2,3,7,8,8a-hexahydronaphthalen-1-yl (2S)-2-methylbutanoate) (b).
Theoretical (harmonic DFPT PBE-TS approach) and experimental vibrational spectra of lovastatine according to inelastic incoherent and terahertz spectroscopy (с). The most important vibrational modes are visualized (d).
С.
d.

## Slide 13
FSD-2016: Residual stress analysis in multi-pass welded specimen
FEM calculations - by group of Prof. Dr. V. Michailov (Brandenburg Uni. of Technology, Germany)
Sample preparation - by group of Prof. P. Petrov (Institute of Electronics of BAN, Sofia, Bulgaria)
Multi-pass welded test specimen
1st weld pass: MSG (Metal Active Gas welding)
2nd and 3rd weld passes: SAW (Submerged Arc Welding)
FEM results for longitudinal residual stress
Residual lattice strain (top) and stress (bottom) compared with FEM results
20 mm thickness
Experiments were performed with new radial collimators

## Slide 14
FSD-2016: TRIP steels (in collaboration with IMF of TU Bergakademie Freiberg)
Typical image from camera
Changes in diffraction pattern vs. plastic deformation
Phase contents vs. plastic deformation
4 phases: austenite, α- and ε-martensite, ZrO2 (amorphous)
Studied samples
Image profile analysis: changes in sample dimensions

## Slide 15
Deformation inside a paleosubduction channel – Insights from microstructures and crystallographic preferred orientations of eclogites and metasediments from the Tauern Window, Austria.
Keppler et al. (2016) J. Struct. Geol. 82, 60-79.
[doi: 10.1016/j.jsg.2015.11.006]
Geological location
Microstructural observations
Crystallographic preferred
Orientation (texture)

## Slide 16
Institute of Archaeology of Russian Academy of Science
Neutron radiography and tomography facility: cultural heritage studies
«Tver’ treasure» was found in 2014
The part of Old-Russian ancient bracelet dated to XIV century.
Neutron tomography reconstructed model
with “hidden” gilding pattern

## Slide 17
Global modernization of the HRFD diffractometer
New Fourier chopper in work position.
Comparison of the old (V-14-10) и new (V-16-10) incident neutron spectra measured using vanadium sample (a). The gain factor of neutron intensity as function of neutron wavelength measured using the standard Al2O3 sample (b).
Neutron guide with vertical parabolic focusing. New mirrors were mounted in old vacuum casing.

## Slide 18
FSD-2016: NEW radial collimators (G.V.=1.81.8 1.8 mm3)
Beam profiles:
analytical calculations and Monte Carlo simulation
Two radial collimators
by JJ X-Ray (Denmark)
Webcam for sample control:
top view of sample position
with radial collimators
Radial collimators on FSD for gauge volume definition in bulk sample during stress measurements
Two strain components can be measured simultaneously using both collimators

## Slide 19
Reconstruction of the Reflex reflectometer into the SESANS spectrometer
End part of a new neutron guide assembled at the 9th beamline.
Incident neutron wavelength distribution spectra on 9th beamline at the previous instrument configuration (black) and with a new neutron guide (red). Long wavelength limit is shifted by 11 Å, due to the move of the background chopper to the new position closer to the source.

## Slide 20
SANS-YuMO: New thermobox and sample holder
New Vacuum system for detectors tube

## Slide 21
Realization of the User Programme at the IBR-2 reactor
D.M. Chudoba
Frank Laboratory of Neutron Physics, Joint Institute for Nuclear Research, 141980 Dubna, Russia
On behalf of

## Slide 22
FLNP User Program
2 rounds
Scientific experts in 3 fields:
Atomic and Magnetic Structure
(7 facilities) – 9 experts from RU, PL, CZ, RU, MGL
Lattice and Molecular Dynamics
(2 facilities) – 3 experts from RU, PL
Nanosystems and Soft Matter
(4 facilities) – 14 experts from HU, RU, PL, FR, SK, EST, UA
Second round 2016: each proposal – 2 experts
IBR-2 reactor operation for physics experiments
(two rounds)
9 cycles (6 – water moderator, 3 cryogenic moderator)
2492 hr (1021 - first round)
(two rounds)
9 cycles (7 – water moderator, 2 cryogenic moderator)
2646 hr (1426 – first round)
2016 (two rounds)
8 cycles (7 – water moderator, 1 cryogenic moderator)
2447 hr

## Slide 23
Chart: 
| physics | chemistry | geosciences | materials science | applied science | biology, biophysics, biochemistry
 | 80 | 23 | 20 | 51 | 8 | 16
2015
2014 – 163 proposals; 150 accepted; 17 countries; 59 visiting users from 12 countries
2015 – 197 proposals; 174 accepted; 19 countries; 67 visiting users from 14 countries
2016 – 238 proposals; 208 accepted; 19 countries; 102 visiting users from 11 countries
Chart: 
| physics | chemistry | biology, biophysics | geosciences | materials science | applied science | Other
 | 76 | 16 | 11 | 9 | 43 | 6 | 2
47%
26%
9.8%
6.7%
5.5%
3.7%
2014
Chart: 
| physics | chemistry | geosciences | materials science | applied science | biosciences | other
 | 110 | 36 | 37 | 121 | 14 | 20 | 4
2016

## Slide 24
Number of articles per year (including published and submitted)
Scientific articles outcome at IBR-2 spectrometer complex (2014-2016)
Statistics of articles per instrument (only published ones are analyzed), prepared by N. Kucerka

## Slide 25
Thank You for Your Attention!