## Slide 1
Spin Dynamics in Intermediate Valence Compounds
A Comparison of Neutron Scattering and ab initio Theory
E. A. Goremychkin
Frank Laboratory of Neutron Physics, Joint Institute for Nuclear Research, Dubna, 141980, Russia
H. Park, R. Osborn
Materials Science Division, Argonne National Laboratory, Argonne, IL 60439-4845, USA
J. M. Lawrence, E.D. Bauer, K. J. McClellan, D. D. Byler
Los Alamos National Laboratory, Los Alamos, NM 87545, USA
D. Christianson, V. R. Fanelli
Oak Ridge National Laboratory, Oak Ridge, TN 37831, USA

## Slide 2
Ground state properties in metallic Rare-Earth compounds defined by a number of competing interactions of 4f electrons with Crystalline Electric Field (CEF) (Δ), f-f exchange mediated by RKKY interaction (Jex) and hybridisation with conduction electrons (Vs-f)
Van Fleck paramagnetism Δ> Jex > Vs-f
Magnetically ordered state Jex > Δ > Vs-f Vs-f
Kondo and Heavy Fermion systems Δ~ Jex ~ Vs-f
Intermediate Valence materials Vs-f> Jex > Δ

## Slide 3
Intermediated Valence arises from strong hybridization between f states and conduction electrons
Ce, Sm, Eu, Yb
Fermi Liquid (FL) model relations link:
γ , χ(0) , ω0=TK , <nf> and provide essential crosscheck for the single-ion character of the IV physics.
T.V. Ramakrishnan, K. Sur, Phys. Rev. B 26, 1798 (1982)
P. Coleman, Phys. Rev. B 28, 5255 (1983)
A.L. Cornelius et al., PRL 88, 117201 (2002)
YbAl3

## Slide 4: Magnetic dynamics in Heavy Fermion Ce3Co4Sn13 and magnetically ordered YbCo2Si2 (weak s-f interaction)
Ce3Co4Sn13
Ce3Co4Sn13 – Heavy Fermion system with γ = 4 J/molK2
E.A. Goremychkin and R. Osborn J. Appl. Phys., 87, 6818 (2000)
YbCo2Si2 – AFM below 1.7К

## Slide 5
Transition from Heavy-Fermion to Mixed-Valence Behaviour in Ce1-xYxAl3:
A Quantitative Comparison with the Anderson Impurity Model
E. A. Goremychkin, R. Osborn, I. L. Sashin et al., PHYSICAL REVIEW LETTERS 104, 176402 (2010)

## Slide 6
E. A. Goremychkin, R. Osborn, I. L. Sashin et al., PHYSICAL REVIEW LETTERS 104, 176402 (2010)
Transition from Heavy-Fermion to Mixed-Valence Behaviour in Ce1-xYxAl3:
A Quantitative Comparison with the Anderson Impurity Model

## Slide 7
R. Osborn, E.A. Goremychkin, I.L. Sashin, A.P. Murani
J. Appl. Phys., 85, 5344 (1999)
E1
E2
Lutetium substitution leads to a substantial decrease in the intensity of the narrow component (E1), with a negligible effect on the broad inelastic peak (E2).
The narrow component (E1) arises from coherent excitation processes within the hybridized 4 f band.
Motivation to perform single crystal INS experiment on MAPS
Spin Dynamics in Intermediate Valence Compound YbAl3

## Slide 8
YbAl3 ~5g MAPS E0 = 120meV
D. Christianson, V. R. Fanelli, J. M. Lawrence, E. A. Goremychkin, R. Osborn, E. D. Bauer, J. L. Sarrao,
J. D. Thompson, C. D. Frost, and J. L. Zarestky PHYSICAL REVIEW LETTERS 96, 117206 (2006)
T = 6K
E2
E2
E1
E1

## Slide 9
Almost all INS experiments on IV systems (powders) show single inelastic
peak at about TK (ω0~55meV) at low temperature
Fermi liquid relations work fine (link γ , χ(0) , ω0=TK , <nf>)
No other Q variation of intensity besides form-factor was observed
AIM explains INS data
All these observations provide essential evidences for
the single-ion character of the magnetic response.
YbAl3?
What about other IV compounds?
CePd3

## Slide 10
Intermediate Valence compound CePd3
A.P. Murani, R. Raphel, Z. A. Bowden, R. S. Eccleston "Kondo resonance energies in CePd3"
PHYSICAL REVIEW B 53 8188 (1996)
E. Holland-Moritz, M. Loewenhaupt, W. Schmatz, D. K. Wohlleben
"Spontaneous Relaxation of the Local 4f Magnetization in CePd3" PHYSICAL REVIEW LETTERS 38, 983 (1977)

## Slide 11
Two recent developments allow us to go beyond the previous qualitative analysis and do a comprehensive quantitative comparison of experiment and theory.
The firs development is the advent of a new generation of inelastic neutron scattering spectrometers with large position sensitive detectors that allow measurements of four dimensional S(Q,ω) in single crystals by rotating the sample during the data collection + development of powerful, user-friendly analysis software HORACE.
R.A. Ewings, A. Buts, M.D. Le, J. van Duijn, I. Bustinduy, T.G. Perring
“Horace: Software for the analysis of data from single crystal spectroscopy experiments at time-of-flight neutron instruments” Nuclear Instruments & Methods A 834, 132-142 (2016).
These developments of instrument technology and software
at ISIS opened new era in the INS research with single crystals!

## Slide 12
The second development is theoretical advance in the calculation of electronic excitations in strongly correlated electron systems, combining Density Functional Theory (DFT) with Dynamical Mean Field Theory (DMFT), to produce ab initio calculations of the dynamic susceptibility that include both single-particle and two-particle vertex corrections, allowing the treatment of systems with both coherent quasiparticles and incoherent spectral weight.
DFT+DMFT allows the incorporation of local correlations, i.e. Hund's rule and spin-orbit coupling as well as on-site Kondo screening, into realistic band structures based on DFT.
● CePd3 calculation : Wien2k+DMFT
→ Lattice constant : 4.126 A
→ U=6eV, J=0.7eV, T=0.01eV
● Spin susceptibility : CTQMC + MaxEntropy
● Momentum resolved dynamic susceptibility χzz”(Q,ω) [μB2/eV]
S(Q,ω)[mb/meV sr f.u.]x13.77 = 2gJ2f2(Q)χzz”(Q, ω)[μB2/eV f.u.]

## Slide 13
At 100 K (a), the band structure shows strongly renormalized but well-defined quasiparticle excitations within f-electron bands that are hybridized with the more dispersive d-bands.
At 400 K (b), the overall dispersion of the quasiparticles is similar, but there is a strong increase in the self energy, with a strong reduction of the coherent quasiparticle spectral weight, particularly close to the Fermi energy.

## Slide 14
Experimental details
Inelastic neutron scattering measurements were carried out using the MERLIN and MAPS spectrometers at the ISIS neutron scattering facility.
The measurements on MERLIN were performed at 5 K using incident energies of 30 meV, 60 meV and 120 meV. The crystal was mounted with [100] direction vertical and angle ϕ between the incident wavevector ki and the [010] direction was rotated in discrete steps of 2O.
The data were analyzed using the Horace software application.
The MAPS experiment was performed at fixed ϕ = 0, i.e., ki||[010] at 6 K and 300 K.
The MERLIN experimental data were placed on an absolute scale by normalizing the intensity to a vanadium standard, allowing a parameter-free comparison of experiment and theory.

## Slide 15
Dynamic magnetic susceptibility of CePd3 at 5 K ((a), (c) MERLIN data) and the DFT+DMFT calculations at 100 K (b), (d) represented by a K-L slice
at H = (1.5±0.25) and (a,b) ω = (35±5)meV and (c,d) ω = (60±10)meV.

## Slide 16
Dynamic magnetic susceptibility of CePd3 at 5 K ((a), (c) MERLIN data) and the DFT+DMFT calculations at 100 K (b), (d) represented by a L-ω slice at
H = (1.5±0.25)
(a,b) K = (0.00±0.25)
(c,d) K= (0.50±0.25).

## Slide 17
Energy dependence of the scattering law of CePd3 at 5 K at the Γ, X, M and R points in the Brillouin zone.
The red lines are the result of the DFT+DMFT calculations
The open circles, closed black circles, and closed blue circles are measurements on MERLIN with incident energies of 30 meV, 60 meV, and 120 meV, respectively.
.
Γ (1.00±0.25, 1.00±0.25, 0.00±0.25), X (1.00±0.25, 1.00±0.25, 0.50±0.25)
M (1.50±0.25, 0.00±0.25, 0.50±0.25), R (1.50±0.25, 0.50±0.25, 0.50±0.25)

## Slide 18
The upper three panels represent the DFT+DMFT calculations of S(Q, ω) at 100 K in the form of a L- ω slice along ΓX, XM and MR directions.
Three white dashed lines, labelled I, II and III, show the direction and position in energy of the one dimensional constant energy cuts at energies of (a,d,g) 60±5 meV (b,e,h) 45.0±2.5 meV and (c,f,i) 25.0±2.5 meV, respectively.
The points represent the inelastic neutron scattering data measured on MERLIN.
The lines represent one-dimensional cuts of the DFT+DMFT calculations.

## Slide 19
Temperature dependence of the dynamic magnetic susceptibility measured on the MAPS spectrometer. The open (closed) circles were measured at 6 K (300 K) using a fixed sample geometry at the energy transfer of (60±10) meV and K = (0.50±0.25). The inset shows how H varies as a function of L. The lines are the results of DFT+DMFT calculations performed at 100 K and 400 K including the H(L) dependence and scaled with the same normalization factor for both temperatures.

## Slide 20
Conclusions
We have performed a quantitative comparison of inelastic neutron scattering from a single crystal of CePd3, measured in four-dimensional (Q, ω)-space, with ab initio calculations, which are in excellent agreement on an absolute scale.
The magnetic fluctuations show a much richer structure than was implied by earlier toy models of hybridized bands.
Our results establish that the Q-dependence of the scattering is caused by particle-hole excitations within f-d hybridized bands that grow in coherence with decreasing temperature.
The transition from coherent f-electron bands to local moment physics, so long postulated in models of heavy fermion and intermediate valence systems, is seen to be accurately modelled by the latest advances in the ab initio theories of correlated electron systems.

## Slide 30: Band Excitations using High Energy Neutrons
J.F. Cooke and J.A. Blackman, Phys Rev B 26, 4410 (1982).
S. K. Sinha (1984)