## Slide 1: Serial Magnetic Measurements of Quadruple Magnets of NICA Booster
A. Shemchuk on behalf of NICA team

## Slide 2
Presentation plan
Introduction
2. Doublet of quadrupole lenses
3. Specification requirements
4. Measurement procedure
5. Design and assembly of the sensor
6. Structure of magnetometric system
7. Results
8. Conclusion

## Slide 3
- Dipole magnets of NICA booster - 40 шт.
-Quadrupole magnets of NICA booster- 48 шт.
-Dipole magnets of NICA collider– 80 шт.
-Quadrupole magnets of NICA collider– 86 шт.
-Quadrupole magnets of SIS-100 (FAIR project) - 175 шт.
Introduction
Scientific and ex-remental department of production and testing of superconducting magnets.
Launch of factory of superconducting magnets, November 28, 2017

## Slide 4
Doublet of quadrupole lenses
Parameter | Unit | Value
Number of magnets | Pc. | 48
Field gradient (inj./max.) | T/m | 1.3 /21.5
Effective magnetic length | m | 0.47
Beam pipe aperture (h/v) | mm | 128 /65
Operating current | kA | 9.68
Ramp rate | T/(m·s) | 14.3
Field error at R= 30 mm |  | ≤ 610-4
Pole radius | mm | 47.5
Fig. 1 3d view of doublet of quadrupole lenses
Tab. 1 Main characteristics of the NICA Booster Magnets
Fig. 2 Installation of a winding in an iron yoke
Fig. 3 Magnet, collected and ready to measurements

## Slide 5
Specification requirements

## Slide 6
Specification requirements
 | Parameter | Tolerance | Accuracy
1 | A gradient in the center of a magnet, G0 | 5*10 | 10
2 | Integral gradient, GL | 5*10 | 10
3 | Effective length Leff | 5*10 | 10
4 | Magnet axis shift Δx | ±0.1 | 0.02 mm
5 | Magnet axis shift Δy | ±0.1 | 0.02 mm
7 | b1, a1 | 3*10 | 10
8 | a2, (b2=1) | 10 | 10
9 | a3, b3 | 10 | 2*10
10 | a4, b4 | 5*10 | 10
- 4
- 4
- 3
- 4
- 4
- 4
- 4
- 4
- 4
- 4
- 4
- 4
- 4
- 4
* Values and precision of definition of harmonics of a magnetic field of bn, an are specified in the relative to the main field (b2 – for a quadrupole magnet) units. These value are defined for rref=30mm radius.

## Slide 7
Measurement procedure
Flux through the radial coil
=
= (sin())
2d representation of the magnetic field
Measured flux harmonics
Ф
P – Number of function measurement points
Fig. 4 Harmonic coil measurement procedure

## Slide 8
Design and assembly of the sensor
Before creation of the sensor for serial tests two prototypes were created. The first turned on radial coils, the second - tangential.
Creation of prototypes
Fig. 5 Radial probe
Fig. 6 Tangential probe

## Slide 9
Design and assembly of the sensor
Fig. 7 The full-size probe for serial measurements
2
3
2
3
4
5
1
1

## Slide 10
Design and assembly of the sensor
Fig. 8 Basic elements of the probe with harmonic coils
Block of harmonic coils
Fiberglass-laminate tube
Plates for precise positioning
A
A

## Slide 11
Zoomed cross-section sheme PCB coil
Measuring coils are executed on technology of the multilayer printed circuit board. The printed circuit board contains three blocks on five identical measuring coils.
Coils contain 400 rounds formed by 20 layers on 20 rounds.
Parameter | Value ,mm
R1 | 6,85
R2 | 9,85
R3 | 23,55
R4 | 26,55
R5 | 40,25
L | 400
Design and assembly of the sensor
Fig . 10 Cross-section A-A
Main parameter of PCB
Fig. 9 Cross-section of PCB coil

## Slide 12
The most important task in assembly - is exact installation of the block of coils relative a rotation axis. Thanks to a measuring arm, the accuracy of installation of coils is about 30 microns.
Design and assembly of the sensor
Fig. 12 Нoles for an adjustment of coils in the sensor
Fig.11 Measurement of coordinates of an axis of the sensor concerning the fiducial platforms of a doublet
Fig.13 Position of coils concerning a spin axis. Construction is executed in the PolyWorks program

## Slide 13
Structure of magnetometric system
Magnetic measurements
«Warm» t= 293 °K
«Cold» t= 4.5 °K
Warm magnetic measurements are carried out in order that at an early stage to reject low-quality magnets. Realization of warm measurements allows to save time and costs of cooling of the rejected magnet.
Fig. 14 Cryogenic measurements
Fig. 13 Warm measurements

## Slide 14
Fig. 15 Schematic chart of acquisition and control.
Structure of magnetometric system

## Slide 15
Results
Fig.16 Sensitivity for harmonics of measurement system
The graph shows the sensitivity of the measuring system to the measured harmonics.
For «D» lens
For «F» lens

## Slide 16
Results
Fig. 16 Measured harmonics of the serial doublet lens DL 20-04
For «D» lens
For «F» lens
bn,an ˂ 10⁻⁴ (n=7..31)

## Slide 17
Results
Fig. 17 Effective length for 10 kA. Left – for DL20-04, right – for DL14-14
∆=0.66 mm
The difference in effective lengths correlates with the difference in measuring the thickness of the core iron. The difference in measuring the lengths of core iron was 0.33 mm.

## Slide 18
 | Parameter | DL-20-04 |  | DL-14-14 |  | σ
 |  | F | D | F | D | 
1 | Integral gradient, GL | 21,1914 | 21,1837 | 21.1438 | 21.1525 | 0.001
2 | Effective length Leff | 496,11 | 495,77 | 495.89 | 495.41 | 0.03
3 | Magnet axis shift Δx | -0,24 | -0,20 | 0.38 | 0.35 | 0.01
4 | Magnet axis shift Δy | -0,51 | -0,48 | -0.63 | -0.64 | 0.01
The table below presents the results of the cryogenic measurements of the two doublets. Values are given for the current 9680 A.
Results
Tab. 2 Measured parameters of the measured parameters of the two doublets at t=4,5°K

## Slide 19
Conclusion
Created magnetometric system is able to measure all the quantities listed in the specifications within the specified tolerances, namely:
Variation of effective length – 10-4
The accuracy of measuring the shift of the magnetic axis of the element relative to its geometrical axis - 0.05 mm
The accuracy of measurement of harmonics - 10-4
At the moment the magnetic measurements group is working on stand string methods. It will allow to independently measure the offset of the axes of the doublet. Also make work on complete full automation of the measurement process.

## Slide 20
Acknowledgements
I want to thank our colleagues from CERN, given the dependence of the thermal compression of the measuring coil. Also thank Karpunin Roman for images under a microscope-section of the coil.
Thank you for
your attention!

## Slide 21
Спасибо за внимание!
Желаем успехов во всех Ваших начинаниях!!!