## Slide 1
Simulation of damage threshold and structure in swift heavy ion tracks in Al2O3
R. A. Rymzhanov1, N.A. Medvedev2, J.H. O’Connel3,
V.A. Skuratov1, A.E.Volkov1,4,5
1 FLNR, JINR, Dubna, Russia
2Institute of Physics, Czech Academy of Sciences, Prague 8, Czech Republic
3CHRTEM, NMMU, Port Elizabeth, South Africa
4NRC”Kurchatov Institute”, Moscow, Russia
5LPI of the Russian Academy of Sciences, Moscow, Russia
46th PAC on
Condensed Matter Physics

## Slide 2
Swift heavy ions (SHI)
Е > 0.5 MeV/nucl, M > 4mp
Snucl/Sel < 0.01 - Lose energy to electronic stopping
Simulate the influence of fission fragments and cosmic rays on material properties

## Slide 3
Practical application of SHI
Membranes and nanowires
GSI, Darmstadt
GSI, Darmstadt
Modification of nanoclusters
Kluth et al, REI-2007, Au in SiO2
Nanostructuring
W.Bolse
200 MeV Au
B. Canut et al., NIMB 245 (2006) 327)
Interlayer transitions
Quantum dots
P. Gaiduk et al., Phys. Rev. B66 045316 (2002)
SixGe1-x
1.3 GeV U

## Slide 4
Fundamental interest
Marek Skupinski (Uppsala)
The relaxation of excitation induced by SHI cannot be described within macroscopic approaches
10-16 10-15 10-14 10-13 10-12 10-11 10-10 10-9 t (sec)
lattice
electrons
SHI
Nanometric spatial and femto-picosecond temporal scales
Extremely high level of material excitation

## Slide 5
Why Al2O3?
Good material for modelling
Radiation resistant material (Perspective for applications in nuclear energetics)
X-[100]
[010]
Y-[120]

## Slide 6
Combined experimental and numerical investigation
Irradiation by Xe, Bi ions
(FLNR, Dubna: IC-100, U-400M)
Experimental
Theoretical
TEM microscopy and analysis
(CHRTEM, SA)
Monte-Carlo model of
electron subsystem excitation
Energy transfer to the lattice
Molecular Dynamics simulation
(LAMMPS code)
Verification of the model
Explanation of observed results
P.N. Terekhin, R.A. Rymzhanov et al.
NIMB 254 (2015) 200–204

## Slide 7
TREKIS: Monte-Carlo model
Time-Resolved Electron Kinetics in SHI Irradiated Solids
1. SHI passage and generation of primary δ-electrons and holes ~10-17 s
2. Spreading of electrons and secondary electron cascading ~10-16 - 10-14 s
3. Auger and radiative decays of core holes ~10-15 s
4. Mobility of valence holes ~10-13s
Collective response of a material is taken into account

## Slide 8
TREKIS: Verification of model
Good coincidence with SRIM, CasP and NIST database
Electronic energy loss of ions and inelastic mean free paths of electrons

## Slide 9
TREKIS: Results
Excitation of target lattice
Mobility of valence holes play an important role for energy transfer to the lattice
100 fs

## Slide 10
MD simulation
MD code
LAMMPS
Z
X
Y
18.8 nm
12.2 nm
5.25 nm
Xe 167 MeV

## Slide 11
Xe 167 MeV
- Al
- O
c)
d)
b)
Y
Z
X
а)
Y
Z
X
~1.8 nm
9.8 nm
V.A. Skuratov, J. O’Connell et al. NIMB 326 (2014) 223–227

## Slide 12
Xe 167 MeV
5%
-5%
0
Radial density of Al2O3
Lattice deformation:
Simulation
Experiment

## Slide 13
Xe 167 MeV
Simulation of X-ray powder diffraction
Aluminum sublattice is damaged stronger than oxygen sublattice

## Slide 14
Bi 700 MeV (44 keV/nm)
Residual stress around ion trajectory
Track structure: underdense core is surrounded by overdense shell
~3.4 nm
Y
Z
X
- Al
- O

## Slide 15
Kr and Fe ions
Kr 107 MeV Fe 22.5 MeV
~1.25 nm
а)
b)
~0.5 nm
dE/dx = 16 keV/nm dE/dx = 10 keV/nm

## Slide 16
Track formation threshold
Calculated threshold value is dE/dxth ~ 6.1 keV/nm

## Slide 17
Track density
  The number of ion tracks saturates at fluence of
  ~ 1.1 x 1012 cm-2
  Effective radius of SHI track ~ 5.4 nm
J. O’Connell et al. VITT 2015

## Slide 18
Z-projection
2.8 nm
Box size 12.2 x 18.8 x 5.2 нм3
Xe 167 MeV ion
Passage of the second ion causes annealing of the defects created by the first one
Is the healing of tracks the probable mechanism of observed saturation?
Z-projection
Y-proj.
Y-proj.
Overlapping of SHI tracks. Xe 167 MeV

## Slide 19
Overlapping of SHI tracks. Xe 167 MeV
6.5 nm
Z-projection
Y-proj.
Z-projection
Y-proj.
Passage of the ion at longer distances from older tracks causes partial annealing of the defects
Effective radius of recovery is ~6.5 nm (experimental ~5.4 nm) and corresponding track density is ~2.7×1012 см-2

## Slide 20
Overlapping of SHI tracks. Bi 700 MeV
Bi 700 MeV ion tracks causes partial recovery of older tracks
6.5 nm
8 nm

## Slide 21
6.5 nm
TEM image of double Bi 700 MeV
Stress field of overlapped tracks
Overlapping of SHI tracks. Bi 700 MeV
  Closely spaced tracks are “connected” with defect structure aligned along atomic planes
Color coding of displacements: X, Y, Z

## Slide 22
Conclusions
The relaxation of excess lattice energy in Al2O3 irradiated by SHI is studied using original MC model and classical MD
The estimation of track size is in a good agreement with recent TEM data. The energy loss threshold of track formation in Al2O3 is determined (dE/dx~ 7 keV/nm).
Simulation of X-ray powder diffraction patterns of irradiated crystal revealed that the Al sublattice is damaged stronger than O sublattice
The effect of recovery of overlapping tracks in Al2O3 is investigated. The effective distance of recovery is ~5.4 nm (TEM) - 6.5 nm (MD) for Xe 167 MeV ion.
Overlapping of Bi tracks causes only partial recovery of existing track forming defect connections between tracks.

## Slide 23
Thank you for your attention
46th PAC on
Condensed Matter Physics

## Slide 24
Interatomic forces
Buckingham-type potential
Verification of potential
Cij, Aij, ρij from
M. Matsui, Geophys. Res. Lett (1996)
Elastic constants | Experimental, GPa | Calculated, GPa
C11 | 498 | 473.6
C12 | 163 | 181.7
C13 | 117 | 150.8
C14 | -23 | -19.2
C33 | 502 | 520.5
C44 | 147 | 115.7
C66 | 167 | 146.3
Tm(exp) = 2345 K

## Slide 25
Track relaxation kinetics
Radial and temporal dependence of the Al2O3 density near Xe 167 MeV ion trajectory
Propagation of elastic waves with frequency of ν ~ 0.5 THz

## Slide 26
Dose of fast fission fragment irradiation is ~1016 cm-2 per year