## Slide 1: DFT-based study of the disordered solid electrolytes
Roman Eremin1,2, Pavel Zolotarev1
1Samara Center for Theoretical Materials Science, Samara University, Samara, Russia
2Samara Center for Theoretical Materials Science, Samara State Technical University, Samara, Russia
Samara Center for Theoretical Materials Science

## Slide 2: Motivation

## Slide 3: Cathode materials
Cathode (LiMeO2)
Anode (graphite)
0%
100%
50%
25%
75%

## Slide 4: Purpose and Tasks
Modeling of the properties of the cathode materials during deintercalation
Sampling of the configurational spaces of disordered structure
Calculations of the structure – energy relations
-1 ball
-3 balls
-2 balls

## Slide 5: Cathode materials: DFT models
LiNiO2 (S.G. R-3m)
12 balls
-1 ball
-2 balls
-3 balls
…
…
…
…
…
-12 balls

## Slide 6: Cathode materials: doping
LiNiO2 (S.G. R-3m)
DOPED
12 balls
-1 ball
-2 balls
-3 balls
…
…
…
…
…
-12 balls

## Slide 7: Cathode materials: doping
Compositional/configurational space sampling
DFT-based structure relaxation (variable models, Bader analysis, etc.)
Structure-energy relations (charge distribution)
R. A. Eremin, P. N. Zolotarev, O. Y. Ivanshina and I. A. Bobrikov, Li(Ni,Co,Al)O2 Cathode Delithiation: A Combination of Topological Analysis, Density Functional Theory, Neutron Diffraction, and Machine Learning Techniques, J. Phys. Chem. C, 2017, 121, 28293−28305.

## Slide 8: Solid electrolytes
Cathode
Anode
Solid electrolyte

## Slide 9: Solid electrolytes: modeling
Modeling approaches
Dynamics
Classical molecular dynamics
Quantum molecular dynamics
Transition states
Nudged elastic band method (NEB)
Monte Carlo modeling
Force field setting
Slow (even for a small system)
All inequivalent transitions to be considered
No information on the transition states
Kinetic and dynamic MC

## Slide 10: Nudged elastic band method

## Slide 11: Solid electrolytes: KFeO2
KFeO2, 4-2-2 supercell
KFeO2, pathways
A
B
C
D
E
F
G
H
J
I
RAB = 3.37778 Å
RCD = 3.39415 Å
REF = 3.41299 Å
RGH = 3.41472 Å
RIJ = 3.42567 Å
A
B
C
D
E
F
G
H
J
I
NEB

## Slide 12: Solid electrolytes: doping effect
N. V. Proskurnina, V. I. Voronin, G. S. Shekhtman, L. N. Maskaeva, N. A. Kabanova, A. A. Kabanov and V. A. Blatov, Ionic Conductivity in Ti-Doped KFeO2: Experiment and Mathematical Modeling, J. Phys. Chem. C, 2017, 121, 21128–21135.
KFe1-xTixO2

## Slide 13: K1-xFe1-xTixO2: configurational space
x ≈ 0.03
64 configurations

## Slide 14: K1-xFe1-xTixO2: space of pathways
128 transitions
x ≈ 0.03

## Slide 15: K1-xFe1-xTixO2: space of pathways
128 transitions

## Slide 16: How to…
… analyze the obtained results?
… go further with respect to dopant content?

## Slide 17: Acknowledgements
We are obliged to computational facilities of Samara University:
‘Sergey Korolev’ and
‘Zeolite’ (Samara Center for Theoretical Materials Science).
This study was supported by
the Russian Federation Government (project No.3.6588.2017/9.10) and
Russian Foundation for Basic Research (project No.18-33-00477).
Thank you for your attention!