## Slide 1
BINP
a.a.krasnov@inp.nsk.su
Electron Clouds
Alexander Krasnov
Budker Institute of Nuclear Physics (BINP), Novosibirsk, Russia
JAS 28 October – 7 November, 2019, Dubna, Russia

## Slide 2
BINP
Contents
Historical review
Electron clouds (EC) sources
EC influence on an accelerator performance
EC formation
Key parameters and equations for EC simulation
LHC arc beam pipe
SuperKEKB, beam pipe in dipoles
Surface conditioning
EC investigations on SPS (CERN),
Photoelectron emission experiments at BINP
SEE in magnetic field, experiments at BINP and at JINR
References

## Slide 3
INP Novosibirsk, 1965
Argonne ZGS,1965
BNL AGS, 1965
Bevatron, 1971
ISR, ~1972
PSR, 1988
AGS Booster, 1998/99
KEKB, 2000
CERN SPS, 2000
G. Budker et al
J.H. Martin, F.E. Mills et al
E.C. Raka
H.A. Grunder,
G.R. Lambertson
E. Calder,
O. Gröbner et al
D. Neuffer,
R. Macek et al
M. Blaskiewicz
H. Fukuma et al
K. Cornelis,
G. Arduini et al
KEK PF, 1988
M. Izawa, Y. Sato,
T. Toyomasu
PEP-II,
MI,
SNS,
CesrTA,
LHC,
…
Slide from Frank Zimmermann

## Slide 4
BINP
F. Zimmermann, “Review of single bunch instabilities driven by an electron cloud”, PHYSICAL REVIEW SPECIAL TOPICS - ACCELERATORS AND BEAMS, 7, 124801 (2004)
“Perhaps the first ever observation of an electron-cloud driven instability was made with a bunched beam at a small proton storage ring of the INP Novosibirsk around 1965. The ring circumference was only 2.5 m. Coherent betatron oscillations and beam losses occurred above a threshold proton intensity of 1–1.5 1010. Soon G. Budker and co-workers identified the instability as one due to electrons (secondary particles). It was cured by a transverse feedback system.
Two years later, another PSR at INP also suffered an electron-cloud instability, in this case with a coasting proton beam. The threshold here corresponded to 1.2 1011 protons, which were distributed over a 6 m circumference. The coasting-beam instability was suppressed by increasing the beam current and the gas density. This compensation scheme allowed storing up to 1.8 1012 protons, i.e., about 15 times the initial threshold value. As pointed out by V. Dudnikov, the fast accumulation of secondary plasma by gas ionization was essential for the stabilization. The existence of an ‘‘island of stability’’ above the threshold was consistent with a previous analysis by B. Chirikov (1965)”
EC in PSR at INP. Novosibirsk
G. Budker, G. Dimov, V. Dudnikov, Experiments on production of intense proton beam by charge exchange injection method;
Proceedings of the International Symposium on Electron and Positron Storage Rings, Saclay, France, VIII, 6.1 (1966)

## Slide 5
BINP
EC driven beam instability
The first numerical simulation of an electron-cloud formation was done by K. Ohmi in 1995. It served to explain coupled-bunch instabilities observed with positron beams at the KEK photon factory.
Coherent single bunch instability has been observed at KEK and SuperKEKB. Freq. signal corresponding head-tail motion has been observed (synchro-betatron oscillation).
For SuperKEKB : Estimated threshold of electron density ~ 2∙105 cm-3
Different types of EC driven instability were observed in
ISR, PS, SPS, KEKB, PEP, TEVATRON, RHIC…
LHC: Up to now main limiting factor – heating of cold beam pipe by electron bombardment. Cooling capacity about 1.2 W/m, if each electron transmits average energy 350 eV, current must be less than 3 mA/m (or 2E16 e/m/s). Taking into account banch spacing 25ns and beam pipe cross-section (about 15 cm2) one can obtained density ~ 3∙105 cm-3
EC influence on an accelerator performance

## Slide 6
BINP
Surface
Metallic surface contains 10 ÷ 100 ML (1 ML ≈ 1015 cm-2 ) of
Chemically bound: MxOy, Mx(OH)y, Mx(HCO3)y, carbon clusters
Physically adsorbed: H2O, organics
Example: Internal surface of a tube with D=5 cm contains 108 ÷ 109 times more molecules than ones inside the tube in gas phase at density 3∙107 cm-3 (10-7 Pa – requirement for SuperKEKB)!
Electrons can provoke dissociation of the molecules which causes desorption of:
H2 - most critical for cryogenic beam pipe (LHC) because H2 can re-desorb on surface with very low binding energy
CO, CO2 and saturated hydrocarbons CxHy (due to catalytic reactions on surface) - defines “vacuum” beam lifetime.
Exercise: Which pumping speed is sufficient to provide gas density at level 3∙108 cm-3 in presence of electron stimulated desorption by electron current 1 mA and efficiency 0,01 molecule/electron?
EC influence on dynamic gas density

## Slide 7
BINP
Residual gas ionization:
For CO and relativistic beam the σ ~ 10-18 cm2. The average electron lifetime are equal to bunch spacing (25 ns in LHC) roughly. If the I=1 A and ng=109 cm2, the Ne is estimated as 150 electron/cm or just 10 electrons/cm3
2. Photoelectrons
EC sources
3. Multipacting
For LHC SR photon flux ~1E17 ph/m/s and estimated photo-electron density ~ 1.5∙105 cm-3

## Slide 8
BINP
EC formation
Beam-Induced Multipacting

## Slide 9
BINP
EC formation
Saturation
The electron-cloud density saturates when the electron losses balance the electron generation rate. This can happen when EC screens beam electric field in average or, at high bunch population, when the kinetic energy at emission is too low to penetrate into the space-charge field of the cloud:
where b denotes the chamber radius (for simplicity we consider a round chamber), Es is the average energy of the emitted secondary electrons, re is the classical electron radius, Nb is bunch population. The transition occurs at a bunch population of about
~1010 for LHC
up to 106 cm-3 for LHC
~3.6∙106 cm-3 for LHC
e-
Note, if acceptable density several times less than saturated value, we can simulate EC neglecting space charge

## Slide 10
BINP
Key parameters for EC simulation
(1)
(2)
s: fitting parameter;
: maximum of the SEY curve dependent on the surface material, roughness…
Emax: electron energy, where the SEY reach the maximum 𝛿𝑚𝑎x:
For the LHC EC simulation are used:
  s = 1.35
  Emax = 300 ÷ 450 eV
(1)
(3)
(2)
𝛿𝑚𝑎x
According to:
R. Cimino, I. R. Collins, M. A. Furman, M. Pivi, F. Ruggiero, G. Rumolo, and F. Zimmermann, “Can Low-Energy Electrons Affect High-Energy Physics Accelerators?,” Phys. Rev. Lett., vol. 93, p. 014801, Jun 2004.

## Slide 11
BINP
Key parameters for EC simulation
(1)
(3)
(2)
𝛿𝑚𝑎x
(1)
(3)
E0 and R0: shape parameters.
For the LHC EC simulation used:
  E0 = 150 eV (Work function?)
  R0 = 0.5 ÷ 1.0
There is another approach for 𝛿𝑒𝑙 (𝐸p) approximation:
According to:
R. Cimino, I. R. Collins, M. A. Furman, M. Pivi, F. Ruggiero, G. Rumolo, and F. Zimmermann, “Can Low-Energy Electrons Affect High-Energy Physics Accelerators?,” Phys. Rev. Lett., vol. 93, p. 014801, Jun 2004.
Empirical, from data on different materials:
Scholtz, J.J., D. Dijkkamp, and R.W.A. Schmitz, Philips Journal of Research, 1996. 50(3-4), 375
Ep[0,100eV]

## Slide 12
BINP
Key parameters for EC simulation
Dependencies on primarily electrons angle incidence (relatively to surface normal vector):
Secondary energy spectrum
Es.max ≈ 1.8 eV, ∆Es ≈ 1 eV

## Slide 13
BINP
Electron cloud formation
at <1
Phenomenologically, neglecting space charge, electron density can be estimated as:
The problem is solved if s <0,02,
and < 0,95 for example
How to reach it:
amorphous carbon coating
High quality NEG (TiZrV)
Laser tritment
Or just Ti but deposited in-situ (!)
Geometrical solutions with low “s”
< 2E5 cm-3
SEY of OFE Copper

## Slide 14
BINP
a.a.krasnov@inp.nsk.su
EC formation
EC numerical simulation made at CERN
EC linear density in LHC dipole chamber
R – elastic scattering is taking into account
NR - elastic scattering is NOT taking into account

## Slide 15
BINP
a.a.krasnov@inp.nsk.su
EC formation
EC numerical simulation made at CERN
Multipacting threshold at long bunch spacing
EC head load at nominal munch spacing 25 ns

## Slide 16
BINP
LHC, Phenomena in cold beam pipe
CB T=1.9K
ID=50mm
Screens against e-
p+
Slots
Cooling tubes
BS T=5 ÷ 20K
OD=49mm
Saw tooth!
γ
γd
e-
e-ph
e-
γd
Molecular physisorption
onto cryogenic surfaces
(weak binding energy)
Cross-section of arc LHC beam pipe in superconducting dipoles
B
Electron Cloud
Cooling capacity at 1.9K is 10s mW/m
Cooling capacity of BS about 2 W/m
Old design
Position of EC strips is defined by maximum of:

## Slide 17
BINP
LH beam pipe
Important solutions made for LHC arc beam pipe
0.02÷0.03
0.5
SR
Slots
Decreasing number of diffusely scattered photons
decreasing number of photo-electrons (3 ÷ 5 times!) and increasing of conditioning effectiveness
Beam screen: screening of CB against SR and EC, power absorption
Copper co-lamination: high electrical conductivity at cryogenic temperature
Saw tooth!

## Slide 18
BINP
a.a.krasnov@inp.nsk.su
SuperKEKB dipole chamber
SR

## Slide 19
BINP
a.a.krasnov@inp.nsk.su
Surface conditioning (SEY must be less 1.3 for LHC arcs)
SEY measurements at CERN for copper samples
Pure copper: δ = 1.35
Surface conditioning (SEY must be less 1.3 for LHC arcs)
SEY measurements at CERN for copper samples:

## Slide 20
BINP
a.a.krasnov@inp.nsk.su
Relation between SEY and ESD during conditioning!
B.Henrist, N.Hilleret, C.Scheuerlein, M.Taborelli, G.Vorlaufer. The variation of the secondary electron yield and of the desorption yield of copper under electron bombardment: origin and impact on the conditioning of the LHC. Proceedings of EPAC 2002, pp. 2553-2555, Paris, France.

## Slide 21
BINP
a.a.krasnov@inp.nsk.su
EC investigations on SPS (CERN)
EC detection with the use microwave phase shift
Details ask Fritz Caspers

## Slide 22
BINP
EC investigations on SPS (CERN)

## Slide 23
BINP
a.a.krasnov@inp.nsk.su
EC investigations on SPS (CERN)

## Slide 24
BINP
EC investigations on SPS (CERN)

## Slide 25
BINP
a.a.krasnov@inp.nsk.su
Photoelectron azimuthal distribution
Experiments at BINP (Novosibirsk)
Sample | Ec [eV] | Specular scattering [%] |  | Quantum yield | Normalized photocurrent [%] |  | 
 |  | Re current | RW power |  | R1 | R3 | R2+R4
Smooth | 49 | 80 | — | 0.047 | 16 | 2.2 | 1.8
Saw tooth N1 | 49 | 3.5 | — | 0.05 | 74 | 18.5 | 4
 | 246 | 2.5 | 3 | 0.06 | 79 | 15 | 3.5
Saw tooth N2 | 98 | 13 | 10±5 | 0.055 | 67 | 16 | 4

## Slide 26
BINP
The experimental set-up
on BEP SR beam line at BINP
In the framework of the HL-LHC project, the vacuum performance of new surface material needs to be studied in details. In particular, amorphous carbon (a-C) coating is proposed as an anti-multipactor surface with the objective to minimize the heat load deposed on the shielded beam screen and the background to the experiment due to proton scattering onto the residual gas. Since the protons in the HL-LHC Inner Triplets generates SR with ~ 10 eV critical energy and ~ 1016 ph/m/s flux, it is therefore of great importance to study the impact of such photons on a-C coating held at room and cryogenic temperature and compare the results against present LHC material.
Collaboration R&D CERN – BINP (Addendum P110/A2)

## Slide 27
BINP
* Calibration and more experiments are needed to check the result
Ec eV | α-C R forward | Cu1 R forward
12,5 | 0,013 | >0,75
25 | - | >0,75
50 | - | >0,7
100 | 0,027 | 0,6…0,75
200 | 0,018 | -
400 | 0,028 | -
800 | 0,021 | -
1250 | 0,015 | -
BEP: Ie up to 650 mA, Ee=193….900 MeV, Ec=12,5… 1250 eV
Forward reflectivity

## Slide 28
BINP
Chart: Azimutal distribution ph in C-a
| -67.5 | -56.25 | -45 | -33.75 | -22.5 | -11.25 | 0 | 22.5 | 45 | 67.5
H2 | 0.53333 | 2.1556 | 4.6667 | 5.7778 | 8.4444 | 12.8889 | 13.7778 | 6.6667 | 0.66667 | 0.35556
Chart: Azimutal distribution ph in Cu
| -67.5 | -56.25 | -45 | -33.75 | -22.5 | -11.25 | 0 | 22.5 | 45 | 67.5
H2 | 23.8095 | 15.2381 | 14.2857 | 15.3968 | 31.746 | 155.5556 | 277.7778 | 22.2222 | 9.3651 | 27.4603
Azimuthal photon distribution
_
+
SR
0
Alpha/2
Alpha/2

## Slide 29
BINP
Chart: Azimutal distribution eh in C-alpha
| -67.5 | -56.25 | -45 | -33.75 | -22.5 | -11.25 | 0 | 22.5 | 45 | 67.5
H2 | 53.3333 | 76.6667 | 86.6667 | 95.5556 | 100 | 103.3333 | 113.3333 | 91.1111 | 67.7778 | 42.2222
Chart: Azimutal distribution e in Cu
| -67.5 | -56.25 | -45 | -33.75 | -22.5 | -11.25 | 0 | 22.5 | 45 | 67.5
H2 | 449.2063 | 511.1111 | 507.9365 | 495.2381 | 492.0635 | 547.619 | 650.7937 | 492.0635 | 457.1429 | 457.1429
Alpha/2
Alpha/2
Azimuthal photo-electrons distribution
_
+
SR
0

## Slide 30
BINP
SEE in magnetic field
Element (from left to right) | ID [mm] | Length [mm] | Gap with right element [mm]
C | - | - | 0.25
M | 0.5 | 2 | 3
D | 4.5 | 1 | 1
BM1 | 4 | 10 | 0
Drift tube | 7 | 325 | 1
BM2 | 7 | 59 | 2 ÷ 3 (to sample)
“C” – thermo-cathode
“M” – modulator
“D” – diaphragm
“BM1, BM2” – beam monitors
“S” – sample
“SM” – sample manipulator
Parameters
-Energy of primarily electrons: 50 ÷ 1500 eV
-Primarily beam pulse current: up to 200 µA
-Primarily electron beam pulse duration: 1 ÷ 10 ns.
-Beam diameter: ~ 1.5 mm
-Maximum magnetic field: 0.05 T
-BM1, Drift tube, BM2 bias: -600 ÷ +600 V

## Slide 31
BINP
First experimental results
Primary
Secondary
Secondary - Primary
BM1
BM2
S

## Slide 32
BINP
Flat
C
D
M
BM1
Drift tube
BM2
B
10
325
60
S

## Slide 33
BINP
SEY vs extracting bias Ubm2
C
D
M
BM1
Drift tube
BM2
B
10
325
60
S

## Slide 34
BINP
C
D
M
BM1
Drift tube
BM2
B
10
325
60
S
Energy distribution
z
0
Ubm1=Udrift=Ubm2=5V
where Ez=Esz+Ubm2 and delay t’ is defined as:

## Slide 35
BINP
C
D
M
BM1
Drift tube
BM2
B
10
325
60
S
Energy distribution

## Slide 36
BINP
everywhere
SEE in magnetic field (JINR)
How to separate primary and secondary electrons in DC mode?
e - gun
Sample
Collector
Separation of primary and secondary electrons takes place in crossing space
I. Meshkov

## Slide 37
BINP
References
[1] G. Budker, G. Dimov, and V. Dudnikov, in Proceedings of the International Symposium on Electron and Positron Storage Rings, Saclay, France, 1966 (Saclay, Paris, 1966), Article No. VIII-6-1.
[2] G. Budker, G. Dimov, and V. Dudnikov, Sov. Atomic. Energy 22, 384 (1967).
[3] V. Dudnikov, in Proceedings of the Particle Accelerator Conference, Chicago, 2001 (IEEE, Piscataway, NJ, 2001).
[4] G. Budker, G. Dimov, V. Dudnikov, and V. Shamovsky, in Proceedings of the International Conference on High Energy Accelerators, ambridge, MA, 1967 (CEA, Cambridge, MA, 1967).
[5] Yu. I. Belchenko, G. Budker, G. E. Derevyankin, G. Dimov, V. Dudnikov, G.V. Roslyakov, V. E. Chupriyanov, and V. G. Shamovsky, in roceedings of the Xth International Conference on Particle Accelerators, Protvino, 1977 (Protvino Institute of High Energy Physics, Serpukhovy, 1977), Vol. 2, p. 287.
[6] B.V. Chirikov, Sov. At. Energy 19, 1149 (1965).
[7] J. H. Martin, R. A. Winje, R. H. Hilden, and F. E. Mills, in Proceedings of the 5th International Conference on High Energy Accelerators, Frascati, 1965 (CNEN, Rome, 1966), p. 47.
[8] J. H. Martin, R. A. Winje, and R. C. Trendler, in Proceedings of the International Conference on High Energy Accelerators, Cambridge, MA, 1967 (Ref. [15]), p. 356. [9] E. C. Raka, in Proceedings of the International Conference on High Energy Accelerators, Cambridge, MA, 1967 (Ref. [15]), p. 428.
[10] K. Ohmi, Phys. Rev. Lett. 75, 1526 (1995).
[11] M. A. Furman and G. R. Lambertson, in Proceedings of the International Workshop on Multibunch Instabilities in Future Electron and Positron Accelerators (MBI’97), Tsukuba, edited by Y.H.
Chin, KEK Proceedings Vol. 97–17 (KEK, Tsukuba, 1997).
[9] K. Ohmi, in Proceedings of the International Workshop on Multibunch Instabilities in Future Electron and Positron Accelerators (MBI’97), Tsukuba (Ref. [8]).
[10] S. S. Win, H. Fukuma, K. Ohmi, and S.-I. Kurokawa, in Proceedings of ECLOUD’02, Geneva (Ref. [6]).
[11] D. Schulte, in Proceedings of ECLOUD’04, Napa, CA (Ref. [1])
[12] F. Zimmermann, “Review of single bunch instabilities driven by an electron cloud”, PHYSICAL REVIEW SPECIAL TOPICS - ACCELERATORS AND BEAMS, 7, 124801 (2004)
[13] K.Ohmi and F.Zimmermann. Head-Tail Instability Caused by Electron Clouds in Positron Storage Rings. Phys. Rev. Lett. 85, 3821, 2000.
[13] B.Henrist, N.Hilleret, C.Scheuerlein, M.Taborelli, G.Vorlaufer. The variation of the secondary electron yield and of the desorption yield of copper under electron bombardment: origin and impact on the conditioning of the LHC. Proceedings of EPAC 2002, pp. 2553-2555, Paris, France.
[14] R.Cimino, I.R.Collins, M.A.Furman, M.Pivi, F.Ruggiero, G.Rumolo, and F.Zimmermann. Can Low-Energy Electrons Affect High-Energy Physics Accelerators? Phys. Rev. Lett. 93, 014801, 2004.
[15] B.Henrist, N.Hilleret, M.Jimenez, C.Scheuerlein, M.Taborelli, G.Vorlaufer. Secondary electron emission data for the simulation of electron cloud. Proc. Mini Workshop on Electron Cloud Simulations for Proton and Positron Beams (ECLOUD'02), Geneva, 15-18 April 2002, pp. 75-78, CERN Report: CERN-2002-001, 2002.
[15] J.M.Jimenez, G.Arduini, P.Collier, G.Ferioli, B.Henrist, N.Hilleret, L.Jensen, K.Weiss, F.Zimmermann. Electron cloud with LHC-type beams in the SPS: A review of three years of measurements. Proc. Mini Workshop on Electron Cloud Simulations for Proton and Positron Beams (ECLOUD'02), Geneva, Switzerland, 15-18 Apr 2002, pp. 17-18, CERN Yellow Report: CERN-2002-001, 2002.
[16] R.Cimino, I.R.Collins, V.Baglin. VUV photoemission studies of candidate Large Hadron Collider vacuum chamber materials. Phisical rewiew special topics – accelerator and beams, v.2, 063201 (1999).
[17].V.V.Anashin, I.R.Collins, R.V.Dostovalov, N.V.Fedorov, O.Gröbner, A.A.Krasnov, O.B.Malyshev and E.E.Pyata. Magnetic and electric field effects on the photoelectron emission from LHC beam screen material. Vacuum, ISSN 0042207X, p. 255-260, vol. 60, N 1-2, January-February 2001.
[18] A.A.Krasnov. Molecular pumping properties of the LHC arc beam pipe and effective secondary electron emission from Cu surface with artificial roughness. Vacuum, vol. 73, pp. 195-199 (2004).
[19] A. Kulikov et al, “The Electron-Cloud Instability at PEP-II,” Proc. 2001 Particle Accelerator Conference (2001), p. 1903S.
[20] S. Heifets, “Electron Cloud at High Beam Currents,” Proc. ECLOUD02 Geneva (2002)
[21] F. Zimmermann, LHC Project Report 95 (1997).
[22] R. Valizadeh, A. Hannah, O.B. Malyshev, T. Sian, J. Mutch, N Sykes, Y. Dan, J.S. Colligon, V. Dhanak, MULTIPACTOR SUPPRESSION BY LASER ABLATION SURFACE ENGINEERING FOR SPACE APPLICATIONS, IPAC2019, Melbourne, Australia, ISBN: 978-3-95450-208-0, JACoW Publishing, doi:10.18429/JACoW-IPAC2019-TUPMP051
[23] E. Belli,* P. Costa Pinto, G. Rumolo, A. Sapountzis, T. Sinkovits, M. Taborelli, B. Spataro, M. Zobov, G. Castorina and M. Migliorati. Electron cloud buildup and impedance effects on beam dynamics in the Future Circular e + e − Collider and experimental characterization of thin TiZrV vacuum chamber coatings, PHYSICAL REVIEW ACCELERATORS AND BEAMS 21, 111002 (2018)
[24] P. Costa Pinto, A. Bellunato, T. Basso, Paul Edwards, M.Mensi, A. Sublet, M. Taborelli, IMPLEMENTATION OF CARBON THIN FILM COATINGS IN THE SUPER PROTON SYNCHROTRON (SPS) FOR ELECTRON CLOUD MITIGATION, Proceedings of IPAC2014, Dresden, Germany, WEPRI043.
[25] ECLOUD’12, https://agenda.infn.it/event/4303/timetable/?view=standard
[26] ECLOUD’18, https://agenda.infn.it/event/13351/timetable/#20180603
[27] ICFA mini-Workshop on "Mitigation of Coherent Beam Instabilities in particle accelerators" MCBI 2019, https://indico.cern.ch/event/775147/timetable/#20190923.detailed
[28] О. Орлов, И.Н. Мешков и др. Стенд по измерению вторичной электрон-электронной эмиссии, XIII Международный научный семинар памяти профессора В. П. Саранцева «Проблемы коллайдеров и ускорителей заряженных частиц» 3-8 сентября 2019 г.

## Slide 38: Thanks for your attention

## Slide 39: SEY model
The predictions from e-cloud simulations rely on confidence in the SEY curves used
Cimino-Collins SEY model, parameterising measured SEY curves of the LHC beam screens:
Dependence on incidence angle:
with:
with:
R. Cimino et al., Phys. Rev. Lett. 93, 014801

## Slide 40: Electron cloud in the LHC
To fill LHC with 25 ns beams in presence of electron cloud it has been necessary to run with high chromaticity and octupole currents throughout the cycle
More scrubbing has been accumulated while running for physics with 25 ns beams during 2015, 2016 and 2017
2015
2016
2017
2018
Notes: In ‘stable’ beam conditions, scrubbing can be directly seen through the decrease of the normalised heat load in the LHC arcs

## Slide 41: Electron cloud in the LHC: the future
In the High Luminosity (HL) era, LHC will also run with double intensity and brightness
Dependence on bunch intensity seems to be favorable in both dipoles and quadrupoles for low enough SEY values (pending experimental verification)
Arc quadrupoles
Arc dipoles
Current value
Future value
Current value
Future value

## Slide 42
Energy spectrum
- Electron kicker detector:
Analyser of the energy spectrum of the electrons
Elena Buratin

## Slide 43: LE-SEY Cu, Ag, Au
Luis Gonzalez
LNF-INFN
E-Cloud’18 June 5th 2018
CLEAN SURFACES
-SEY drastically decreases at impinging energies close to zero.
-Different work functions were measured for each clean surface, in good agreement with literature results*
“AS RECEIVED” SURFACES
-LE-SEY remain above 0.5 for all “as received” surfaces.
-Similar behaviour of Ag and Au – Including WF does not change with respect CLEAN.
-Cu shows a different trend and an increase in the WF
WF = 4.4
WF = 5.3
WF = 4.6
Ag
Au
Cu
ΔWF
3
A. Kawano, Progr. Surf. Sci. 83, 1-165 (2008).
*
SEY From Noble Metals