## Slide 1
Super-conducting magnets
for ring accelerators

## Slide 2
Dr. Martin N. Wilson
Dr. Hamlet Khodzhibagiyan

## Slide 3
Constant orbit during acceleration
B increase with time
ω and ωRF increase with energy
RF generator
RF cavity
B
injection
extraction
r
R=C/2π
E
Bending
magnet
bending radius
Modern accelerators:
the synchrotron
the cyclotron
…for high energy physics…and for something else…
beam energy record-holder (LHC)
beam power record-holder (PSI cyclotron)
ring cyclic accelerators: synchrotrons

## Slide 4
„Living legendes“: PS and AGS
Alternating Gradient Synchrotron under construction, c. 1957
AGS @ Brookhaven 33 GeV p, 1960
CERN 1959, PS
PS @ CERN 28 GeV p, 1959
Both are still operational today
Synchrotrons

## Slide 5
Colliders
Tevatron, Batavia, Illinois, USA
pp-bar
Energy: 1 TeV
Circumference 6.3 km
Average beam current: 0.02-0.06 A
Magnetic dipole field max 4.4 T
1983-2011

## Slide 6
Colliders
e p
Energy: 0.03 TeV (e), 0.92 TeV (p)
Circumference 6.3 km
Average beam current: 0.04-0.09 A
Magnetic dipole field max 5 T
HERA, Hamburg, Germany
Lepton-proton
collider
1992-2007

## Slide 7
RHIC:
Relativistic
Heavy Ion
Collider
Colliders
Brookhaven Nat’l Labs, Long Island, USA
pp, Au Au, Cu Cu, d Au
Energy: 0.1TeV/n
Circumference 3.8 km
Average beam current: 0.05-0.1 A
Magnetic dipole field max 3.5 T
2001--

## Slide 8
Colliders
CERN Large Hadron Collider (LHC)
pp, Pb Pb
Energy: 7 / 2.76 TeV/n
Circumference 26.7 km
Average beam current: 0.6 / 0.06 A
Magnetic dipole field max 8.3 T
2007--

## Slide 9
the base of accelerators’ business
(bring all the injected particles to the target)
Stability of the particles’ motion
equation of particle motion in the electro-magnetic field of accelerator/collider

## Slide 10
Stability of the particles’ motion
(bring all the injected particles to the target)
Take
particles from ion source (injector)
Accelerate, store,
collide
Extract
to target
Ring accelerator
Bend in a circle
Focus around ideal orbit
Accelerate, group
Main
accelerator systems
Dipole
magnets
Quadrupole
magnets
RF-stations
Collider
B
injection
extraction
r
R=C/2π
E
Bending
magnet
bending radius

## Slide 11
Magnetic field strength
??
2nd-Newton law
3rd -Newton law
Bρ-magnetic rigidity – ability to keep the particle with P on the circular orbit…

## Slide 12
Why use superconducting magnets
??

## Slide 13
Superconductivity
high current density =>
higher magnetic fields (than in “warm” magnets)
need no power for the magnets, only for its cooling)
smaller, lighter, cheaper magnets
smaller, lighter, cheaper accelerators
smaller running costs
Superconductivity is the set of physical properties observed in certain materials, wherein electrical resistance vanishes and from which magnetic flux fields are expelled.

## Slide 14
Superconductivity – brief history
H. Kamerlingh-Onnes (right) and his assistant Gerrit Flim (left) in their lab. 1911.
4.2 K ≈ - 269°C

## Slide 15
Superconductivity – brief history
1933 – Deutsch physicists Walther Meissner and Robert Ochsenfeld discover that not strong magnetic field does not penetrate into the body of the superconductors – diamagnetic property of superconductors
(T<Tc – the currents flux occur in thin surface layer of the superconductor. Its magnetic field compensate external magnetic field)
1935 – first theoretical works on SC by Heinz and Frits London
(suggest to consider superconductivity as macroscopic quantum effect )
1950 Ginsburg and Landau proposed a macroscopic theory for SC
Meissner effect
Magnetic levitation

## Slide 16
1957 – BCS - theory
Pairs can drift through the crystal lattice without energy loss on interactions with atoms
- works only at LOW temperature !
Superconductivity – brief history
John Bardeen
Leon N Cooper
John Robert Schrieffer

## Slide 17
Superconductivity – Two types of conductors
Type-1 superconductor completely expels magnetic field from its interior by acting as a perfect diamagnetic
Type-2 superconductor: the magnetic field is confined to filamentary structure
more than 20 pure metals
(mercury, lead, titanium)
usually they have not good
conductivity @ room temperature
Bc ~ 10^-3 – 10^-2 T
not useful for sc-magnets
several hundreds materials:
(alloys, intermetallic, ceramic)
Bc ~ 10 – 10^2 T
NbTi Tc=9.8 K Bc=10 T
Nb3Sn Tc=18 K Bc=25
OK for sc-magnets

## Slide 18
Superconductivity - Critical field
Type-1
Type-2

## Slide 19
Superconductivity – critical surface
Martin Wilson lecture

## Slide 20
Superconductivity – critical line for 4.2 K

## Slide 21
High-temperature superconductors (abbreviated high-Tc or HTS) are materials that behave as superconductors at unusually high temperatures.
The first high-Tc superconductor was discovered in 1986 by IBM researchers Georg Bednorz and K. Alex Müller, who were awarded the 1987 Nobel Prize in Physics .
Superconductivity – high temperature superconductors
Whereas "ordinary" or metallic superconductors usually have transition temperatures (temperatures below which they are superconductive) below 30 K (−243.2 °C) and must be cooled using liquid helium in order to achieve superconductivity, HTS have been observed with transition temperatures as high as 138 K (−135 °C), and can be cooled to superconductivity using liquid nitrogen.
LHe
LNi

## Slide 22
certain compounds of copper and oxygen (so-called "cuprates") were known to have HTS properties, and the term high-temperature superconductor was used interchangeably with cuprate superconductor for compounds such as bismuth strontium calcium copper oxide (BSCCO) and yttrium barium copper oxide (YBCO).
Yttrium barium copper oxide (YBCO) is a family of crystalline chemical compounds.
Many YBCO compounds have the general formula YBa2Cu3O7−x (also known as Y123), although materials with other Y:Ba:Cu ratios exist, such as YBa2Cu4Oy (Y124) or Y2Ba4Cu7Oy (Y247).
Superconductivity – high temperature superconductors

## Slide 23
Superconductivity – Two types of conductors
chart is not completed…

## Slide 24
Martin Wilson lecture
Magnetic field: ways to create and form them – (1) - iron

## Slide 25
Magnetic field: ways to create and form them – (2) - solenoids
Martin Wilson lecture

## Slide 26
Magnetic field:
dipoles
quadrupoles

## Slide 27
Magnetic field: ways to create and form them – (3) – transverse uniform
fields
Martin Wilson lecture

## Slide 28
Magnetic field: ways to create and form them – dipole field from overlapping cylinders with current => Cosine theta magnets
Martin Wilson lecture

## Slide 29
ideal shape of current area = cross-section of ellipses
real cross-section of «cos θ» coils
Magnetic field: ways to create and form them – dipole field from overlapping cylinders with current => Cosine theta magnets

## Slide 30
Magnetic field: ways to create and form them –cosine theta magnets
Martin Wilson lecture

## Slide 31
Martin Wilson lecture
Magnetic field: ways to create and form them – (4) – transverse gradient
fields

## Slide 32
Magnetic field: ways to create and form them – (5) – super ferric magnets: sc-coil + iron for the field forming
uniform (dipole) field
gradient (quadrupole) field
Nuclotron - magnets

## Slide 33
Magnetic field: ways to create and form them – engineering current density
Martin Wilson lecture

## Slide 34
Magnetic field: ways to create and form them – engineering current density
Martin Wilson lecture

## Slide 35
Magnetic field: ways to create and form them – engineering current density
Normal conductors
Je ≈ 150 A/mm^2

## Slide 36
Superconductivity – the last slide
3 kinds of superconductors
  - type 1 – useless for sc-magnets production
  - type 2 – OK for sc-magnets
  - HTS – good for high field and temperature but current density still is a problem in high magnetic field
type 2 and HTS – used for sc-magnets production
all existing sc-accelerators up to date use NbTi
engineering current density is a crucial factor in the magnet design and economy

## Slide 37
Superconducting
Materials
Superconducting
Magnets
  high current wires
  high current tapes
  high current cables
SC-magnets production

## Slide 39
SC-magnets production
“Nuclotron” - cable

## Slide 40
SC-magnets production
LHC-sc-wires (for Rutherford cable)

## Slide 41
SC-magnets production
NbTi----SC-wires production technology
1 Cu lid
2 NbTi billet
3 Cu extrusion can
4 evacuate and seal
5 heat treatment
6 extrude
7 single core rod
8 hexagonal rod
9 stack
10 evacuate and seal
11 pre-heat and extrude
12 multi-core rod
13 cold draw
14 multi-core wire
15 heat treatment
16 twist
17 anneal
18 insulate
19 test
20 dispatch
multifilament wires have good current carrying capability 100-1000A
accelerators sc-magnets require ability to operate with 10kA-100kA currents
Je≈500 A/mm^2

## Slide 42
Magnets
Rutherford cable
Nuclotron cable
1 – CuNi tube
2 –SC-wire
3 – NICr-wire
4 – Isolation
5- Isolation

## Slide 43
Rutherford cable
SC-magnets production
production of Rutherford cable

## Slide 44
SC-magnets production
Rutherford cable machine @ CERN

## Slide 45
SC-magnets production
winding of LHC dipole

## Slide 47
SC-magnets production
adding the iron

## Slide 48
SC-magnets production
Nuclotron- cable machine @ JINR

## Slide 49
SC-magnets production
cs-coils production for Nuclotron- magnets

## Slide 50
SC-magnets production
super ferric Nuclotron- magnets assembly

## Slide 51
SC-magnets’ physics
quench -
sudden, unexpected and unrecoverable transition of superconductor in the device (magnet, bus bar, current lead…) to the normal state.
enforce the convention of the stored energy into heat (mostly)
this can lead to the damage of the device
use magnet quench protection system !!!
quench protection – the art of preventing of any damages of sc-magnet concerned with the phenomena or its serving after the quench occurs

## Slide 52
SC-magnets’ physics
Critical surface and magnet load line
- relates magnet field to its current

## Slide 53
SC-magnets’ physics
why do magnets quench ?
Internal to the magnet:
wire movement, resin cracking, shearing on coil windings
accidents, helium leaks in cooling tubes, leaks in vacuum parts
External to the magnet:
radiation, damaged cryo-supply-lines, sensors, valves, flow meters, earth-quake
Specific heat of the all substances falls with temperature
(~2000 times less @ 4.5 K than @ room temperature)
smallest energy release can rise superconductor temperature above the critical surface
conductors of the magnets are stressed by magnetic forces – sometimes they move suddenly under this force – and mechanical stress come out
this movement => frictional heating
for NbTi 10μm motion can raise local temp. to 7.5 K

## Slide 54
Amount of energy released

## Slide 55
SC-magnets’ physics
Degraded performance and “training” of the magnets

## Slide 57
Stable operating condition
External perturbation:
flux jump
conductor motions
insulation cracks
AC loss
heat leaks
nuclear
…
Approach Jc(T, B, …)
Quench
yes
no
Stable operating condition
Transition to normal state and Joule heat generation in current sharing
heat generation >
heat removal
stability analysis
and design
Heat balance
Perturbation spectrum
Magnet stability and quench

## Slide 58
Perturbation overview

## Slide 59
T
Jc
B
14.5 T
9 K
typical NbTi
5 T
4.2 K
3000 A/mm2
operating plane
J
B
Jop
Bop
Bc
Bmax
Jc
Margin in critical current
Tcs
J
T
Jop
Top
Tc
Margin in temperature
Margin along the loadline
Jop/JC ≈ 0.5
Bop/Bmax ≈ 0.8
Tcs-Top ≈ 1…2 K
SC-magnets
choose of operation parameters

## Slide 60
SC-magnets
examples

## Slide 61
SC-magnets
examples
3.45 T
NbTi Rutherford cable
a single-layer coil
cold iron as both yoke and collar.
forced-flow helium @ 4.6K
The arc dipoles have 8cm aperture and 9.7m length
RHIC

## Slide 62
Developed at 1980-th…
“Nuclotron”-cable
SC-magnets for synchrotrons
SC-cable
“Nuclotron”- magnets

## Slide 63
Nuclotron technology
Iron Yoke
SC coil
Thermal shield
Vacuum shell
Beam Pipe
Support
Current:
~10 000 А
4.2 K
Cooled by LHe

## Slide 64
First Superconducting heavy ion accelerator
Nuclotron – Superconducting Synchrotron
operation since 1993
Thank you

## Slide 69
Case Study___task_1

## Slide 70
Case Study___task_2
What is the engineering current density Je of the NICA collider dipole magnet ?
Exclude not necessary data…

## Slide 71
Case Study___task_3
What altitude must take hovering in place flying-cow (500kg) to have the same energy as stored in NICA collider magnet with magnetic field 1.8 T ?
aperture height = 70mm
N-coil-turns = 10
magnet inductance = 450 μH

## Slide 72: Сверхпроводящие провода и кабели, технология их изготовления
Ic/I0 в зависимости от dB/dt для двух типов кабелей, применяемых в обмотках магнитов для синхротронов.

## Slide 73
Engineering critical current density versus magnetic field for low temperature superconductor wires, high temperature superconductor wires and tapes and MgB 2 wires.

## Slide 74
Luca Bottura lecture
Superconductivity – critical surface

## Slide 77
Tev,76 mm
4.5T,4.2K
1980’s
1990’s
2000’s
2010’s
2020’s ?
Superconducting magnets
Maximum energy and 70% of price are determined by the magnets

## Slide 78
SC-magnets
examples