## Slide 1
ELCHEM_NS
M.V. Avdeev, I.A. Bobrikov, I.V. Gapon, A.I. Ivankov, V.I. Petrenko, D.V. Soloviev, S.V. Sumnikov, A.V. Tomchuk (FLNP JINR)
D.M. Itkis (MSU)
F.S. Napolsky (Dubna University)
Leader: Mikhail V. Avdeev
Leader’s assistants: Ivan A. Bobrikov, Viktor I. Petrenko
A system for neutron operando monitoring and diagnostics of materials and interfaces for electrochemical energy storage devices at the IBR-2 reactor
Theme 04-4-1121-2015/2020
Project
Current state: June 2019
2018-2020

## Slide 2
Study of operating electrodes and interfaces (operando mode)
Main objective
Growth of dendrites
Negative
Electrode
Formation of solid electrolyte interphase (SEI)
Lithium intercalation
Structural Research of Electrochemical Accumulators
Electrode structure evolution
Interface evolution

## Slide 3
Project objectives
Development of common approaches to the effective use of neutron scattering methods (diffraction, reflectometry, small-angle scattering) in the analysis of the structural evolution of various types of electrodes and interfaces for electrochemical energy storage devices during operation (operando mode).
Design and development of specialized electrochemical cells and sample environment systems for operando research in neutron scattering experiments.

## Slide 4
Diffraction
Reflectometry
Small-angle
scattering
Si1-yMy
Сu/Ni/Ti
Si
n
Si1-yMy
Сu/Ni/Ti
Si
n
Si1-yMy
Si
n
Сu/Ni/Ti
Electrolyte
Electrolyte
Electrolyte
ELCHEM_NS Project

## Slide 5
Neutron Difftraction (ND):
HRFD, RTD
Small-Angle Neutron Scattering (SANS):
YuMO
Neutron Reflectometry (NR):
GRAINS
YuMO (SANS)
HRFD, RTD (ND)
GRAINS (NR)
Instruments involved
IBR-2 pulsed reactor, FLNP JINR
ELCHEM_NS Project

## Slide 6
Collaboration
Dubna University/ Engineering Center
Test assembly and electrochemical measurements of the cells and sample environment systems for neutron scattering experiments;
Electrochemical support of neutron scattering experiments.
MSU
Design and draft projects:
Electrochemical cells for neutron scattering experiments;
Sample environment systems for in situ neutron scattering experiments.
Scientific support.
FLNP JINR
Manufacturing:
Electrochemical cells for neutron scattering experiments;
Sample environment systems for in situ neutron scattering experiments.
Organization and support of R&D line for deposition and polishing of crystalline substrates;
Preparation and conduct of neutron scattering experiments at IBR-2;
Diagnostics and special treatment of samples after neutron scattering experiments.
ELCHEM_NS Project

## Slide 7
 |  | 2018 | 2019 | 2019
ND | Specialized Li-ion cells for multiple charge/discharge |  |  | 
 | Sample environment system for operando experiments |  |  | 
 | Multichannel cell charge/discharge line |  |  | 
NR | Specialized Li-ion cells with heterogeneous electrodes |  |  | 
 | Sample environment system for operando experiments |  |  | 
 | System for post experiment sample diagnostics, storage and treatment |  |  | 
SANS | Specialized Li-air cells for multiple charge/discharge |  |  | 
 | Sample environment system for ex-situ experiments |  |  | 
 | Sample environment system for operando experiments |  |  | 
Schedule

## Slide 8
NCA/C pack loses 30% capacity after 700 Cycles,
Current leakage ~1μA per an hour for 500 mAh cell
Cell upgrade:
Old type PTFE case was replaced with the PEEK type case.
Inner case construction was modified.
Beam attenuator (BN plate) was replaced with B4С.
To make seals fitted to the PEEK cases the press forms were constructed and were used for producing numerical seals.
Results:
less active materials are used, cells are more chemically stable and easier to assembly.
tests and real experiments with electrode and solid electrolyte materials have been done.
Bobrikov et al, 2019
Neutron diffraction cell development
Practical cathode material LiNi0.8Co0.15Al0.05O2 (NCA)

## Slide 9
Neutron diffraction cell development
Bobrikov I.A., Samoylova N.Y., Ivanshina O.Y., Vasin R.N., Sumnikov S.V., Kornieieva K.A., Balagurov A.M. Electrochimica Acta. 2018. Т. 265. С. 726-735
Maximum Capacity ~400 Wh/kg
ND cell

## Slide 10
Bobrikov et al, 2019
Electrochemical laboratory development
New Equipment:
Metrohm Fischer titrator 917
Despergator up to 25000 rpm
Potentiostat BIOLOGIC SP-300
High temperature inert gas furnace up to 1200˚ C
Storage of d-electrolytes for neutron scattering experiments (DMC, PC, EC)
3-axes for non-standard samples and electrochemical cells at X-ray diffractometer

## Slide 11
X-ray diffractometer
XRD experiments
Malvern PANalytical Emyrean
X-Ray operando diffraction scan of electrochemical cell
Bobrikov et al, 2019
Diffraction pattern evolution

## Slide 12
NCA (+) opposite to graphite (-)
Phase stability during operation.
Trace of structural changes in electrodes
+
-
NCA (+) opposite to Li (-)
Phase stability during first cycle.
Trace of structural changes in cathode
+
-
From model to real systems
Notes: For that reason we have studied two systems: 1) real commercial battery based on NCA cathode for third and consequent cycles. We could not study the first cycle in commercial battery because first cycle is a procedure which is always done at a factory. 2) special designed electrochemical cell to check the same but at first cycle after cell assembling

## Slide 13
U=2.5-4.33 V
C=3100mAh
Δt = 1.5-5 min
Operando Neutron Diffraction study of industrial batteries
C=3105 mAh
C=2990 mAh
NCA
LiC6
Cт=278.9 mAh/g
mcathode=14.6 g
C=1852 mAh
1 (101)
2 1 (003)
LixNi0.8Co0.15Al0.05O2
Notes: Commercial battery 18650 type as it is with capacity 3100 mAh has been measured at different C-rate. Exposition time was from 1.5 up to 5 minutes for every diffraction pattern in high intensity. On these color picture you see diffraction pattern evolution in dependence on time or state of charge. Red color charge-discharge curve. Here I would like to mark so call cathode window where only cathode’s peaks are visualized and the same for anode window. One can see that without dependence on C-rate (speed of charge-discharge) there are significant changes of cathode and anode crystal structures. Тайпикал.

## Slide 14
Optimization of reflectometry cells and sample environment system
Synthesis of complex heterogeneous film electrodes
Complimentary diagnostics of electrode surfaces after neutron scattering experiments
Processing of crystalline substrates after neutron scattering experiments
Remote control
Principal scheme of experiment
Neutron Reflectometry
Li-ion batteries with metal anodes and liquid electrolytes

## Slide 15
Neutron Reflectometry Cell
PEEK case
Single crystal block Si
Counter electrode
Seal groove
RE connector
WE/CE connectors
Pressing plates (Al)
Electrolyte filling

## Slide 16
Neutron Reflectometry
z
M.V. Avdeev, A.A. Rulev, E.E. Ushakova, Ye.N. Kosiachkin, V.I. Petrenko, I.V. Gapon, E.Yu. Kataev, V.A. Matveev, L.V. Yashina, D.M. Itkis, Appl. Surf. Sci. 486 (2019) 287-291
Formation of Solid Electrolyte Interphase (SEI)
on plane metal anodes
Si
Ti
Cu

## Slide 17
Neutron Reflectometry
Effect of concentrating electrolyte on interface structure
0.1M LiClO4/d-PC
5M LiTFSI/d-PC
Visual control at micron-size scale is required!
Solution under consideration –
cell with transparent window
(control of dendrite growth and
subsidiary gas bubble formation)

## Slide 18
Neutron Reflectometry
V. I. Petrenko, Ye. N. Kosiachkin, L. A. Bulavin, M. V. Avdeev, J. Surf. Investigation (2019) in press
Maximization of
d2, nm
2, 10-6 Å-2
2 map
(electrode Cu, 50 nm, best choice!)
Electrode
Electrolyte
Interface depth
SLD, 10-6 Å-2
Interface depth
SLD, 10-6 Å-2
Electrode
Electrolyte
Adsorption layer
Optimization of electrode structure
d1
1
s
SLD, 10-6 Å-2
Optimal value

## Slide 19
Neutron Reflectometry
Optimization of electrode structure: minimizing Ti-lyer
Magnetron Sputtering Facility, MIRROTRON Ltd., Budapest, Hungary
NR
GINA, BNC, Budapest
XRR
Malvern PANalytical,
FLNP JINR, Dubna
Si(crystal)/
/Ti [0-10 nm ]Cu[10-50 nm]
Uniform deposition of Ti down to thickness of 1 nm
Good adhesion Cu on Si without Ti; low stability in time
Best choice  Cu electrode, 50 nm thick
Ti [5 nm]
Ti [1 nm]
Ti [0 nm]

## Slide 20
Neutron Reflectometry
Optimization of electrode structure: quasi-homogeneous electrode
Si (crystal)/[Ti 0.5 nm/NiMo 1.0 nm]20
Si (crystal)/[Ti 0.7 nm/NiMo 0.7 nm]20
NR
Homogeneous approximation
GINA, BNC, Budapest
Deposition by MIRROTRON Ltd.,
Budapest
XRR
Malvern PANalytical,
FLNP JINR, Dubna
d1 = 32.7 (30) nm
1 = 6.47 (6.49)  10-6 Å-2
Si (crystal)/[Ti 0.5 nm/NiMo 1.0 nm]20
d1 = 31.3 (30) nm
1 = 51.7 (54.9)  10-6 Å-2
Uniform deposition at thickness 0.5 nm
Homogeneous approximation works well (systematic errors < 10%)

## Slide 21
Small-Angle Neutron Scattering
Li-O batteries (Maximum Theoretical Capacity ~900 Wh/kg)
Parasitic effect 
passivation of porous carbon electrode by Li2O2

## Slide 22
Small-Angle Neutron Scattering
Ex-situ studies
Engineering Center, State University ‘Dubna’;
Chemical Department, Moscow State University
1 cm
Background
(quartz cell)
Dry electrode
Soaked electrode
Laboratory Electrochemical Cell
Samples for SANS
1 cm

## Slide 23
YuMO, IBR-2 (Dubna)
Small-Angle Neutron Scattering
Ex-situ studies
T.K. Zakharchenko, M.V. Avdeev, A.V. Sergeev, A.V. Chertovich, O.I. Ivankov, V.I. Petrenko, Y. Shao-Horn, L.V. Yashina, D.M. Itkis, Nanoscale 11 (2019) 6838-6845

## Slide 24
Small-angle Neutron Scattering
Requirements to SANS cell
low coherent scattering from separators;
sufficiently thick carbon electrode;
sufficiently thin separator, electrolyte region and lithium electrode;
low incoherent background from all components;
air-tight construction;
O2
O2
Lithium
Separator
+
-
Carbon electrode
n
Electrolyte
In situ cell
Choice of materials
YuMO, IBR-2 (Dubna)

## Slide 25
Small-angle Neutron Scattering
In situ cell
Sapphire (0.8 mm)
Sealing (Torr Seal glue)
Neutron beam
Sapphire (0.8 mm)
Spring for WE
Spring for CE
Cu ring for CE
Insulating collar
Assembled chamber
Mounting rods
Beam window ( 13 mm)
Holes for flange rods
Cathode : SIGRACET Carbon paper (0.32 mm)
Separator: Dupont polyimide (0.02 mm)
Anode: Li foil (0.2 mm) on Al support (0.5 mm)
Windows: Sapphire (0.8 mm)

## Slide 26
Small-angle Neutron Scattering
In situ cell
O2
Planned Tests –
October 2019

## Slide 27
Model real-time experiments
YuMO, IBR-2 (Dubna)
Evaporation of electrolyte (1 M LiTFSI in MeCN) from carbon electrode
Minimal time step ~10 min
Small-angle Neutron Scattering

## Slide 28
Practical activities
Cooperation Agreement with Engineering Incubator Ltd. (Dubna, Moscow Reg.) “Studies of the influence of the microstructure of electrodes of chemical current sources on their functional characteristics”
Cooperation Agreement with LITION Ltd. (Dubna, Moscow Reg.) “Influence of evolution of electrode structures on functional characteristics of chemical current sources”
Visit of LG Technology Center Moscow (LGTCM) delegation to JINR, Dubna, October 1, 2018

## Slide 29
Participants
FLNP JINR
M.V. Avdeev, V.I. Petrenko, A.V. Tomchuk, I.V. Gapon, Y.N. Kosiachkin, I.A. Bobrykov, S.V. Sumnikov, A.M. Balagurov, O.Yu. Ivanshina, N.Yu. Samoylova, D.V. Soloviev, A.I. Ivankov
MSU, Moscow
D.M. Itkis, A.A. Rulev, T.K. Zakharchenko, L.V. Yashina
Dubna University, Dubna
F.S. Napolsky, E.E. Ushakova, M. Erdauletov, V.A. Krivchenko

## Slide 30
Conclusions
ND
Specialized Li-ion cells for multiple charge/discharge
Sample environment system for operando experiments
NR
Specialized Li-ion cells with heterogeneous electrodes/liquid electrolytes
SANS
Prototype of specialized Li-air cells for multiple charge/discharge
Sample environment system for ex-situ experiments
Project implementation is in accordance with plan: