## Slide 1
Atomistic simulations of swift heavy ion tracks in Al2O3
R. A. Rymzhanov1, N.A. Medvedev2, V.A. Skuratov1 and A.E.Volkov1,3,4
1 FLNR, JINR, Dubna, Russia
2Institute of Physics, Czech Academy of Sciences, Prague 8, Czech Republic
3NRC”Kurchatov Institute”, Moscow, Russia
4LPI of the Russian Academy of Sciences, Moscow, Russia
BIOMAT-2016

## Slide 2
Swift heavy ions (SHI)
Е > 1 MeV/nucl, M > 4mp
Maximal energy of generated electrons ~10 keV
Simulate the influence of fission fragments and cosmic rays on material properties
Lose energy to electronic stopping

## Slide 3
Practical application of SHI
Membranes and nanowires
GSI, Darmstadt
GSI, Darmstadt
Modification of nanoclusters
Kluth et al, REI-2007, Au in SiO2
Nanostructuring
W.Bolse
200 MeV Au
B. Canut et al., NIMB 245 (2006) 327)
Interlayer transitions
Quantum dots
P. Gaiduk et al., Phys. Rev. B66 045316 (2002)
SixGe1-x
1.3 GeV U

## Slide 4
Fundamental interest
Marek Skupinski (Uppsala)
The relaxation of excitation induced by SHI cannot be described within macroscopic approaches
10-16 10-15 10-14 10-13 10-12 10-11 10-10 10-9 t (sec)
lattice
electrons
SHI
Nanometric spatial and femto-picosecond temporal scales
Extremely high level of material excitation

## Slide 5
Why Al2O3?
Good material for modelling
Radiation resistant material (Perspective for applications in nuclear energetics)
X-[100]
[010]
Y-[120]

## Slide 6
Combined experimental and numerical investigation
Irradiation by Xe, Bi ions
(FLNR, Dubna: IC-100, U-400M)
Experimental
Theoretical
TEM microscopy and analysis
(CHRTEM, SA)
Monte-Carlo model of
electron subsystem excitation
Energy transfer to the lattice
Molecular Dynamics simulation
(LAMMPS code)
Verification of the model
Explanation of observed results
P.N. Terekhin, R.A. Rymzhanov et al.
NIMB 254 (2015) 200–204

## Slide 7
TREKIS: Monte-Carlo model
Time-Resolved Electron Kinetics in SHI Irradiated Solids
1. SHI passage and generation of primary δ-electrons and holes ~10-17 s
2. Spreading of electrons and secondary electron cascading ~10-16 - 10-14 s
3. Auger and radiative decays of core holes ~10-15 s
4. Mobility of valence holes ~10-13s
Collective response of a material is taken into account

## Slide 8
TREKIS: Verification of model
Good coincidence with SRIM, CasP and NIST database
Electronic energy loss of ions and inelastic mean free paths of electrons

## Slide 9
TREKIS: Results
Excitation of target lattice
Mobility of valence holes play an important role for energy transfer to the lattice
100 fs

## Slide 10
MD simulation
MD code
LAMMPS
Z
X
Y
18.8 nm
12.2 nm
5.25 nm
Xe 167 MeV

## Slide 11
Interatomic forces
Buckingham-type potential
Verification of potential
Cij, Aij, ρij from
M. Matsui, Geophys. Res. Lett (1996)
Elastic constants | Experimental, GPa | Calculated, GPa
C11 | 498 | 473.6
C12 | 163 | 181.7
C13 | 117 | 150.8
C14 | -23 | -19.2
C33 | 502 | 520.5
C44 | 147 | 115.7
C66 | 167 | 146.3
Tm(exp) = 2345 K

## Slide 12
Xe 167 MeV
- Al
- O
c)
d)
b)
Y
Z
X
а)
Y
Z
X
~1.8 nm
9.8 nm
V.A. Skuratov, J. O’Connell et al. NIMB 326 (2014) 223–227

## Slide 13
Xe 167 MeV
5%
-5%
0
Radial density of Al2O3
Lattice deformation:
Simulation
Experiment

## Slide 14
Xe 167 MeV
Simulation of X-ray powder diffraction
Aluminum sublattice is damaged stronger than oxygen sublattice

## Slide 15
Track relaxation kinetics
Density of material at 3 nm from the Xe 167 MeV ion trajectory
Propagation of elastic waves with frequency of ν ~ 0.5 THz

## Slide 16
Bi 700 MeV (44 keV/nm)
b)
~3 nm
а)
Y
Z
X
Residual stress around ion trajectory
Track structure: underdense core is surrounded by overdense shell

## Slide 17
Kr and Fe ions
Kr 107 MeV Fe 22.5 MeV
~1.25 nm
а)
b)
~0.5 nm
dE/dx = 16 keV/nm dE/dx = 10 keV/nm

## Slide 18
Track formation threshold
Calculated threshold value is dE/dxth ~ 7 keV/nm
Threshold value of lattice energy to form ion track is ~ 3.2±0.4 eV/atom

## Slide 19
Track density
  The number of ion tracks saturates at fluence of
  ~ 1.1 x 1012 cm-2
  Effective radius of SHI track ~ 5.4 nm
J. O’Connell et al. VITT 2015

## Slide 20
Overlapping of SHI tracks
Z-projection
2.8 nm
Box size 12.2 x 18.8 x 5.2 нм3
Xe 167 MeV ion
Passage of the second ion causes partial annealing of the defects created by the first one
Is the healing of tracks the probable mechanism of observed saturation?
Z-projection
Y-proj.
Y-proj.

## Slide 21
Overlapping of SHI tracks
6 nm
Z-projection
Y-proj.
Z-projection
Y-proj.
Passage of the ion at longer distances from older tracks causes partial annealing of the defects
Effective radius of recovery is ~6.5 nm (experimental ~5.4 nm) and corresponding track density is ~2.7×1012 см-2

## Slide 22
Overlapping of SHI tracks
Critical excess lattice energy to observe recovery of defects is ~ 0.4 eV/atom

## Slide 23
Conclusions
The relaxation of excess lattice energy in Al2O3 irradiated by SHI is studied using original MC model and classical MD
The estimation of track size is in a good agreement with recent TEM data. The energy loss threshold of track formation in Al2O3 is determined (dE/dx~ 7 keV/nm).
Simulation of X-ray powder diffraction patterns of irradiated crystal revealed that the Al sublattice is damaged stronger than O sublattice
The effect of recovery of overlapping tracks in Al2O3 is investigated. The effective distance of recovery is ~5.4 nm (TEM) - 6.5 nm (MD) for Xe 167 MeV ion.

## Slide 24
Thank you for your attention
BIOMAT-2016