## Slide 1: First Experience of Production and Testing the Superconducting Quadrupole and Corrector Magnets for the SIS100 Heavy Ion Accelerator of FAIR
E. Fischer, Y. Bespalov, V. Borisov, H. Khodzhibagiyan, D. Khramov, D. Nikiforov,
T. Parfylo, M. Petrov, A. Shemchuk, D. Zolotykh
JINR, Dubna, Russia
A. Waldt, A. Bleile, GSI, Darmstadt, Germany

## Slide 2
The SIS100 Lattice Structure
  Doublet Modules
  Quadrupole Units
2. Main Quadrupoles and Correctors
  Design of the Superconducting Magnets
  Status of Series Production
  Test Results and Reproducibility
3. Summary
Outline
Notes: 2
2

## Slide 3
◄ The six sections of the synchrotron ring
with its Bypass Lines, the cryogenic and
electrical supply systems.
Cryomagnetic components in sector 5 ►
SIS100 Lattice Structure

## Slide 4
main dipoles
three families of quadrupole magnets
F1, F2, QD
See also E. Fischer et al.
Start of the Series Production for the Cryogenic Magnet Corrector Modules of FAIR
https://jacow.org/ipac2019/papers/THPTS010.pdf
Examples of the SIS100 Operation Cycles

## Slide 5
Example: Type 2.5
Unit Configuration |  |  | Doublet Configuration |  | 
Upstream | Centre | Downstream | Joined Name | Short Name | Quantity
QDB | -TRP- | SF2 | QDB-TRP-SF2 | 2.123 | 15
QDBs | -TRP- | SF2s | QDBs-TRP-SF2s | 2.13s | 2
QDBb | -T- | SF2Mb | QDBb-T-SF2Mb | 2.4 | 5
QDBx | -T- | SF2Mx | QDBx-T-SF2Mx | 2.4x | 1
VQD | -CR- | SF2B | VQD-CR-SF2B | 2.5 | 6
BQD | -C- | SF1H | BQD-C-SF1H | 1.6A | 12
VQD | -CR- | SF1B | VQD-CR-SF1B | 1.7B | 12
BQD | -C- | SF2H | BQD-C-SF2H | 2.8C | 12
BQD | -CR- | SF2J | BQD-CR-SF2J | 2.9D | 12
MQDb | -C- | SF1Bb | MQDb-C-SF1Bb | 1.E | 5
MQDi | -C- | SF1Bi | MQDi-C-SF1Bi | 1.Ei | 1
 |  |  | Total |  | 83
Unit (type SF2B)
Doublet (cold mass)
Integrated QDM
Abbreviations | 
QD | Defocusing quadrupole
F1 | Focusing quad. 1
F2 | Focusing quad. 2
B | Beam position monitor
V | Vertical chrom. sextupole
H | Horizontal chrom. sextupole
S | Steering magnet
M | Multipole corrector magnet
C | Cryo-ion-catcher (collimator)
T | Drift tube
b | modified busbars
i | injection Y cryostat
x | extraction Y cryostat
s | Star shape chamber
P | Cryo-sorption-pump
R | Roughing pump with CWT
Quadrupole Units and Doublet Modules
SIS100 Lattice Structure

## Slide 6
Common Girder and Suspension
Focusing QP-Magnet (within unit)
Steering Magnet
Defocusing QP-Magnet (within Unit)
Local Current Leads
Common Girder and Suspension
He-Supply and Return, Magnet cooling
Bus Bar System
Bus Bar System
Sextupole Magnet
Cryo Catcher
Roughing CWT
Beam Vacuum Chamber, Defocusing
Beam Vacuum Chamber, Focusing
Voltag Breaker
Beam Position Monitor
QP Units and Doublet Modules

## Slide 7
All SIS100 lattice quadrupole and corrector magnets have to be made in JINR, Dubna. The Nuclotron-type design, based on a cold, window-frame iron yoke and a winding of the hollow superconductor, was chosen for the SIS100 magnets.
Characteristic | Lattice Quadrupole | Corrector magnet |  | 
 |  | Multipole (Q/S/O) | Steerer | Chrom. Sextupole
Number of magnets | 166 | 12 | 84 | 42
Max. field strength, T/mn-1 | 27.77 | 0.75/25/333,3 | 0.37 | 232
Effective magnetic length, m | 1.264 | 0.75 | 0.403/0.41 | 0.383
Aperture diameter, mm | 100 | 150 | 135 | 120
Operation current | 10512 | 250/246/240 | 245/241 | 252
Magnet weight, kg | 850 | 200 | 120 | 145
Characteristics of the magnets
Main Quadrupoles and Correctors

## Slide 8
Steerer
Sextupole
Multipole Corrector
Gamma Jump Quadrupole
Main Quadrupole
Design of the superconducting Magnets

## Slide 9
Magnet yokes
Magnet type | at JINR | Completion % | Incoming inspection pass
Quadrupole | 173 | 100 | 173
Sextupole | 85 | 100 | 85
Steerer | 44 | 100 | 44
Status of Series Production
Superconducting coils
Magnet type | Produced at JINR | Completion % | Incoming inspection pass
Quadrupole | 34 | 20 | 34
Sextupole | 21 | 25 | 21
Steerer | 22 | 50 | 22
Units | Assembled and delivered | Completion %
Series 2.5 | 12 | 100
Series 1.7B | 8 | 33
Total | 20 | 12
Magnet and Unit assembling

## Slide 10
For details of cryogenic procedures and magnetic measurement systems see, e.g.:
V. Borisov et al.
Magnetic Field Performance of the First Serial Quadrupole Units for the SIS100 Synchrotron of FAIR https://jacow.org/ipac2021/papers/tupab383.pdf
A. Shemchuk et al.
Magnetic Field Measurements for the Collider Magnets and FAIR Quadrupole Units
RuPAC 2021, WEB02
T. Parfylo et al.
Vibrating Wire System for Fiducialization NICA Booster Superconducting Quadrupole Magnets
RuPAC 2021, WEPSC17
Test Results and Reproducibility
D. Nikiforov et al.
SC Magnets for Project of NICA
RuPAC 2021, WEB01

## Slide 11
Typical example for geometrical proof of QP aperture
All quadrupole apertures are within the specification

## Slide 12
Description | Drawing size, mm | Real size, mm | Δ, mm
AA-BB | 1400±0,05 | 1400.03 | 0.03
R1-R5 | 1380±0,05 | 1380.05 | 0.05
R2-R6 |  | 1380.05 | 0.05
R3-R7 |  | 1380.04 | 0.04
R4-R8 |  | 1380.05 | 0.05
R1-R3 | 368 ±0,02 | 368.02 | 0.02
R2-R4 |  | 368.02 | 0.02
R5-R7 |  | 368.02 | 0.01
R6-R8 |  | 368.02 | 0.02
A-l – A-r | 380 ±0,02 | 379.99 | -0.01
A-l – A-r |  | 0.02 | 0.00
M-l – M-r |  | 379.99 | -0.01
M-l – M-r |  | 0.02 | 0.00
B-l – B-r |  | 379.99 | 0.02
B-l – B-r |  | 0.02 | 0.00
Adjustment of Units in the Doublet
Geometrical measurements to the reference points of the MM

## Slide 13
Magnetic Axis Measurements @ RT using vibrating wire technique

## Slide 14
Angle of the QPs Magnetic Axis

## Slide 15
Typical cooldown scenario for QPUs
Training current = 12.6 kA
Operation current = 10.5 kA
Training Statistics of the Series Quadrupoles
RMS distribution quenches of training current = 6..7
RMS distribution quenches of operating current = 2..3
Current cycle for magnet training
Operation current 250 A
Training current 300 A
Training of the sextupole magnets
Cold Tests

## Slide 16
Reference cycle
Series Number of Magnet
Dynamic heat releases of quadrupole magnets
Tolerance value (2.0 W)
Quadrupole magnet
Median (17.7 W)
Cold Tests

## Slide 17
Frequency, Hz
Heat release matrix of the quadrupole
Steering magnets
Median (9.41 W)
Sextupole magnets
Median (2.77 W)
Dynamic heat releases of the corrector magnets
Cold Tests

## Slide 18
Typical current dependance of Integral transfer functions. Inset graph: distribution of ITF of 22 series magnets « 900 A.
sextupole

## Slide 19
Relative variations of gradient at the center of quadrupole magnets vs. yokes production sequence
Integral Multipoles of the Quadrupole Magnets .
Typical current dependances of b6 . Points with error bars are averaged values and standard deviation for series of 25 magnets
Measuring probe inside the magnet:
1 - quadrupole
2 - probe
3 - ball bearings
and adjustable
housings
4 - inside precision
ceramic ball
bearing
5 - frame

## Slide 20
Relative variations of the integral gradient vs.
production sequence of the quadrupole yokes
Distribution of relative variations of the integral gradient

## Slide 21
100 % of all yokes for QP-unit magnets were already delivered to JINR
20 QP-units are assembled, successfully tested at JINR and were delivered to FAIR
Next 8 Units are under preparation for shipment in October 2021
The first Unit series 2.5 was completed in March this year, the second series 1.7B will follow in October.
JINR had established an effective and stable production and testing scenario for the Quadrupole Units
The optimisation of the production technology and detailed methodological adjustment of the measurement techniques resulted in the proven and continuously high quality of the series magnets.
Summary

## Slide 22
Thank you for your attention !