## Slide 1: Structural effects in nanoceramics induced by swift heavy ion irradiation
A.K. Mutali1,2,3, A.D. Ibrayeva2,3, V.A. Skuratov3,4, A.S. Sohatsky3, Е. Korneeva3, A. Janse van Vuuren5, M.V. Zdorovets1,2,6
1L.N. Gumilyov Eurasian National University, Nur-Sultan, Kazakhstan
2 The Institute of Nuclear Physics’ Astana branch, Nur-Sultan, Kazakhstan
3 G.N. Flerov Laboratory of Nuclear Reactions of Joint Institute for Nuclear Research, Dubna, Russia
4 National Research Nuclear University MEPhI, Moscow, Russia
5Centre for HRTEM, Nelson Mandela Metropolitan University, Port Elizabeth, South Africa
6 Ural Federal University, Yeketerinburg, Russia
JINR Association of Young Scientists and Specialists Conference "Alushta-2021"
Alushta-2021

## Slide 2
Swift heavy ions (SHI)
E > 0.5 MeV/u, M > 4mp, Se>>Sn
Sn/Se < 0.01 – majority of energy losses is electron stopping power
Simulate the influence of fission fragments and cosmic rays on material properties
Introduction
2
1-10 keV/u
0.5 to 100 MeV/u

## Slide 3: How do swift heavy ions make tracks?
C.Trautman (International school on Radiation Effects in Solids, Erice, Italy, July 2004)
Swift heavy ions E > 0.5 MeV/nucl, A > 4, Se>>Sn → latent tracks
3

## Slide 4
Electron source deflection coils
Gun deflection coils
Condenser stigmator
Mini condenser lens
Image deflection coils
Objective stigmator
Diffractive stigmator
C1 aperture
C2 aperture
Objective aperture
SA aperture
Энергодисперсионный детектор Super-X
Компьютеризованный держатель образца
Flucam
Camera CETA-16M
Condenser lenses C1 and C2
Upper objective lens
Lower objective lens
Diffractive and Intermediate lens
Projector lenses P1 and P2
Источник электронов с полевой эмиссией (Field Emission Gun) в сборе с 200 кВ ускорителем и управляющей электроникой
Beamstop
Бланкер пучка
Флюоресцентный экран
S/TEM TALOS F200i
thermoscientific
4

## Slide 5: Material
Si3N4 as candidate material for inert matrix fuel hosts
The small absorption cross section for thermal neutrons
The resistance at irradiation with neutrons, α particles,
and fission fragments
Good thermal and mechanical properties
Si3N4 is the ONLY nitride ceramic where latent tracks have been registered
Radiation defects induced by swift heavy ions simulating fission fragments impact still remain less studied in comparison with neutron and conventional (low energy) ion irradiation
5
S.J. Zinkle, V.A. Skuratov and D.T. Hoelzer.
Nucl. Instr. Meth. B 191 (2002),758
Aim of this work is to study radiation stability of nanocrystalline Si3N4 in a wide range of electronic stopping powers

## Slide 6: TEM Sample Preparation
Nanopowder
Mix powder in C2H5OH
Centrifuge
Ultrasound
TEM grid
3 mm
6
Scanning/Transmission Electron Microscopes (S/TEM) accelerate electrons through samples, collecting the transmitted electrons to image materials at the nanoscale
As this technique captures electrons that pass through a sample, samples need to be electron transparent
This is typically requires:
Thin Samples, samples thickness <150 nm for regular imaging, <50 nm for HRTEM
Uniform thickness over the area of interest
Clean samples free from contamination

## Slide 7
Swift Heavy Ion (SHI) irradiation
Incident ion | Energy, MeV | Fluence, cm-2
Bi | 714 | 5×1011 (a single ion track regime)
 | 354 | 
 | 287 | 
 | 241 | 
 | 164 | 
 | 106 | 
 | 83 | 
 | 27 | 
Xe | 220 | 5×1011
 | 156 | 5×1011
 | 53 | 
 | 38 | 
All samples were irradiated at accelerators in FLNR JINR (Dubna, Russia) and INP (Nur-Sultan, Kazakhstan).
TEM research was conducted in HR TEM Center of Nelson Mandela University (Port-Elizabeth, South Africa) and Nanocenter of FLNR JINR (Dubna, Russia)
7

## Slide 8
TEM images of n-Si3N4 + Bi, +Xe ions
n-Si3N4 + Bi354M-5e11_DF
n-Si3N4 + Bi714M-5e11_DF
n-Si3N4 + Xe220M-5e11_DF
n-Si3N4 + Xe156M-5e11_BF
n-Si3N4 + Xe53M-5e11_DF
n-Si3N4 + Bi241M-5e11_DF
n-Si3N4 + Xe38M-5e11_BF
n-Si3N4 non irradiated_BF
8

## Slide 9
Result Summary
Latent tracks in nanocrystalline Si3N4 irradiated with 156, 220 MeV Xe and 714 MeV Bi ions and fluence of 5e11 cm-2 corresponding to a single ion track regime, have been studied using high resolution transmission electron microscopy.
For the first time, parameters of latent tracks in nanocrystalline ceramic matrix were determined in a wide range of electron stopping powers Se.
The threshold electron stopping power for latent track formation in nanocrystalline Si3N4 was found to equal ~7.5 keV/nm.
Need further detailed investigation
Future plans for the next year: the study of the radiation resistance of Y2O3, TiO2, CeO2, Al2O3, Cr2O3, Y4Al2O9, Spinel to irradiation with high-energy heavy ions.
Xe 38 MeV
Xe 156 MeV
Xe 53 MeV
Xe 220 MeV
Bi 106 MeV
Bi 164 MeV
Bi 241 MeV
Bi 287 MeV
Bi 354 MeV
Bi 710 MeV
Bi 1030 MeV
Xe 220 MeV
Set ~ 7.5 keV/nm
Bi 714 MeV

## Slide 10
Thank you for your attention!