## Slide 3
EP450 ODS steel (VNINM, Moscow)
Y2Ti2O7 nanoparticles
Y4Al2O9 nanoparticles

## Slide 4
А
B
C

## Slide 5
Helium bubble
Fe82H-ODS
Helium bubble
The mechanical state of ODS alloys can affect the gas swelling of these materials, which has not yet been investigated.
The mechanism of bubble growth during high temperature annealing is still unclear.

## Slide 6
Cr16 ODS
AISI410S
EP450 ODS

## Slide 7
Implantation area
1.
2.
4.
5.
3.
Implantation area

## Slide 8
JEOL JEM – 2100 TEM (HRTEM, NMMU, SA)
Notes: TEM analysis of gas porosity was carried out at a voltage of 200 kV
Here we used a brigh field mode to obtain images of gas bubbles due to the Fresnel contrast

## Slide 9
Dislocation
GB
GB
GI
GB
AISI 410S, [He] = 1 at. %, 0.2 dpa
Cr16 ODS, [He] = 1 at. %, 0.2 dpa
AISI 410S, [He] = 0.2 at. %, 0.04 dpa
GI
GI

## Slide 10
(Cr,W)23C6
[He] = 0.2 at%, 0.04 dpa
[He] = 1 at%, 0.2 dpa

## Slide 11
Notes: Comparing the helium porosity parameters in these samples shows that the overall swelling of EP450 ODS is much higher than that of conventional and Cr16 ODS samples

## Slide 12
Tow bubbles before contact
On contact and merge
After merge and relaxation
Matrix
Diffusion of helium atoms and vacancies
Small bubble
Large bubble
Regadless of the type of material, the bubble growth occurs by the mechanism of bubble migration and coalescence during high-temperature annealing.

## Slide 14
Cr16 ODS alloy
EP450 ODS alloy
Y2Ti2O7
Y2Ti2O7
Al2O3

## Slide 15
Y2Ti2O7
Y2Ti2O7
Al2O3