## Slide 1: Operation Performance of the SIS100 Series Magnets Produced and Tested at the JINR for FAIR
E. Fischer, H. Khodzhibagiyan, Y. Bespalov, V. Borisov, E. Iskornev, D. Khramov, B. Kondratiev,
D. Nikiforov, T. Parfylo, M. Petrov, A. Shemchuk, D. Zolotykh
JINR, Dubna, Russia
http://sarantsev22.jinr.ru
2022 September 20-25
Alushta, Crimea
ЭКСПЛУАТАЦИОННЫЕ ХАРАКТЕРИСТИКИ МАГНИТОВ СЕРИИ SIS100, ПРОИЗВЕДЁННЫХ И ИСПЫТАННЫХ В ОИЯИ ДЛЯ FAIR

## Slide 2
Outline
Introduction
Nuclotron Magnets as Starting Point
      R & D for the fast ramped sc Magnets
      Prototypes for the SIS100 Main Magnets
Series Production and Testing for SIS100 at JINR
      Design of the Quadrupole Units
      Production Status
      Test Results and Operation Performance
Summary

## Slide 3
Heavy Ion Synchrotron with superconducting magnets
100 Tm rigidity
Bmax = 1,9 T, dB/dt = 4 T/s, fcycle = 1 Hz
1100 m circumference
sc dipoles
sc quadrupoles
sc correctors
cold beam pipe:
vacuum quality critical for
beam lifetime: < 10-12 mbar
www.fair-center.eu
Introduction: SIS100 – the core component

## Slide 4
Basic Design: Nuclotron Type Magnet
Bmax = 1.9 T
dB/dt = 4 T/s
fast ramping ~ 1 Hz
field homogeneity ± 6·10-4
for SIS100 Dipole development
super-ferric, window-frame
sc coil (Nuclotron type cable)
coil and yoke cooled by forced flow of two-phase He @ 4.5 K
1 - сooling tube CuNi
2 - sc wire NbTi
3 - CrNi wire
4 - rapton tape
5 - glasfiber tape
Nuclotron cable:
1 - yoke end plate, 2 – brackets,
3 - coil end loop, 4 - beam pipe,
5 - helium headers, 6 – suspension.
200
292
110
55
Nuclotron Dipole
Nuclotron Magnets as Starting Point

## Slide 5
Reduce effects due to the high ramp rate:
  lower loss at 4 K in
  wire, cable, iron and beam pipe
Improve magnetic field quality
by modification of the iron yoke
Improve mechanics
to guarantee
≥ 5108 cycles for
20 years lifetime at 1 Hz
The magic triangle
      R & D for the fast ramped sc Magnets
Cold mass of the Nuclotron dipole:
1 - yoke end plate
2 - brackets
3 - coil end loop
4 - beam pipe
5 - helium headers
6 - suspension
7 - laminated yoke
Test measurements on magnet modifications
FEM calculations on detailed 3D-models
Main reasons for superconducting SIS100:
- Capital and operating costs
- High current Uranium beam modes with intermediate charge states, require ultra low vacuum pressures which can be achieved in long term operation only by cold beam pipes acting as a cryopump with stable temperatures well below 15 K for all operating cycles

## Slide 6
  AC loss reduction: FEM Calculations
Vectors of the longitudinal induction BZ(t) in the yoke
Loss density in the end plate:
Replace by nonmagnetic, high resitive material
      R & D for the fast ramped sc Magnets

## Slide 7
Vectors of eddy current density in brackets during triangular current cycle
Hysteresis loss in the brackets
=> AC loss in the yoke restraint
      R & D for the fast ramped sc Magnets
  AC loss reduction: FEM Calculations
      R & D for the fast ramped sc Magnets

## Slide 8
Analysis of:
Wire and cable design
Insulation concept
Winding scheme
Technological optimization
ANSYS Models
Substrate: comb or block
Model coils production
Mechanical tests
Coil Mechanics
stress strain load tests on the
complete coil winding pack:
      R & D for the fast ramped sc Magnets

## Slide 9
Modificated Nuclotron dipoles with:
1▲ partly removed brackets and end plates
2▲ and laser cut lamination slits
3▲ stainless steel brackets and end plates
4▲ reduced coil end shape
1
1
2
0.1mm laser cut
4
3
  AC loss reduction: Test Models
      Prototypes for the SIS100 Main Magnets

## Slide 10
new wire
original
wire
AC Loss Reduction for the Nuclotron DP
1. Removed brackets (of made from SS)
2. Laser cut lamination slits
3. Minimized coil ends
4. New sc wire design !
5. Next change: to laminated isotropic 1.0 mm thick M600-100A silicon steel
      Prototypes for the SIS100 Main Magnets

## Slide 11
Nuclotron Quadrupole :
Nominal gradient: 34 T/m
Ramp rate: 68 T/ms
▲Test measurements on quadrupole modifications
◄ FEM calculations on detailed 3D-models
  AC loss reduction:
  Test on Quadrupole
      Prototypes for the SIS100 Main Magnets

## Slide 12
Significant differences between Nuclotron-type Model Dipole and the SIS100 First of Series Magnet:
2-layer straight magnet → 1-layer curved magnet
Main Advantages:
Reducing the size of the cross section of the magnet, and consequently reducing losses and hydraulic resistance
Reduction of peak field to 1.9 T → reduction of field errors due to reduced iron saturation
Low loss sc wire (CuMn matrix)
New challenges in manufacturing:
winding of curved coil and stacking of curved yoke
increased cable diameter reduced available space for electrical insulation and structural components in the coil
Parameter | N-type | FoS
Effective length | 2.756 m | 3.062 m
Bending angle | 0 deg | 3.33 deg
Bmax | 2.1 T | 1.9 T
Max. ramp rate | 4 T/s | 4 T/s
Layers*turns | 2*8 | 1*8
Operating current | 7 kA | 13 kA
Outer diameter of the cooling tube | 5 mm | 5.7 mm
Number of strands | 31 | 23
Strand diameter | 0.5 mm | 0.8 mm
Cable diameter | 7.36 mm | 8.29 mm
  New Generation of Superferric Magnets: SIS100 Dipole Design
      Prototypes for the SIS100 Main Magnets

## Slide 13
 | GSI | NICA | NICA | 
 | SIS100 | Booster | Collider | 
cable |  |  |  | 
tube inner diameter | 4.7 | 3 | 3 | mm
number of strands | 21 | 18 | 16 | 
critical current (at 2.5 T and 4.5 K) | 19.8 | 14.2 | 16.8 | kA
dipole |  |  |  | 
ﬁeld strength | 1.9 | 1.8 | 1.8 | T
ﬁeld ramp rate | 4 | 1.2 | ≤ 0.5 | T/s
pole gap height | 68 | 64 | 70 | mm
magnet length | 3.1 | 2.2 | 1.94 | m
curvature radius | 52.625 | 14.090 |  | m
operation current | 13.1 | 9.68 | 10.4 | kA
inductance | 0.55 | 0.63 | 0.45 | mH
maximum AC loss | 100 | 8.4 | 8 | W
→
→
→
  New Generation of Nuclotron-Type Dipoles
      Prototypes for the SIS100 Main Magnets

## Slide 14
All SIS100 lattice quadrupole and corrector magnets have to be made in JINR, Dubna. The 108 main dipoles are in the responsibility of GSI, Darmstadt.
Characteristic | Lattice Quadrupole | Corrector magnet |  | 
 |  | Multipole (Q/S/O) | Steerer | Chrom. Sextupole
Number of magnets | 166 | 12 | 84 | 42
Max. field strength, T/mn-1 | 27.77 | 0.75/25/333,3 | 0.37 | 232
Effective magnetic length, m | 1.264 | 0.75 | 0.403/0.41 | 0.383
Aperture diameter, mm | 100 | 150 | 135 | 120
Operation current | 10512 | 250/246/240 | 245/241 | 252
Magnet weight, kg | 850 | 200 | 120 | 145
Characteristics of the magnets
Series Production and Testing at JINR

## Slide 15
Steerer
Sextupole
Multipole Corrector
Gamma Jump Quadrupole
Main Quadrupole
      Design of the Quadrupole Units

## Slide 16
Example: Type 2.5
Unit Configuration |  |  | Doublet Configuration |  | 
Upstream | Centre | Downstream | Joined Name | Short Name | Quantity
QDB | -TRP- | SF2 | QDB-TRP-SF2 | 2.123 | 15
QDBs | -TRP- | SF2s | QDBs-TRP-SF2s | 2.13s | 2
QDBb | -T- | SF2Mb | QDBb-T-SF2Mb | 2.4 | 5
QDBx | -T- | SF2Mx | QDBx-T-SF2Mx | 2.4x | 1
VQD | -CR- | SF2B | VQD-CR-SF2B | 2.5 | 6
BQD | -C- | SF1H | BQD-C-SF1H | 1.6A | 12
VQD | -CR- | SF1B | VQD-CR-SF1B | 1.7B | 12
BQD | -C- | SF2H | BQD-C-SF2H | 2.8C | 12
BQD | -CR- | SF2J | BQD-CR-SF2J | 2.9D | 12
MQDb | -C- | SF1Bb | MQDb-C-SF1Bb | 1.E | 5
MQDi | -C- | SF1Bi | MQDi-C-SF1Bi | 1.Ei | 1
 |  |  | Total |  | 83
Unit (type SF2B)
Doublet (cold mass)
Integrated QDM
Quadrupole Units and Doublet Modules
      Design of the Quadrupole Units

## Slide 17
Egbert Fischer, MAC-7 Meeting, 2-3 April 2012, Jülich
17
December 2010
Scheme of the new SC-magnet test facility at JINR Dubna
1600 m2 main hall
700 m2 auxiliary facilities
February 2012
September 2012
Test facility at JINR
SC Magnet Production and Testing
for NICA and FAIR
Notes: 17

## Slide 18
Opening Ceremony for the Production and Test Facility
28.11.2016

## Slide 19
Superconducting coils
Magnet type | Produced at JINR | Completion % | Incoming inspection pass
Quadrupole | 53 | 32 | 53
Sextupole | 24 | 30 | 24
Steerer | 27 | 61 | 27
Magnet type | at JINR | Completion % | Incoming inspection pass
Quadrupole | 173 | 100 | 173
Sextupole | 85 | 100 | 85
Steerer | 44 | 100 | 44
Magnet yokes
      Production Status

## Slide 20
All quadrupole apertures are within the specification
      Production Status: Quality Control
Typical example for geometrical proof of QP aperture

## Slide 21
Quality improvement
In the process production appears nonconformity of design documentation and issued Nonconformity Report (NCR)
Chart: Reduction Major NCRs
| 2020 | 2021
Opened major NCR | 20 | 4
Closed major NCR | 19 | 4
Chart: Reduction Minor NCRs
| 2020 | 2021
Opened minor NCR | 69 | 31
Closed minor NCR | 66 | 27
      Production Status

## Slide 22
Magnet and Unit assembling and testing
Units | Ready for test | Ready for delivery | Delivered | Completion %
Series 2.5 | - | - | 12 | 100
Series 1.7B | 2 | 6* | 16 | 92
Series 1.6A | 12 | 0 | 0 | 25
Series 2.8C | 0 | 0 | 0 | 0
      Status: Production, Testing and Delivery

## Slide 23
Actions for high test intensity of the QPUs
Month | 2020 | 2021 | 2022 | 2023
January |  | CV-19 |  | 
February |  | CV-19 |  | 4
March |  |  | 8* | 6
April |  | 8 |  | 8
May |  |  | 8 | 8
June |  |  |  | 8
July |  |  | 8 | 8
August |  |  |  | 8
September | 2 | 8 | 8 | 8
October |  |  | 8 | 8
November | 2 |  | 8 | 8
December | CV-19 | 8 | 8 | 8
Subtotal | 4 | 24 | 56 | 82
- Delivered
- Delay (Covid)
* Contract freeze by FAIR
      Status: Production, Testing and Delivery
Delivery schedule for SIS100
- The rate of unit cryogenic testing was planned to
increase from 4 units per month in February 2022
to 8 units per month in October 2022.
- Completion of testing of all 166 units was planned for December 2023.

## Slide 24
Magnetic Axis Measurements @ RT using vibrating wire technique
      Test Results and Operation Performance

## Slide 25
QPU of the VQD type (QP + Sextupole)
      Test Results: QPs Magnetic Axis

## Slide 26
Typical cool down scenario for QPUs
Current cycle for magnet training
Preparation of a SIS100 Quadrupole Unit for cold tests
      Test Results: Training of the Quadrupole Magnets

## Slide 27
Training current = 12.6 kA
Operating current = 10.5 kA
RMS distribution quenches of training current = 5..6
RMS distribution quenches of operating current = 2
Training Statistics of the Series Quadrupoles
Batch 1 (Type 2.5)
Batch 2 (Type 1.7B)
Batch 3 (Type 1.6A)
Learning curves (operating current)
Learning curves (training current)
= 58;
= 14;
= 34;
= 24;
Nummer of the magnets
      Test Results: Learning curve for magnet production

## Slide 28
Control of the cooling rate is important for mechanical stability and so for magnet field quality !
      Test Results: Training and Cooling Rates

## Slide 29
Heat release matrix for the quadrupole
      Test Results: AC Losses at 4,5 K
Steerer

## Slide 30
Gradient dependence of the Mean Integrated Transfer Function, errors give the standard deviation within the series. The inset graph shows ITF distribution of 29 series quadrupoles at 900 A.
sextupole
      Operation Performance

## Slide 31
Relative variations of gradient at the center of quadrupole magnets vs. yokes production sequence
Integral Multipoles of the Quadrupole Magnets
Current dependence of the b6 mean value and their standard deviation
      Operation Performance

## Slide 32: Gradient dependence of the standard deviation of the field integral variation
Relative variations of the integral gradient vs. production sequence of the quadrupole yokes
Distribution of the relative variations of the integral gradient
      Operation Performance

## Slide 33
Summary
All the iron yokes for the 173 quadrupoles, 85 sextupoles and 44 steerer magnets were manufactured and had passes the incoming inspection.
A stable production, testing and approval process was established in 2021.
About 35% of the work on the manufacture and cryogenic testing of SIS 100 quadrupole units was completed by the beginning of 2022.
JINR had fulfilled all the necessary organisation and practical conditions to complete its SIS100 contracts by end of 2023 timely and with high quality.
Beginning of March this year the contract work was frozen by FAIR management referring to political decisions.

## Slide 34
Thank you for your attention !
Additional slides - Main References:

## Slide 35
References (1/6)
[1] G. Moritz, C. Muehle, M. Anerella, A. Ghosh, W. Sampson, P. Wanderer, E. Willen, N. Agapov, H. Khodzhibagiyan, A. Kovalenko, W.V. Hassenzahl, M.N. Wilson “Towards fast-pulsed superconducting synchrotron magnets”, Proc. of the 2001 Particle Accelerator Conf., Chicago, pp.211-213.
[2] A. D. Kovalenko, N.N. Agapov, H. G. Khodzhibagiyan,…,et all “Superconducting fast-cycling dipole magnets for the GSI future accelerator facility”, Proceedings of EPAC 2002, Paris, pp.2406-2408.
[3] Kovalenko A, Agapov N, Khodzhibagiyan H and Moritz G “Fast cycling superconducting magnets: new design for ion synchrotrons”, Physica C: Superconductivity, Volumes 372-376, Part 3, August 2002, Pages 1394-1397 (EUCAS 2001)
[4 ] N. Agapov, S.A. Averichev, A.M. Donyagin, I. Eliseeva, I. Karpunina, H.G. Khodzhibagiyan, A. D. Kovalenko, G.L. Kuznetsov, V.N. Kuzichev, G. Moritz, C. Muehle, P. Nikitaev, and A. Starikov “Experimental study of a prototype dipole magnet with iron at T=80 K for the GSI fast cycling synchrotron”, IEEE Trans. Appl. Supercond., vol. 12, N1, 2002, pp.116-119.
[5] A. D. Kovalenko, A. Kalimov, H.G. Khodzhibagiyan, G. Moritz, and C. Muehle, “Optimization of a superferric Nuclotron type dipole for the GSI fast pulsed synchrotron”, IEEE Trans. Appl. Supercond., vol. 12, N1, 2002, pp.161-165.
[6] A. Kovalenko, N. Agapov, S. Averichev, A. Donyagin, H. Khodzhibagiyan, G. Kuznetsov, A. Starikov, G. Moritz, E. Fisher, G. Hess, and C. Muehle “Superferric model dipole magnet with the yoke at 80 K for the GSI future fast cycling synchrotron”, IEEE Trans. Appl. Supercond., vol. 13, N2, 2003, pp.1335-1338.
[7] Alexandre D. Kovalenko, Nicolay N. Agapov, Vladimir G. Aksenov, Irina E. Karpunina, Hamlet G. Khodzhibagiyan, Grigori L. Kuznetsov, Michail A. Voevodin, Gebhard Moritz, Egbert Fisher, Guenter Hess, and Carsten Muehle “Progress in the design and study of a superferric dipole magnet for the GSI fast-pulsed synchrotron SIS100”, IEEE Trans. Appl. Supercond., vol. 14, N2, 2004, pp.321-324.
[8] A. Kovalenko, N. Agapov, A. Donyagin, I. Eliseeva, H. Khodzhibagiyan, G. Kuznetsov, A. Smirnov, G. Moritz, E. Fisher “Design and study of a superferric model dipole and quadrupole magnets for the GSI fast-pulsed synchrotron SIS100”, Proc. EPAC 2004, Lucerne, pp.1735-1737.
[9] E. Fischer, H. Khodzhibagiyan, A. Kovalenko, and G. Moritz “Supraleitendes Kabel und verfahren zur Herstellung desselben”, EU-patent Nr. 04009730.5, 23.04.04.
[10] E. Fischer, P. Akishin, H. Khodzhibagiyan, A. Kovalenko, G. Kuznetsov, G. Moritz, A.Smirnov, “Minimization of AC power losses in fast cycling window frame 2 T superferric magnets with the yoke at 4.5 K”, report at ASC 2004, Jacksonville.

## Slide 36
[11] A. Kovalenko, N. Agapov, E. Fischer, H. Khodzhibagiyan, G. Kuznetsov, G. Moritz, and A. Smirnov “New results on minimizing AC power losses in a fast cycling 2 T superferric dipole with a cold yoke”, IEEE Trans. Appl. Supercond., vol. 16, N2, 2006, pp.338-341.
[12] H. G. Khodzhibagiyan, E. Fischer, and A. D. Kovalenko “New design for the SIS100/300 magnet cooling”, IEEE Trans. Appl. Supercond., vol. 16, N2, 2006, pp.411-414.
[13] E. Fischer, G. Moritz, GSI, R. Kurnyshov, A. Kovalenko, H. Khodzhibagiyan , P. Shcherbakov “Analysis of the Superferric Quadrupole Magnet Design for the SIS100 Accelerator of the FAIR Project”, Proceedings of EPAC 06, Edinburgh, GB, June 2006, pp. 2586-2588.
[14] V. Mikhaylov, A. Alfeev, A. Butenko, A. Eliseev, H. Khodzhibagiyan, A. Kovalenko, O. Kozlov, A. Starikov, V. Seleznev, V. Volkov, JINR, E. Fischer, P. Spiller, J. Stadlmann “Basic aspects of the SIS100 correction system design”, Proceedings of EPAC 06, pp. 240-242, Edinburgh, GB, June 2006, pp. 240-242.
[15] A. Kovalenko, N. Agapov, A. Alfeev, H. Khodzhibagiyan, G. Kuztetsov, V. Seleznev, A. Shabunov, A. Starikov, E. Fischer, G. Moritz, C. Muehle, P. Spiller, A. Kalimov “Full Length Superferric Dipole and Quadrupole Prototype Magnets for the SIS100 at GSI: Status of the Design and Manufacturing”, Proceedings of EPAC 06, Edinburgh, GB, June 2006, pp 2583-2585
[16] G. Moritz, E. Fischer, H. Khodzhibagiyan, A. Kovalenko, A. Nyilas, R. Burgmer, D. Krischel, P. Schmidt, W. Gärtner, M. Gehring, W. Walter and A. Wessner “Mechanical Coil Structure of the FAIR SIS 100 Magnets”, IEEE Trans. Appl. Supercond., vol. 17, N2, 2007, pp.1169-1172. (ASC 06, Seattle, USA, Sep. 2006).
[18] E. Fischer, A. Alfeev, A. Kalimov , H. Khodzhibagiyan, A. Kovalenko, G. Kuznetsov, G. Moritz, C. Muehle, and V. Seleznev “Status of the Design of a Full Length Superferric Dipole and Quadrupole Magnets for the FAIR SIS 100 Synchrotron”, IEEE Trans. Appl. Supercond., vol. 17, N2, 2007, pp.1078-1082. (ASC 2006, Seattle)
[19] E. Fischer, H. Khodzhibagiyan, and A. Kovalenko “Full Size Model Magnets for the FAIR SIS100 Synchrotron”, IEEE Trans. Appl. Supercond., vol. 18, N2, 2008, pp.260-263. (MT-20 August 27 - 31, 2007, Philadelphia, USA)
[20] E. Fischer, H. Khodzhibagiyan, A. Kovalenko, and P. Schnizer „Fast Ramped Superferric Prototypes and Conclusions for the Final Design of the SIS 100 Main Magnets“, IEEE Trans. Appl. Supercond., vol 19, N3, June 2009, pp. 1087-1091 (ASC 2008, Chicago)
[21] K. Sugita, E. Fischer, H. Khodzhibagiyan, H. Mueller, J. Macavei, and G. Moritz “Design Study of the Multipole Corrector Magnet for SIS 100”, IEEE Transactions on Applied Superconductivity, Vol. 19, N 3, June 2009, pp. 1154-1157 (ASC 2008, Chicago).
References (2/6)

## Slide 37
[22] A. Kovalenko, N. Agapov, A. Alfeev, A. Bychkov, A. Gromov, H. Khodzhibagiyan, G. Kuztetsov, A. Shabunov, A. Starikov, E. Fischer, G. Moritz, P. Spiller ” Full size prototype magnets for heavy ion superconducting synchrotron SIS100 at GSI: Status of manufacturing and test at JINR”, Proceedings of EPAC08, Genoa, Italy, pp. 2443-2445
[23] E. Fischer, P. Schnizer, A. Akishin, H. Khodzhibagiyan, A. Kovalenko, R. Kurnyshov, P. Sherbakov, G. Sikler, and W. Walter “Full size model manufacturing and advanced design status of the SIS100 main magnets”, WAMSDO-2008 Workshop Proceedings, CERN, pp. 147 – 156.
[24] E. Fischer, A. Mierau, P. Schnizer, A. Bleile, W. Gaertner, O. Guymenuk, H. Khodzhibagiyan, C. Schroeder, G. Sikler, and A. Stafiniak „Thermodynamic Properties of Fast Ramped Superconducting Accelerator Magnets for the FAIR Project“, Advances in Cryogenic Engineering N55, 2010, pp.989-996, (CEC 2009, USA).
[25] E. Fischer, P. Schnizer, A. Akishin, H. Khodzhibagiyan, A. Kovalenko, R. Kurnyshov, P. Sherbakov, G. Sikler, and W. Walter “Full size model manufacturing and advanced design status of the SIS100 main magnets”, WAMSDO-2008 Workshop Proceedings, CERN, pp. 147 – 156.
[26] E. Fischer, P. Schnizer, H. Khodzhibagiyan, A. Kovalenko, R. Kurnyshov, P. Akishin, A. Mierau, B. Schnizer, P. Shcherbakov, K. Sugita “Common design aspects for fast ramped superconducting accelerator magnets”, (Magnet Workshop @ PAC09).
[27] E. Fischer, P. Schnizer, A. Mierau, A. Bleile, C. Heil, H. Khodzhibagiyan, R. Kurnyshov, B. Schnizer, P. Shcherbakov, C. Schroeder, A. Stafiniak, S.Y. Shim, “SIS100 main magnets: Test results and operation parameters”, GSI scientific report 2009, FAIR-Accelerators-02, Darmstadt.
[28] L. Potanina, V. Pantsyrny, A. Shikov, N. Salunin, I. Gubkin, V. Korpusov, H. Khodzhibagiyan, A. Kovalenko, “Superconductor wire and cable development for FAIR”, GSI scientific report 2009, FAIR-Accelerators-30, Darmstadt.
[29] H G Khodzhibagiyan, V M Drobin, E Fischer, A D Kovalenko, V I Pantsyrny, L V Potanina, A K Shikov and N M Vladimirova, “Design and study of new cables for superconducting accelerator magnets: Synchrotron SIS 100 at GSI and NICA collider at JINR”, 2010 J. Phys.: Conf. Ser. 234 022017, doi: 10.1088/1742-6596/234/2/022017.
[30] K. Sugita, E. Fischer, H. Khodzhibagiyan, and J. Macavei „Design Study of Superconducting Corrector Magnets for SIS 100“, IEEE Trans. on Appl. Supercond., Vol. 20, No. 3, pp.164-167, June 2010, (MT-21, October 2009, Hefei, China).
[31] A. Kovalenko, A. Bychkov, E. Fischer, H. Khodzhibagiyan, G. Kuznetsov, J.P. Meier, P. Schnizer, A. Shabunov, P. Spiller, J. Stadlmann, G. Titova “The FAIR SIS100 Synchrotron: Engineering Design of Superconducting Magnetic Modules”, IEEE Trans. on Appl. Supercond., Vol. 20, No. 3, pp.180-183, June 2010 (MT-21, October 2009, Hefei, China).
References (3/6)

## Slide 38
[32] L. Potanina, V. Pantsyrny, A. Shikov, N. Salunin, I. Gubkin, V. Korpusov, H. Khodzhibagiyan, A. Kovalenko, E. Fischer, H. Mueller, G. Moritz „Experimental Results on the Development of Superconducting NbTi/Cu-Mn/Cu Wires for Magnet Systems of SIS100 and SIS300 Synchrotrons of FAIR“, IEEE Trans. on Appl. Supercond., Vol. 20, No. 3, pp.1395-1398, June 2010 (MT-21, October 2009, Hefei, China).
[33] E. Fischer, P. Schnizer, K. Sugita, J. Meier,A. Mierau, P. Spiller, O. Kester, GSI, H. Khodzhibagiyan, G. Trubnikov, “Superconducting quadrupole module system for the SIS100 synchrotron”, Proceedings of IPAC2011, San Sebastián, Spain, pp. 143-145.
[34] E. Fischer, H. Khodzhibagiyan, P. Schnizer, and A. Bleile “Status of the superconducting magnets for the SIS100 synchrotron and the NICA project”, IEEE Trans. Appl. Supercond., v. 23, N3, June 2013, pp. 4100504.
[35] Kovalenko A.D., Kekelidze V.D., Trubnikov G.V., Khodzhibagiyan H.G., “Superconducting Magnets of the Nuclotron and Their Improvement for the Heavy Ion Synchrotron SIS100 at FAIR Project”, Nuclear Energy vol. 112, N2, pp. 68-76,
[36] E. Fischer, P. Schnizer, K. Sugita, J. Meier, A. Mierau, P. Spiller, O. Kester, H. Khodzhibagiyan, G. Trubnikov “Superconducting quadrupole module system for the SIS100 synchrotron”, Proceedings of RUPAC2012, Saint-Petersburg, Russia, pp. 143-145.
[37] A Bleile, E Fischer, H Khodzhibagiyan, A Mireau and P Schnizer, “Investigation of the cooling conditions for the fast ramped superconducting magnets of the SIS100 Synchrotron”, Journal of Physics: Conference Series 507 (2014) 032007, doi: 10.1088/1742-6596/507/3/032007.
[38] P.J. Spiller, R. Balss, A. Bleile, L.H.J. Bozyk, J. Ceballos Velasco, T. Eisel, E.S. Fischer, P. Forck, P. Hülsmann, M. Kauschke, O.K. Kester, H. Klingbeil, H.G. König, H. Kollmus, P. Kowina, A. Krämer, J.P. Meier, A. Mierau, C. Omet, D. Ondreka, N. Pyka, H. Ramakers, P. Schnizer, H. Welker, St. Wilfert, A. Iluk, H.G. Khodzhibagiyan, D. Urner, “Status of the FAIR Synchrotron Projects SIS18 Upgrade and SIS100”, Proceeding of IPAC2014, Dresden, pp. 1857-1860.
[39] S.A. Kostromin, N.N. Agapov, V.V. Borisov, A.R. Galimov, V. Karpinsky, H.G. Khodzhibagiyan, V.S. Korolev, D. Nikiforov, N.V. Semin, A.Y. Starikov, G.V. Trubnikov, “Facility for Assembling and Serial Test of Superconducting Magnets”, Proceeding of IPAC2014, Dresden, pp. 2700-2702.
[40] E. Fischer, and H. Khodzhibagiyan, “Superferric magnets: Nuclotron-NICA-FAIR experience and plans”, Proceeding of the International Workshop on celerator Science and Technology for Electron-Ion Collider EIC’14, Newport News, USA, 17-21 March 2014.
References (4/6)

## Slide 39
[41] Khodzhibagiyan H., Agapov N., Borisov V., Galimov A., Korolev V., Nikiforov V., Karpinskiy V., Kostromin S., Starikov A., and Trubnikov G., “Facility for Superconducting Magnet Assembling and Serial Testing”, Proceeding of the 13th Cryogenics 2014, IIR International Conference, April 2014, Prague, Czech Republic, pp. 66-70.
[42] Bleile A., Fischer E., Khodzhibagiyan H., Schnizer P., “Heat exchangers for stable two phase Helium cooling in parallel superconducting magnet channels”, Proceeding of the 13th Cryogenics 2014, IIR International Conference, April 2014, Prague, Czech Republic, pp. 30-34.
[43] A. Mierau, P. Schnizer, E. Fischer, H. Mueller, H. Khodzhibagiyan, S. Kostromin, L. Serio, S. Russenschuck, O. Dunkel, “Testing of the superconducting magnets for the FAIR Project”, IEEE Trans. Appl. Supercond., v. 26, Issue 4, June 2016, 4401605.
[44] E. Fischer ; C. Roux ; K. Sugita ; P. Schnizer ; A. Bleile ; A. Mierau ; J. Meier ; H. Khodzhibagiyan, S. Kostromin, “Production Status of the SIS100 Superconducting Magnets for FAIR”, IEEE Trans. Appl. Supercond., v. 26, Issue 4, June 2016, 4005405.
[45] S. Kostromin, V. Borisov, A. Donyagin, A. Galimov, O. Golubitskiy, H. Khodzhibagiyan, S. Korovkin, A. Kudashkin, G. Kuznetsov, D. Nikiforov T. Serochkina, A. Shemchuk, A. Starikov, A. Tikhomirov, “Commissioning of Facility for Assembling and Tests of Superconducting Magnets”, Proceeding of the 7th International Particle Accelerator Conference IPAC 2016, May 2016, Busan, Korea, DOI: 10.18429/JACoW-IPAC2016-TUPMB051.
[46] Egbert Fischer; Kei Sugita; Pierre Schnizer; Hamlet Khodzhibagiyan, “Nuclotron-type cables: from fast ramped superconducting magnets to multipurpose application”, IEEE Trans. Appl. Supercond., v. PP, Issue 99, 2017, DOI: 10.1109/TASC.2017.2663840.
[47] E. Fischer, A. Bleile, J. Meier, A. Mierau, P. Schnizer, P. Spiller, K. Sugita, H. Khodzhibagiyan, S. Kostromin, G. Trubnikov, “The FAIR-NICA Collaboration for Production and Testing of Superconducting Accelerator Magnets”, Proceedings of RUPAC2016, Saint-Petersburg, Russia, Presented on RUPAC2016, Saint-Petersburg, Russia.
[48] Nikiforov D., Galimov A., Kostromin S., Khodzhibagiyan H., Emelianov N., CREATION OF CRYOGENIC TESTING BENCH FOR SUPERCONDUCTING MAGNETS OF NICA AND SIS100 PROJECTS, В сборнике: Refrigeration Science and Technology 24. Сер. "24th IIR International Congress of Refrigeration, ICR 2015" 2015, pp. 4204-4210.
[49] Mierau A., Schnizer P., Fischer E., Mueller H., Khodzhibagiyan H., Kostromin S., Serio L., Russenschuck S., Dunkel, TESTING OF THE SUPERCONDUCTING MAGNETS FOR THE FAIR PROJECT, O.IEEE Transactions on Applied Superconductivity, 2016, v. 26. N 4, p. 7426765.
References (5/6)

## Slide 40
[50] Fischer E., Roux C., Sugita K., Schnizer P., Bleile A., Mierau A., Meier J.-P., Khodzhibagiyan H., Kostromin S., PRODUCTION STATUS OF THE SIS100 SUPERCONDUCTING MAGNETS FOR FAIR. IEEE Transactions on Applied Superconductivity. 2016. Т. 26. № 4. С. 7442794.
[50] Fischer E., Sugita K., Schnizer P., Khodzhibagiyan H., NUCLOTRON-TYPE CABLES: FROM FAST RAMPED SC. MAGNETS TO MULTIPURPOSE APPLICATION, IEEE Transactions on Applied Superconductivity. 2017. Т. 27. № 4. С. 7839916.
[51] H. Khodzhibagiyan, V. Borisov, V. Kekelidze, S. Kostromin, D. Nikiforov, A. Starikov, G. Trubnikov, E. Fischer, “Status of Manufacturing and Testing of Superconducting Magnets for NICA and FAIR Projects”, IEEE Transactions on Applied Superconductivity, 2018, vol. 28, N 3, Article Sequence Number: 4000405, DOI: 10.1109/TASC.2017.2772830.
[52] A. Mierau1, E. Fischer, F. Kaether, C. Roux, A. Bleile, V. Marusov, K. Sugita, P. Szwangruber, H. Weiss, H. Khodzhibagiyan, S. Kostromin, “Testing of the superconducting magnets for the SIS100 Synchrotron”, IEEE Transactions on Applied Superconductivity, 2018, vol. 28, N 3, Article Sequence Number: 4001505, DOI: 10.1109/TASC.2017.2777832.
[53] H. G. Khodzhibagiyan, V. V. Borisov, V. D. Kekelidze, S. A. Kostromin, D. N. Nikiforov, A. Yu. Starikov, G. V. Trubnikov, E. Fischer, A. Bleile, V. Datskov, F. Kaether, A. Mierau, C. Roux, P. Spiller, K. Sugita, “Production and Test Status of the Superconducting Magnets for the NICA project and the SIS100 Synchrotron”, IEEE Transactions on Applied Superconductivity, 2019, vol. 29, Article Sequence Number: 4100806, DOI: 10.1109/TASC.2019.2901591.
[54] H. Khodzhibagiyan, A. Bleile, V. Borisov, V. Datskov, E. Fischer, S. Kostromin, A. Mierau and D. Nikiforov, “Cryogenic test results of the superconducting magnets for the NICA complex and the SIS100 synchrotron of FAIR”, Proc. ICEC27-ICMC 2018, September 2018, Oxford, United Kingdom, 2019 IOP Conf. Ser.: Mater. Sci. Eng. 502 012096.
[55] A. Bleile, V. Datskov, E. Fischer, H. Khodzhibagiyan, A. Mierau, D. Nikiforov, “Hydraulic adjustment of the two-phase helium forced flow cooled superconducting magnets of the SIS100 heavy ion synchrotron for FAIR”, IOP Conference Series: Materials Science and Engineering, vol. 502, no. 1, Apr. 2019 (ICEC27-ICMC 2018, September 2018, Oxford, United Kingdom).
[56] P. Spiller, P. Bartolome, J. Blaurock, … H. Khodzhibagiyan, …D.F.A. Winters” The FAIR Heavy Ion Synchrotron SIS100”, Journal of Instrumentation 15(12):T12013-T12013, Dec. 2020, DOI:10.1088/1748-0221/15/12/T12013.
[57] A Bleile, I Datskov, E Fischer, H Khodzhibagiyan, V Marusov, C Roux, P Spiller, K Sugita and A Szwangruber, “Cryogenic testing of fast ramping superconducting magnets for the SIS100 synchrotron”, IOP Conf. Series: Materials Science and Engineering 755 (2020), doi:10.1088/1757-899X/755/1/012133.
References (6/6)