## Slide 1
photoluminescence of swift heavy ion
irradiated Magnesium aluminate spinel
single crystals
M. Mamatova*, V.A. Skuratov, A. Olejniczak, N.S. Kirilkin
Flerov Laboratory of Nuclear Reactions, JINR
Sector №8. Ion-implantation nanotechnology and radiation materials science
XXVI International Conference of Young Scientists and Specialists (AYSS-2022)
24 – 28 October 2022, Dubna, Russia

## Slide 2
introduction
Important properties:
Wide band-gap (~9 eV);
High hardness (16 GPa);
Thermal stability (Tmelt = 2135 ˚C);
Low density ~ 3.58 g·cm-3;
High transparent in the visible and infrared wavelength regions;
Excellent radiation resistance.
Schematic illustrations of MgAl2O4 structure :
A
of space group (Fd3m).
The cations occupy
1/8 () of the tetrahedral sites (Td point symmetry) and
1/2 ( ) of the octahedral sites (D3d local symmetry), and
there are 32 oxygen ions in the unit cell.
host for inert matrix fuels in light water reactors
transmutation target for minor actinides and long life fission products
diagnostic/optical windows of fusion devices (ITER, DEMO..)
aerospace engineering
laser technology
Potential applications:

## Slide 3
to study a swift heavy ions-induced defects in single crystals using optical spectroscopy methods.
Information about radiation defects induced by swift heavy ions in spinel has been lacking, especially in the range of high ionization energy losses.
MOTIVATION
The aim of the present work is
E~ 70 – 100 MeV
Modelling of the actinide fission fragments impact

## Slide 4
Swift heavy ion irradiation:
High-density electronic excitation
Ion tracks
Amorphization
The phase transformation from spinel to defective rock-salt structure at the core region through the movements of cations from IV-site to VI-site under a condition of high electronic excitation
[*] S.J. Zinkle, V.A. Skuratov, NIMB, B 141, 1998.
[**] K. Yasuda and et.al., NIMB, B 250, 2006.
>100 dpa,
Highly resistant to radiation damage
Ion tracks in spinel irradiated with 430 MeV Kr ions to
a fluence of 1.1· 1012 cm-2 at RT
Schematic diagram of the radiation-induced microstructure induced by a single ion of 200 MeV Xe or 350 MeV Au

## Slide 5
C. Kinoshita. Microstructural evolution of
Irradiated ceramics. In: Radiation effects in
Solids. Eds. K.Sickafus, E.Kotomin and
B.Uberaga. Nato Science series. V.232, p.193.
Spinel is not amorphized by electron, neutron and low-energy ion irradiation at T>300 K.
Strong resistance to void or cavity formation in

## Slide 6
SWIFT HEAVY ION IRRADIATION PARAMETERS
Samples were irradiated at IC-100 and U-400 cyclotrons at room temperature in FLNR JINR (Dubna).
Ion type & Energy, MeV | Fluence, cm-2 | Rp, μm | Se, keV/nm
40Ar, 46 | 1010 – 1013 | 8.47 | 7.3
100Kr, 107 | 1010 – 1014 | 10.9 | 14.87
132Xe, 150 | 1010 – 1013 | 11.37 | 21.97
208Bi, 670 | 1010 – 1013 | 26.1 | 36.6

## Slide 7
I. Photoluminescence measurement setup
Scheme and photo of the experimental setup for PL measurements using confocal scanning microscope NTEGRA Spectra NT-MDT
Scheme of laser light focusing in the near-surface layer of the sample and electronic () and nuclear () stopping power

## Slide 8
II. Time-resolved Photoluminescence measurement setup
Setup for measurement of the photoluminescence kinetics.
1 – Head of the pulse laser,
2 – Photomultiplier Detector Assembly (PMA 175),
3 – Picosecond Diode Laser driver (PDL800-D).
Frequency ~ 1 MHz

## Slide 9
III. Photoluminescence measurement setup
*Belarusian State University (Minsk, Belarus)
Excitation was provided by
UV (355 nm)
Blue (473 nm)
Green (532 nm)
stationary laser sources
Registration of the
emission by Peltier-cooled CCD-matrix Andor Technology DU401A-BV
Micro Raman spectrometer Nanofinder High End (LOTIS TII Japan-Belarus)
combined with a 3D scanning confocal microscope

## Slide 10
RESULTS
Dependence of the photoluminescence spectra of MgAl2O4 on the excitation wavelength

## Slide 11
RESULTS

## Slide 12
RESULTS
Photoluminescence decay curves of spinel irradiated by Xe ions.
Ion fluence is 1.2×1012 cm-2.
Photoluminescence spectra of spinel irradiated by Xe ions
in the fluence range of 1010-5·1013 cm-2

## Slide 13
Photoluminescence intensity profiles

## Slide 14
RESULTS
The plan view microstructure of MgAl2O4 irradiated with 670 MeV Bi ions to a fluence of 1011 cm-2:
a) TEM image;
b) HR TEM image
a)
b)

## Slide 15
summary
Photoluminescence spectra of intact spinel crystals excited by 355, 445, 473 and 532 nm laser light are composed of emission bands/lines attributed to Mn2+ and Cr3+ impurities.
Irradiation of MgAl2O4 crystals with high-energy Kr and Bi ions results in appearance of intense non-elementary bands in 1.55 - 3.1 eV spectral range. Intensity of these bands increases with the ion fluence up to 1013 cm-2 (till ion track overlapping).
The emission decay times in 1.9 – 2.5 eV bands are ranged from 8 ns (500 nm, 2.5 eV) to 13.7 ns (650 nm, 1.9 eV).
Thank you for attention!

## Slide 17
Photoluminescence intensity profiles