## Slide 1: A structural phase transition in La2Ti2O7 at high pressure
Lab: Frank Laboratory for nuclear Research (JINR, Dubna, Russia).
Speaker: Asif Asadov.
Authors : A.G. Asadov1,2, D.P. Kozlenko2, A. Mammadov1, R. Mehdiyeva1,
S.E. Kichanov2, E.V. Lukin2, O.N. Lis2, A.V. Rutkauskas2.
Collaborations: 1 Institute of Physics, Azerbaijan National Academy of Sciences, Baku AZ-1143, Azerbaijan.
2 Frank Laboratory of Neutron Physics, JINR, 141980 Dubna, Russia.

## Slide 2: Usage areas
High pressure sensors
Actuator
Fuel cells technology
Energy conversion technology
Solid State memory
Asif Asadov AYSS-2022 Condense Matter Physics

## Slide 3: Measurments
Neutron diffraction at ambient condition (DN-6):
Asif Asadov AYSS-2022 Condense Matter Physics
The crystal structure of La2Ti2O7 was tested by neutron diffraction method, which allows determination of light oxygen atoms coordinates with much better accuracy. The neutron powder diffraction measurement at ambient conditions was performed with the DN-6 diffractometer at the IBR-2 high-flux pulsed reactor (FLNP JINR, Dubna, Russia). Diffraction patterns were collected at scattering angles 2=90. The spectrometer resolution at  = 2 Å is d/d = 0.022 for this angle. The typical data collection time was 20 min. The sample volume was about 5 mm3.
a) DN-6 diffractometer beam line b) Detectors

## Slide 4
X-ray diffraction at pressure range 1 atm – 32 GPa:
Asif Asadov AYSS-2022 Condense Matter Physics
The X-ray diffraction experiments were carried out with the Xenocs Xeuss 3.0 specialized diffractometer (Xenocs SAS, France). The used Mo Kα X-ray radiation with the wavelength
λ= 0.71078 Å was generated by the GeniX3D source. X-ray diffraction patterns were collected using the DETRICS detector at sample-detector distances of 0.5 m.
a) Xenocs Xeuss 3.0
b) Genix3D source
c) DETRICS dedector

## Slide 5
Raman Spectroscopy at pressure range 1atm-30 GPa
Asif Asadov AYSS-2022 Condense Matter Physics
Raman spectra were collected using a LabRAM HR spectrometer (Horiba Gr, France) with a wavelength excitation of 633 nm emitted from He–Ne laser, 1800 grating, a confocal hole of 100 μm, and 50 objective.

## Slide 6: Results and Discussions.
Asif Asadov AYSS-2022 Condense Matter Physics
Neutron diffraction pattern of La2Ti2O7 at ambient temperature and pressure.
Neutron diffraction.
Expected and modelled space groups:
P21, P2, P2/m – monoclinic
Pna21, Cmc21 - orthorhombic
The schematic representation of modelled crystal structure of La2Ti2O7 compound.
Neutron diffraction confirms that crystal structure at ambient condition is monoclinic P21!!!

## Slide 7
Asif Asadov AYSS-2022 Condense Matter Physics
X-ray diffraction measurements.
At P>16.3 GPa, several new diffraction peaks located at 2 ~ 6.4; 7.5; and 9.4; were detected, at the same time, reflection at 2 ~ 8.0; 9.7; 21.0 disappear. The significant changes in relative intensities of other diffraction peaks were detected. This kind of high pressure structure estimated as new P2 monoclinic phase .

## Slide 8
Asif Asadov AYSS-2022 Condense Matter Physics
The compressibility of the lattice parameters :
kai = -(1/ai0)(dai/dP)|T, ai = a, b, c
were calculated for low-pressure and high-pressure phase of La2Ti2O7. The values
ka1 = 0.00022(1) GP-1 kb1 =0.0010(1) GPa-1 kc1 =0.0022(1) GPa-1 - low pressure phase
ka2 =0.00017(1) GPa-1, kb2 = 0.0008(1) GPa-1, kc2 =0.0017(2) GPa-1 - high pressure phase

## Slide 9
Asif Asadov AYSS-2022 Condense Matter Physics
The volume compressibility data were fitted by the third-order Birch-Murnaghan equation of state:
Here x = V/V0 is the relative volume change, V0 is the unit cell volume at P = 0, and B0, B' are the bulk modulus
B0 = -V(dP/dV)T
B' = (dB0/dP)T
The fitted values B0 = 183(4) GPa at B' = 5(1) for the initial monoclinic P21 phase at low pressures (P< 16.3GPa).
B0 = 201(1) GPa with fixed B' = 4(0) for the pressure induced phase P2 of La2Ti2O7 were calculated for high pressures (P>16.3GPa).
The obtained values of bulk modulus are higher than the previous ones .

## Slide 10
Asif Asadov AYSS-2022 Condense Matter Physics
Raman spectroscopy measurements.
The low frequency vibration modes in the wavelength range 50–490 cm-1 can be attributed to the La–O vibrations; the modes in the range 490–575 cm-1 associated with the vibrations of the distorted TiO6 octahedra; the symmetric and asymmetric stretching modes of the of Ti–O vibrations are located in the range of 785-814 cm-1 .

## Slide 11
Asif Asadov AYSS-2022 Condense Matter Physics
The dependences of the relative displacement of La3+ ions relative to each other are shown in the Figure (a) . There are the changes in the relative distance  between lanthanum ions in different crystallographic positions. After the phase transition above 16.3 GPa, an increase in the magnitude of the displacement of rare-earth ions is observed, which indicates the grow of a disordering of the crystal structure of La2Ti2O7 at high pressure.
The Raman spectra doublet at ~790 cm-1 Figure (b) which is associated with a distortion of the TiO6 octahedra, have similar behavior under pressure. Then the pressure increases, a slight symmetrization of the TiO6 octahedra is observed, but after the phase transition, the octahedra distortions begin to increase.
a)
b)

## Slide 12: Conclusion.
Neutron diffraction confirms that, at ambient conditions La2Ti2O7 structure is P21 monoclinic and unit cell parameters : a = 7.752(4) Å, b = 5.510(2) Å,
c = 12.962(3) Å, β = 98.7(2).
In X- ray diffraction spectrum of La2Ti2O7 distinctive differences observed for low and high pressure region. The structure of high pressure spectrum allow us to model this phase as P2 monoclinic. This kind of phase transition happen at P≈17.3 Gpa.
Phase Transition related with displacement of La3+ ions in unit cell and distortion of TiO6 octahedrons.
Raman spectrum confirms phase transition at high pressure region which is happen at exactly in vibration of distorted TiO6 octahedrons modes and Ti-O stretch modes region.
Asif Asadov AYSS-2022 Condense Matter Physics

## Slide 13: Thank for your attention!!!