## Slide 1
EFFECT OF CARBON ADDITIVES ON THE STRUCTURE OF ELECTRODES FOR HIGH ENERGY DENSITY Li-ION BATTERIES
Meir Yerdauletov[2,3,4], Philipp Napolsky[1,2], Mikhail Avdeev[1,2], Victor Krivchenko[1]
[1]Dubna University, Dubna, Moscow Region, 141980 Russia
[2]Frank Laboratory of Neutron Physics, Joint Institute for Nuclear Research, Dubna, Moscow region, 141980 Russia
[3]Institute of Nuclear Physics, Ministry of Energy of the Republic of Kazakhstan, Almaty, 050032 Kazakhstan
[ 4]L.N. Gumilev Eurasian National University, Astana, 010000 Kazakhstan

## Slide 2
Comparison of specific energy and specific power of various energy storage systems. From the diagram, it can be seen that LICs bridge the gap between lithium-ion batteries and double-layer capacitors, making them promising for high power applications where long run times between recharges are important.
Energy storage systems

## Slide 3: Li ion batteries vs Supercapacitors

## Slide 4: Hybrid Li ion capacitors

## Slide 5
Study of the electrochemical characteristics of positive electrodes based on activated carbons, obtained from various biowaste.
Prototyping a Lithium Metal Capacitor with Increased Energy Density prismatic form factor.
Investigate Lithium deposition with neutron radiography and tomography
The aim of the work: Development of lithium-metal capacitors with increased specific energy and power
.
Tasks to be solved as part of the work:

## Slide 6
Electrolytes
1M LiClO4 in FEC-DME_3-7
1M LiDFOB in EC-DMC-DEC-1-1-1
1M LiDFOB in FEC-DME_3-7
1M LiDFOB in FEC-DME_3-7_LiNO3-3wt
1M LiDFOB in VC-DME_3-7
1M LiPF6 in EC-DMC-DEC-1_1_1(Sigma)
EXPERIMENTAL PARAMETERS
CATHODE COATING
Active material - activated carbon from rice hulls [90%]
Conductive additive - carbon nanotubes [5%]
Polymer binder - PVDF [5%]
Mass loading of the electrode coating - 2.5 mg/cm2
Anode
Lithium metal 150 µm thick
Separator
Celgard 2500
Elements
Coin cell 2032

## Slide 7
Galvanostatic curves

## Slide 8: Results Scanning electron microscopy (SEM, Jeol JSM-6490LA) Transmission electron microscopy (TEM, JEM-2100analysis)
SEM micrographs of
carbonized Rice Husk
SEM micrographs of
activated Rice Husk
TEM micrographs of
activated Rice Husk

## Slide 9: Neutron tomography
Tomography experiments were done at TITAN beamline of WWR-K reactor Almaty INP. As convertor used 6LiF/ZnS scintillators with thicknesses of 100 μm, Hamamats CCD -chip based camera, and L/D was typically set at 350. Pixel resolution was 45 μm.
The neutron tomography method was used to visualize the lithium and electrolyte distribution regions flowing inside the cell in the initial and final states of lithium-ion batteries.
Capacity 0 %
Capacity 50 %
Capacity 100 %

## Slide 10
Conclusions
F uture Plans
1)
All the carbon structure s use d in the
e xpe rime nts provide s kine tic transport of
lithium ions into the crystals of active
mate rial
1.
2.
3.
Mak ing prototy pe s of Li ion batte ries /capacitors in cylindrical form
2)
3)
4)
Ne utron radiography showe d electrolyte deposition in Coin 2032 cells
De ve lopme nt of scie nt ific and te chno log ical
criteria for the creation of e le ctrolyte s,
e le ctrode coatings and de sign of lithium-ion
batte rie s, allowing to work in t he are a
of e xtre me ly low te mpe rature s (be low -40C).
De ve lopme nt of te chno logica l solut io ns for
cre ating new ge ne ratio n lit hium-io n batte rie s at
the level prototypes wit h the ir s ubse que nt
introductio n into pilot and se rial productio n
Cathode materials obtained from biowaste
Prototype of Li ion capacitors were made