## Slide 1
24 – 28 October 2022, Dubna, Russia
R&D tellurium-loaded
liquid scintillator
I. Suslov, I. Nemchenok, A. Bystryakov
XXVI International Scientific Conference of Young Scientists and Specialists

## Slide 2
Neutrinoless double β-decay
2
Observation of 0vββ decay would imply:
- lepton number violation;
- presence of a Majorana term for the neutrino mass;
- сonstraints on neutrino mass hierarchy and scale;
- hint on origin of matter/anti-matter asymmetry.
1. Shimizu I. and Chen M. (2019) Double Beta Decay Experiments With Loaded Liquid Scintillator. Front. Phys. 7:33.

## Slide 3
3
Element/isotope, concentration | Scintillation base | Element-containing additive | Light yield4
Nd, up to 6.5 g/l [2] | PC1 | 2-Methylvalerate | 80%
150Nd, [3] up to 20 g/l up to 2 g/l | PC1 PC1 | Tris(trimethylhexanoate) Complexes with fluorinated β-diketonates | 90% 62%
Nd, 0.32% [4] | LAB2 | 4-Methyloctanoate | 64%
Mo, 0.027 – 0.43% [5] | Toluene | Nanoparticles of AMoO4 (A= Ca, Sr, Ba) | –
Sn, 32.6%, [6] | PC | Tetramethyltin | 57%
Sn, 0.5 – 10% [7] | LAB | Tetrabutyltin | 96% – 55%
Cd, 1.5% [8] | LAB + TBP3 | Chloride | 47%
Zr, 1.4% [9] | Anisole | Tetrakisisopropylacetoacetate | 30 – 40%
Zr, up to 2.5 g/l [10] | PC1 | Dipivaloylmethanate | 63%
Zr, 0.33% [11] | Toluene | Nanoparticles of ZrO2 | -
136Xe, ≤ 3% [12] | Decane + PC1 | Gaseous 136Хе | -
Te, 0.5% [13] [14] | LAB | Complex of telluric acid with butanediol + N,N-dimethyldodecylamine | 64% 67%
1 Pseudocumene; 2Linear alkylbenzene; 3Tributylphosphate; 4 Relative to unloaded LS
Element-loaded liquid scintillators for searching 0νββ
2. I.R. Barabanov, et al., Instruments and Experimental Techniques. 55 (2012) 545–550.
3. I.R. Barabanov, et al., Physics of Atomic Nuclei. 82 (2019) 89–97.
4. I.B. Nemchenok, et al., Bulletin of the Russian Academy of Sciences: Physics. 75 (2011) 1007.
5. S. Arai, et al., Journal of the Ceramic Society of Japan. 127(2019).
6. M.J. Hwang, et al., NIM A. 570 (2007) 454–458..
7. O. Chkvorets, et al., Journal of Physics: Conference Series. 1342 (2020) 12112.
8. I.B. Nemchenok, et al, Bulletin of the Russian Academy of Sciences: Physics. 76 (2012) 1187–1190.
9. Y. Fukuda, et al., Journal of Physics: Conference Series. 1342 (2020) 12093.
10. L.B. Bezrukov, et al., Russian Journal of Inorganic Chemistry. 66 (2021) 421–426.
11. A. Watanabe, et al., Nanomaterials. 11 (2021).
12. Y. Gando, (2019). http://arxiv.org/abs/1904.06655 (accessed September 24, 2021).
13. S. Biller, S. Manecki, Journal of Physics: Conference Series. 888 (2017) 12084.
14. Patent CN № 112608263 (B), pub. 2022-05-27. G01T 1/20

## Slide 4
Tellurium-containing additive:
solubility in the scintillation base;
no absorption in UV-VIS region (300 – 600 nm);
individual compound;
being in a solid state of aggregation at the temperature of use (preferable);
stability to hydrolysis, atmospheric oxygen and other environmental influences;
non-toxicity;
non-flammable and explosion safety.
Scintillation base:
–high boiling point;
–explosion and fire safety, high flash point;
–non-toxicity;
–low corrosive activity in relation to the materials of the detector;
–availability and low cost.
Linear alkylbenzene:
Composition of Te-LS and its requirements
Scintillation additives:
Structure formula of diphenyltellurium (a) di-2-ethylhexanoate,
(b) oxide with di-(2-ethylhexyl)phosphoric acid) (complex)
PPO
POPOP
4
(a)
(b)

## Slide 5
Light yield (relative to unloaded LS) and transparency data at λ=430 nm (optical path 10 cm, relative to air) of Te-LS with a (a) diphenyltellurium di-2-ethylhexanoate, (b) diphenyltellurium oxide•L constant concentration PPO, POPOP (0.5%, 0.0025%, respectively)
Scintillation characteristics.
Concentration dependency
5
Te, % | Tλ=430 nm ±1, % | 
 | (a) | (b)
0 | 90.9 | 90.9
0.1 | 90.2 | -
0.25 | 90.3 | 87.9
0.5 | 88.9 | 87.1
0.75 | 88.7 | 87.0
1.0 | 86.2 | 85.1
1.25 | - | 83.8

## Slide 6
Scintillation characteristics.
Optimization PPO and POPOP
Te-LS light yield as a function of the concentration (1) PPO (concentration POPOP – 0.0025%), (2) POPOP with a constant concentration PPO (for (a) 1% Te, 2% PPO, for (b) 1% Te, 0.5% PPO) relative to unloaded LS
6
(1)
(2)

## Slide 7
Scintillation characteristics.
Optimization secondary scintillation solvent
7
DIPN, % | Light yield, rel. units |  | Tλ=430 nm ±1, % | 
 | (a) | (b) | (a) | (b)
0 | 0.42±0.02 | 0.55±0.03 | 86.6 | 85.1
10 | 0.50±0.03 | 0.60±0.03 | 83.1 | 82.9
20 | 0.55±0.03 | 0.67±0.03 | 82.9 | 82.6
30 | 0.57±0.03 | 0.71±0.04 | 81.0 | 80.8
40 | - | 0.74±0.04 | - | 79.9
50 | - | 0.78±0.04 | - | 79.0
60 | - | 0.88±0.04 | - | 77.1
70 | - | 0.88±0.04 | - | 74.0
diisopropylnaphthalene
Te-LS light yield with different concentration DIPNmix with a constant concentration 1% Te, PPO, POPOP (for (a) – 2% PPO, 0.04% POPOP; for (b) – 0.5% PPO, 0.0025% POPOP)

## Slide 8
Scintillation characteristics.
Stability
Stability of light yield and transparency for Te-LS samples with a content
(a) 1%Te (in form of diphenyltellurium di-2-ethylhexanoate), 2%PPO, 0.04%POPOP, 30% DIPN,
(b) 1%Te (in form of diphenyltellurium oxide•L), 0.5%PPO, 0.0025%POPOP, 30% DIPNmix,
8
Date | Tλ=430 nm ±1, % | 
 | (a) | (b)
22.12.20 | 81.0 | -
31.03.21 | 81.0 | -
29.06.21 | 81.2 | -
29.09.21 | 82.3 | -
21.12.21 | 80.4 | -
31.03.22 | 80.9 | 80.9
20.06.22 | 82.6 | 79.9
22.09.22 | 81.7 | 79.7
(b)
(a)

## Slide 9
Te-LS sample | Scintillation composition | Light yield1, relative units
Our research (a) | 0.5% Te, 1% PPO, 0.04%POPOP, 30% DIPN | 0.72±0.03
Our research (a) | 1% Te, 2% PPO, 0.04%POPOP, 30% DIPN | 0.58±0.03
Our research (b) | 0.5% Te, 0.5% PPO, 0.0025%POPOP | 0.73±0.04
Our research (b) | 1% Te, 0.5% PPO, 0.0025% POPOP, 30% DIPNmix | 0.71±0.03
Patent CN 112608263 (B)2 [14] | 0.5% Te, 2.5 g/L PPO, 3 mg/L bis-MSB | ~0.67
SNO+2 [15] | 1% Te, 6 g/L PPO | ~0.65
Scintillation characteristics.
Comparison with other Te-LS
14.Patent CN № 112608263 (B), pub. 2022-05-27. G01T 1/20
15. T. Kroupova, Water phase results and 0νββ prospects of the SNO+ experiment, in: Proceedings of European Physical Society Conference on High Energy Physics — PoS(EPS-HEP2019), Sissa Medialab, Trieste, Italy, (2020)
1Relative to unloaded LS
2Tellurium in form of complex telluric acid with butanediol-1,2 and N,N-dimethyldodecylamine

## Slide 10
10
Conclusion
1. The samples of the new liquid scintillator with a tellurium concentration up to 1% were obtained and good light yield.
2. In aim to improve the light yield of the new scintillator:
scintillation additive concentrations are optimized;
secondary solvent diisopropylnapthalene are used;
different tellurium additives - diphenyltellurium dicarboxylates and complex of diphenyltellurium oxide with organic ligand are tested.
3. Long-term stability properties of a new Te-LS’s are showed.

## Slide 11
Backup
11

## Slide 12
Block diagram of the installation for measuring the light yield and energy resolution of the LS: 1 - light-protective box; 2 - radioactive source; 3 – cell with LS; 4 - PMT; 5 – high voltage source; 6 - preamplifier; 7 - amplifier; 8 - signal converter
Measurement technique
Light yield:
UV-VIS spectra: UNICO UV 2804 in a 10 cm cuvette relative to air at a wavelength of 390 to 600 nm.
Tellurium-containing additives: UV-VIS, IR, Raman-spectroscopy, elemental analysis (C, H, Te), Differential Scanning Calorimetry (melting point), ICP-AES (MS) (in plans)
12
Experimental conditions:
teflon cuvette with uviol glass;
volume – 40 ml, height – 2 cm;
207Bi A=2.5 kBq;
difference measurement method

## Slide 13
Scintillation characteristics.
Absolute light yield
1in form di-2-ethylhexanoate diphenyltellurium
2LS based on diisopropylnapthalene with light yield 12.300 photons/ 1 MeV e-
LS sample | Scintillation composition | Absolute LY, photons/MeV | Evaluation method
unloaded-LS | 0.5% PPO, 0.0025%POPOP | 8646±400 | Relative to EJ-3092
Te-LS | 0.5% Te1, 1% PPO, 0.04% POPOP, 30% DIPN | 6399±320 | Relative to EJ-309
Te-LS | 1% Te1, 2% PPO, 0.04% POPOP, 30% DIPN | 5128±256 | Relative to EJ-309
RENO | 0.3% PPO, 0.0030% bis-MSB | ~8000 | Relative to anthracene
Daya Bay | 0.3% PPO, 0.0015% bis-MSB | 8700 | Relative to anthracene
Stereo | 0.3% PPO, 0.0020% bis-MSB | 8400 | Quantum efficiency of PMT
13

## Slide 14
Synthesis of diphenyltelluirum derivatives
14