## Slide 1: MeV energy electron and proton irradiation effects in semiconductor materials for space applications
Vika Arzumanyan
V. Harutyunyan, A. Sahakyan, N. Grigoryan, A. Martirosyan
Yerevan, Armenia
Email: vika.arzumanyan@yerphi.am
XXVI International Scientific Conference of Young Scientists and Specialists
(AYSS-2022), Dubna, Russia

## Slide 2
Inner Radiation Belt:
Protons and electrons ≤ 1.5MeV
Outer Radiation Belt:
Energetic protons ≥ 10MeV
Energetic electrons ≥ 2 MeV, ≤ 10MeV
Earth’s Radiation Belts

## Slide 4: Aim
The radiation defects’ concentration and the introduction rate of radiation defects depending on the electron irradiation dose in semiconductor crystals of n-Si and n-GaP and proton irradiation dose in n-type and p-type Si crystals were studied.
The aim is to identify an effective property of the irradiated sample in order to express changes in the structures and physical properties of semiconductors so that materials with specific predictable parameters can be created.
V. Arzumanyan. MeV energy electron and proton irradiation effects in …

## Slide 5: Experimental methods
Electron irradiation
Energy – 3.5 MeV
Bunch charge – 60 pC
Bunch length – 0.4 ps
Repetition rate – 12 Hz
Intensity- 109el/cm2·s
Proton irradiation
Energy -18MeV
Mean current -1μA
Intensity- 1012p/cm2·s
V. Arzumanyan. MeV energy electron and proton irradiation effects in …
AREAL Facility at CANDLE, Armenia
Cyclotron C-18 at Radioisotope Production Center, Armenia

## Slide 6: Experimental methods
Parameters of each sample were measured using a direct current Hall effect method:
Magnetic flux - 0.5 Т
Electric current - 0.05—1 mA.
The mean experimental error for the measurements was determined to be no greater than ± 7%.
V. Arzumanyan. MeV energy electron and proton irradiation effects in …
6mm
3mm
0.5mm

## Slide 7: Experimental results
Fig. 1. Radiation defect concentration () vs irradiation dose for proton and electron irradiation of n-type silicon crystals.
Fig. 2. Radiation defect concentration () vs irradiation dose for proton irradiation of p-type silicon crystal.
V. Arzumanyan. MeV energy electron and proton irradiation effects in …

## Slide 8: Experimental results
By application of the fitting method to the dose-dependence curves, it was found that the empiric exponential function provided the best agreement with the experimental data, independent of the particle type, energy and irradiation dose. The exponential function used is represented in Eq. (1):
where 𝑛0 is the concentration of charge carriers before irradiation, and 𝑛(𝐷) is their concentration at a given irradiation dose 𝐷, at room temperatures; and 𝐷0 is the irradiation dose at which the carrier concentration 𝑛(𝐷) at a temperature 𝑇 = 300 K decreases by a factor of e. The introduction rate of radiation defects (∆Ndef)⁄∆D versus the irradiation dose D can be presented according to Eq. (2):
V. Arzumanyan. MeV energy electron and proton irradiation effects in …

## Slide 9: Experimental results
Fig. 4. Introduction rate of radiation defects vs dose for proton in p-type silicon crystal.
Fig. 3. Introduction rate of radiation defects vs dose for proton and electron irradiation in n-type silicon crystals.
V. Arzumanyan. MeV energy electron and proton irradiation effects in …

## Slide 10: Experimental results
Fig. 5. Introduction rate of radiation defects vs. irradiation dose for n -type silicon doped with different concentrations of carbon atoms. The induced radiation defects values for each applied dose are presented in the insert.
Fig. 6. Introduction rate of radiation defects vs. irradiation dose for n-GaP samples with an initial specific resistivity of 0.15 Ω·cm, irradiated by electrons with energies of 50 MeV and 7.5 MeV. In the insert is shown the induced radiation defects values for each applied dose.
V. Arzumanyan. MeV energy electron and proton irradiation effects in …

## Slide 11: Effects of sequential proton-electron irradiation
Fig.7. Charge carriers’ concentration depending on 3.5MeV energy electron irradiation dose.
Fig.8. Charge carriers’ concentration depending on electron irradiation dose, previously irradiated by different proton irradiation doses.
V. Arzumanyan. MeV energy electron and proton irradiation effects in …

## Slide 12: Space Environment Simulating Setup
Parameters of Research Stand
Vacuum - 10-5 Torr (1.33x10-3 Pa )
3.5 MeV energy electron beam with energy
Measurement temperature range from -100 ℃ to +100℃,
Solar ultraviolet radiation.
V. Arzumanyan. MeV energy electron and proton irradiation effects in …

## Slide 13: Conclusion
The concentration of radiation induced defects, determined as a function of irradiation dose, can be interpolated by means of the empirical exponential function
The radiation defects generation efficiency is determined by the initial carrier concentration of the semiconductors, the energy and type of the irradiation particles, in addition to the presence of non-active impurities in the samples.
For sequential proton+electron irradiated samples it was observed that after proton irradiation the parameters of silicon crystal become resistant to electron irradiation in some dose ranges.
V. Arzumanyan. MeV energy electron and proton irradiation effects in …

## Slide 14: Future works
It is planned to carry out neutron irradiation of semiconductor samples by IBR-2 reactor at JINR, Dubna.
It is planned to investigate the influences of different combinations of sequential irradiations on semiconductor materials.
IBR-2
V. Arzumanyan. MeV energy electron and proton irradiation effects in …

## Slide 15: Thank You for Your Attention!