## Slide 1: Prospects of catalytically-induced decomposition of methane to produce core-shell structured contrast agent for medical imaging
Aleksei P. Kozlov1,2, Evgeniya V. Suslova1, Vladislav A. Rozhkov1,3
1 Lomonosov Moscow State University, Faculty of Chemistry, Moscow, Russia
2 Moscow Aviation Institute, Moscow, Russia
3 Joint Institute for Nuclear Research, Dubna, Russia
kozlov.aleksei.p@gmail.com
The XXVI International Scientific Conference of Young Scientists and Specialists (AYSS-2022)
24-28 October 2022,
MLIT, JINR

## Slide 2: Introduction
The XXVI International Scientific Conference of Young Scientists and Specialists (AYSS-2022)
24-28 October 2022, MLIT, JINR
2
Medical Imaging
  Applicable for everyone
  Affordable
  Non-invasive
  Essential in clinical practice
  Plays a key role in early disease detection
Contrast agents (CAs)
  Ion-chelate CAs
  Nanoparticles-based CAs
wikipedia.org

## Slide 3: Nanoparticle CAs
10.1007/s13391-014-4383-0; 10.1016/j.jechem.2020.10.049
The objective of the work: to test the reaction of catalytically-induced decomposition of Methane to produce core-shell structured contrast agent
  Have hierarchical architecture
  Have signal-generating metal-containing particles
  Have matrix to be loaded with such metal particles
  The matrix have surface functionalization to enable targeting binding to specific biomolecules
  The CA have core-shell structure to ensure integrity and safety
Catalytic Methane Decomposition (CMD)
  Conversion of Methane to Hydrogen over metal particles with a side reaction of deposition of Carbon
  Exploiting the deposition of Carbon to enclose metal-containing particles
The XXVI International Scientific Conference of Young Scientists and Specialists (AYSS-2022)
24-28 October 2022, MLIT, JINR
3

## Slide 4: Experimental. Nanoparticle CA synthesis
Chemical Vapor Deposition at 900 °C
MgO template
Flow of N2 through Hexane as the Carbon source
Boiling in HCl solution to remove the template
Step 1 – Graphene Nanoflakes (GNF) preparation
Step 2 – GNF oxidation (GNFo)
Step 3 – La-loaded GNFo (GNFo-La)
GNF treatment with boiling HNO3
Filtration of resulting GNFo
Addition of La(NO3)3 soluiton to the GNFo dispersion under sonication
Subsequent annealing under N2 flow at 400 °C, with or without of CMD
The XXVI International Scientific Conference of Young Scientists and Specialists (AYSS-2022)
24-28 October 2022, MLIT, JINR
4

## Slide 5: Results. Nanoparticle CA without CMD
The XXVI International Scientific Conference of Young Scientists and Specialists (AYSS-2022)
24-28 October 2022, MLIT, JINR
5
3D Spectral CT monochrome (a) and solution-calibrated, colored (b) images of phantom with test tubes filled with GNFo-La (red), GNFo-Nd (blue), and GNFo-Gd (green) nanoparticle CA

## Slide 6: Results. Testing the CMD reaction
Band, cm-1 | Characteristic of
120 | La-O, lattice vibrations
190 | 
330 | 
440 | 
730 | N-O vibrations
1050 | 
1120 | 
1350 | 
1450 | 
1630 | 
1580 | G band of graphite
The XXVI International Scientific Conference of Young Scientists and Specialists (AYSS-2022)
24-28 October 2022, MLIT, JINR
6
Conditions of CMD: preheating the sample up to 400 °C in N2 flow, switching to Methane for 10 minutes, cooling down
Raman survey spectra

## Slide 7: Results. Nanoparticle CA before and after CMD. Raman spectroscopy
The XXVI International Scientific Conference of Young Scientists and Specialists (AYSS-2022)
24-28 October 2022, MLIT, JINR
7
Band | D | G | 2D | D+D’ | 2D’
Position, cm -1 | 1350 | 1590 | 2700 | 2940 | 3180
D’’ | D | A | G
Gaussian | Gaussian | Gaussian | Pseudo-Voigt
Survey spectra
1000-2000 cm-1 region

## Slide 8: Results. Nanoparticle CA before and after CMD. X-Ray photoelectron spectroscopy
The XXVI International Scientific Conference of Young Scientists and Specialists (AYSS-2022)
24-28 October 2022, MLIT, JINR
8
Survey spectra
C1s region

## Slide 9: Results. Nanoparticle CA before and after CMD. Transmission electron microscopy
La2O3 after CMD
The XXVI International Scientific Conference of Young Scientists and Specialists (AYSS-2022)
24-28 October 2022, MLIT, JINR
9
GNFo-La after CMD

## Slide 10: Conclusion
The catalytically-induced reaction of decomposition of Methane over La-containing nanoparticles to produce core-shell structured contrast agent were tested;
Raman spectroscopy and X-Ray photoelectron spectroscopy data suggest that the reaction contributes to Carbon spectra. Transmission electron microscopy demonstrates thin layer over nanoparticles. All together, it indicates formation of Carbon layers over La-containing nanoparticles;
Further research is required to estimate kinetics and mechanisms of the reaction;
The method may be applicable for contrast agents for medical imaging.
This study was financially supported by the Russian Scientific Foundation (project no. 22-15-00072).
The XXVI International Scientific Conference of Young Scientists and Specialists (AYSS-2022)
24-28 October 2022, MLIT, JINR
10
Thanks for your attention!