## Slide 1: Physicochemical properties of hydrothermally synthesized nanocomposites of graphene-oxide and Zn/Ga-dopped cobalt ferrite
Marija Grujičić, Željko Mravik, Milica Pejčić, Danica Bajuk-Bogdanović, Ivana Stojković Simatović, Sonja Jovanović
The XXVI International Scientific Conference of Young Scientists and Specialists (AYSS-2022)
Notes: Hello, my name is Marija and the title of my work is…..
Nanocomposites consist of two materials, and first of them is cobalt ferrite dopped with Zn and gallium….

## Slide 2: Spinel ferrites
Metal oxides of general formula MFe2O4
Oxygen atoms are densely packed in a surface-centered cubic lattice
Depending on the cation distribution between tetrahedral (A) and octahedral (B) positions, the structure can be described by the formula:
Inverse spinel (δ = 1)
М2+ ions occupy B positions*
Fe3+ ions are distributed between the A and B positions
*M2+= Co2+, Zn2+, Ni2+, Mn2+ ,…
(M2+1-δFe3+δ)A(M2+δFe3+2-δ)BO4

## Slide 3: Graphene oxide
Two - dimensional material formed by covalent bonding of oxygen groups to a monolayer of graphene
Each layer can be considered a surface layer
Oxygen functional groups enable further binding of graphene oxide

## Slide 4: Synthesis of composites
Solvothermal synthesis of cobalt ferrite nanoparticles (CoFe2O4, CFO), cobalt ferrite doped with zinc (Co0,5Zn0,5Fe2O4, CFO_Zn) and galium (CoFe1,5Ga0,5O4, CFO_Ga) with oleic acid as the surfactant (180 °С, 8 h)
Exchange of ligands with dihydrocaffeic acid (DHCA)
Synthesis of graphene oxide by modified Hammer method
Hydrothermal synthesis of composites with 5% and 15% share of spinel ferrite nanoparticles on graphene oxide (120 °С, 3 h)

## Slide 5: Characterization methods
X-ray diffraction (XRD)
Scanning electron microscopy (SEM)
Transmission electron microscopy (ТЕМ)
Fourier-transform infrared spectroscopy (FTIR)
Raman Spectroscopy
Cyclic voltammetry (CV)

## Slide 6: Spinel ferrite nanoparticles
XRD diffractogram
ТЕМ micrographes
Average size = 5 ± 1 nm
Pure ferrite phase

## Slide 7: Spinel ferrite nanoparticles
FTIR analysis
Δ = 142 cm-1
Covalent bridging bidentate interaction
Stretching vibration of metal and oxygen atoms in the tetrahedral position 580-603 cm-1
Asymmetrically stretching vibration of the carboxyl group 1550 cm-1
Symmetrically stretching vibration of the carboxyl group 1408 cm-1

## Slide 8: Spinel ferrite nanoparticles
Raman spectroscopy
Seven Raman active modes
А1g mode - symmetrical stretching vibration (МА-О)
Еg mode - symmetrical bending vibration (МВ-О)
F2g(3) mode – asymmetrical bending vibration (МВ-О)
F2g(2) mode – symmetrical stretching vibration (МВ-О)
F2g(1) mode - translation mode of the FeO4 group

## Slide 9: Spinel ferrite nanoparticles
FTIR analysis after ligand exchange
Asymmetrically stretching vibration of the carboxyl group 1562 cm-1
Symmetrically stretching vibration of the carboxyl group 1383 cm-1
binding through the carboxyl and catechol groups
Δ = 179 cm-1
Covalent bridging bidentate interaction
Binding of DHCA to the surface of the nanoparticle 1631, 1541, 1489, 1397 cm-1

## Slide 10: Graphene oxide
ТЕМ
SEM
Layered structure
Transparent for electron beam

## Slide 11: Graphene oxide
XRD diffractogram
FTIR analysis
С=О stretching vibration 1725 cm-1
С=С и С=О stretching vibration 1621 cm-1
СО stretching vibration 1067 cm-1
Diffraction maximum at 12.3°
Oxidation increases the distance between two layers

## Slide 12: Composites
SEM
Agglomerated layers
There is no difference between compo-sites with different share of nanoparticles
ТЕМ
Large difference in distribution density
High dispersion of nanoparticles on the graphene oxide layer

## Slide 13
Composites
FTIR analysis
The same characteristic vibrations as with graphene oxide
The band at 1617 cm-1 exhibit downshifts to lower wavenumber which is correlated to the presence of hydrogen bonding

## Slide 14: Cyclic voltammetry
Composites
Divalent cations (Co2+) act as active sites for charge adsorption
Trivalent iron ions (Fe3+) participate in Faraday reaction
Surface oxygen groups are responsible for the existence of pseudocapacity
A box-like shape is most noticable in the samples CFO_Ga_GO_5% и CFO_Ga_GO_15%
E vs. SCE (V)
E vs. SCE (V)
E vs. SCE (V)
E vs. SCE (V)
E vs. SCE (V)
E vs. SCE (V)
Specific current (A/g)
Specific current (A/g)
Specific current (A/g)
Specific current (A/g)
Specific current (A/g)
Specific current (A/g)

## Slide 15: Cyclic voltammetry
Composites
The value of specific capacity is greatly influenced by the interaction between graphene oxide and spinel ferrite
The highest value of specific capacity is shown by the composite CFO_GO_15% of 36.86 F g-1 at a polarization rate of 5 mV s-1
Specific capacity (F/g)
Specific capacity (F/g)
Specific capacity (F/g)
Specific capacity (F/g)
Specific capacity (F/g)
Specific capacity (F/g)
Polarization rate (mV/s)
Polarization rate (mV/s)
Polarization rate (mV/s)
Polarization rate (mV/s)
Polarization rate (mV/s)
Polarization rate (mV/s)

## Slide 16: Conclusion
TEM analysis of composites shows different distribution densities
The formation of a hydrogen bond between spinel nanoparticles and graphene oxide was confirmed by FTIR analysis
Co2+ contributes to the capacity of the electric double layer, while Fe3+ contributes to the pseudocapacity
The composite CFO_GO_15% has the highest value of specific capacity of 36.86 F g-1 at a polarization rate of 5 mV s-1

## Slide 17: Acknowlegement
The present study was founded by the Ministry of Science, Education and Technological Development of the Republic of Serbia
The resuls are published in article:
ELECTROCHEMICAL PROPERTIES OF COMPOSITES OF GRAPHENE-OXIDE AND COBALT-FERRITE DOPED WITH ZINK AND GALLIUM
doi: 10.5937/tehnika2202155G

## Slide 18: Thank you for your attention!

## Slide 19
Hydrothermally treated graphene oxide
SEM
FTIR analysis
Agglomerated layers of graphene oxide
Partial reduction of СО group

## Slide 20: Cyclic voltammetry
Spinel ferrite nanoparticles
Divalent cations (Co2+) act as active sites for charge adsorption
Trivalent iron ions (Fe3+) participate in Faraday reactions
Specific capacities are 4.68; 5.78; and 3.75 F g-1 for CFO_DHCA, CFO_Zn_DHCA and CFO_Ga_DHCA at a polarization rate of 5 mV s-1

## Slide 21: Cyclic voltammetry
Graphene oxide
Hydrothermally treated graphene oxide
A box-like shape is observed
Surface oxygen groups are responsible for the existence of pseudocapacity
Specific capacity 9.17 F g-1 at a polarization rate of 5 mV s-1
A redox peak at 0.4 V contributes to pseudocapacity
Specific capacity 3,91 F g-1 at a polarization rate of 5 mV s-1