## Slide 1
JOINT INSTITUTE FOR NUCLEAR RESEARCH
Frank Laboratory of Neutron Physics
Investigation of superconductivity and magnetism in layered nanostructures by PNR with secondary radiation registration
Zhaketov V.D.
Khaydukov Yu.N., Petrenko A.V., Nikitenko Yu.V., Aksenov V.L.
The XXVI International Scientific Conference of Young Scientists and Specialists (AYSS-2022)
Dubna (Russia), 24-28 October 2022

## Slide 2
OUTLINE
Superconducting technologies in nanoelectronics
Polarized neutron reflectometry with registration of secondary radiation
Rare-earth elements for spintronics
Further perspective – rare earth metals dysprosium and holmium
2 / 15

## Slide 3
Advantage of superconducting technologies:
No electrical resistance
Superconducting electrons are ‘quantum fluid’
Rich physics due to proximity effects
Ability to control the magnetic properties of the system
Main analogues
quantum non-superconducting technologies:
entangled quantum states of atoms or photons, quantum dots, etc.
Decoherence of a quantum system with time
Josephson qubit
Meissner effect
Proximity effect
ferromagnetic
superconductor
Superconductivity
penetration
Leakage of
magnetism
SUPERCONDUCTING TECHNOLOGIES IN NANOELECTRONICS
3 / 15

## Slide 4
v
1. Scheme of classical spin valve
2. Superconducting spin valve
3. Controlling magnetism
FM
SC
FM
M1
M2
FM
SC
FM
M1
M2
4. Non-collinear spin valves
SUPERCONDUCTING SPIN VALVES
A. Singh et al. // Physical review X 5, 021019 (2015)
A. Golubov, M. Kupriyanov // Nature Materials, Vol. 16, Feb. 2017
Yury Khaydukov et al. // EU Patent application 21153254.4-1212
4 / 15

## Slide 5
F
S
Ferromagnet / superconductor
Inverse proximity effect
Magnetic states of S-FM systems under the influence of proximity effects
Normal metal / superconductor
Low-dimensional systems
Influence of magnetism on the superconducting properties of the system
Influence of superconductivity on the magnetic properties of the system
Inhomogeneous structures?
S-FM structure
Inhomogeneous S-FM structure
PROXIMITY EFFECTS IN THE PHYSICS OF SUPERCONDUCTIVITY
5 / 15

## Slide 6
incoming
neutron
GISANS
Off-specular scattering
POLARIZED NEUTRON REFLECTOMETRY
Polarized neutron reflectometry – experimental method for investigation of metallic low-dimensional heterostructures, polymer films, biological systems, free surface of liquids, magnetic fluids etc.
6 / 15

## Slide 7
Charged particles (n, α); (n, t); (n, p)
Gamma-quanta (n, γ)
Fission fragments (n, f)
Spin-flip neutrons
Noncoherent scattered neutrons by nuclei
Inelastically scattered neutrons
Diffusely scattered neutrons on medium inhomogeneities
i – isotope, j – type of secondary radiation
Neutron
detector
detector of secondary radiation
sample
Zhaketov V.D. et al. // Journal of Surface Investigations, vol. 15, no. 3, pp. 549-562 (2021)
Zhaketov V.D. et al. // Journal of Surface Investigations, vol. 13, no. 3, pp. 478-487 (2019)
REGISTRATION OF SECONDARY RADIATION
7 / 15

## Slide 8
magnetic
particles
RKKI
RARE-EARTH ELEMENTS (GADOLINIUM) FOR SPINTRONICS
CGS units
CGS units
Ta(20nm)
V(150nm)
Fe1-xVx(1nm)
V, Cr (1.2nm)
Nb(150nm)
Si(0.5mm)
Fe1-xVx(1nm)
Al2O3
Nb(25nm)
Gd()
x 12
Nb/FeV/V
H=20 Oe - Tb≈150 K
Nb/FeV/V
H=1000 Oe - Tb≈50 K
[Nb/Gd]x12
H=1000 Oe - Tb≈8 K
Gadolinium is a localized ferromagnet with a rather low (compared to Fe, Co, and Ni) bulk Curie temperature of Tm = 293 K. Strong localization of the magnetic moment stabilizes ferromagnetism even in ultrathin Gd layers.
Gd has ability to couple with other ferromagnets, forming nontrivial magnetic ordering patterns which can be used for the creation of superconducting spin valves.
Niobium and gadolinium components are not mutually soluble in either the solid or liquid phase.
Gadolinium has record cross-section of -reaction.
Zhaketov V.D. et al. // JETP, vol. 129, No.2, pp. 258-276 (2019)
Khaydukov Yu.N. et al. // Phys. Rev. B, 97, 144511 (2018)
8 / 15

## Slide 9
Structures Nb(25nm)/Gd(df)/Nb(25nm) were investigated
Observed reducing of Tc with increasing of magnetic moment
Superconducting coherent length in gadolinium
Dependance
Khaydukov Yu.N. et al. // Phys. Rev. B, 97, 144511 (2018)
EFFECT OF MAGNETISM ON SUPERCONDUCTIVITY IN NB/GD/NB TRILAYERS
Q(nm-1)
9 / 15

## Slide 10
Results of experimental data fitting
Reducing the magnetic moment of structures [Nb(25 nm)/Gd(x=1.2, 3, 5 nm)]х12 below
Transition of a ferromagnetic structure to superconducting state
The superconductor displaces the magnetic field
The penetration depth was >
Khaydukov Yu.N. et al. // Phys. Rev. B, 99, 140503 (2019)
DIAMAGNETISM OF PERIODIC FERROMAGNETIC-SUPERCONDUCTING STRUCTURE
Al2O3
Nb(25nm)
Gd()
x 12
10 / 15

## Slide 11
2018
Recently, a new proximity effect has been described in ferromagnetic-superconducting layered nanostructures, which is characterized by a large scale (10 nm) of the interaction of superconductivity and magnetism, and which takes place for any ferromagnets.
2022
Giant electromagnetic proximity effect in
superconductor/ferromagnet superlattices
A.V. Putilov, S.V. Mironov, A.S. Mel’nikov, A.I. Buzdin
ELECTROMAGNETIC PROXIMITY EFFECT
11 / 15

## Slide 12
Al2O3
Nb(100nm)
Gd(3,6,12nm)
V(70nm)
Nb(15nm)
Secondary radiation channel (gamma-quanta)
Determination of the nuclear profile of the Gd layer
Polarized neutrons
determination of the magnetic profile of the Gd layer
and superconducting layers;
nuclear profile for sum of elements
At present, the Al2O3//Nb(100nm)/Gd(3nm)/V(70nm)/Nb(15nm) structure, where Gd is a ferromagnet and Nb and V are superconductors, has been studied. A change in the magnetization in superconducting layers (at area 10 nm close to F-layer) under the influence of superconductivity at a level of 4-10% was found, which corresponds to the implementation of the inverse proximity effect. Further plans are in detailed processing of experimental data and new experiments.
ELECTROMAGNETIC PROXIMITY EFFECT. EXPERIMENTAL RESULTS
12 / 15

## Slide 13
Investigated structures:
1) Dy (2000 Å) 2) Ho (2000 Å) 3) [Dy (60 Å)/Ho (60 Å)]×34
Dy
Ho
FURTHER PERSPECTIVE – RARE EARTH METALS DYSPROSIUM AND HOLMIUM
Devyaterikov D.I. et al. // Journal of Surface Investigations, Vol. 16, No. 5, pp. 839-842 (2022)
Devyaterikov D.I. et al. // Physics of Metals and Metallography, Vol. 122, No. 5, pp. 465-471 (2021)
Further prospects are connected with the study of the effect of superconductivity on the helicoidal magnetic ordering in the Nb/Dy, Nb/Ho superlattice.
13 / 15

## Slide 14
Conclusion
Superconducting technologies are good candidate to replace classical semiconductor technologies. The creation of superconducting spin valves is one of the promising applications.
One of the effective methods for studying magnetism of heterostructures is polarized neutron reflectometry, which makes it possible to obtain chemical and magnetic depth profiles with nanometer resolution. Registration of secondary radiation make possible to determine distribution of separate elements.
Gadolinium is perspective element for creation of devices for spintronics. Detailed investigation of such systems demonstrate electromagnetic proximity effects at such systems.
Further prospects are connected with the study of the dysprosium and holmium as helimagnet elements with non-trivial magnetic order for creation of spintronics devices.
14 / 15

## Slide 15
Thank you for your attention!