## Slide 1
Characterization of Tobacco stalk Ash
Muthukumaran R.
Department of Chemistry
Mizoram University
Aizawl – 796 004
INDIA

## Slide 2
Calcium, carbon, and oxygen (orange), Silica (green) and aluminum and oxygen-containing
particles (yellow) [filler]
Inorganic Particles of Tobacco Filler
(phytolithic)
Halstead MM, Watson CH, Pappas RS (2015) J Anal Toxicol 39: 698-701

## Slide 3
Baliga VL, Miser DE, Sharma RK et al. (2003) Physical Characterization of the Cigarette Coal: part 1—Smolder Burn, J Analy Appl Pyroly. 68: 443-65
Inorganic Particles of Cigarette Ash

## Slide 4
Inorganic Particles of Cigarette Ash
Baliga VL, Miser DE, Sharma RK et al. (2003) J Analy Appl Pyroly. 68: 443-65

## Slide 5
Manufacturing tuibur
9” dia x 18” height
18” dia x 18” height
Tobacco stalk Ash
Tobacco stalk Ash
Feed stock solution, pH 9-10.5 (20L)
Feedstock Generation

3“ thick earth
Connector
(15 cm iron pipe of 1” dia)
Water Stream
Mixing of ‘diluted’ smoke into downstream
Production Unit
24” dia x 18” height
Pipes connected to upstream
Upper Steel Container
1’ dia x 3’ height
Lower Container
Feed stock solution, pH 9 - 10.5 (20L)
Smoldering Tobacco
Stalk
Smoke
Bamboo Joint
1” dia pipe
1” dia pipe
0.5” dia pipe
Air flow
Air flow
Water flow
Water flow
Water hole
Smoke
Aspirator Unit
Smoke Generator Unit

Filtration Unit
18” dia x 18” height
Ash + Raw Tuibur
Filtered Tuibur, pH 9-10.5 (20L)

Notes: The mean nicotine content of TSIW samples was 12.23 mg g-1 and ranged from 10.04 mg g-1 (Lunglei site 1) to 18.25 mg g-1 (Aizawl site 1).

## Slide 6
Tobacco stalk: Tobacco stem, petiole, midrib
Smoldering Tobacco stalk under aerobic conditions
Combustion of tobacco stalk

## Slide 7
What is the nature and composition of inorganic particulate constituents on the surface & interior of the tobacco stalk (tuibur)?
What is the potential microstructural features of inorganic particulate matter present in tobacco ash generated from tobacco stalk?
Key Questions

## Slide 8
Inorganic Particulate Matter – Tobacco Stalk

## Slide 9
XR-PD of Tobacco stalk Ash

## Slide 10
Ca 2P
C 1S
O 1S
X-ray Photoelectron spectroscopy (XPS) of Tobacco stalk Ash

## Slide 11
Cl 2P
K 2P
XPS of Tobacco Ash

## Slide 12
Mg 1S
Si 2P
XPS of Tobacco Ash

## Slide 13
S 2P
Al 2P
XPS of Tobacco Ash

## Slide 14
Fe 2P
P 2P
Hg 4f
XPS of Tobacco Ash

## Slide 15
1 µm
2 µm
SEM of Tobacco Ash

## Slide 16
300 nm
SEM of Tobacco Ash

## Slide 17
200 nm
SEM of Tobacco Ash

## Slide 18
EDAX of Tobacco Ash

## Slide 19
EDAX of Tobacco Ash

## Slide 20
Raman Spec. Tobacco Ash ( 473 nm and 785 nm)

## Slide 21
Raman Spec. Tobacco Ash ( 473 nm and 785 nm)

## Slide 22
Frequencies , cm1 |  |  |  | Assignments
Mineral |  |  | Other compounds | 
Aragonite | Calcite | Calcite |  | 
135, 146 | 158 | 158 |  | T (Ca, Mg, CO3) Ti-O vibration mode
197 |  |  |  | T (Ca, Mg, CO3)
277 | 282 | 282 |  | T (Ca, Mg, CO3)
 |  |  | 385 | Ca-O stretch lattice mode(2(E)) of Si-O in anatase
 |  |  | 458 | 2(PO4)3 stretching mode
 |  |  | 510 | Al-O-Si bending mode
 |  |  | 630 | Si-O-Si stretching vibration Eg mode of anatase
702 | 716 |  |  | in-plane bending (4) modes of the carbonate ion
854 |  |  |  | 2((CO3)2) out-of-plane bending in aragonite
 |  |  | 992 | 1((SO4)2) symmetric stretch
1082 | 1088 |  |  | symmetric stretching mode 1((CO3)2)
Raman Freq. Tobacco Ash ( 473 nm)

## Slide 23
C 1S
Raman Spec. Tobacco Ash ( 473 nm and 785 nm)

## Slide 24
Tobacco Stalk Ash |  | 
element | Conc. (g/g) | S.D
Al | 6999.59 | 65.004
Ba | 322.33 | 2.42
Cd | 0.426 | 0.005
Co | 2.469 | 0.016
Cr | 10.141 | 0.050
Cu | 45.78 | 0.133
Fe | 3441.17 | 15.92
Mn | 306.42 | 1.91
Ni | 16.781 | 0.842
Pb | 2.332 | 0.125
S | 20304.72 | 512.24
Sr | 1135.95 | 12.496
V | 9.123 | 0.11
Zn | 195.59 | 1.357
ICP-AES Analysis of Tobacco Ash

## Slide 25
a) Identification and classification of some of the ‘insoluble’ inorganic particulate phase on the surface of tobacco stalk and tobacco ash (biogenic or environmental)
b) Evaluation of the size distribution and micro-structural features of inorganic particulate matter
Phase identification (aragonite and Calcite) of insoluble inorganic particulate matter
XPS analysis of Ca, Fe, C, S, P, Al, Si and Hg species at different electronic environments on tobacco ash surface
Conclusion

## Slide 26
Dept Bio-Techonology, New Delhi, INDIA
UGC-DAE Kolkata Centre, Kolkata, INDIA
JINR, FLNP, Dubna, RUSSIA
Mizoram University, INDIA
NEIST, Jorhat, INDIA ; Tezpur University, INDIA
Dr. Inga Zinicovscaia, FLNP, JINR, Dubna
Prof. G. Arzumanyan, Raman Spec., JINR, Dubna
Prof. Vicoria Vartic, Raman Spec., JINR, DUBNA
Acknowledgement

## Slide 27
Thank You!