## Slide 1: Прогресс 2020 – 2023 гг. в разработке аэрогелевых черенковских счетчиков в Новосибирске
А. Ю. Барняков и др.
План:
Счетчики АШИФ
  Эксперимент КЕДР и СНД
  Долговременная стабильность счетчиков АШИФ
  АШИФ с КФЭУ, модернизация счетчика АШИФ для эксперимента СНД
Детекторы черенковских колец с фокусировкой
  Счетчики с линзой Френеля (mRICH for EIC project)
  ФАРИЧ для Супер С-Тау фабрики
Позиционно-чувствительные фотодетекторы
  Матрицы КФЭУ
  ФЭУ с МКП

## Slide 2: Progress 2020 – 2023 in aerogel Cherenkov counters development in Novosibirsk
A. Yu. Barnyakov & other.
Contents:
ASHIPH counters
  The KEDR and the SND experiments
  Long-term stability of the ASHIPH counters
  ASHIP with SiPM, upgrade of the ASHIPH system for the SND experiment
RICH detectors with focusing of the light
  RICH with Fresnel lens (mRICH for EIC project)
  FARICH for the Super Charm-Tau Factory
Position-sensitive photon detectors
  SiPM arrays
  MCP-PMTs

## Slide 3: ASHIPH technique is 30 years old!!!

## Slide 4: ASHIPH detectors
Aerogel SHIfter and PHotomultiplier
Suggested at BINP. A.Onuchin et.al. NIM A315(1992)517
PMMA light guide doped with BBQ dye
is used as wavelength shifter

## Slide 5: KEDR experiment at VEPP-4M
Physics program
Precise particle mass measurements: J/ψ, ψ(2S), ψ(3770), τ lepton, D mesons, Υ mesons
Measurements of ψ and Υ mesons lepton width
R measurement in 2-10 GeV c.m. energy range
γγ→hadrons and other 2γ processes
Branching fractions measurements in charm and bottom quark systems (above 10-4)
VEPP-4M
Symmetric e+e-- collider
Ec.m. = 2–10 GeV
L = (1÷80) x 1030 cm-2s-1
Precise energy calibration:
  RD: (5÷15)x10-6
  CBS: 3x10-5

## Slide 6: KEDR ASHIPH system
160 counters in 2 layers
Solid angle 96% of 4π
n=1.05, VΣ=1000 l, high transparency SAN-96 aerogel
π/K- separation in the momentum range 0.6÷1.5 GeV/с
160 MCP PMTs, photocathode diameter ø18mm, able to work in the magnetic field up to 2 T
Fully installed in the detector in 2013. Now is in operation.

## Slide 7: KEDR ASHIPH system (2)
Npe = 6.4±0.2 – layer 1
Npe = 5.0±0.2 – layer 2
Npe = 10.9±0.2 – sum of the signals in 2 layers (80%)
π/K-separation at 1.2GeV/c is 4.3σ
A.Yu.Barnyakov et al., NIM A824 (2016) 79

## Slide 8: SND at VEPP-2000
Symmetric e+e− collider with round beams
2Emax=2000 МeV
L=1031сm-2s-1 at E=510 МeV
L=1032сm-2s-1 at E=1000 МeV
VEPP-2000 beam pipe
Tracking system
Aerogel Cherenkov counters
NaI(Tl) crystals
Vacuum phototriodes
Fe absorber
Muon system
VEPP-2000 s.c. focusing solenoids
EMC

## Slide 9: ASHIPH counters for SND
π/K separation from 300 to 870 MeV/c
Cylindrical shape: R=105÷141 mm
Case material: 1mm of Al
3 segments of 3 counters in each
Solid angle: ~60% of 4π
Thickness: 0.09 Xo
Outline
1 - PMT, 2 – aerogel, 3 - WLS
2
1
3
Refraction index: n=1.13±0.01
Density: ρ=0.65 g/cm3
Lsc=19 mm at =400 nm
Labs=100 cm at =400 nm
Aerogel parameters
Scheme: ASHIPH
WLS position: displaced by ~5° from counter center
Aerogel thickness: ~30 mm
Counter Design

## Slide 10: SND ASHIPH: π/К separation
● π ○ K
Amplitude
Efficiency
For momenta above 350 MeV/с separation level is sufficient
Below 350 MeV/c separation will be supplemented by other subsystems (DC)
● π ○ K
P, MeV/c | εK , % | Επ , % | Sep, σ
300 | ~10 | 68 | 1,7
350 | ~7 | 90 | 2,8
400 | ~5 | 96 | 3,4
600-800 | ~9 | >99 | 3,7
A Yu Barnyakov et al 2014 JINST 9 C09023

## Slide 11: Long-term stability of ASHIPH counters
ASHIPH prototype for the KEDR.
After tests with mixed hadron beams at JINR (Dubna) in 2000 is under operation from time to time.
A Yu Barnyakov et al 2014 JINST 9 C09005
One of the first ASHIPH counters for the KEDR detector was under operationin the experiment from 2000 to 2003.

## Slide 12: Amplitude decrease reasons for the ASHIPH system which is in operation at the KEDR detector since 2014
ASHIPH counters with 2MCP-PMTs from 1999÷2000
ASHIPH counters with 3MCP-PMTs from 2006÷2007
– 1999
– 3MCP 2006
– 2MCP 2008
Evaluated with help of cosmic tracks hitted the WLS

## Slide 14: ASHIPH option for Super C-Tau factory
1400 counters 18x30x8 cm3
System consists of 3 layers:
n=1.03 (8 cm) – 2000 liters
n=1.015 (8+8 cm) – 4000 liters
28k SiPM 3x3 mm2
WLS based on PMMA doped by BBQ
0.3x6x28 cm3
π/К – separation up to 3.5 GeV/c
µ/π – separation from 0.5 to 0.9 GeV/c

## Slide 15: Upgrade of ASHIPH system for the SND
Change of MCP-PMT to SiPM lead to increase of amplitude by two or more times:
– ASHIPH system with n=1.05: 4.5 pe → 8÷10 pe
– ASHIPH system with n=1.13: 9.5 pe → 18÷20 pe
π/K-separation become more reliable
n=1.13
Parametric simulation results
Aerogel radiator made from 38 sintered blocks 50х50х25 mm3
Aerogel radiator made from single block 200х200х40 mm3
Scheme with consequently-parallel
connection of SiPM

## Slide 16: RICH with Fresnel lens

## Slide 17: EIC project
Key EIC Characteristics (parameters)
– High particle collision rate
– Large center-of-mass energy range
– electrons
– protons
– Polarized beams of electrons and ions
– Large range of ion species
– At least one large-acceptance detector
– Projected budget: – Start date:
Almost approved concept since begin of 2022

## Slide 18: ECCE-PID & mRICH system concepts
Physics requirements
  pion, kaon and proton ID
  over a wide range |η| ≤ 3.5
  with better than 3σ separation
  significant pion/electron suppression
Momentum-rapidity coverage
  forward: up to 50 GeV/c
  central: up to 6 GeV/c
  backward: up to 10 GeV/c
Demands different technologies
Cherenkov detectors:
  dRICH = dual RICH (aerogel + gas)
  hpDIRC = high-performance DIRC (synthetic fused silica)
  mRICH = modular RICH (aerogel + Fresnel lens)
ECCE = EIC Comprehensive Chromodynamics Experiment
68 modular counters oriented to IP:
– aerogel n=1.03 100x100x40 mm3
– acrylic Fresnel lens with focal distance 6”
– position sensitive photon detector HRRPD (MCP-PMT) or SiPM arrays

## Slide 19: Aerogel RICH with Fresnel lens
Such approach allows us to improve Cherenkov angle resolution and optimize photo detectors area!

## Slide 20: The thick aerogel for mRICH
There are two way to increase the aerogel thickness:
Arrange the stack of several aerogel samples with moderate thickness like as 20 mm
Produce the larger (thicker) aerogel samples as for LHCb (n=1.03; 200x200x50 mm3)
In both cases there is no reason to make the aerogel thickness more than
In case of approach “stack” the additional Cherenkov photons loss is occured due to reflectance and scattering on the additional surfaces
There are two not cuttied surfaces in aerogel
  “Optical surface@ – which contacts only with air during the production
  “Bottom” it contacts with metallic frame during the production processes
Several configuration of the aerogel Cherenkov radiators were tested with relativistic elecron beams at BINP beam test facilities in 2022.
According to Marco Contalbrigo, so far the only manufacturer that achieved thickness larger than 2cm is in Russian.

## Slide 21: Beam tests schem of aerogel RICH in 2022 at BINP
Three short runs (2 shifts: 12+12 hours) with electrons E=2.5 GeV was done in May, November and December 2022.
Four MaPMTs H12700 (Hamamatsu) with pixel 6x6 mm were placed in such way to register 85% (for May run) and 60% (for Nov and Dec run) of Cherenkov photons per track.
Three GEMs with spatial resolution 𝜎𝑋,𝑌≤100 µm were used at beamline.
  Two before aerogel sample and one behind
Two approaches to create a thick aerogel Cherenkov radiators (single thick tile or stack of two tiles) were compared with help of beam tests and G4 simulation
GEM2
GEM3
GEM1

## Slide 22
BINP beam test facility
4 MaPMT H12700

## Slide 23: Scheme&Results of beam test (May 2022)

## Slide 24: Влияние эффектов поверхности в стопке (457f3+457f4)
“Opt.s”+“Bot.s” PD
“Opt.s”+“Opt.s” PD

## Slide 25: Влияние эффектов поверхности в стопке (457f3+457f4)(2)
“Bott.s”+“Opt.s” PD
“Bot.s”+“Bot.s” PD
Due to scattering effects on the bottom aerogel surfaces the Npe loss is about 3–4% for single layer samples and about 6% for stack of two samples. While the resoultion degradation becomes sensable (13%) only in case of stack of two aerogel samples.

## Slide 26: TBeam simulation with G4: input data.
To perform quntitively comparison TBeam results with G4 simulation it is necessary to implement in simulation very correct data on aerogel parameters (n, Lsc, thick) and also about photon detector parameters such like Geometry and PDE.
As a QE() we will use data for MaPMT H12700 from manufacturier (Hamamatsu) data-sheet (DS) normalized on our own direct measurement QE(=409nm) performed with laser light sourse(see the pictures below: left).
Also it is necessary to take into account that flat-pannel MaPMTs have non 100% photoelectron collection efficiency (CE). According to invetigations (Ref. arXiv:1506.04302v2 [physics.ins-det] 5 Oct 2015) about 20% of photoelectrons are able to give by 5 times smaller amplitude than a single photoelectron peak due to skip of the first dynode stage (see the pictures below: right). It means that if the read out electronics discriminator threshold is set ~0.1-0.2pe we will lose about 20% of photoelectrons.
In the G4 simulation is implemented recalculated photon detection efficiency (PDE):

## Slide 27: Tbeam and G4sim comparison (single – thin 457-3)
457_3
n=1.027
A0=0.78
Lsc = 50 mm
19.0 mm
Experiment
Simulation
(2)

## Slide 28
The new aerogel samples were produced in 2022 to be tested in mRICH prototype with mixed hadron beams in 2023-2024.
    Refractive index of all tiles n = 1.028±0.001;
    Lsc(400nm) for all blocks ≥43mm;
    7 aerogel tiles 30 mm 100x100 mm
    4 aerogel tiles 40 mm 100x100 mm
    1 aerogel tile 50 mm 80x80 mm;
The general idea of the experiment was to investigate the quality of new aerogels and estimate the impact from aerogel itself to overal mRICH prototype resolution.
PD and beamline configurations were the same as in Novembe 2022. It allow us to perform direct comparison of results from these two beam test campaigns (Nov and Dec 2022).
Scheme&Results of beam test (Dec 2022)
50
80
80
230
230
40
op460f11
n=1.027
115
115

## Slide 29: Aerogel with 30 mm thickness (460f4)
460f4_4
T(5 hours)=470˚C
n=1.027
Lsc(400nm)=47.0±0.7 mm
460f4_3
T(5 hours)=600˚C
n=1.029
Lsc(400nm)=41.8±0.7 mm

## Slide 30: Aerogel with 40 mm thickness (460f11)
460f11_21
T(5 hours)=470˚C
n=1.028
Lsc(400nm)=48.2±0.7 mm
460f11_22
T(5 hours)=600˚C
n=1.029
Lsc(400nm)=42.7±0.7 mm

## Slide 31: Aerogel with 50 mm thickness (460f15)
460f15_1
T(5 hours)=470˚C
n=1.027
Lsc(400nm)=43.7±0.6 mm
460f15_3
T(5 hours)=600˚C
n=1.029
Lsc(400nm)=41.7±0.6 mm

## Slide 32: Dependence of Npe and on aerogel thickness
Npe dependes on the aerogel thickness as expected and limitted by the Releigh light scattering law.
Some ssytematical increase of Npe (~13÷15%) are observed in new thick aerogels after increase of backing temperature (470˚C –> 600˚C). This effect could not be quantatively explained by increase of refractive indexes (1.027 –> 1.029) and it is contra to Npe decrease (~5÷6%) expected due to Releigh light scattering decrease
(as expected), while for several aerogel samples some deviations from the dependence are observed. The reason of this effect could be in some impurites inside the aerogel which are able to give additional small angle forward scattering.

## Slide 33: Cherenkov angle single photon resolution (SPR)
19.0+17.6 mm
457f3+457f4
17.6 mm
457f4
40. mm
460f11_22
19.0 mm
457f3
50. mm
460f15_3
30.0 mm
460f4_3
Photon detector
Cherenkov light
t
L=175 mm
,
,
 | 457f4 | 457f3 | 460f4_3 | 457f3_f4 | 460f11_22 | 460f15_3
t/L, mm | 17.6/185 | 19.0/175 | 30.0/185 | 36.6/185 | 40.0/185 | 50.0/185
, mrad | 14.46±0.06 | 15.92±0.06 | 16.96±0.05 | 20.8±0.1 | 24.0±0.1 | 26.7±0.1
Npe* – 60% of the ring | 4.01±0.01 | 4.16±0.01 | 7.69±0.02 | 5.51±0.02 | 8.22±0.03 | 8.05±0.02
,mrad | 7.2 | 7.8 | 6.1 | 8.9 | 8.4 | 9.4
, mm | 1.11±0.03 | 1.08±0.04 | 1.20±0.02 | 1.33±0.06 | 1.35±0.04 | 1.37±0.07
 | 5.9 | 6.15 | 6.65 | 7.5 | 7.7 | 8.1
 | 457f4 | 457f3 | 460f4_3 | 457f3_f4 | 460f11_22 | 460f15_3
t/L, mm | 17.6/185 | 19.0/175 | 30.0/185 | 36.6/185 | 40.0/185 | 50.0/185
 | 14.46±0.06 | 15.92±0.06 | 16.96±0.05 | 20.8±0.1 | 24.0±0.1 | 26.7±0.1
Npe* – 60% of the ring | 4.01±0.01 | 4.16±0.01 | 7.69±0.02 | 5.51±0.02 | 8.22±0.03 | 8.05±0.02
 | 7.2 | 7.8 | 6.1 | 8.9 | 8.4 | 9.4
 | 1.11±0.03 | 1.08±0.04 | 1.20±0.02 | 1.33±0.06 | 1.35±0.04 | 1.37±0.07
 | 5.9 | 6.15 | 6.65 | 7.5 | 7.7 | 8.1
How much effect from Fresnel lens is expected?!

## Slide 34: FARICH – Focusing Aerogel RICH

## Slide 35: FARICH option for SCTF
T.Iijima et al., NIM A548 (2005) 383 A.Yu.Barnyakov et al., NIM A553 (2005) 70
n=1.030 6.0mm
n=1.027 6.3mm
n=1.024 6.7mm
n=1.022 7.0mm
The first 4-layer monolithic sample
Increase Npe due thickness increase without σΘc degradation
The Belle II (ARICH) is the first application of the method
Proximity focusing RICH
4-layer focusing aerogel
  nmax = 1.05 (1.07?), total thickness 35 mm
21 m2 – total area of photon detectors
  • SiPMs – barrel part (16 m2)
  • MCP-PMT – endcap parts (4 m2)
~106 pixels 3х3 mm2 with pitch 4 mm
A.Yu. Barnyakov, et al., NIM A 732 (2013) 352
The capability of µ/π-separation at the level of ≥3σ for P=1 GeV/c was shown at CERN beam test in 2012
Notes: Идея ФАРИЧ появилась в 2004 г.
Точность измерения черенковского угла связана с точностью измерения скорости, а значит с качеством разделения частиц.

## Slide 36
GEM
MaPMT H12700 (Hamamatsu)
with mask 3х3 mm2
2 aerogel pcs
230x230x35 mm
The largest 4-layers focusing aerogel samples

## Slide 37
Beam test results
Pixel 6x6 mm
Geom.Eff. ~ 80%
Pixel 3x3 mm
Geom.Eff. ~ 20%

## Slide 38: Cherenkov angle Single PhotoElectron (SPE) resolution
PTEP 2016, 033H01
Belle II
Аэрогель: 20+20 mm (Tchiba Univ.)
n(400nm): 1.045 +1.055
Pixel: 5x5 mm
4-layers (Novosibirsk) –>
1.039 ÷ 1.046
6x6 mm
Simulation
Measured
–
–
3x3 mm
4-layers (ideal profile)
1.041 ÷ 1.050
3x3 mm

## Slide 39: Position-sensitive photon detectors

## Slide 40: FEE based on FPGA-TDC
DC-DC convertor board
goes behind the backplane
51×84 mm2 size
provides power to SiPMs, amplifiers, FPGA
uses air inductive coils to operate in the detector magnetic field
power, trigger & clock connectors
Amplifier board
27×27 mm2 size
14-layer PCB
30x gain, 64 channels
couples to KETEK 8×8 SiPM array
TDC board
64 channels
2 TDC + 4 threshold FPGAs
10ps precision
Simulated single photon pulse shapes from amplifier for different input resistance. ~ 22mV amplitude can be achieved.
• Each module readouts 6 arrays 8x8 pixels and equipped with optical transceiver.
• Thickness of 5-layer design is less than 5 cm.

## Slide 41: The first tests of FaRICH-Auslese-System
ToT
Time, ns
The tests performed bu Mechael Traxler, Matthias Hoek and Merlin Böhm at HIM-Institute in Mainz.
Everything works as expected: ToT(Time) is as expected for single photon distribution.
Single photon detection time resolution without any corrections and proper TDC calibration is about 380ps (it is good enough value for FARICH), while intrinsic resolution of TDC is about 8÷12 ps.
A lot of dark counts are in the data (every 3rd hit is noise). Thermostabilization or cooling is needed for future tests.
FPGA-TDC (FaRICH-Auslese-System) to readout 2304 SiPMs developed and produced in GSI.
Time, ns

## Slide 42: Позиционно-чувствительные ФЭУ с МКП
HRPPD (Income)
10x10 см; пиксел 2.5x2.5 мм
Цена: ~20k$
Hamamtsu R10754-016-M16(N)
4х4 пикселя; 5х5 мм
Цена: 900 тыс. Йен
59 мм
Planacon XP85112
8х8 пикселей; 6х6 мм
Цена: 15k$
NNVT (Китай)
Цена: 18кЕвро
Коллектор ФЭУ с МКП
Концепция Экран ФЭП
(лето 2022г.)
Доступность: ???
Цена: ???

## Slide 43: Round vs Square MCP-PMT for the RICH
516 PMTs 58х58 mm (PC 50x50 мм) –>
16х16=256 pixels 2.9х2.9 mm
594 PMTs Ø58 mm (PC Ø50 mm) –>
216 pixels 2.9х2.9 мм

## Slide 44: Round vs Square MCP-PMT for the RICH (2)
Square shape MCP-PMT
(for )
Round shape MCP-PMT
(for )
To evaluate expected performance we can use recent FARICH beam test data:
– photoelectron collection efficiency ()
– Geometrical Efficiency of Test Beam setup (is determined by fill factor of photon detectors for the experimental setup)
µ/π @ 1 GeV/c:
π/K @ 6 GeV/c:

## Slide 45: Addendum

## Slide 46: HRPPD Hihg Rate Picosecond Photon Detector

## Slide 47: Aerogel degradation due to water adsorption(1)
Aerogel internal surface is 106 times greater than external. Adsorption of water is very fast process (1-10 hours).
Degradation of the light absorption length is very slow process (1-2 months) after water absorption.
The time and the level of the degradation are depend on the impurities in aerogel from raw materials and production procedure (Fe, Mn, Cr, etc.).
Concentration of metals in aerogel, ppb |  |  |  | 
Fe | Cu | Mn | Cr | Ni
500 | 56 | 7 | 26 | 

## Slide 48: Aerogel degradation due to water adsorption(2)
The refractive index (n-1) and light scattering length depends on amount of adsorbed water and are changed less than 10% after water adsorption of 2-4% of aerogel mass.
The light absorption length (Labs) in different aerogel samples after baking is the same, but after water impregnation could be very different
It is possible to make aerogel selection after water impregnation
One atom Fe is able to attract 6 molecules of water
To achieve maximum degradation of Labs it is enough to adsorb 1ppm of water.
(NIM A598 (2009) 166-168)