## Slide 1
Структурные исследования литий-ионных аккумуляторов на их функциональные характеристики
M.Yerdauletov[1,2,3], P.Napolsky[4,1], M.Avdeev[1,4], V.Krivchenko[4], K.Nazarov[1,2], B.Muhametuly[1/2]
[1] Frank Laboratory of Neutron Physics, Joint Institute for Nuclear Research, Dubna, Moscow Region, 141980 Russia
[2] Institute of Nuclear Physics, Ministry of Energy of the Republic of Kazakhstan, Almaty, 050032 Kazakhstan
[3] L.N.Gumilev Eurasian National University, Astana, 010000 Kazakhstan
[4] Dubna State University ‘Dubna’, Moscow Region, 141980 Russia

## Slide 2
John B. Goodenough
M. Stanley
Whittingham
Akira Yoshino
Nobel Prize in Chemistry 2019
Development of lithium-ion batteries
Notes: The beginning of widespread use in the mid-1990s of lithium power sources led to fundamental changes in the modern way of life. The importance of this type of energy storage devices was recently recognized by the Nobel Committee, which awarded the 2019 Chemistry Prize to M.S. Whittingham, J. Goodenough, and A. Yoshino "for the development of lithium-ion batteries." The use of layered cathodes and lithium salts in liquid electrolytes was a revolutionary step in the development of compact energy storage devices. The basis of corresponding lithium-ion batteries is the ability of electrode materials to intercalate and deintercalate lithium ions during the cyclic processes of charging/discharging the battery. Today such kind of energy storage devices demonstrate a competitive combination of energy capacity, price and satisfaction to ecological requirements, which is well illustrated by the fact of a continuous increase in sales of electric automobiles worldwide.

## Slide 3
Energy storage systems
LIB – Li ion batteries
LIC – Li ion capacitors
EDLC – Electric double layer capacitors

## Slide 4
Effect of battery form
Research effects of additives to electrodes by small-angle neutron scattering
Investigate Lithium and electrolyte deposition in batteries by neutron tomography
Possibility for using activated carbon from biowastes in electrodes
Aim: Structural studies of lithium-ion batteries and research by neutron methods
Tasks :

## Slide 5
Nanostructured Conductive Additives
X.-M. Liu et al., Composites Science and Technology 72 (2012) 121
Gaining cycling stability of Si- and Ge-based negative Li-ion high areal capacity electrodes by using carbon nanowall scaffolds
Mironovich, K.V., Evlashin, S.A., Bocharova S.A.; Yerdauletov M.S.; Dagesyan S.A.;Egorov A.V.;Itkis, D.M., Krivchenko, V.A. J. Mater. Chem. A 5 (2017) 18095
Carbon nanotube (CNT)-based composites as electrode material for rechargeable Li-ion batteries

## Slide 6
Carbon Nanotubes vs. Carbon Black
Technical specifications | Unit of measurement | Meaning
SWCNT content* | wt.% | 99 ± 0.5
SWCNT length | μm | > 5
Specific surface area | m2/g | 800—1600
SEM
LFP cathode

## Slide 7
P. Napolsky, M. Avdeev, M. Yerdauletov, et al., Energy Technology 8 (2020) 2000146
Small-angle neutron scattering from cathodes
YuMO (SANS)
IBR-2 reactor, FLNP JINR
YuMO

## Slide 8
P. Napolsky, M. Avdeev, M. Yerdauletov, et al., Energy Technology 8 (2020) 2000146
Small-angle neutron scattering from cathodes
YuMO (SANS)
IBR-2 reactor, FLNP JINR
YuMO
No incorporation of C45 into LFP matrix pores slight increase in wettability.
Incorporation of CNTs into LFP matrix pores; significant improvement in wettability.

## Slide 9: Neutron Tomography
As convertor used 6LiF/ZnS scintillators with thicknesses of 100 μm, Hamamats CCD -chip based camera, and L/D was typically set at 350. Pixel resolution was 45 μm.
The neutron tomography method was used to visualize the lithium and electrolyte distribution regions flowing inside the cell in the initial and final states of lithium-ion batteries.
Capacity 0 %
Capacity 50 %
Capacity 100 %
TITAN beamline
WWR-K reactor INP, Almaty
K.M. Nazarov, et al., Eurasian Journal of Physics and Functional Materials, 2021, 5(1), 6-14

## Slide 10: Hybrid Li ion capacitors

## Slide 11
anode material for Li-ion battery
Theoretical capacity = 4200 mAh/g
10 times bigger than graphite
Synthesis and production of anode material from biowaste
Shell nut
Chemical activation Carbonization (300-500°C)

## Slide 12
Electrochemical measurements from biowaste
capacity = 4000 mAh/g
SiO2
Si
Activated carbon

## Slide 13
Figure 1. Scanning electron microscope microphotographs of RH-derived activated carbon, captured at varying magnifications (more detailed image is in Supplementary materials).
Figure 2. C-rate performance of activated carbon-based electrodes in different electrolytes (a). Gravimetric capacitance of the electrodes in different electrolytes at different current densities (b). Cycling stability of the coin cell with lithium anode and electrolyte E2 (c). Areal capacitance has been calculated taking into account the area of the electrode. Gravimetric capacitance has been calculated taking into account mass of activated carbon in single electrode.
Characterization of Activated Carbon from Rice Husk for Enhanced Energy Storage Devices
Meir S. Yerdauletov, Kuanysh Nazarov//Molecules 2023, 28(15), 5818;

## Slide 14
Raw material | Negative electrode in electrochemical cell | Electrolyte | Specific capacitance, F/g | Cycles, N | Capacitance (Energy density) decay after cycling, % | Source
Rice husk | Li | 1M LiDFOB in FEC:DME (3:7 vol.)+LiNO3 3%wt. | 140 | 10000 | 25 | This work
Coconut shell | Li4Ti5O12 | 1M LiPF6 in EC:DMC (1:1) | 159 | 2000 | near 15 | DOI: 10.1038/srep03002
Teakwood sawdust | Li4Ti5O12 or LiC6 | 1M LiPF6 in EC:DMC (1:1) | 131 | 2000 | near 15-30 | https://doi.org/10.1016/j.electacta.2017.01.060
Human hair | Li4Ti5O12 | 1M LiPF6 in EC:DMC (1:1) | 115 | 1000 | 15-20 | http://dx.doi.org/10.1016/j.electacta.2015.09.127
Polymer derived high surface area porous carbon | Li4Ti5O12 | 1M LiPF6 in EC:DMC (1:1) | 123 | 2000 | near 20 | http://dx.doi.org/10.1016/j.electacta.2014.03.079
Orange Peel | Li4Ti5O12 or LiC6 | 1M LiPF6 in EC:DMC (1:1) | 112.5 | 2500 | 15-40 | DOI: 10.1002/slct.201700574
Rice Husk | Li4Ti5O12 | 1M LiPF6 in EC:DMC (1:1) | 120 | 2000 | 10 | http://dx.doi.org/doi:10.1016/j.electacta.2016.06.055
Comparison of specific capacitance and electrochemical test conditions for different activated carbons.

## Slide 15
Conclusions
Carbon structures used in the experiments provide differerent kinetic transport of Li-ions into crystals of active materials;
SANS me asure me nts explained why CNT ne twork e mbe dde d in e le ctrode layer provide s its greater wettability by an e le ctrolyte compare d to carbon black use d as conductive additive ;
The neutron tomography method was used to visualize the lithium and electrolyte distribution regions flowing inside the cell in the initial and final states of battery charge;
Cathode and anode electrodes obtained from biowaste have much prospect for Li capacitor. It is a good subject for further neutron research.
Acknowledgment: JINR-Kazakhstan Cooperation Program

## Slide 16
Thank you for your attention