Species similarity of corneal collagen in grafts of animal origin

M. Naumenkoa,b, S. Anisimovc,d, I.Popov c, N.Anisimova c,d, M.Orlova c, O. Lisa, Yu. Gorshkovaa,b,*

a Joint Institute for Nuclear Research, Russia, 141980, Dubna, Moscow region, 6 Joliot-Curie str.

e-mail: Yulia.Gorshkova@jinr.ru

b Institute of Physics, Kazan Federal University, 16A, Kremlevskaya St., Kazan, 420008, Russian Federation.

c Private Eye Center Vostok-Prozrenie, 10/1, Polini Osipenko Str., Moscow, 123007, Russian Federation

d Federal State Budgetary Educational Institution of Higher Education "A.I. Yevdokimov Moscow State University of Medicine and Dentistry" of the Ministry of Healthcare of the Russian Federation, 20/1, Delegatskaya Str., Moscow, 127473, Russian Federation

Received November 12, 2023

Abstract – The species similarity of corneal collagen in animal grafts was studied using small-angle X-ray scattering and Raman spectroscopy. Detailed analysis of the Raman spectra in the range of 1500-1700 cm-1 for human, porcine, and horse grafts demonstrated that bands associated with proteins and amino acids do not exhibit obvious differences in the structure of corneal grafts. Parameters of the internal structure of collagen obtained from scattering spectra also indicate the species similarity of corneal collagen in grafts. Satisfactory results of layer-by-layer intralamellar implantation of porcine and horse grafts "Corneoplast" are presented.

INTRODUCTION

Corneal surgery (keratoplasty) is considered almost the only way to restore vision in almost one-third of patients with reversible blindness. Worldwide, this is almost 42 million patients. However, donor material for keratoplasty is medically and economically unaffordable for a large part of the population. To solve this problem, the most promising direction is considered to be the creation of xenografts based on corneas of farm animals, especially materials based on porcine corneas [1].  When creating animal-based implants, the problems of immunogenicity, biocompatibility and long-term preservation of optical transparency after implantation arise. There is an unsolved problem - to achieve sufficiently deep decellularization of the transplant material while maintaining transparency. Due to the reagents used for its realization it is possible to reduce the immunogenicity of the implant. At the same time, structural and functional damage caused by tissue swelling, toxicity of reagent residues, residues of noncollagen soluble proteins and other components of the extracellular matrix remain an obstacle for wide introduction of xenografts in ophthalmology. One option for reducing the ability of collagen to hydrate is collagen crosslinking. An early study of corneal grafts ("Corneoplast") showed that dehydrothermal crosslinking (DTC) can be used to increase the resistance of grafts to hydration without critical loss of optical and strength properties [2]. It was previously shown that DTC affects the structure of corneal collagen [2]. Species differences in the effect of DTC on corneal collagen of animal species promising for xenotransplantation remain unstudied.

The aim of this work was to investigate the species similarity of corneal collagen subjected to DTC in animal grafts, namely human, horse and pig, based on data obtained by small-angle X-ray scattering (SAXS) and Raman spectroscopy (RS).

MATERIALS AND METHODS

The material for keratoplasty Corneoplast used in the present work is a devitalized cornea fixed by dehydrothermal crosslinking (based on the patent of the Russian Federation No. 2748951 dated 02.06.21). The grafts were disks cut from pig and horse corneas with a diameter of 12 mm, treated by DTC method at 120 ℃.

Small-angle X-ray scattering

SAXS experiments were performed on the SAXS/WAXS station Xeuss 3.0 (Xenocs, France) at FLNP JINR. The measurements were carried out in point geometry using a GeniX 3D microfocus X-ray source with wavelength λ = 1.5419 Å. The samples were measured under vacuum at room temperature. The characteristic size D was determined from the relation D = 2 π/Q, where the scattering vector Q depends on the wavelength of the radiation and scattering angle 2θ as Q = (4π/λ) sin(θ).

Raman spectroscopy

Raman spectra were obtained on a Confotec MR200 confocal Raman spectrometer (SOL instruments). A diode-pumped solid-state laser with λ = 532 nm was used as an excitation source. Raman experiments were carried out using a 1200 lines/mm diffraction grating, a 100 µm confocal aperture and a x20 magnification lens.

In vivo testing

Corneoplast material was implanted into eight eyes of four rabbits. All animal manipulations were performed in accordance with the European Convention for the Protection of Vertebrate Animals Used for Experimental and Other Scientific Purposes (Strasbourg, 1986). The operation consisted of layer-by-layer and end-to-end implantation of graft fragments, pig and horse. Alloimplantation of rabbit cornea was performed as a control. In the postoperative period, biomicroscopy and optical coherence tomography (OCT) were performed on REVO tomograph (Optopol, Poland).

RESULTS AND DISCUSSION

The characteristic distance D obtained from SAXS curves (Fig. 1a) was used as a parameter to identify the similarity of corneal collagen from different animal species. We found the repeat distance of collagen fibrils (Df), the average distance between triple helices in the quaternary structure (Dtr.h), and the distance between neighboring amino acid residues along the central axis of the helical structure (Dam.ac). The obtained values of Df (n = 9) are 62.6, 63.6, 63.2, 63.8 nm; Dtr.h are 1.05, 1.10, 1.11, 1.10 nm; Dam.ac are 0.27, 0.28, 0.28, 0.28 nm for horse, human, pig, pig (H2O2) grafts, respectively. The error in determining the characteristic distance in all cases does not exceed 5% of the value. All samples have peak in the region of Q from 1.5 to ~2 nm-1, that may indicate the presence of triglycerides, the main source of which, presumably, are the membranes of cellular elements of the corneal stroma [3]. The slope n in the double logarithmic representation of SAXS curves in Fig. 1a is responsible for the morphology of the сcollagen lamellae. The difference in n values for human graft is associated with age-related changes in collagen structure. Fig. 1b-e show microphotographs of the surfaces of the studied grafts.

| a |  | b |  | d |  |
| --- | --- | --- | --- | --- | --- |
|  |  | c |  | e |  |
| Fig.1. a – SAXS curves of stromal corneal grafts obtained for different species; microphotographs of the surfaces of the studied grafts, objective magnification x20: b – horse, c – human, d – pig, e – pig treated by H2O2 |  |  |  |  |  |

Raman spectroscopy was used for chemical identification of materials and determine the information about the secondary structure of proteins [4]. Fig. 2a shows a typical spectrum of collagen I. To investigate the differences in the molecular structures of the graft collagens, the focus was on the bands associated with amino acids and proteins. The secondary structure of collagen was analyzed by deconvolution of the amide I region (Fig. 2, b-e). The data show that collagen has the same β-structure conformation [5,6,7] and the frequency values are correlated for different species. However, not all observed peaks directly related to the collagen structure. Peak at ~ 1555 cm-1 is identified as a vibrational mode characteristic of an indispensable amino acid (tryptophan), which is known as a part of proteins of all known living organisms, but is not contained in proteins of connective tissues, in particular, in collagen protein [8,9]. Tryptophan may be part of pigments that are clearly visible on micrographs of grafts (Fig. 1b-e).

| a |  | b |  | d |  |
| --- | --- | --- | --- | --- | --- |
|  |  | c |  | e |  |
| Fig 2. a – Raman spectra of grafts of different species (ν - stretching mode; δ - in-plane bending mode); deconvolution of amide band I b – horse, c – human, d – pig, e – pig_H2O2 |  |  |  |  |  |

Six months after surgery, the grafts implanted in the corneal layers were biomicroscopically identified (Fig. 3). The porcine graft shows a slight vascular reaction in the form of pannus, while the horse graft did not cause a noticeable vascular reaction. In both cases, there is slight infiltration around the edges of the grafts.

|  | Fig 3. Biomicroscopy (top row) and OCT (bottom row) 6 months after surgery |
| --- | --- |

On optical coherence tomography 6 months after end-to-end and intralamellar implantation (Fig.3), a continuous layer of epithelium normal in thickness is determined, the layered structure characteristic of corneal tissue is preserved, full integration of the material with the recipient's cornea is noted. During intralamellar surgery, the implanted material is a hyperreflective meniscus. The results indicate a minimal inflammatory response to the implantation of xenomaterials into the eyes of experimental rabbits, independent of the species of grafts.

CONCLUSION

The methods of small-angle X-ray scattering and Raman spectroscopy showed a high species similarity of the collagen structures of grafts of various animal origins, subjected to dehydrothermal cross-linking or treated with hydrogen peroxide, to native human ones. The Corneoplast material is sufficiently biocompatible and capable of integration with the recipient's cornea in an animal experiment. The results obtained clearly indicate that the studied grafts are quite suitable for veterinary practice and can become an alternative to human donor material for lamellar keratoplasty in the future.

REFERENCES

- Sharifi R. et al. Finding an optimal corneal xenograft using comparative analysis of corneal matrix proteins across species //Scientific Reports. 2019. Т. 9. №. 1. P. 1876.

- Anisimov S. I. et al. Dehydrothermal crosslinking of the material "Corneoplast": possibilities of controlling physical, structural and biological properties. Experimental study //The EYE EYE. 2023. Т. 25. №. 3. P. 215-223.

- Mohd Sobri S. N. et al. Structural studies of epithelial mesenchymal transition breast tissues //Scientific reports. 2020. Т. 10. №. 1. P. 1997.

- Wen Z. Q. Raman spectroscopy of protein pharmaceuticals //Journal of pharmaceutical sciences. 2007. Т. 96. №. 11. P. 2861-2878.

- Ye H. et al. Burn-related collagen conformational changes in ex vivo porcine skin using Raman spectroscopy //Scientific Reports. 2019. Т. 9. №. 1. P. 19138.

- Połomska M. et al. Effects of Temperature on the FT NIR Raman Spectra of Fish Skin Collagen //Applied Sciences. 2021. Т. 11. №. 18. P. 8358.

- Becker L. et al. Raman microspectroscopy identifies fibrotic tissues in collagen-related disorders via deconvoluted collagen type I spectra //Acta Biomaterialia. 2023. Т. 162. P. 278-291.

- Paul C., Leser S., Oesser S. Significant amounts of functional collagen peptides can be incorporated in the diet while maintaining indispensable amino acid balance //Nutrients. 2019. Т. 11. №. 5. P. 1079.

- Takeuchi H. Raman structural markers of tryptophan and histidine side chains in proteins //Biopolymers: Original Research on Biomolecules. 2003. Т. 72. №. 5. P. 305-317.