## Slide 1
Kinetics of fullerene aggregation in polar liquids and their mixtures with water
T.V. Tropin, N. Jargalan, O.A. Kyzyma, M.V. Avdeev, V.L. Aksenov
Frank Laboratory of Neutron Physics, Joint Institute for Nuclear Research, Dubna, Russia
The XXI International Scientific Conference of Young Scientists and Specialists, JINR, Dubna, Russia, October 2-6, 2017

## Slide 2
Fullerenes С60 in solutions
Molecular solutions of С60
Colloidal solutions of С60
(including water!)
Dissolves in many liquids!
Cluster formation observed!
Perspective biomedical applications!
Investigations of solutions of C60 are interesting both from the viewpoint of fundamental investigations and for the perspective practical applications.
С60/C6H6
С60/H2O
1 nm

## Slide 3
Fullerenes – perspective for biomedicine!
Cancer treatment
Hepatoprotective effect
N. Gharbi, M. Pressac, et. al, “[60]Fullerene is a powerful antioxidant in vivo with acute or subacute toxicity” // Nano Lett, 5(12) 2578-2585, 2005.
S. Prylutska, I. Grynyuk, et. al, “C60 fullerene as synergistic agent in tumor-inhibitory doxorubicin treatment” // Drugs in R&D 14 333-340 2014.
T.I. Halenova, I.M. Varenyuk, et. al, “Hepatoprotective effect of orally applied water-soluble pristine C60 fullerene against CCl4-induced acute liver injury in rats” // RSC Advances 102 2016.
Antioxidant, antitumor properties of fullerene-water solutions!
Synergetic effect with different drugs!

## Slide 4
Obtaining fullerene-water solutions
From non-polar C60 solution
H2O
C60 in an organic solution
Non-miscible with water
(benzene)
Ultrasound treatment,
400-600 W, 20-50 kHz
Stable colloidal solution
From polar C60 solution
C60/N-methylpyrrolidone
(NMP)
NMP/nC60
H2O
NMP< 0.005 vol.%
Similar medical effects
Similar stability
Smaller cluster sizes?
Easier in preparation!
NMP less toxic than benzene!
±
+

## Slide 5
Investigate and describe cluster growth in C60/NMP and C60/NMP/H2O solutions
Propose a qualitative description of the water addition to C60 solution in polar solvent

## Slide 6
Formation of charge-transfer complexes Solvatochromic effect
Cluster formation and growth
TEM image of C60/polar-solvent
Absorption spectra of fullerene solution by UV-Vis spectrometry
C60/NMP solution: kinetic effects
C60-NMP complex, d=6.95 D

## Slide 7: Dissolution and complex formation in C60/NMP
A model treatment of UV-Vis spectra allowed determining both dissolution and complex formation rates with respect to temperature and stirring speed
N. Jargalan, T.V. Tropin et al., Nanosystems: physics, chemistry, mathematics, 2016, 7 (1), p. 99–103
Buger-Lambert-Beer law
not satisfied

## Slide 8
C60/NMP and C60/NMP/H2O: DLS measurements
Pure C60/NMP solution
C60/NMP/water solutions
Large clusters in “old” C60/NMP solution detected;
V.L. Aksenov, M.V. Avdeev, T.V. Tropin, et. al, // Physica B V.385–386 PP.795–797 2006
N. Jargalan, T.V. Tropin, M.V. Avdeev, et. al // Solid State Phenomena 2018 (accepted)
O.A. Kyzyma, M.V. Avdeev, O.I. Bolshakova // Environ Sci Technol 2018 (submitted)
Rclusters > 100 nm
Rclusters < 50 nm
Time
Cluster decomposition effect takes place on water addition;
The effect bears a critical character (X>0.4)!

## Slide 9
Theoretical description

## Slide 10
Solvent.
Addition of C60, stirring.
Dissolution of С60. Molecular solution under certain conditions.
Formation of С60-solvent complexes, change of the color of solution.
Growth of huge С60 clusters. Decrease of the monomers concentration.
Hours
Days
Modeling confined cluster growth in polar solutions of С60
Model parameters and functions:
A(t‘) – concentration of C60 complexes
csat – saturation concentration;
f(n,t‘) – cluster size distribution function;
τ,τ‘ – characteristic times of dissolution and complex formation.
Other model parameters: D, σ, ceq.
Cluster formation and growth takes place as a two-step process: complexes formation with solvent molecules, further clusters growth.
Values of model parameters obtained from experiments. The solutions of kinetic equations for real-time systems obtained via extrapolation procedure.
T.V. Tropin, M.V. Avdeev, O.A. Kyzyma, R.A. Yeremin, N. Jargalan, M.V. Korobov, V.L. Aksenov // Phys. Status Solidi B, V. 248, Nos. 11, pp. 2728-2731, 2011

## Slide 11
Modeling real-size clusters in C60/NMP
Cluster sizes: R>100 nm, n>107 (…equations)!
Complex formation time ~hours, τc~107!

## Slide 12
T.V. Tropin, M.V. Avdeev, V.L. Aksenov Cryst. Rep., 2018 (accepted)
Confined growth model master-curve
Master-curve found for the <r> and cmon dependence. This allows modeling growth of real-size fullerene aggregates.
Evolution of mean cluster size, <r>
Master-curve for <r> and cmon
Notes: Для первые модели основные кинетические уровнение не изменяет, но вероятност изменял по следущие формы. Здесь 𝜏 – характристик время которые отвечающие комплекс образования.
На рисунке показывает разница между старые и новые вероятность с временами. Черные кривие это старые значание, осталные кривие соответствуют новые значение по разные значение 𝜏.

## Slide 13
T.V. Tropin, M.V. Avdeev, V.L. Aksenov Cryst. Rep., 2018 (accepted)
Confined growth model cluster size distributions (CSD)
Master-curve found for the <r> and cmon dependence. This allows modeling of real-size particles.
“Early” CSDs
“Late” CSDs
Lifshitz-Slyozov CSD

## Slide 14
Water addition: cluster state reorganization
C60/NMP
C60/NMP/H2O
Water addition
UV-Vis, SANS, DLS data, mass spectrometry…
An effect with a critical character!
>100 nm clusters
~30-50 nm clusters
H2O
C60/NMP

## Slide 15
Cluster state reorganization: model approach
An effect with a critical character!
Effect of NMP: non-linear increase of water solubility of drugs!
Model of dissolution:
  C60-NMP complexes have non-zero solubility in water,
  Diffusion coefficients and surface tension change proportionally with X.
X=0 – no water added;
X=1 – infinite amount of water added.
Sanghvi, R., et. al. Solubility improvement of drugs using N-methyl pyrrolidone. Amer. Assoc. of Pharm. Sci., 9(2), 366–376 2008.
- model parameter
T.V. Tropin, V.L. Aksenov JETP Letters 2018 (submitted)
How does solubility of complexes in NMP-water mixture change?!

## Slide 16
Modeling C60/POL dissolution by water
Change of the average cluster size <R> after water addition, depending on X for different values of model parameter: decreasing C60-POL solubility in water.

## Slide 17
Modeling C60/POL dissolution by water
Change of characteristic concentration and relaxation time on dissolution affects the average cluster size in the desired way.
Model predictions:
Solubility in water: ← may be important for dialysis!
At dissolution rates above 1:1000 cluster sizes should not decrease!
T.V. Tropin, V.L. Aksenov JETP Letters 2018 (submitted)

## Slide 18
Conclusions
Fullerene aggregates in NMP and NMP/H2O were studied experimentally. Cluster sizes changes from >100 nm to 30-50 nm on water addition.
DLS, UV-Vis, SANS measurements. A model for kinetics of UV-Vis change.
A model approach for description of the kinetics of cluster growth in polar solutions of C60 has been developed.
One-component segregation, confined growth (complex formation), master-curve approach, CSDs obtained for any t.
C60/POL water dissolution model proposed.
Critical decomposition explained.
Model predictions for C60-NMP complexes solubility in water, and for the critical X value were obtained.
Calculations performed at the LIT/JINR HybriLIT cluster.
This work has been supported by the JINR grant for young scientists #17-401-03.

## Slide 19
THANK YOU FOR ATTENTION!

## Slide 20
Публикации
Т.В. Тропин, N. Jargalan, М.В. Авдеев, О.А. Кизима, D. Sangaa, В.Л. Аксенов // Физика твердого тела, Т. 56, вып. 1, С. 147-150, 2014.
Н. Жаргалан, Т.В. Тропин, М.В. Авдеев, В.Л. Аксенов // Поверхность. Рентгеновские, синхротронные и нейтронные исследования, 2015, №1, с. 16-20.
N. Jargalan, T.V. Tropin, M.V. Avdeev, V.L. Aksenov // Nanosystems: physics, chemistry, mathematics, V. 7 (1), pp. 99-103, 2016.
T.V. Tropin, J.W.P. Schmelzer, V.L. Aksenov // J. Mol. Liq., V. 235, pp. 172-177, 2017.
Т.В. Тропин, М.В. Авдеев, В.Л. Аксенов // Кристаллография 2018 (в печати).
N. Jargalan, T.V. Tropin, M.V. Avdeev, V.L. Aksenov, D. Sangaa // Solid State Phenomena, 2018 (accepted).
Т.В. Тропин, В.Л. Аксенов // Письма в ЖЭТФ, 2018 (submitted).

## Slide 21
Разбавление водой – сравнение с МУРН
Сравнение теории с экспериментом по рассеянию нейтронов
V.L. Aksenov, M.V. Avdeev, T.V. Tropin, et. al. // Phys. B Condens. Matter. 385–386 (2006) 795–797. doi:10.1016/j.physb.2006.06.086

## Slide 22
Разбавление водой – сравнение с МУРН
Сравнение теории с экспериментом по рассеянию нейтронов
V.L. Aksenov, M.V. Avdeev, T.V. Tropin, et. al. // Phys. B Condens. Matter. 385–386 (2006) 795–797. doi:10.1016/j.physb.2006.06.086

## Slide 23
SANS signal modeling for C60/NMP solution
Mean cluster size
Modeled SANS curves
Optimal conditions for SANS measurements
T. V. Tropin, N. Jargalan, et. al // Phys. Solid State. 56 (2014) 148–151