## Slide 1
JOINT INSTITUTE FOR NUCLEAR RESEARCH
Frank Laboratory of Neutron Physics
PROXIMITY EFFECTS AT SUPERCONDUCTING AND FERROMAGNETIC HETEROSTRUCTURES
Zhaketov Vladimir
134th session of the Scientific Council at JINR, 21-22 September, 2023. Dubna, Russia.

## Slide 2
COLLABORATION
Zhaketov V., Nikitenko Yu., Aksenov V. – JINR, Russia
Norov D. – Moscow State University, Russia
Khaydukov Yu. - Max-Planck-Institute, Germany
Devyaterikov D., Kravtsov E. - Institute of Metal Physics, Russia
2 / 17

## Slide 3
OUTLINE
Polarized neutron reflectometry
Rare-earth elements for spintronics
Influence of superconductivity on helimagnetism
3 / 17

## Slide 4
incoming
neutron
GISANS
Off-specular scattering
POLARIZED NEUTRON REFLECTOMETRY
Polarized neutron reflectometry – experimental method for investigation of metallic low-dimensional heterostructures, polymer films, biological systems, free surface of liquids, magnetic fluids etc.
4 / 17

## Slide 5
Charged particles (n, α); (n, t); (n, p)
Gamma-quanta (n, γ)
Fission fragments (n, f)
Spin-flip neutrons
Noncoherent scattered neutrons by nuclei
Inelastically scattered neutrons
Diffusely scattered neutrons on medium inhomogeneities
i – isotope, j – type of secondary radiation
Neutron
detector
detector of secondary radiation
sample
Zhaketov V.D. et al. // Journal of Surface Investigations, vol. 15, no. 3, pp. 549-562 (2021)
Zhaketov V.D. et al. // Journal of Surface Investigations, vol. 13, no. 3, pp. 478-487 (2019)
REGISTRATION OF SECONDARY RADIATION
5 / 17
Registration of secondary radiation in neutron reflectometry makes it possible to determine the isotopic profiles of elements.

## Slide 6
A gamma radiation signal was obtained from an ultrathin (1 nm) layer of gadolinium placed in a neutron resonator. The mass of gadolinium used in the experiment (3 micrograms) is 25 times less than in the previous experiment (Zhang et al., PRL 72 (1994)).
The work was performed on the REMUR spectrometer (IBR-2, Dubna) in collaboration with colleagues from JINR (Dubna), IPM RAS (Yekaterinburg), and MPI FKF (Stuttgart)
GAMMA RADIATION SIGNAL FROM AN ULTRATHIN LAYER OF GADOLINIUM
@ Khaydukov

## Slide 7
F
S
Ferromagnet / superconductor
Inverse proximity effect
Magnetic states of S-FM systems under the influence of proximity effects
Normal metal / superconductor
Low-dimensional systems
Influence of magnetism on the superconducting properties of the system
Influence of superconductivity on the magnetic properties of the system
Inhomogeneous structures?
S-FM structure
Inhomogeneous S-FM structure
PROXIMITY EFFECTS IN THE PHYSICS OF SUPERCONDUCTIVITY
7 / 17

## Slide 8
v
1. Scheme of classical spin valve
2. Superconducting spin valve
3. Controlling magnetism
FM
SC
FM
M1
M2
FM
SC
FM
M1
M2
4. Non-collinear spin valves
SUPERCONDUCTING SPIN VALVES
A. Singh et al. // Physical review X 5, 021019 (2015)
A. Golubov, M. Kupriyanov // Nature Materials, Vol. 16, Feb. 2017
Yury Khaydukov et al. // EU Patent application 21153254.4-1212
8 / 17

## Slide 9
magnetic
particles
RKKI
RARE-EARTH ELEMENTS (GADOLINIUM) FOR SPINTRONICS
CGS units
CGS units
Ta(20nm)
V(150nm)
Fe1-xVx(1nm)
V, Cr (1.2nm)
Nb(150nm)
Si(0.5mm)
Fe1-xVx(1nm)
Al2O3
Nb(25nm)
Gd()
x 12
Nb/FeV/V
H=20 Oe - Tb≈150 K
Nb/FeV/V
H=1000 Oe - Tb≈50 K
[Nb/Gd]x12
H=1000 Oe - Tb≈8 K
Gadolinium is a localized ferromagnet with a rather low (compared to Fe, Co, and Ni) bulk Curie temperature of Tm = 293 K. Strong localization of the magnetic moment stabilizes ferromagnetism even in ultrathin Gd layers.
Gd has ability to couple with other ferromagnets, forming nontrivial magnetic ordering patterns which can be used for the creation of superconducting spin valves.
Niobium and gadolinium components are not mutually soluble in either the solid or liquid phase.
Gadolinium has record cross-section of -reaction.
Zhaketov V.D. et al. // JETP, vol. 129, No.2, pp. 258-276 (2019)
Khaydukov Yu.N. et al. // Phys. Rev. B, 97, 144511 (2018)
9 / 17
1 – ZFC
2 - FC
1 – ZFC
2 - FC
- superparamagnetism
– superspin glass
M. Knobel et al. // JNN, vol. 8, 2836-2857, 2008

## Slide 10
Structures Nb(25nm)/Gd(df)/Nb(25nm) were investigated
Observed reducing of Tc with increasing of magnetic moment
Superconducting coherent length in gadolinium
Dependance
Khaydukov Yu.N. et al. // Phys. Rev. B, 97, 144511 (2018)
EFFECT OF MAGNETISM ON SUPERCONDUCTIVITY IN NB/GD/NB TRILAYERS
Q(nm-1)
10 / 17

## Slide 11
Results of experimental data fitting
Reducing the magnetic moment of structures [Nb(25 nm)/Gd(x=1.2, 3, 5 nm)]х12 below
Transition of a ferromagnetic structure to superconducting state
The superconductor displaces the magnetic field
The penetration depth was >
Khaydukov Yu.N. et al. // Phys. Rev. B, 99, 140503 (2019)
DIAMAGNETISM OF PERIODIC FERROMAGNETIC-SUPERCONDUCTING STRUCTURE
Al2O3
Nb(25nm)
Gd()
x 12
11 / 17

## Slide 12
Investigated structures:
1) Dy (2000 Å) 2) Ho (2000 Å) 3) [Dy (60 Å)/Ho (60 Å)]×34
Dy
Ho
FURTHER PERSPECTIVE – RARE EARTH METALS DYSPROSIUM AND HOLMIUM
Devyaterikov D.I. et al. // Journal of Surface Investigations, Vol. 16, No. 5, pp. 839-842 (2022)
Devyaterikov D.I. et al. // Physics of Metals and Metallography, Vol. 122, No. 5, pp. 465-471 (2021)
12 / 17
Systems with nontrivial magnetic ordering are promising for studies of proximity effects, since they have low phase transition temperatures
Dy (2000 Å)
T=
Dy (2000 Å)
T=
[Dy (60 Å)/Ho (60 Å)]×34
Dy
Ho

## Slide 13
It can be seen that with decreasing temperature, S increases, which indicates that with decreasing temperature, the helimagnetic ordering transforms into a fan one, since the collinear component of the magnetization increases.
PNR data for structure
[Dy (60 Å)/Ho (60 Å)]×34/ Nb (60 Å)
13 / 17
N.G. Pugach et al. // arXiv:2110.00369v1
EFFECT OF SUPERCONDUCTIVITY ON HELIMAGNETIC ORDERING
But at the opposite behavior is observed, i.e., a decrease in S, which indicates the recovery from the fan phase - helimagnetic. This behavior is due to the fact that the helimagnetic phase is more favorable for the existence of superconducting correlations.
Zhaketov V.D. et al. // Solid state physics, 2023, 65, 7
N.G. Pugach et al. // Phys. Rev. Appl. 18, 5, 054002 (2022).

## Slide 14
T↓
T↓<Tc(Nb)
Helimagnetic ordering
Fan ordering
Helimagnetic ordering
Al2O3
Nb(40nm)
Dy(6nm)
Nominal structures
Nb(10nm)
Ho(6nm)
x 34
S-leakage
EFFECT OF SUPERCONDUCTIVITY ON HELIMAGNETIC ORDERING
14 / 17

## Slide 15
Trilayer systems:
Al2O3(R, A- plane)//Nb(250Å)/RE(1÷10Å)/Nb(250Å)/Ta(30Å)
Al2O3(R, A- plane)//[Nb(250Å)/RE(20,40,60Å)]x12/Nb(50Å)
Superlattices:
RE=Dy, Ho
Khaydukov Yu.N. et al. // Phys. Rev. B, 97, 144511 (2018)
Khaydukov Yu.N. et al. // Phys. Rev. B, 99, 140503 (2019)
STRUCTURAL PROPERTIES OF NB/DY AND NB/HO SUPERLATTICES
X-ray reflectometry
Atomic force microscopy
X-ray diffraction
1 - [Nb(25 nm)/Dy(2 nm)]12,
2 - [Nb(25 nm)/Ho(2 nm)]12,
3 - [Nb(25 nm)/Dy(6 nm)]12,
4 - [Nb(25 nm)/Ho(6 nm)]12.
The interlayer boundaries are characterized by the root-mean-square roughness amplitude for all layers no more than Rq~1.5 nm. The data demonstrate the homogeneity of these systems at the level of Nb/Gd structures.
Nb(5nm)

## Slide 16
Conclusion
16 / 17
One of the effective methods for studying magnetism of heterostructures is polarized neutron reflectometry, which makes it possible to obtain chemical and magnetic depth profiles with nanometer resolution. Registration of secondary radiation make possible to determine distribution of separate elements.
Rare-earth elements are perspective element for creation of devices for spintronics. Main reasons: good interfaces between boundaries and weak magnetism. Correlations length of superconductivity for Gd 4 nm. It has been observed diamagnetism for periodic superconducting ferromagnetic Gd/Nb system.
Further prospects are connected with the study of the dysprosium and holmium as helimagnet elements with non-trivial magnetic order for creation of spintronics devices. Changing of magnetic orderding under influence of superconductivity was demonstrated for system Nb/[Dy/Ho].

## Slide 17
Thank you for your attention!