## Slide 1
Investigation of the crystal structure properties of Bi-activated strontium aluminates
O.N. Lis, S.E. Kichanov, N.M. Belozerova, Yu. V. Bokshyts, G.P. Shevchenko, D.P. Kozlenko

## Slide 2
Bi-activated strontium aluminates
Bismuth is a non-toxic metal with a large number of possible valence states which, together with its tendency to form clusters, make it a versatile but complex dopant for possible luminescence applications.
The properties of phosphors depend on the composition of the matrix, the type of activator, its concentration, and, consequently, on the type of crystal structure, replacement positions and environment.

## Slide 3
Experimental methods
X-ray diffraction PANalytical Empyrean Advance X-ray diffractometer
Raman spectroscopy SOL instruments λ =532 nm, 633 nm
Structure of synthesized compounds

## Slide 4
X-ray diffraction patterns of strontium aluminate compounds Color labeling of the corresponding diffraction peaks of the monoclinic (M) and cubic (C) phases.
Sample 9
SrAl2O4/Sr3Al2O6:Bi2O3/Bi2O4
Structural studies of crystal phosphors
s.g. P21
s.g. Pa
№ of sample | Activator oxide | Molar ratio of initial reagents
Sample 0 | No | Sr(NO3)2:Al2O3 = 1:1
Sample 1 | Bi2O3 1.5% | 
Sample 2 | Bi2O3 3% | 
Sample 3 | Bi2O4 1.5% | 
Sample 4 | Bi2O4 3% | 
Sample 5 | No | Sr(NO3)2:Al2O3 = 5:3
Sample 6 | Bi2O3 1.5% | 
Sample 7 | Bi2O3 3% | 
Sample 8 | Bi2O4 1.5% | 
Sample 9 | Bi2O4 3% | 
Synthesis conditions
Sr3Al2O6
SrAl2O4

## Slide 5
Structural studies of crystal phosphors
The relative decrease in the unit cell volumes of the monoclinic (orange triangles) and cubic phases (violet points) of studied strontium aluminates.
Sr3Al2O6
SrAl2O4
The average lengths of the Sr-O bonds of the strontium aluminate compounds. b) The average Al-O bond lengths of the tetragonal oxygen coordination for monoclinic and cubic phases of the strontium aluminates compounds.

## Slide 6
Structural studies of crystal phosphors
The position of characteristic Raman lines for the monoclinic (a) and cubic (b) phase of the strontium aluminate compounds.

## Slide 7
Optical properties of phosphors
2D excitation – emission map for Sample 9. Such fluorescence signal distribution is typical for a whole set of studied bismuth-activated strontium aluminates.
Measured fluorescence data for selected strontium aluminate compounds (Samples 2,4,7,9): (a) excitation (λem=390 nm, dashed lines) and emission (λex=320 nm, solid lines) spectra revealing a sharp emission peak at 390 nm; (b) excitation (λem=520 nm, dashed lines) and emission (λex=290 nm, solid lines) spectra revealing a broadband emission centered at ~520 nm; The peak positions corresponding to different radiative transitions are labeled with corresponding wavelength values.

## Slide 8
Conclusions
The results clearly indicate the formation of monoclinic SrAl2O4 and cubic Sr3Al2O6 phases of strontium aluminates during synthesis, and the relative content of these phases can be controlled through the ratio of the initial components in the chemical synthesis. Changes in the crystal structural parameters, bond lengths, and frequencies of characteristic vibration modes indicate the incorporation of bismuth ions into the crystal lattice of both phases.
Based on structural and spectral data, we can declare that the fluorescent properties of the studied strontium aluminates can be controlled through the formation of a two-component system in which the bismuth ion activators can be located in various crystallographic coordination.
The increase in luminescence intensity can be explained by the redistribution of the activator ion Bi3+ both between the monoclinic and cubic phases as well as between different strontium positions in the crystal structure.

## Slide 9
Thank you for attention!