## Slide 1
Polyacrylamide brushes synthesized with “grafting through” approach: characterization and scaling analysis
Avdeev M.M.1,2, Shibaev A.V.2, Maslakov K.I.3, Dvoryak S.V.3, Lokshin B.V.4, Gorshkova Yu.E1,5, Tropin T.V.1, Philippova O.E.2
1 Frank Laboratory of Neutron Physics, Joint Institute for Nuclear Research, Dubna, Russia 2 Faculty of Physics, M.V. Lomonosov Moscow State University, Moscow, Russia 3 Chemistry Department, M.V. Lomonosov Moscow State University, Moscow, Russia 4 Nesmeyanov Institute of Organoelement Compounds, Russian Academy of Sciences, Moscow, Russia
5Institute of Physics, Kazan Federal University, Kazan, Russia
Joint Institute for Nuclear Research
Frank Laboratory of Neutron Physics
Dubna 2023

## Slide 2
Fig. 1.1. Scheme of the structure of an ordinary polymer brush
2a
What are polymer brushes and what are they used for?

## Slide 3
Fig. 1.2. Stimuli-responsive coatings
Fig. 1.1. Scheme of the structure of an ordinary polymer brush
2a
What are polymer brushes and what are they used for?
Zhe Chen, et. al.. Langmuir 2012 28 (37), 13452-13458

## Slide 4
Fig. 1.3. Lubricants and protective coatings
Fig. 1.2. Stimuli-responsive coatings
Fig. 1.1. Scheme of the structure of an ordinary polymer brush
2a
What are polymer brushes and what are they used for?
Zhe Chen, et. al.. Langmuir 2012 28 (37), 13452-13458
Qiangbing Wei, et. al.; Macromolecules 2013 46 (23), 9368-9379

## Slide 5
What are polymer brushes and what are they used for?
Fig. 1.4. Stabilization and integration of nanoparticles in nanocomposites
Fig. 1.3. Lubricants and protective coatings
Fig. 1.2. Stimuli-responsive coatings
Fig. 1.1. Scheme of the structure of an ordinary polymer brush
2a
Zhe Chen, et. al.. Langmuir 2012 28 (37), 13452-13458
Qiangbing Wei, et. al.; Macromolecules 2013 46 (23), 9368-9379

## Slide 6
“grafting-to”
Mushroom-like brush
“grafting-from”
“grafting-through”
Polymer brush synthesis: “grafting through” approach

## Slide 7
Polymer brush synthesis: “grafting through” approach
“grafting-to”
“grafting-from”
“grafting-through”
Mushroom-like brush
Dense brush

## Slide 8
Polymer brush synthesis: “grafting through” approach
“grafting-to”
“grafting-from”
“grafting-through”
Mushroom-like brush
Dense brush
???

## Slide 9
Goals
Objectives
GOALS & OBJECTIVES
Investigate the features of “grafting-through” approach
Scaling analysis of the polymer brush thickness
Tuning the polymer brush thickness by changing the external conditions

## Slide 10
Sample preparation: Step 1 – surface activation
After piranha etching
Silicon substrate
piranha – H2SO4 + H2O2 (3:1)
in H2O
Andrew S. D’Souza, et. al. Journal of the American Ceramic Society, Vol. 82, 5, 1998, 1289-1293

## Slide 11
Sample preparation: Step 2 – monomer grafting
TMSPMA(MPS)

## Slide 12
Sample preparation: Step 3 – polymerization process

## Slide 13
Free-radical polymerization
Thermal catalysis at T = 30-60°C
Preparation time: 12 hrs
Reaction mixture
  Monomer – 10 wt%
  Initiator – 0.16 wt%
Reaction vessel
acrylamide (monomer)
Ammonium persulfate (initiator)
Sample preparation: Step 3 – polymerization process
TMSPMA (anchor)
Substances

## Slide 14
X-Ray Reflectometry (XRR)
Atomic-Force Microscopy (AFM)
Thickness and SLD profiles analysis
Surface morphology analysis
device: NTEGRA (NT MDT Spectrum Instruments)
Probe: NSG01(monocrystal. Si, R = 10 nm, k=5.1 N/m)
Measurements were carried out at FLNP JINR
device: EMPYRIAN (Malvern Pananalytical)
Tubes: Cu (λ = 1.54), Co (λ = 1.79A)
Measurements were carried out at FLNP JINR
Investigation methods
Fresnel law

## Slide 15
Dynamic light scattering (DLS)
Diffusion analysis of free-polymer coils
Chemical composition analysis
device: ALV 5000 MULTIPLE TAU DIGITAL CORRELATOR with goniometer
λ =632.8нм
Measurements were carried out at Faculty of physics of Lomonosov MSU
X-Ray Photoelectron Spectroscopy (XPS)
device: Kratos Axis Ultra DLD
Съемка – AlKa mono c нейтрализатором
XPS measurements were made at XPS facility of Lomonosov MSU
Investigation methods

## Slide 16
Fourier-transform infrared spectroscopy (FTIR - ATR)
device: VERTEX 70v
Diamond crystal
FTIR measurements were made at INEOS RAS
Investigation methods
Chemical composition analysis

## Slide 17
C-H def.
XPS
N-H val.
С-H val.
С=O val.
FTIR ATR
Si peaks
polymer
anchor
Si
Polymer brush formation
Figure 2.1. High-resolution C1s, O1s, Si2p and N1s XPS spectra of substrates at different stages of preparation
Figure 2.2 FTIR-ATR spectra at each stage of preparation
C1s
O1s
Si2p
N1s

## Slide 18
Polymer brush formation
Fig. 2.4. AFM images of pristine(a) and polymer covered(b) Si substrates.
Fig. 2.3. XRR curves: dependences of the reflectivity (R) on the scattering vector (q) for the dried samples at different preparation stages.

## Slide 19
Grafting and polymerization at low temperatures
Fig. 2.5. Temperature dependence of the brush thickness H (red dots), hydrodynamic radius of residual polymer coils in solutions (black squares), and the half of the mean distance on the surface between the attached chains (blue triangles)
Fig. 2.6. effective grafting density evaluated from XRR and DLS data

## Slide 20
Grafting and polymerization at low temperatures
Fig. 2.6. Log-log plot of the polymer chains hydrodynamic radii (Rh) vs. brush thickness (H) for the scaling analysis of the polymer chains in the bulk and on the surface
Fig. 2.7. Dependence of brush thickness on the washing time

## Slide 21
Grafting and polymerization at low temperatures
Grafting to
Grafting through
Grafting from

## Slide 22
Conclusions
the polyacrylamide brushes with different thickness were synthesized and chemically attached to flat silica surface using the “grafting through” technique.
pros and cons of the grafting-through approach:
  “+” “-”
  cheap chaotic structure
  simple hard to control
  high grafting density residual product
  “clean” synthesis
new features of “grafting-through” approach:
  the intermediate stretch of attached polymer chains
  possibility of the thickness control by temperature variation
The work is financially supported by the Russian Science Foundation (project № 21-73-10197)
Colloids and Surfaces A: Physicochemical and Engineering Aspects. Submitted Avdeev, Mikhail M. et.al. “Brushes Synthesized by “Grafting Through” Approach: Characterization and Scaling Analysis”

## Slide 23
Thank you for your attention!

## Slide 24
6
Polymer brush formation
Elemental composition calculated from high-resolution XPS spectra, at.%.
Figure 2.1. Survey XPS spectra of substrates at different stages of preparation

## Slide 25
6
Polymer brush formation
Spectrum | Binding energy, eV | Content, at. % |  |  |  | Species
 |  | Reference | Step 1 | Step2 | Step 3 | 
O1s | 531.4 | – | – | – | 13.5 | O=C
 | 532.4–532.5 | 32.9 | 34.1 | 29.7 | 5.0 | SiO2, HO−C
 | 533.6 | – | – | – | 1.0 | C−O−C, O=C−O
C1s | 285.0 | 12.9 | 18.5 | 27.1 | 39.0 | C−C,H (sp3)
 | 286.3–286.6 | 2.8 | 2.8 | 2.9 | 3.3 | С−O
 | 287.9–288.1 | 0.5 | 0.6 | 0.6 | 14.4 | O−C−O, C=O, O=C−N
 | 289.2–289.3 | 0.6 | 0.6 | 1.1 | 0.7 | O=C−O
N1s | 399.8 | – | – | – | 13.5 | −NH2
Si2p3/2 | 98.8–99.0 | 41.4 | 34.6 | 30.5 | 7.4 | Si0
 | 102.6–103.0 | 8.9 | 8.8 | 8.1 | 2.2 | SiO2
Table 2. Binding energies of components in high-resolution XPS spectra of polymer brush on silicon wafer surface at different stages of preparation, their attribution to different species and the content of these species.