## Slide 1: Athenkosi Siyalo
PhD Physics (UWC)
Supervisor: Prof. Sylvain Halindintwali (UWC)
A comparative study of the effect of the sol-gel, combustion, and solid-state reaction methods on the photoluminescence properties of Zn4B6O13:Eu3+ nanophosphors.
Co-supervisor: Prof. Leelakrishna Reddy (UJ)

## Slide 2: Presentation outline
Introduction
Aims &Objectives
Applications
Synthesis
Results and discussion
Conclusion and future work
References
Acknowledgements

## Slide 3: Introduction
Zn4B6O13
Importance of synthesis methods for structural and photoluminescence properties.
Eu3+
Conduction band
Valence band
~ 5.73 eV
Zn4B6O13
Eu 5d
Eu 4f
Conduction band
Valence band
EG
Zn4B6O13: Eu3+
~ 5.73 eV
Highly crystalline
Wide bandgap
Photoluminescent
Intrinsic impurities
Successful incorporation
In host
Tunable colour emission
Intense colour emission
Improve life-time decay
Why these materials?
EG

## Slide 4: Luminescence
Cathodoluminescence
Thermoluminescence
Electroluminescence
Photoluminescence
Fluorescence
Phosphorescence

## Slide 5
Aim
The study aims to compare sol-gel, combustion, and solid-state methods to understand their influence on structural and photoluminescent properties.
Objective
To synthesize pure, singly doped Dy3+ Zn4B6O13 nanophosphors via sol-gel, chemical combustion, solid-state methods.
To identify crystal phase structure of the prepared phosphor materials.
To examine the surface morphology and chemical composition of the materials
To identify the most effective synthesis method for enhancing luminescent efficiency.

## Slide 6: Applications
LEDS
Laser
Solid state lighting
Color display
X-ray imaging
Phototherapy
[1-5]

## Slide 7: Synthesis methods
Sol-gel
Combustion
Solid- state
Fast Preparation
Fast crystallites growth
Conducted under low-
pressure and temperature
Allow control of morphology
Low preparation cost
Highly pure materials
Uniform size
Expensive
Allow control of morphology
It can be done at small scales
Time consuming
Simple
Pestle and Mortar
Homogeneous materials
Low cost
Allow control of morphology
[1-3]
Characterization : XRD, SEM & EDS, PL, and CIE

## Slide 8: X-ray diffaction
XRD results for Zn4B6O13:1% Eu3+
Cubic crystal structure:
The Debye-Scherrer equation
S.No | Sample Zn4B6O13:Eu3+ | Crystallite size (nm) | Lattice Parameters | Lattice angles
1 | (Sol-gel) | 98.05 | 7.47407 Å | 90o
2 | (Combustion) | 95.93 | 7.47547 Å | 90o
3 | (Solid state) | 96.81 | 7.47148 Å | 90o

## Slide 9: Scanning Electron Microscopy
Micrographs for phosphors prepared by (a) Sol-gel, (b) Combustion, and (c) Solid-state reaction methods.
Histograms for phosphors prepared by (a) Sol-gel, (b) Combustion, and (c) Solid-state reaction methods.
890 nm
750 nm
500 nm

## Slide 10: Energy Dispersive Spectra

## Slide 11: Photoluminescence Spectroscopy
Excitation spectra
Emission Spectra
Average lifetime decay
λexc = 246 nm
λemi = 614 nm

## Slide 12: Colour chromaticity
S.No. | Sample ID | CIE-coordinates
1 | Zn4B6O13:Dy3+ (Sol-gel) | (0.642, 0.353)
2 | Zn4B6O13:Dy3+ (Combustion) | (0.641, 0.352)
3 | Zn4B6O13:Dy3+ (Solid state) | (0.644, 0.354)

## Slide 13: Conclusion
Zn4B6O13:Eu3+ phosphor successfully synthesized
All samples resembled cubic crystal structure.
Intense photoluminescence emission at .
Sol-gel exhibited intense PL emission at = 245
All synthesis methods yielded phosphors with red colour emissions.
Potential applications in Red LEDs.
For future work new strategy of studying the impact of co-doping the host material with rare earth ions.

## Slide 14: References
LIANG, P., Mingzhen, W.A.N.G. and Zhihong, L.I.U., 2017. Synthesis and spectroscopic studies of Zn4B6O13 and Eu/Tb single-doped Zn4B6O13 phosphors. Journal of Rare Earths, 35(5), pp.441-445.
Shrivastava, R., Kaur, J., Dubey, V. and Jaykumar, B., 2015. Luminescence studies on europium-and dysprosium-doped di-strontium magnesium silicate phosphor. Research on Chemical Intermediates, 41, pp.3699-3708.
Shrivastava, R., Kaur, J., Dubey, V., Jaykumar, B. and Loreti, S., 2015. Photoluminescence and thermoluminescence investigation of europium-and dysprosium-doped dibarium magnesium silicate phosphor. Spectroscopy Letters, 48(3), pp.179-183.
Zatsepin, D.A., Zatsepin, A.F., Boukhvalov, D.W., Kurmaev, E.Z., Pchelkina, Z.V. and Gavrilov, N.V., 2016. Electronic structure and photoluminescence properties of Zn-ion implanted silica glass before and after thermal annealing. Journal of Non-Crystalline Solids, 432, pp.183-188.

## Slide 15: Acknowledgements

## Slide 16: Thank you!