## Slide 1
Junior Researcher
Of Laboratory of Radiation Materials Science
Institute of Nuclear Physics, Kazakhstan
Kim Yelena Radikovna
Scientific supervisor: The head of the laboratory of RM INP
PhD, Merezhko Mickhail Sergeevich
STUDY OF MECHANICAL PROPERTIES AND FRACTURE FEATURES OF FERRITE-MARTENSITIC STEEL EP-450 IRRADIATED BY NEUTRONS IN THE BN-350 REACTOR
Merezhko M.S., Merezhko D.A., Tsai K.V., Kislitsin S.B., Short M.P

## Slide 2: The ratio of natural and anthropogenic emissions into the atmosphere
https://triptonkosti.ru/12-foto/vybrosy-vrednyh-veschestv-v-atmosferu-prezentaciya-85-foto.html
https://energystats.enerdata.net/renewables/renewable-in-electricity-production-share.html
Substance | Emissions, million t./year | 
 | Natural | Anthropogenic
Solid particles | 770…2200 | 185…415
 | 5000 | 304
 | 650 | 100
 | 770 | 53
 | 485000 | 18300
 | 2600 | 88
Substance | Emissions, million t./year | 
 | Natural | Anthropogenic
Solid particles | 770…2200 | 185…415
 | 5000 | 304
 | 650 | 100
 | 770 | 53
 | 485000 | 18300
 | 2600 | 88
https://telegra.ph/Doklad-po-teme-EHnergetika-09-13
2
Nuclear energy structure to reach 20% by 2030
Share of renewable sources in electricity production - %
Nuclear energy as a transitional form to green energy

## Slide 3
Expected temperatures and damaging doses for different nuclear reactors
Challenges to the use of ion irradiation for emulating reactor irradiation GS Was Journal of Materials Research 30 (9), 1158-1182
High requirements for structural materials of nuclear
power plants
3
VHTR – Helium-cooled, graphite-moderated reactor
SCWR - Supercritical water-cooled reactors
GFR - graphite moderated reactor
LFR - Lead cooled fast reactor
MSR - Molten salt reactors
SFR - sodium cooled reactors
Fusion – thermonuclear reactors
TWR - Traveling Wave Reactor
28th International Scientific Conference of Young Scientists and Specialist

## Slide 4
BN – 600 BN-800 BN-1200
BN series reactors
4
28th International Scientific Conference of Young Scientists and Specialist

## Slide 5: Problems of radiation materials science Swelling and embrittlement
Swelling-induced embrittlement and subsequent failure of an EBR-II duct assembly of 304 steel during routine operations
Destruction of three fuel assembly wrappers of the BOR-60 reactor during routine work
5
Garner,F.A. 3.02 // Comprehensive Nuclear Materials (Second Edition). Oxford: Elseiver, 2020, - P.57 – 168.
28th International Scientific Conference of Young Scientists and Specialist

## Slide 6: EP-450 steel
Low induced radioactivity;
Low swelling;
High resistance to high temperature and helium embrittlement.
Low temperature radiation embrittlement;
Relatively low corrosion resistance.
Ferrite-martensitic steel is currently the most priority candidate materials for the fabrication of fuel elements and fuel assembly (FA) cladding for fast reactors and the first wall for fusion reactors.
Advantages
Disadvantages
6
28th International Scientific Conference of Young Scientists and Specialist

## Slide 7
Fuel assembly
Fuel assembly wrapper
BN-350 reactor
https://mavink.com/explore/Spent-Fuel-Rods
https://commons.wikimedia.org/wiki/File:Сравнение_активных_зон_реакторов.svg
7
28th International Scientific Conference of Young Scientists and Specialist

## Slide 8
C-1
181
C-1 сп
201
50-53 dpa
280 – 420
8
28th International Scientific Conference of Young Scientists and Specialist

## Slide 9
Chemical composition, % mass.
Characteristics of EP-450 steel
GOST | Fe | C | Si | Mn | S | P | Cr | Ni | Nb | Mo | V | B
TU 14-1-3820-84 | Осн. | 0,12 | 0,5 | 0,8 | 0,015 | 0,025 | 11−13,5 | 0,05− 0,30 | 0,3−0,6 | 1,2−1,8 | 0,1−0,3 | 0,015
Unirradiated | 84,8 | - | 0,30 | 0,5 | 0,01 | 0,02 | 12,9 | 0,18 | 0,26 | 1,1 | 0,15 | -
Irradiated, 51 dpa, 350 | 83,3 | - | 0,37 | 0,5 | 0,02 | 0,06 | 13,1 | 0,15 | 0,26 | 1,7 | 0,27 | -
Irradiated, 53 dpa, 295 | 81,6 | - | 0,37 | 0,49 |  |  | 13,1 | 0,15 | 0,26 | 1,71 | 0,27 | -
GOST | Fe | C | Si | Mn | S | P | Cr | Ni | Nb | Mo | V | B
TU 14-1-3820-84 | Осн. | 0,12 | 0,5 | 0,8 | 0,015 | 0,025 | 11−13,5 | 0,05− 0,30 | 0,3−0,6 | 1,2−1,8 | 0,1−0,3 | 0,015
Unirradiated | 84,8 | - | 0,30 | 0,5 | 0,01 | 0,02 | 12,9 | 0,18 | 0,26 | 1,1 | 0,15 | -
 | 83,3 | - | 0,37 | 0,5 | 0,02 | 0,06 | 13,1 | 0,15 | 0,26 | 1,7 | 0,27 | -
 | 81,6 | - | 0,37 | 0,49 |  |  | 13,1 | 0,15 | 0,26 | 1,71 | 0,27 | -
Heat treatment
1050 ℃ - 30 minutes
720 ℃ - 60 minutes
The specified heat treatment mode is necessary for degassing and cleaning the surface, as well as for regulating the ratio of ferrite and sorbite grains in steel.
9
28th International Scientific Conference of Young Scientists and Specialist

## Slide 10
Research equipment
Scanning electron microscope
Hitachi TM-4000 PLUS
Tensile testing machine
Instron 1195
Transmission electron
microscope
JEOL JEM-2100
10
28th International Scientific Conference of Young Scientists and Specialist

## Slide 11
Irradiated sample parameters
11
28th International Scientific Conference of Young Scientists and Specialist

## Slide 12
Type | Density, kg/
Unirradiated | 7,73
Irradiated, 53 dpа, 295 | 7,75
Irradiated, 51 dpa, 350 | 7,75
Irradiated, 51 dpа, 405 | 7,75
Type | 
Unirradiated | 7,73
 | 7,75
 | 7,75
 | 7,75
12
Type | Temperature, | Dose, dpa
Irradiated - 1 | 405 | 53
Irradiated - 2 | 350 | 50
Irradiated - 3 | 295 | 53
Type |  | Dose, dpa
Irradiated - 1 | 405 | 53
Irradiated - 2 | 350 | 50
Irradiated - 3 | 295 | 53
Irradiated sample parameters
28th International Scientific Conference of Young Scientists and Specialist

## Slide 13
The fragments of the diagrams characterized by strengthening and corresponding to neck formation in some cases turned out to be unusually large. In such cases, to calculate the value of the total elongation, the tensile diagrams were cut off to the point where the load was reduced to 10% of the maximum load.
Standard test methods for tension testing of metallic materials
13
Engineering diagrams
Chart: Elongation, %
28th International Scientific Conference of Young Scientists and Specialist

## Slide 14
The fragments of the diagrams characterized by strengthening and corresponding to neck formation in some cases turned out to be unusually large. In such cases, to calculate the value of the total elongation, the tensile diagrams were cut off to the point where the load was reduced to 10% of the maximum load.
Standard test methods for tension testing of metallic materials
13
Engineering diagrams
Chart: Elongation, %
28th International Scientific Conference of Young Scientists and Specialist

## Slide 15
The fragments of the diagrams characterized by strengthening and corresponding to neck formation in some cases turned out to be unusually large. In such cases, to calculate the value of the total elongation, the tensile diagrams were cut off to the point where the load was reduced to 10% of the maximum load.
Standard test methods for tension testing of metallic materials
13
Engineering diagrams
Chart: Elongation, %
28th International Scientific Conference of Young Scientists and Specialist

## Slide 16
The fragments of the diagrams characterized by strengthening and corresponding to neck formation in some cases turned out to be unusually large. In such cases, to calculate the value of the total elongation, the tensile diagrams were cut off to the point where the load was reduced to 10% of the maximum load.
Standard test methods for tension testing of metallic materials
13
Engineering diagrams
Chart: Elongation, %
28th International Scientific Conference of Young Scientists and Specialist

## Slide 17
Mechanical characteristics
15
28th International Scientific Conference of Young Scientists and Specialist

## Slide 18
Microstructure of EP-450 steel
The steel is characterized by a two-phase structure, which is preserved even after neutron irradiation
16
28th International Scientific Conference of Young Scientists and Specialist

## Slide 19
Phase | Unirradiated | Irradiated, 53 dpa, 405 | Irradiated, 51 dpа, 350 | Irradiated, 53 dpa, 295
Ferrite | 24 | 62 | 47 | 51,9
Tempered martensite (Sorbite) | 76 | 38 | 53 | 48,1
Phase | Unirradiated |  |  | 
Ferrite | 24 | 62 | 47 | 51,9
Tempered martensite (Sorbite) | 76 | 38 | 53 | 48,1
Correlation of two phases
17
With increasing irradiation temperature, the quantity of ferrite phase becomes greater compared to martensite phase.
28th International Scientific Conference of Young Scientists and Specialist

## Slide 20
Microhardness
Type | Unirradiated | Irradiated, 53 dpa, 405 | Irradiated, 51 dpa, 350 | Irradiated, 53 dpa, 295
Inner | 262,54,9 | 286,410,9 | 402,9 | 453,910,8
Outer | 264,94,9 | 294,86,7 | 398,76,1 | 4509,8
Type | Unirradiated |  |  | 
Inner |  |  |  | 
Outer |  |  |  | 
Phase | Unirradiated | Irradiated, 53 dpa, 405 | Irradiated, 51 dpа, 350 | Irradiated, 53 dpa, 295
Tempered martensite (sorbite) | 263,71,2 | 3202,2 | 369,8 | 401,92,4
Ferrite | 220,62,4 | 279,64,1 | 335 | 358,42,8
Phase | Unirradiated |  |  | 
Tempered martensite (sorbite) |  |  |  | 
Ferrite |  |  |  | 
Microhardness by phases
18
28th International Scientific Conference of Young Scientists and Specialist

## Slide 21
19
Structure of EP-450 steel after mechanical testing
Unirradiated
28th International Scientific Conference of Young Scientists and Specialist

## Slide 22
20
Irradiated
Т = 405
28th International Scientific Conference of Young Scientists and Specialist
Structure of EP-450 steel after mechanical testing

## Slide 23
21
28th International Scientific Conference of Young Scientists and Specialist
Structure of EP-450 steel after mechanical testing
Irradiated
Т = 350

## Slide 24
22
28th International Scientific Conference of Young Scientists and Specialist
Structure of EP-450 steel after mechanical testing
Irradiated
Т = 295

## Slide 25
Fractography
For the unirradiated sample, the fracture pattern is ductile and fibrous. In orientation, it is oblique fibrous-scaly pits formed by the fusion of micropores. Fracture cups are visible, elongated downwards towards the sample. As the irradiation increases and the irradiation temperature changes, the fracture pattern changes to brittle, indicating low-temperature radiation embrittlement.
23
28th International Scientific Conference of Young Scientists and Specialist

## Slide 26
The initial structure of EP-450 steel
(а) fraction of the ferrite grain and phase boundaries, (b) tempered martensite (sorbite) secondary precipitation of carbide phases of the type M23C6 and MC.
24
(а) | (b)
28th International Scientific Conference of Young Scientists and Specialist

## Slide 27
Microstructure of EP-450 steel irradiated by Т = 405
(а) The ferrite grain and phase boundaries, (b) Secondary phase reflexes , (c) -phase particles, (d) dislocation structure of ferrite with  -phase particles
(а) | (b) | (c) | (d)
25
28th International Scientific Conference of Young Scientists and Specialist

## Slide 28
(а) | (b) | (c) | (d)
Microstructure of EP-450 steel irradiated by Т = 350
(а) Tempered martensite – ferrite grain, (b) secondary precipitates at phase boundaries and
subgrain boundaries,
(c) dislocation loops, (d) -phase particles on dislocations
Vacancy pores are present in steel in very small quantities. The pore sizes are 1.6 – 3.4 nm. The average pore diameter is 2.7 nm. The particles of the -phase have sizes of 5-16 nm, the average size is 9 nm. The particle density is (1 – 3)1023м-3. The particles are formed on dislocations and grown dislocation loops.
26
28th International Scientific Conference of Young Scientists and Specialist

## Slide 29
Microstructure of EP-450 steel irradiated by Т = 295
(а) The ferrite grain and phase boundaries, (b) radiation pores, (c) dislocation structure of ferrite and -phase particles on dislocations, (d) dislocation loops
(а) | (b) | (c) | (d)
Vacancy pores have a spherical shape and sizes in the range of 2.5 – 10 nm. The average pore size is 5.4 nm. The average pore density is ~11022м-3. Swelling in some areas reaches ~ 0.1%.
Particle sizes are 2.5 – 6 nm, average size is 3.8 nm. Minimum particle density is ~ 2.41023м-3. Moire contrast (d) was obtained on the particles at 600k magnification, which confirms the nature of secondary emissions.
(e)
27
O.V.Borodin, V.V.Bryk, V.N.Voyevodin, I.M.Neklyudov, V.K.Shamardin, Investigation of microstructure of ferritic-martensitic steels containing 9 and 13% Cr irradiated with fast neutrons, J. Nucl. Mater. 207 (1993) 295–302. doi:10.1016/0022-3115(93)90272-Z.
28th International Scientific Conference of Young Scientists and Specialist

## Slide 30: Conclusion
As a result of tensile tests, the strength and ductility characteristics were obtained, and the value of the deformation work was calculated.
It was shown that irradiation of EP-450 steel with fast neutrons leads to a decrease in ductility and an increase in the strength of the material, while the uniform deformation of the material irradiated to 51 dpa decreases catastrophically - to 1-2% due to the effect of low-temperature radiation embrittlement. In this case, the deformation is limited within several ferrite grains favorably oriented to the loading axis. According to fractographic studies of the fracture zone, in unirradiated steel, the destruction is viscous, and in irradiated to 51 dpa - brittle-viscous or brittle, depending on the irradiation temperature.
28
28th International Scientific Conference of Young Scientists and Specialist

## Slide 31
Thank you for your attention!
Kim Yelena
Junior Researcher of
Laboratory of Radiation Material Science
Institute of Nuclear Physics
Kazakhstan
Yelenakimr@gmail.com