## Slide 1: Crystal and magnetic properties of Tb2Ni2X, (X = Al, Ga)
MSc Nanoscience (2024)
Name: Zandile Mpupa (UWC)
Supervisor: M.B. Tchoula Tchokonte (UWC)
Co-Supervisor: B.M. Sondezi (UJ)

## Slide 2: Content
Introduction
Methodology
Results and discussion:
  Structural characterization
  Magnetization and magnetic susceptibility
  Heat capacity
Conclusion

## Slide 3: Introduction
It is well known that rare earth (RE) based intermetallic compounds reveal various interesting magnetic properties depending on the crystallized structures and the constituent elements, paving the way for potential applications in different fields.
The study of ternary intermetallic compounds with the composition RE2T2X (where RE represents rare earth elements, T represents transition metals, and X represents p-block elements) in particular has garnered significant interest due to their diverse ground state properties.

## Slide 4: Introduction
To probe the type of crystal structure and magnetic properties of Tb2Ni2X, (X =Al, Ga) compounds, we undertake to investigate the XRD, magnetic susceptibility, (T), magnetization, M(0H), and heat capacity, Cp(T) measurements.

## Slide 5: Methodology

## Slide 6
Sample preparation.
  arc furnace
  purity of samples~9,9999%
  Ingot ~3g
XRD
  Powder XRD measurements (CuKα=1,54Å)
  Collected over 2θ (150 -900)
  TOPAS academic program (quantitative and qualitative)
SEM and EDS
  Morphology and homogeneity
Magnetics Proerties and heat capacity
  PPMS-Dynacool + VSM
    DC magnetic measurements were performed at the temperature range (2-300)K with the applied field of upto 7T
  PPMS-Dynacool
    Heat capacity was measured with 2𝛕 relaxation method with zero magnetic field over temperature (2-250K)

## Slide 7: Results and discussion

## Slide 8: Structural characterization: SEM & EDS
Figs. (a) & (b): SEM micrograph of (a) Tb2Ni2Al (b) Tb2Ni2Ga compounds with length scales of 10m and magnification 2000 times.
  Micro-structure of a smooth surface is observed.
  Morphologically Al compound has more stress points and the crystal points are more obvious.
  In Fig. b the apparent dark shades indicate areas that are Ga-rich in the analyzed surface which is confirmed from the EDS results.
EDS gives the atomic ratio of the elements.
  Tb2Ni2.024(2)Al0.925(2) and Tb2Ni2,006(2)Ga1,052(2) nominally equal to the desired 2:2:1 phase within the experimental uncertainty.

## Slide 9: Structural characterization: XRD
RT powder XRD patterns for (a) Tb2Ni2Al and (b) Tb2Ni2Ga samples (green symbols) together with the full-profile LSQ refinement fits (red solid curves) to the measured data. The blue curves represent the difference between the observed and the calculated. The vertical ticks are the Bragg reflection.
  All peaks are indexed according to the W2CoB2-type structure with space group Immm. No evidence of impurity peaks are observed.
  The obtained lattice parameters and the unit volumes are Tb2Ni2Al: a = 4.1789(8) Å, b = 5.405 Å, c = 8.375 Å and V = 189.17 Å3; Tb2Ni2Ga: a = 4.1876(7) Å, b = 5.367(1) Å, c = 8.308 Å and V = 186.71(6) Å3.

## Slide 10: Structural characterization: XRD
The resulting atomic coordinates and the refinement indices are listed in Tables 1 & 2 and the resulting orthorhombic crystal structure is depicted in Fig.
Values of lattice parameters and the atomic coordinates are in good agreement with those reported in the literature [K. Miliyanchuk et al., JSSC296 (2021) 121978].
Small values of discrepancy factors confirm the good quality of the refinement as well as the high quality of the samples
The average grain size of the compounds was calculated using the Scherrer equation [Langford & Wilson, JAC11 (1978) 102]:
K = 0.9: dimensionless number known as Scherrer constant; : Bragg peak width at FWHM; : Bragg angle.

## Slide 11: Magnetization
M(0H) data measures at 1.7 K in fields up to 7 T for the Tb2Ni2X (X = Al , Ga)
Hysteresis below 3 K for Al compound with increasing and decreasing 0H.
Deviation from linear behavior of M(0H) above 6 T, suggesting metamagnetic behavior.
M(0H) values at 7 T for compounds is less than 1.1B and much smaller than the theoretical value of the free-ion trivalent Tb: .
The shortfall can be attributed to effect of CEF and/or magnetocrystalline anisotropy.

## Slide 12: Magnetic susceptibility
(T) data measured in ZFC and FC modes in an applied field of 0.1 T and in the temperature range of 1.7 – 300 K. Insets show the expanded view of (T) at low temperatures showing a distinct maximum which hints to AFM ordering with the arrows indicating AFM phase transition TN.

## Slide 13: Magnetic susceptibility
(T) curve in ZFC mode bifurcates from the FC curve in a manner characteristic of materials with competing magnetic interaction, and materials with high anisotropy and low ordering magnetic transition temperature, where the domain wall width can be comparable to the lattice space, thus resulting in a large pinning effect [Y. Zhang et al., JPD:AP49 (2016) 145002]

## Slide 14: Magnetic susceptibility
The value of TN, was obtained from these anomalies, using Fisher’s criterion [M.E. Fisher, Phil. Mag. 7 (1962) 1731]: TN is taken at the maximum of the curves as indicated by the arrows in Fig.
That give TN = 41 K, and 41.5 K for Al and Ga compounds, respectively.

## Slide 15: Inverse magnetic susceptibility
χ−1(T) of the Tb2Ni2X (X = Al, Ga) compounds measured in an applied field of 0.1 T and the temperature range 1.7 ≤ T ≤ 300 K.
Above 100 K, χ−1(T) data follow the CW relationship:
LDQ fit to the CW Eq. gives: p = 21.5(4) K, eff =10.172(2) B for Al compound and p = 17(1) K, eff =10.520(4) B for Ga compound.

## Slide 16: Inverse magnetic susceptibility
The negative p values hint at the predominance of AFM exchange interaction between the Tb moments.
The observed eff values for both compounds are close to the theoretical value of the trivalent Tb ion .
Below 100 K, deviation of χ−1(T) from the CW relationship, likely due to magnetocrystaline anisotropy.

## Slide 17: Heat capacity
Cp(T) of (a) Tb2Ni2Al and (b) Tb2Ni2Ga, together with Cp(T) of the non-magnetic Y2Ni2X (X = Al, Ga) (triangle symbols) and the mass corrected (circle symbols).
Mass corrected Cp(T) of Y2Ni2X was obtained by changing the temperature scale of Cp(T) to T*:
The mass correction was used because of the large difference of the atomic mass between Tb and Y atoms, since lattice Cp is a function of T/D and D is related to the formula mass: .

## Slide 18: Heat capacity
The arrows indicate the position of TN at 40.4 K and 41.4 K for Al and Ga, respectively.
The horizontal dot lines are the Dulong-Petit value 3NR = 124.71 J/mol.K
The solid red curves represent the Debye formula fit:
LSQ fit to the data gives: D,Al = 236.9(1) K, Al = 69(1) mJ/mol.f.u.K2 and D,Ga = 225.3(2) K, Ga = 49.5(7) mJ/mol.f.u.K2 for Al and Ga, respectively.

## Slide 19: Heat capacity
D,Al, and D,Ga same order of magnitude, indicate the similarity of lattice vibration in both compounds.
However D,Al, > D,Ga may originate from the smaller formula weight of the Al compound, compared to that of the Ga compound since .
Also note that Cp(T) data of the Y2Ni2Al and Tb2Ni2Ga compounds reach the value of Dulong-Petit around 150 K while Tb2Ni2Al and Y2Ni2Ga reach this value above 175 K.

## Slide 20: Heat capacity: Magnetic heat capacity C4f (T)
The figure shows the 4f-electronic magnetic entropy contribution to the total heat capacity, C4f(T) of (a) Tb2Ni2Al and (b) Tb2Ni2Ga compounds.
C4f(T) was obtained by subtracting the lattice contribution Cp(T*) of Y2Ni2X from the experimental Cp(T) of Tb2Ni2X:
The solid red curves represent the LSQ fits of the AFM spin-wave expression:
B: Constant dependent on the crystal structure,: energy gap in the spin-wave spectrum.
LSQ fits parameters of Tb2Ni2Al and Tb2Ni2Ga:
        γ =90(2) and 75(2) mJ/mol.f.u.K2
        B =1.00(5) and 0.70(4) mJ/mol.f.u.K4
        =47(3) and 26(2) K

## Slide 21: Heat capacity: Magnetic heat capacity C4f (T)
The insets display the magnetic entropy, S4f(T) obtained by integrating C4f(T)/T curve:
S4f(T) of both compounds reaches 2Rln(2) close to their TN values, which hints at a ground state doublet for these compounds.
S4f(TN) = 1167 J/mol.f.u.K for Al and 16.58 J/mol.f.u.K fo Ga compounds.
These values are about 27% (Al) and 39% (Ga) of the expected high-temperature limit 2Rln(13)=42.6 J/mol.K.
The observed experimental high-temperature limit at 100 K of S4f amount to 57% and 71.1% of 2Rln(13) for Al and Ga compounds, respectively.
These lower values S4f at 100 K are a direct consequence of CEF.

## Slide 22: Conclusion
XRD studies confirm both compounds' orthorhombic W2CoB2 – type with space group Immm (No. 71).
The results of (T), and Cp(T) measurements indicated that both compounds orders AFM below TN = 41 K for Al and 41.5 for Ga.
(T) at high temperatures for both compounds follow the CW relationship.
(T) at low temperatures collected in FC and ZFC modes bifurcate below TN.
M(0H) shows hysteresis below 3 T for Al compound and metamagnetic behavior above 6 T for Ga compound.
The spin-wave spectrum describes Cp(T) data below TN.
The Debye theory of lattice heat capacity describes Cp(T) data of the non-magnetic compounds.
S4f(T) data indicates a ground state doublet and a CEF for both compounds.

## Slide 23: Acknowlegment
Financial support from SA-NRF (81296, UID 111174)
Nanoscience Bursary,
The Research Development Office of UWC,
The University Research Committee of UJ,

## Slide 24
Thank you for your attention