## Slide 1
THE ROLE OF ALLOYING ELEMENTS IN THE FORMATION OF MECHANICAL PROPERTIES OF AISI 316L N STEEL, IRRADIATED BY NEUTRONS
Author: Bobrussova Yulia Alexandrovna
Engineer of the Laboratory of Radiation Materials Science of the Institute of Nuclear Physics of Almaty, Kazakhstan
Supervisors: PhD Merezhko M. S., PhD Merezhko D.A.
Institute of Nuclear Physics
The Republic of Kazakhstan
28th International Scientific Conference of Young Scientists and Specialists (AYSS-2024)

## Slide 2
Nuclear power stations on the world map
Modern nuclear power industry
Nowadays, 440 nuclear reactors (power units) with a total electrical capacity of 394 GW are in operation in 32 countries of the world;
Many of the operating reactors were connected to the power grid in the 1980s and are now between 25 and 50 years old.
54 units are currently under construction.
02
Getaldić A. et al. Nuclear and Radiological Data Available in the International Atomic Energy Agency (IAEA) Databases //Rudarsko-geološko-naftni zbornik. – 2023. – Т. 38. – №. 1. – С. 49-58.

## Slide 3
Austenitic steels are the main material of many critical components of modern nuclear reactors.
The planned service life is 40-60 years.
It is economically feasible to extend the service life of existing reactors to 80-100 years.
The baffle ring
Protective tube unit
Core barrel
WWER 1000
03
Austenitic steels in reactors
Secures fuel assembly heads, protects regulators and in-reactor control channels.
Weight: 68 tones
Designed to form the core and reduce the neutron flux to the reactor vessel wall.
Weight: 38 tones
It contains fuel assemblies and distributes coolant flow rates at the reactor inlet and outlet.
Weight: 76 tones
Конструкции твэлов, каналов и активных зон энергетических реакторов/ Г.Н. Колпаков, О.В. Селиваникова. – Томск, 2009. – 118 с.
Notes: В ВВР – 200 тонн конструкций из аустенитки.

## Slide 4
Modernization of existing steels by alloying
Alloying - adding of the impurity to the composition of materials to change (improve) physical and/or chemical properties of the basic material.
Promising chemical elements for alloying austenitic steels are nitrogen, manganese, copper and tungsten.
N
Mn
Cu
W
Nitrogen: stabilises the austenitic matrix, increases the strength of the material and enables the nickel content of the steel to be reduced;
Manganese: reduces yield strength (additionally with nitrogen), reduces chromium segregation during irradiation, improves fluidity during metal melting;
Copper: increases plasticity, improves corrosion resistance (potentially);
tungsten: an effective hardening element.
04

## Slide 5
Steels | Cr | Ni | Mn | Si | Mo | C | N | Cu | W
AISI 304 | 17,9 | 7,90 | 0,90 | 0,58 | - | 0,08 | - | - | -
AISI 316 LN | 17.5 | 12.5 | 1.8 | 0.50 | 2.5 | 0.03 | 0.07 | 0.30 | -
211L | 17.7 | 12.5 | 4.1 | 0.44 | 2.5 | 0.02 | 0.34 | 0.31 | -
212L | 17.7 | 12.6 | 5.1 | 0.44 | 2.5 | 0.01 | 0.36 | 2.8 | -
213L | 17.7 | 12.6 | 5.1 | 0.45 | 2.0 | 0.01 | 0.32 | 2.8 | 1
05
AISI 316
Basis for the alloying
211 L
Increased manganese and nitrogen concentration for stabilisation of the austenitic structure and additional hardening
212 L
The manganese content was increased to 5% in order to further stabilise austenite. Copper content was increased to 2.8% to improve corrosion properties
213 L
Additional tungsten alloying for improved corrosion resistance at high temperatures
AISI 304
It was taken for comparison purposes
Chemical composition of studied steels, (weight.%)

## Slide 6
SAMPLE PREPARATION
Neutron irradiation
In December 2023, samples were irradiated in the WWR-K reactor in the central channel 5-7 at level 3 in the reactor core to fluence Ft = 3.18×1018 n/cm2 (thermal neutrons)  0,00022 dpa.
06
The mechanical plates were cut;
Polished;
Samples were knocked out in the form of a ‘double blade’;
The samples were annealed at 1050 oC;
Cutting and polishing

## Slide 7
Tensile breaking machine Instron 1195
Microhardness tester
Micro Vicker Hardness Tester
SEM
Hitachi TM-4000 PLUS
Used equipment
07

## Slide 8: Microhardness of steels before and after irradiation (kg/mm2):
08
Chart: 
| AISI 304 | AISI 316LN | 211 L | 212 L | 213 L
Unirradiated | 160 | 158 | 195 | 198 | 214
Irradiated to fluence 3.18*10^18 | 182 | 183 | 233 | 240 | 221
22-25 (kg/mm2)
38-42 (kg/mm2)
7 (kg/mm2)

## Slide 9
Engineering tensile diagrams of the steels studied
09
Relative elongation, %
σ, MПa
σ, MПa
UNIRRADIATED
IRRADIATED
to fluency 3.18e18 (n/cm2)
AISI 304
AISI 316
213 L
211 L
212 L
AISI 304
AISI 316
213 L
211 L
212 L
Relative elongation, %

## Slide 10
10
Comparison of Mechanical Properties of Steels
Chart: Yield strength, (MPa)
| AISI 304 | AISI 316LN | 211 L | 212 L | 213 L
Unirradiated | 223 | 215 | 357 | 340 | 358
Irradiated to fluence 3.18e18 (n/cm^2) | 295 | 305 | 448 | 461 | 455
Chart: Tensile strength, (MPa)
| AISI 304 | AISI 316LN | 211 L | 212 L | 213 L
Unirradiated | 743 | 583 | 691 | 692 | 736
Irradiated to fluence 3.18e18 (n/cm^2) | 739 | 606 | 746 | 759 | 741

## Slide 11
11
Comparison of Mechanical Properties of Steels
Chart: Uniform elongation, %
| AISI 304 | AISI 316LN | 211 L | 212 L | 213 L
Unirradiated | 91.4 | 70 | 40.6 | 43 | 40.9
Irradiated to fluence 3.18e18 (n/cm^2) | 91.1 | 59.1 | 45.5 | 38.4 | 38
Chart: Total elongation, %
| AISI 304 | AISI 316LN | 211 L | 212 L | 213 L
Unirradiated | 95.8 | 81.6 | 49.8 | 50 | 47.8
Irradiated to fluence 3.18e18 (n/cm^2) | 92.3 | 66.1 | 47 | 44.6 | 44.5

## Slide 12
Microstructure of unirradiated steels after mechanical testing
Steels AISI 304
3: 4 мм
2: 3 мм
1: 1 мм
0: fracture zone
х600
Х1,5k
3
2
1
0
Shear lanes
Larger deformation lanes near the fracture zone
12

## Slide 13
х600
Х1,5k
13
Shear lanes
Intergranular cracks are noticeable
Сталь AISI 316
3
2
1
0
3: 4 мм
2: 3 мм
1: 1 мм
0: fracture zone
Microstructure of unirradiated steels after mechanical testing

## Slide 14
х600
Х1,5k
14
Shear lanes
The grains are showing
Сталь 213 L
3
2
1
0
3: 4 мм
2: 3 мм
1: 1 мм
0: fracture zone
The deformation lanes ‘overlap’ each other
Microstructure of unirradiated steels after mechanical testing

## Slide 15
Fractography of the investigated steels
AISI 304
AISI 316LN
213 L
15
UNIRRADIATED
IRRADIATED
to 3.18e18 (n/cm2)
118 μm
73.5 μm
59 μm
103 μm
228 μm
103 μm

## Slide 16
AISI 304
AISI 316LN
213 L
16
UNIRRADIATED
IRRADIATED
to 3.18e18 (n/cm2)
Fractography of the investigated steels

## Slide 17
Conclusion
Mechanical tests of samples of stainless austenitic steels AISI 304, AISI 316LN and its modifications irradiated with neutrons in the VVR-K reactor were carried out and the effect of alloying on the strength and ductility of AISI 304 and AISI 316LN steels was analyzed. In particular, it was found that:
17
Nitrogen and tungsten alloying results in hardening of the steel. Steel 213 L alloyed with tungsten has the highest microhardness value and the tensile strength of this steel is comparable to that of AISI 304.
Elongation rates, both uniform and complete, decreased for all steels after neutron irradiation, except for the AISI 304 alloy;
Copper alloying affected the mechanical characteristics to a lesser extent.

## Slide 18
THANK YOU FOR YOUR ATTENTION!
Do you have any questions?
Bobrusova@inp.kz