## Slide 1: Templated electrodeposition of indium nanowires and measuring their electrical resistance
Shashkov A.V., Noyan A.A., Napolskii K.S.
e-mail: shashkovav@my.msu.ru
Lomonosov Moscow State University
Department of chemistry
Dubna – 2024

## Slide 2: Nanowires
(In) Xu S. H. et al.//Phys. Lett. Sect. A Gen. At. Solid State Phys. 2011. V. 375. № 16
(Ag) novarials.com
(Rh) Leontiev A.P. et al.//Electrochim. Acta. 2015. V. 155.
(ZnO) Wang N. et al.//Mater. Sci. Eng. R. 2008. V. 60. № 1–6

## Slide 3
A, B – superconductors,
С – non-superconducting layer
Application of nanowires

## Slide 4: Differences in physical properties
Xu S. H. et al.//Phys. Lett. Sect. A Gen. At. Solid State Phys. 2011. V. 375. № 16
Steinhögl W. et al.//Phys. Rev. B Condens. Mater. Mater. Phys. 2002. V. 66. № 7
Dependence of melting temperature on the diameter of In nanowires:
Dependence of electrical resistance on the diameter of Cu nanowires:

## Slide 5: Purpose of the study
Development of a method for obtaining arrays of In nanowires and measuring the electrical resistance of individual In nanowires of different diameters

## Slide 6: Obtaining a template for electrodeposition
Anodizing conditions and parameters of the resulting pores1:
Electrolyte | Voltage (V) | Temperature (°C) | Pore diameter (nm)
0,3 M H2C2O4 | 40 | 0 | 30
0,1 M H3PO4 | 195 | 0 | 160
Structure of porous film of anodic aluminum oxide (AAO)2:
1Nielsch K. et al.//Nano Lett. 2002. P. 677-680
2Lee W. et al.//Chem. Rev. 2014. V. 114. № 15

## Slide 7: Selection of electrodeposition conditions
Dependence of pore filling (χ) on deposition potential:
CV for smooth electrode without IR compensation:

## Slide 8: Electrodeposition of In nanowires
[In3+] | 0,25 M
[NH2SO3-] | 2,15 M
[Na+] | 2,35 M
[Cl-] | 1,00 M
pH | 1,99
Full composition of indium plating electrolyte:
1 – Cu plate
2 – O-ring
3 – Sample
4 – In counter electrode
4′ – In reference electrode
Electrodeposition cell:
Typical electrodeposition current transient:

## Slide 9: SEM
Lateral cleavage of In/AAO nanocomposite
Nanowires extracted from the template

## Slide 10: XRD of In/AAO
In (2 0 0)
2θ, deg | (h k l) | T (hi)
54,477 | (1 1 2) | 2,17
56,592 | (2 0 0) | 6,83
– reflex intensity for the sample, – reflex intensityfrom literature, n – number of reflexes considered
Harris index calculation:

## Slide 11: Results of resistance measurements of nanowire arrays
Measured section of the circuit:
№ | D (nm) | Part of the sample | R (Ω)
1 | 200 | 1 | 3030 ± 80
2 | 50 | 1 | 668 ± 4
3 | 50 | 1 | 487,7 ± 1,8
4 | 50 | ½ | 421,9 ± 1,2
5 | 40 | 1 | 42,35 ± 0,06
6 | 40 | 1 | 12,47 ± 0,01
7 | 40 | ½ | 56,24 ± 0,08
8 | 40 | ¼ | 101,2 ± 0,1
Slope = 0,01778 ± 0,00003

## Slide 12: Measuring the resistance of single nanowires
R – resistance of the entire array
R0 – resistance of single nanowire
Nb – number of burned nanowires
Nsum – total number of nanowires
= 4560 ± 50 Ω
D (nm) | (Ω) | l (cm) | ρ (µΩcm)
40 ± 3 | 4620 ± 20 | 0,00435 | 13,4 ± 2,0
50 ± 3 | 2550 ± 30 | 0,00440 | 11,4 ± 1,4
200 ± 5 | 155 ± 6 | 0,00525 | 9,3 ± 0,5
D (nm) |  | l (cm) | ρ (µΩcm)
40 ± 3 | 4620 ± 20 | 0,00435 | 13,4 ± 2,0
50 ± 3 | 2550 ± 30 | 0,00440 | 11,4 ± 1,4
200 ± 5 | 155 ± 6 | 0,00525 | 9,3 ± 0,5

## Slide 13: Theoretical calculation of resistance
According to the model Fuchs-Sondheimer*:
*Sondheimer E. H.// Adv. Phys. 1952. V. 1. № 1. P. 1–42
le – mean free path of an electron in a bulk material
d – nanowire diameter
p – specular reflection coefficient
ρ – electrical resistance of nanowire
ρ0 – electrical resistance in a bulk In
le = 57 ± 5 nm
p = 0,5

## Slide 14: Conclusions
Textured In nanowires of different diameters were obtained by electrochemical deposition of metal from a sulfamate-chloride electrolyte into anodic aluminum oxide template
In situ method for measuring the electrical resistance of an array of nanowires has been developed
A method for determining the resistance of a single nanowire has been proposed and developed
The influence of size effects on the value of specific electrical resistance In of nanowires has been shown for the first time

## Slide 15: Additional slides

## Slide 16: Burn-off graphs for nanowires of different diameters
= 2540 Ω
> = 2550 Ω
> = 155 Ω
= 127 Ω

## Slide 17: Calculation by Mayadas-Shatzkes model*
le – mean free path of an electron in a bulk material
d – nanowire diameter
R – reflection coefficient
ρ – electrical resistance of nanowire
ρ0 – electrical resistance in a bulk In
*Mayadas A. F., Shatzkes M.// Phys. Rev. 1970. V. 1. P. 1382
le = 15,0 ± 1,5 nm
R = 0,5