## Slide 1: Photonuclear production of platinum radioisotopes promising for theranostics
A. S. Madumarov, N. V. Aksenov, G. A. Bozhikov
JINR
Association of Young Scientists and Specialists
XXVIII International Scientific Conference of Young Scientists and Specialists (AYSS-2024)
October 28 - November 1, 2024

## Slide 2: Auger Emitters in Medicine
High LET
(about 104-107 Grey/decay/nm3)
Requirements:
-EC/IT decay
-Half life: several hours - days
-Decay into stable or long-lived isotope
-Mild gamma radiation
-Strong bond with a carrier
-Production
Available radionuclides:
67Ga, 111In, 123,125I, 99mTc, 201Tl
Taken from Web site of Department of Nuclear Physics Research School of Physics & Engineering ANU College of Physical & Mathematical Sciences

## Slide 3: Nuclear properties of 195mPt
Theranostics (personalised medicine)
Nuclide | T1/2, d | E, keV | Yield per 100 decays | Decay type | Auger electrons per decay
195mPt | 4.02 | 98.9 | 11.4 | IT | 36.6
 |  | 129.8 | 2.83 |  | 

## Slide 4: Platinum complexes
Carboplatin
Cisplatin
Oxaliplatin
Miboplatin
Pt→*Pt same efficacy, smaller toxic effect!

## Slide 5: 195mPt Production
Reactions | Cross section, <> | Specific activity (SA)
Reactor |  | 
194Pt(n,γ)195mPt | 0.09 | Max SA = 44 MBq/mg Pt
Accelerator |  | 
199Hg(γ,α)195mPt | (Max yield  1.1 GBq) | High SA  370 GBq/mg
197Au(γ,np)195mPt |  210-3 | SA  37 GBq/mg
192Os(α,n)195mPt | 3.710-3 (Max yield: 1 MBq) | No carrier added, high SA
196Pt(γ,n)195mPt 195Pt(γ, γ’)195mPt | (Yield  1 MBq/mg Pt) | Max SA  259 MBq/mg Pt
No method to produce with high specific activity and yield!
Hoeschele,
1982
Dikiy,
2007
Dikiy, 2005
Qaim, 2008

## Slide 6: Photonuclear method
Reactions involved:
192Pt(,n)191Pt
196Pt(,n)195mPt
195Pt(,)195mPt
E, MeV | Radionuclide | Specific activity A, MBq/mg | Yield, kBq/(μАmgh) | Radionuclide ratio [Ym/Yx]
23 | 195mPt | 0.20 | 8.55 | 0.15
 | 191Pt | 1.30 | 57.0 | 
Irradiation parameters:
W = 0.57 kW
Ie = 12 μA
Ee = 23 MeV.

## Slide 7: Found in literature
High specific radioactivities of cobalt, platinum and iridium from photonuclear reactions by Darleane Christian, Don S. Martin, Jr.
December 1951, Ames Laboratory

## Slide 8: Target composition
Target: {cis-[Pt(NH3)2Cl2], KMn8O16}. m(cis-[Pt(NH3)2Cl2]) ≈ 20 mg.
m(cis-[Pt(NH3)2Cl2]):m(KMn8O16) = 1:b, where b = 1, 2, 5, 8, 10.
Szillard-Chalmers technique for specific activity elevation:
1. Cisplatinum – recoil nuclei emitter
2. Cryptomelane K2(Mn4+,Mn2+)8(0,OH)16 (KMn8O16) – recoils acceptor
3. Initial Pt compound and released atoms of Pt* show different chemical properties
Target assembly
Irradiation

## Slide 9: Radioactive platinum separation
Decantation
KMn8O16
10 ml H2O (80-90 С)
10 ml H2O (80-90 С)
cisPt
Dissolution in
1 М HCl + 1.5 % H2O2
Target cisPt+KMn8O16
Evaporation
0.5 ml 0.1 M HCl
Separation
Dowex 50Wx8
Platinum elution

## Slide 10: Isolation of Pt out of cryptomelane
Chart: Eluate, ml
| 0.5 | 1 | 1.5 | 2 | 2.5 | 3 | 3.5 | 4 | 4.5 | 5 | 5.5 | 6 | 6.5 | 7
Pt | 837.8656 | 887.75 | 2249.8154 | 1232.5784 | 182.8765 | 47.6149 | 10.7276 | 0 | 9.1264 | 11.5024 | 16.421 | 0 | 12.3526 | 0
Mn-54 | 0 | 6.6699 | 154.8408 | 419.7105 | 537.5457 | 529.3935 | 413.2876 | 332.0135 | 254.4449 | 200.8385 | 176.3822 | 115.3648 | 65.958 | 49.1597 | 26.4326 | 18.2805 | 9.6343 | 6.1264
0.1 M HCl
3 M HCl
Resin Dowex50Wx8 (200 mesh), H+
h = 4.3 cm
Ø10-11.3 cm

## Slide 11: Ratio impact on yield and SA of 195mPt

## Slide 12: Conclusions
Photonuclear method:
Maximum yield and carrier discard are found for platinum to be 81% and 90% respectively, further improvements of the technique are being explored.

## Slide 13
Thank you for your kind attention!