## Slide 1: Radioactive and stable enriched isotopes for SHE factory: Application as targets and substances in ECR -sources
Aleksandr Bodrov, Aleksei Sabel’nikov, Yurii Albin, Daler Abdusamadzoda, Nikolay Aksenov
FLNR JINR
JINR Association of Young Scientists and Specialists Conference “Alushta-2024”

## Slide 2: Relevance
For synthesis of SHE nuclei it is necessary to produce more massive and low degradable targets from U, Pu, Am, Cm, Bk, Cf
For intensive beams on ECR-source we should have a high pure metal-organic compounds (54Cr - chromocene and 50Ti - titanocene)
Developing of regeneration and separation techniques to renew target and ion-source material

## Slide 3: Target production
―
+
Backing foil
Rubber gasket
PTFE chamber
Cathode
Anode
Clamping screw
thermostat
PTFE cell of different shape
PTFE cell in assembly
Manufacturing conditions
Backing foil – 1,5 μm Ti
Organic solutions– isopropanol/isobutanol
Solutions of Am(NO3)3/ Pu(NO3)4 UO2(NO3)2/Th(NO3)4 are added in isopropanol
Bake backing foil with material for 20 min under 400°C every layer

## Slide 4: Radioactive targets for SHE factory
Target Th-232
d = 700 μg/cm2
Integral 2.4*1019
Target U-238
d = 700 μg/cm2
Integral 2.56*1019
Target Pu-242
d = 700 μg/cm2
Integral 1.62*1019

## Slide 5: Regeneration of target material
Stage 1
Dissolution of Cm targets in mix of HNO3 + HF or HNO3 (conc) under IR-lamp.
Stage 2
Loading of Cm solution on anion-exchange column in mix 10М HNO3 and CH3OH (volume ratio - 1:10)
Stage 3
Elution of mix 1М HNO3 and CH3OH for purification from Ce, Fe, alkaline and alkaline-earth elements
Collection of Cm fraction in 1M HNO3
Test segment of 245Cm target
242Pu on the column
Regeneration of actinides is significant stage for manufacturing targets: pure material – satisfactory morphology of layer surface!

## Slide 6: Method MIVOC (Metal Ions from Volatile compounds)
[1] Metal ion beams from an ECR ion source using volatile compounds, Nucl instr. Meth. B. V. 94. 1994,P.P. 291-296,
https://doi.org/10.1016/0168-583X(94)95368-6.
This method was developed to vaporize non-volatile metals. For example Ni (nickelocene) and Fe (ferrocene) in Finland [1].
Principle of method is difference of pressure when pressure of volatile compound increases under normal temperature and low pressure.
Ionized in plasma chamber and accelerate.

## Slide 7: Synthesis of Chromocene
Chromium chloride 54CrCl3
Cp254Cr
Yield of the 1st stage – maximum 80%
Yield of the 2nd stage – maximum 50%
All stage yield is – 40%,
excluding regeneration on the 2nd stage

## Slide 8: Synthesis of Сp*TiМе3
trimethyl(pentamethyl-cyclopentadienyl) titanium | Yellow cristals | Neutral compound with chemical formula (C5Me5)2TiMe3 sublimed in vacuum, soluble in benzene and THF. Thermally unstable, very sensitive to light, oxygen and air moisture.

## Slide 9: Data about 54Cr and 50Ti
The consumption in a stable mode is 70 mg / day according to the chromocene.
The maximum beam current of 54Cr according to the source sector is 25 µA at the output from the accelerator and 50Ti – the maximum current is 17 µA for DC-280.
On domestic Cp254Cr chromocene, SHE Factory worked 96 days for the reactions 238U(54Cr, 4n)288Lv and 238U(54Cr, 3n)289Lv and U-400 worked 21 days for the reaction of 208Pb(54Cr, 4n)258Sg
Two events were obtained for the reaction of 242Pu(50Ti, 4n)288Lv

## Slide 10: Conclusions
Techniques have been developed for the synthesis of organometallic compounds of titanium and chromium to produce ion beams of 50Ti and 54Cr from an ECR source for synthesis of SHE nuclei.
A technique for radiochemical regeneration from irradiated curium targets has been developed and Th, U, and Pu targets have been assembled for experiments on the SHE synthesis.
The first data on the condition of targets after prolonged irradiation were obtained (integral up to 3*1019)

## Slide 11
Thank you for kind attention!