## Slide 1: Development of FARICH detector for the SPD experiment: status and prospects
A.Yu.Barnyakov on behalf of PID group
SPD Collaboration Meeting
20-24 May 2024, KBTU, Almaty, Kazkhstan

## Slide 2: PID system: requirements
The main task of SPD PID system is
π/K-separation up to P=5÷6 GeV/c
For reliable π/K-separation at P=6 GeV/c the RICH detector is required:
– (aerogel),
–

## Slide 3: FARICH motivation
~
~
T.Iijima et al., NIM A548 (2005) 383 and A.Yu.Barnyakov et al., NIM A553 (2005) 70
Thicknesses and refractive indexes in each layer are adjusted in such way that Cherenkov rings from each layer overlap in the same region of the position-sensitive photon detector.
The number of detected Cherenkov photons increases due to increase of the thickness without degradation of Cherenkov angle resolution due to uncertainties of photon emission point.
To get from aerogel with n=1.05 & thickness 1 cm is too hard practice task!!!

## Slide 4
GEM
MaPMT H12700 (Hamamatsu)
with mask 3х3 mm2
2 aerogel pcs
230x230x35 mm
The largest 4-layer focusing aerogel samples were produced in Novosibirsk and tested at BINP in 2022-2023
Refractive index profile is measured with help of digital X-ray setup at the BINP.
Single photon Cherenkov angle resolution is investigated with relativistic electrons at BINP beam test facilities ”Extracted beams of VEPP-4M complex”.
• Pixel 3x3 mm
• Geom.Eff. ~ 20%
•

## Slide 5: TBeam 2023 res.:
04/23: L≈200 mm
Geom.Eff. ~ 80%
12/23: L≈180 mm
Geom.Eff. ~ 56%
12/23: L≈180 mm
Geom.Eff. ~ 36%
04/23: L≈200 mm
Geom.Eff. ~ 20%
12/23: L≈180 mm
Geom.Eff. ~ 9%
12/23: L≈180 mm
Geom.Eff. ~ 2%
: – 5.5 GeV/c 6 GeV/c 6.5 GeV/c 8.0 GeV/c
µ: – 1.2 GeV/c 1.4 GeV/c 1.5 GeV/c 1.6 GeV/c
No mask:
3 mm
mrad

## Slide 6: FARICH system conceptual design
Aerogel:
74 tiles
Photon detector: 548 PMT 51х51 mm
FARICH system:
• 4-layer aerogel with nmax=1.05 (or less)
• Focus distance – 20 cm
• PS PD – MCP-PMT or SiPM arrays with pixel 3÷6 mm
550 PMTs per endcap if lateral sizes ~51x51 mm
2200 PMTs per endcap if lateral sizes ~27х27 mm

## Slide 7: Simulation FARICH in SPD
Reconstruction: fit analytical formula to (θc,φc) distribution to obtain β
particles momentum 6 GeV/c
MC
RD
Nucl. Instrum. Meth. A, 732:352–356, 2013

## Slide 8: FARICH prototype with full ring detection
970 мм
420 мм
340 мм
• Tunable focal distance from 5 to 60 cm
• Aerogel tiles with lateral dimensions up to 200x200 mm2
• 2 DiRICH boards (GSI) to readout up to 12 multi-anode PMTS with 768 pixels in total – option #1
• 6 DiRICH boards (GSI) to readout up to 36 multi-anode PMTS with 2304 pixels in total –option #2

## Slide 9: FARICH prototypes
Step #1 (2024/25): 6x6mm
Step #2 (2025/26): 3x3mm
• 6x6=36 MCP PMTs from Ekran FEP
• 3x3mm pixel
•
• 6 DiRICH boards (GSI) to readout 2304 chan.
53 mm
51 mm
51 mm
46 mm
N6021 (NNVT)
H12700
(Hamamatsu)
XP8122
Planacon
154 mm
• 4 MCP PMTs N6021 from NNVT
• 4 MaPMTs H12700 from Hamamtsu
• 1 XP85122 Planacon MCP PMT from from Photonis
•
• 2 DiRICH boards (GSI) to readout chan.
N6021 (NNVT)
Ekran FEP

## Slide 10: MCP PMT rectangular shape from Ekran FEP
Multi-alkali PCs sputtered on ordinary glass
It is planed to use UV-glass to enhence PDE in blue region
Ceramic components from China (NNVT) deliverd to Ekran FEP
Ekran FEP also works with vendors from Saratov to produce ceramic components inside the Russia
Ekran FEP design of MCP PMT with 8x8 3x3 mm pixels
MCPs: • For the first rectangular PMTs usage of MCPs made by Ekran FEP is planed
• For the first serial batch implementation of MCPs from VTC Baspik is planed
• Until the Autumn the first Russian rectangular-shape multi-anode MCP PMTs partially based on Chinese components are expected
• Until the end of year MCP PMTs totally based on Russian components are expected

## Slide 11: On aerogel optimization for the SPD project
4-layer aerogel with and thickness was optimized for SCTF to provide reliable separation at
For SPD aerogel lower index looks more suitable to provide and separation at higher momenta. Lower means:
  Larger difference in π– and K–mesons Cherenkov angles;
  lower impact from dispersion;
  but lower number of Cherenkov photons which could be compensted by increase of aerogel thickness especially if the pixel size is about .
More optimal aerogel for SPD looks like:
> Maximal refractive index
> Aerogel thikness is about
> 3 or 4 number of layers with 15 or 10 mm thick each
There is a room for optimization with help of simulation or even ML approaches
There is a room for optimization with help of simulation or even ML approaches
R&Ds on production of optimal SPD aerogel and test its performances are required.

## Slide 12: Summary & Plans for 2024/2025
We are going (and almost ready) to prepare and carry out tests with FARICH prototype based on available components at hadron beams to demonstrate its current PID capabilities:
  • 4-layer aerogel tiles with nmax=1.05 and t=35mm (optimized for SCTF project)
  • Multi-anode PMTs (from Hamamatsu, NNVT, Photonis) with pixels
  • DiRICH (GSI) based readout system
Optimize (with help of simulation) and produce first aerogel tiles for the SPD experiment requirements (nmax=1.04 and t=40mm)
Test and compare performances of position-sensetive MCP PMTs with rectangular shapes:
  • N6021 from NNVT (China) – pixels
  • For the first time produced in Russia from Ekran FEP – pixels
Start developmant of FARICH prototype based on Russian position-sensetive MCP PMTs

## Slide 13: BACK UP SLIDES

## Slide 14: FARICH technique milestones
T.Iijima et al., NIM A548 (2005) 383 and A.Yu.Barnyakov et al., NIM A553 (2005) 70
n=1.030 6.0mm
n=1.027 6.3mm
n=1.024 6.7mm
n=1.022 7.0mm
The first 4-layer monolithic sample
Increase Npe due thickness increase without σΘc degradation
2004÷2005
Excellent PID capability were shown at CERN beam test in 2012
A.Yu. Barnyakov, et al., NIM A 732 (2013) 352
The Belle II (ARICH) is the first application of the method
2017
Two 4-layer focusing aerogel blocks
230x230x35 mm
2022÷2023
Notes: Идея ФАРИЧ появилась в 2004 г.
Точность измерения черенковского угла связана с точностью измерения скорости, а значит с качеством разделения частиц.

## Slide 15
Recent beam test results
Pixel 6x6 mm
Geom.Eff. ~ 80%
Pixel 3x3 mm
Geom.Eff. ~ 20%
Main results:
• Npe 16 (~ 0.8 of Ring)
• ( 6mm)
• ( 3mm)

## Slide 16: Cherenkov angle Single Photo-Electron (SPE) resolution
Aerogel: 20+20 mm (Chiba Univ.)
n(400nm): 1.045 +1.055
Pixel: 5x5 mm
4-layers (Novosibirsk) –>
1.039 ÷ 1.046
6x6 mm
–
–
3x3 mm
4-layers (ideal profile)
1.041 ÷ 1.050
3x3 mm
PTEP 2016, 033H01
Belle II
Simulation
TBeam
Geom.Eff. ~ 80%
Geom.Eff. ~ 20%
Beam test results are in good agreement with MC simulation and corresponds to:
π/K–separation at level of up to P=4.5 GeV/c for 6x6 mm pixel
π/K–separation at level of up to P=8.5 GeV/c for 3x3 mm pixel
Geom.Eff. ~ 90%
Dimensions of focusing aerogels 23x23x3.5 cm allow us to design the full-scale FARICH systems for the future particle physics experiments.

## Slide 17: FARICH based on existing solutions
MCP PMT available from vendors:
2x548 PMTs:
• 2x35kPixels
• Pixel ~6x6 mm
Existing FEE aka DiRICH (GSI):
• 1 DiRICH board per each 6 PMTs
• 2x100 DiRICHs per 2 end-caps
• 2x100 optical links to DAQ sys.
• 10÷20 TRB3 interfaces
Expected performance:
• π/K–separation up to 5 GeV/c
• µ/π–separation up to 1.1 GeV/c
• K/p–separation from 3 to 9 GeV/c
59 mm
Planacon XP85112 (USA)
8x8 pixels with 6x6 mm
NNVT N6021 (China)
8x8 pixels with 5.9x5.9 mm
51 mm

## Slide 18: FARICH based on 3x3mm pixels
Suitable PDs with 3x3mm pixels
2x2600 PMTs:
• 2x166.4kPixels
• Pixel 3x3 mm
Specialazed FEE is required!!!
• FaRICH-Auslese-System (GSI) – design inspired by DiRICH approach to readout of SiPM arrays or MCP PMTs with 3x3mm pixels?!
• ASICs developed at BINP for SR detector to readout Hybrid Photo Detectors?!
Expected performance:
• π/K–separation up to 8.5 GeV/c
• µ/π–separation up to 1.7 GeV/c
• K/p–separation from 3 to 14 GeV/c
27 mm
SiPM arrays, Joinbon (China)
64 3x3mm pixels, PDE~40%
DCR ~1÷2•106cps/ch.@300°K
MCP PMT, Ekran FEP (RU)
64 2.5x2.5mm pixels
Still under R&D

## Slide 19: Momentum measurements with FARICH
where – particle mass, – particle momentum, – refractive index of aerogel, and are single photon Cherenkov angle resolution and number of detected photons per track correspondingly measured with relativistic electron beams.