## Slide 1: Determination of the natural frequencies of ultralight sensor support trusses of silicon tracking systems
Maribel Herrera for et al.(*)
Scientific-Methodological Seminar, LHEP, JINR, Dubna, Russia.
April 25th, 2024
(*) Ligdenova T. (JINR), Ceballos C. (JINR), Dementev D. (JINR), Igolkin S. (SPbSU), Zherebchevsky V. (SPbSU)

## Slide 2
Intro
“Igolking” ultralight supporting trusses: High-Young’s-modulus carbon threads laminated together in epoxies.
From SPbSU to tracking systems @ ALICE-ITS2 (CERN), sPhenix (BNL), CBM (FAIR), MPD-ITS (JINR), SPD (JINR), BM@N (JINR)
Usually placed in the zone of highest radiation levels
(Polymerization of the carbon fibers joins together thousands of individual carbon threads. )
What will happen in the long-run (~10 years) to the supporting trusses of a tracker in high luminosity experiments?
Degradation of the mechanical properties causing:
Systematic displacement of the atteched sensors
Apperance of resonance vibrations of the trusses

## Slide 3
The experiment: Joining the IBR-2 User Club
Evaluation Criteria: Decrease of the value of the natural frequency of the structure (fn) after irradiation.
What to do?: Determine fn before and after irradiation.
How to?: This work
High Dose Irradiation

## Slide 4
The acoustic experiment
1- Truss under test
2- Truss vibration exciter of variable frequency
3- Vortex sensor probe
4- Driver for connecting the probe to a PC
5- Electric conductive plate
For determining fn :
The exciter’s frequency was varied from 30 Hz to 300 Hz.
At each step the variation of the gap between the vortex sensor and the conductive plate was recorded (S/R 1 kHz).
The obtained signal was converted into a frequency spectrum by means of the Fourier Transform.
The amplitude of the oscillation was determined as a standard deviation of the measured gap values for the recorded time period.
The same process was repeated each frequency step [f-step 30 – 300 / 10Hz, then 1Hz around the peak].
  All oscillation amplitudes were plotted as the function of the exciter’s frequency.
  The natural frequency of the truss (fn) was determined from the resulting peak.
FT
fn = 77 ± 0.55 Hz

## Slide 5
The counter check: Simulations
Material definition?
Idea: To model the truss in ANSYS and calculate the resulting natural frequency (fn).
Required input data:
Geometrical characteristics ✓
Density ✓
Exact material definition X
  Impregnated fiber M55J for the ribs of the frame.
  Prepreg consisting of M55J for the longitudinal beams.
  Not possible to determine the exact characteristics of the carbon fiber-resin composite.
  Datasheet contains information only about the Modulus of Elasticity (ME) in one direction.
ANSYS
Real truss
Idea+: To model the structure as an isotropic material based on M55J that behaves mechanically as the real one.
Required input data:
Geometrical characteristics ✓
Density ✓
Aproximate material definition ✓
Modulus of Elasticity X

## Slide 6
The counter check: Searching for the ME
Total = 30
Sagging measurements from the producer are available
Trusses datasheet
(mL); mL = {50 g; 100 g; 150 g; 200 g}
Experimental data
= Fexp
Notes: sim

## Slide 7
The counter check: Searching for the ME
Total = 30
Sagging measurements from the producer are available
Trusses datasheet
Experimental data
ANSYS model for mL= 200 g
= Fexp
Isotropic M55J
Variable ME
The ME was varied until (200 g) - (200 g) | = min
(mL); mL = {50 g; 100 g; 150 g; 200 g}
Notes: sim

## Slide 8
The counter check: Searching for the ME
Total = 30
Sagging measurements from the producer are available
Trusses datasheet
Experimental data
ANSYS model for mL= 200 g
= Fexp
Isotropic M55J
Variable ME
The ME was varied until (200 g) - (200 g) | = min
= Fsim
(mL); mL = {50 g; 100 g; 150 g; 200 g}
Notes: sim

## Slide 9
The counter check: Searching for the ME
Experimental data
= Fexp
The ME was varied until (200 g) - (200 g) | = min
= Fsim
Load mass (gr) | 50 | 100 | 150 | 200
Deflection (mm) | 0.07±0.01 | 0.12±0.01 | 0.18±0.02 | 0.24±0.01
Isotropic M55J
Variable ME
Average over 30 samples
System approximation
ANSYS model for mL= 200 g
: Deformation of the truss
g : Gravitational acceleration
mt: Mass of the truss
fn : Natural frequency of the loaded truss
mL: Mass load
(mL); mL = {50 g; 100 g; 150 g; 200 g}
Notes: sim

## Slide 10
The counter check: Searching for the ME
Experimental data
= 74.41 Hz
The ME was varied until (200 g) - (200 g) | = min
= Fsim
Load mass (gr) | 50 | 100 | 150 | 200
Deflection (mm) | 0.07±0.01 | 0.12±0.01 | 0.18±0.02 | 0.24±0.01
Isotropic M55J
Variable ME
Average over 30 samples
System approximation
ANSYS model for mL= 200 g
(mL); mL = {50 g; 100 g; 150 g; 200 g}
: Deformation of the truss
g : Gravitational acceleration
mt: Mass of the truss
fn : Natural frequency of the loaded truss
mL: Mass load
Notes: sim

## Slide 11
The counter check: Searching for the ME
Experimental data
= 74.41 Hz
The ME was varied until (200 g) - (200 g) | = min
= 73.7 Hz
Load mass (gr) | 50 | 100 | 150 | 200
Deflection (mm) | 0.07±0.01 | 0.12±0.01 | 0.18±0.02 | 0.24±0.01
Isotropic M55J
Variable ME
Average over 30 samples
System approximation
ME (GPa) | Deflection (mm) | fn (Hz)
300.0 | 0.099 | 115.14
135.0 | 0.219 | 77.244
133.0 | 0.229 | 76.654
128.9 | 0.239 | 73.669
100.0 | 0.293 | 66.475
ANSYS model for mL= 200 g
ME = 128.9 GPa
~ 0.9%
(mL); mL = {50 g; 100 g; 150 g; 200 g}
: Deformation of the truss
g : Gravitational acceleration
mt: Mass of the truss
fn : Natural frequency of the loaded truss
mL: Mass load
Notes: sim

## Slide 12
The counter check: Simulations
Isotropic M55J
ME = 128.9 GPa
ANSYS
Real truss
Idea+: To model the structure as an isotropic material based on M55J that behaves mechanically as the real one.
Required input data:
Geometrical characteristics ✓
Density ✓
Aproximate material definition ✓
Modulus of Elasticity ✓
= 77.0±0.55 Hz

## Slide 13
The counter check: Simulations
Isotropic M55J
ME = 128.9 GPa
ANSYS
Real truss
Idea+: To model the structure as an isotropic material based on M55J that behaves mechanically as the real one.
Required input data:
Geometrical characteristics ✓
Density ✓
Aproximate material definition ✓
Modulus of Elasticity ✓
= 77.0±0.55 Hz
= 78.9±1.21 Hz
~ 2.5%

## Slide 14
Conclusions
- An acoustic-based experimental setup for measuring the natural frequency of the ultra-light mechanical structures used as support of the tracking sensors in large experimental setups like NICA’s MPD experiment has been assessed.
- A model of the truss was implemented in ANSYS by approximating its composition to an isotropic material with equivalent mechanical characteristics as the real trusses.
- The natural frequency values obtained from the experiment and from the simulations are in good agreement both for loaded and unloaded trusses.

## Slide 15
To be published in
Creative Commons Attribution-NonCommercial-NoDerivatives 4.0 International License.
ISSN 0035-001X
Impact Factor = 1.7
Official invitation for publishing

## Slide 16
Thank you!

## Slide 17
Backup

## Slide 18
The counter check: Simulations
Isotropic M55J
ME = 128.9 GPa
ANSYS
Real truss
Idea+: To model the structure as an isotropic material based on M55J that behaves mechanically as the real one.
Required input data:
Geometrical characteristics ✓
Density ✓
Aproximate material definition ✓
Modulus of Elasticity ✓