## Slide 1
13 June 2024, Dubna, Russia
Tellurium-Loaded Organic Scintillators
to Search for
Neutrinoless Double Beta Decay
I. Suslov, I. Nemchenok, A. Klimenko, A. Bystryakov, I. Kamnev
59th Meeting of the PAC for Particle Physics

## Slide 2
Neutrinoless double β-decay
2
Observation of 0vββ-decay would imply:
lepton number violation;
presence of the Majorana term for neutrino mass;
сonstraints on neutrino mass hierarchy and scale;
hints at origin of matter/antimatter asymmetry.
1. Šimkovic F., et al., Physical Review C 77.4 (2008): 045503.
2. Meija J., et al., Pure and Applied Chemistry 88.3 (2016): 293-306.

## Slide 3
3
Experiments searching for 0νββ
Fundamental parameters drive the sensitive background and exposure and consequently the sensitivity of recent and future phases of existing experiments [3]
3. Agostini M., et al., Rev. Mod. Phys. 95, 025002

## Slide 4
4
Element/isotope, concentration | Scintillation base | Element-containing additive | Light yield6
Nd, up to 6.5 g/l | PC1 | 2-Methylvalerate | 80%
150Nd, up to 20 g/l up to 2 g/l | PC1 PC1 | Tris(trimethylhexanoate) Complexes with fluorinated β-diketonates | 90% 62%
Nd, 0.32% | LAB2 | 4-Methyloctanoate | 64%
Nd, 1 – 3% | PMMA3 | Complex of Nd(NO3)3 with HMPA5 | 58 – 25%
Mo, 0.027 – 0.43% | Toluene | Nanoparticles of AMoO4 (A= Ca, Sr, Ba) | –
Sn, 32.6%, | PC | Tetramethyltin | 57%
Sn, 0.5 – 10% | LAB | Tetrabutyltin | 96% – 55%
Sn, 3 – 15% | Polystyrene | Tetraphenyltin, tributyltin methacrylate | 83 – 37%
Cd, 1.5% | LAB + TBP4 | Chloride | 47%
Cd, 0.5 – 2% | PMMA | Complex of CdCl2 with HMPA | 84 – 67%
Zr, 1.4% | Anisole | Tetrakisisopropylacetoacetate | 30 – 40%
Zr, up to 2.5 g/l | PC1 | Dipivaloylmethanate | 63%
Zr, 0.33% | Toluene | Nanoparticles of ZrO2 | -
136Xe, ≤ 3% | Decane + PC1 | Gaseous 136Хе | -
Te, 0.5% | LAB | Complex of telluric acid with butanediol hexanediol | 71% 67%
1 Pseudocumene; 2Linear alkylbenzene; 3Polymethylmethacrylate; 4Tributylphosphate;
5Hexamethylphosporoamide; 6 Relative to unloaded scintillator
Element-loaded organic scintillators in 0νββ search

## Slide 5
5
Why tellurium?
Recent estimations show that almost the only available technique for future mega-projects to search for 0𝜈𝛽𝛽-decay with sources of several hundred tons and more is using liquid scintillators loaded with natural tellurium [4].
High natural abundance (34%) allows using natural tellurium in experiments without expensive enrichment.
The longest half-life of ordinary SM-allowed double beta decay (T1∕2 2𝜈𝛽𝛽 = 8.2 × 1020) among all 𝛽𝛽-candidates minimizes an unavoidable background contribution from the 2𝜈𝛽𝛽 mode in the ROI of 0𝜈𝛽𝛽-decay.
4. Biller S.D. // Physical Review D - 2013. Vol. 87, № 7. P. 071301.

## Slide 6
Scintillation base:
high boiling point;
explosion and fire safety, high flash point;
non-toxicity;
low corrosive activity in relation to the materials of the detector;
availability and low cost.
Linear alkylbenzene [5 – 8]:
Polystyrene [9, 10]:
5. V. Albanese, et al., JINST. 16 (2021) P08059.
6. W. Beriguete, et al., NIMA. 763 (2014) 82–88
7. C. Buck, et al., JINST. 14 (2019) P01027–P01027.
8. S.J. Haselschwardt, et al., NIMA. 937 (2019) 148–163.
9. Alekseev I. et al., NIMA. (2016) Т. 11, № 11, С. P11011.
10. Arnold R. et al., NIMA. (2005) Т. 536, № 1-2, С. 79-122.
Composition of TeOS. Scintillation base
6
Diisopropylnapthalene [7]:

## Slide 7
Requirements for tellurium-containing additives:
solubility in scintillation base;
absence of absorption bands in the visible region of the spectrum;
stability to hydrolysis, atmospheric oxygen and other environmental factors;
compatibility of different detector materials;
feasibility of large-scale production;
non-toxicity, explosion and fire safety.
Composition of TeOS. Tellurium-containing additives
R = -CH(C2H5)(CH2)3CH3
(c) Te(But)2
(b) Complex
(a) Hexanoate
7

## Slide 8
Scintillation characteristics.
Comparison with other TeLS
1Relative to unloaded LS
2 Tellurium in form of complex telluric acid with hexanediol-1,2 and N,N-dimethyldodecylamine
3 Tellurium in form of complex telluric acid with butanediol-1,2 and N,N-dimethyldodecylamine
TeLS sample | Scintillation composition | Light yield1, rel. units
Hexanote [11] | 0.5% Te, 1% PPO, 0.04%POPOP, 30% DIPN | 0.72±0,03
 | 1% Te, 2% PPO, 0.04%POPOP, 30% DIPN | 0.58±0,03
Complex [12] | 0,5% Te, 0.5% PPO, 0.0025%POPOP | 0.73±0,04
 | 1% Te, 0.5% PPO, 0.0025% POPOP, 30% DIPN | 0.71±0,03
Te(But)2 | 0,5% Te, 0.5% PPO, 0.0025% POPOP, 1% octylamine | 0.63±0,03
 | 1% Te, 1.5% PPO, 0.0025% POPOP, 2% octylamine | 0.54±0,03
IHEP CAS2 [13] | 0.6% Te, 2,5 g/l PPO, 3 mg/l bis-MSB | ~0,65
SNO+3 [14] | 1% Te, 6 g/l PPO | ~0,65
11. I. Suslov, et al., NIMA 1040 (2022): 167131.
12. I. Suslov, et al., PEPAN Letters, 250 (2023): 1187-1190
13. Ding Ya-Yun, et al., NIMA 1049 (2023): 168111.
14. Auty, D. J., et al., NIMA 1051 (2023): 168204.

## Slide 9
Scintillation characteristics.
Stability of TeLS
Stability of the light yield (a) and the transparency (b) for TeLS samples with a 1%-Te content of different tellurium-containing additives
9
(b)
(a)

## Slide 10
TePS with complex of diphenyltellurium oxide and D2EHPA.
Scintillation characteristics
Light yield as a function of tellurium concentration (relative unloaded plastic scintillator) and transparency at λ=430 nm (optical path – 1 cm, relative to air) of TePS with complex and constant concentration PPO, POPOP (1.5%, 0.015%, respectively)
Te, % | Tλ=430 нм ±1, %
0 | 87.5
0.1 | 81.3
0.25 | 79.6
0.5 | 79.2
0.75 | 79.3
1.0 | 75.9
1.25 | 75.9
1.5 | 73.5
10
Tellurium concentration, %
0
0,1
0,25
0,5
0,75
1
1,25
1,5

## Slide 11
11
Conclusion
— For the first time, diphenyltellurium dicarboxylates, a complex compound of diphenyltellurium oxide with di-(2-ethylhexyl)phosphoric acid and tellurium dibutanediol-1,2-ate have been proposed for the use as tellurium-containing additives.
— A series of new TeLSs with a tellurium concentration of up to 3% has been developed, with good scintillation and optical properties.
— A several-month-lasting stability of liquid scintillator properties has been proven.
— For the first time in the world, plastic tellurium-loaded scintillators have been obtained. Scintillation and optical properties of the materials developed allow us to recommend them for the use in large-scale detectors to search for neutrinoless double β-decay.

## Slide 12
Backup
12

## Slide 13
Block diagram of the installation for measuring the LS light yield and energy resolution: 1 – light-tight box; 2 – radioactive source; 3 – cell with LS; 4 – PMT; 5 – high-voltage source; 6 – preamplifier; 7 – amplifier; 8 – signal converter
Measurement technique
Light yield:
UV-VIS spectra: UNICO UV 2804 in a 10-cm cuvette relative to air at a wavelength of 390 to 600 nm.
Tellurium-containing additives: UV-VIS, IR, Raman spectroscopy, elemental analysis (C, H, Te), Differential Scanning Calorimetry (melting point), ICP-AES (MS) (in plans)
13
Experimental conditions:
Teflon cuvette with uviol glass;
volume – 40 ml, height – 2 cm;
207Bi;
subtractive measurement method.

## Slide 14
Scintillation characteristics.
Absolute light yield
1di-2-ethylhexanoate diphenyltellurium
2LS based on diisopropylnapthalene with light yield of 12.300 photons/ 1 MeV e-
LS sample | Scintillation composition | Absolute LY, photons/MeV | Evaluation method
unloaded LS | 0.5% PPO, 0.0025%POPOP | 8646±400 | Relative to EJ-3092
TeLS | 0.5% Te1, 1% PPO, 0.04% POPOP, 30% DIPN | 6399±320 | Relative to EJ-309
TeLS | 1% Te1, 2% PPO, 0.04% POPOP, 30% DIPN | 5128±256 | Relative to EJ-309
RENO | 0.3% PPO, 0.0030% bis-MSB | ~8000 | Relative to anthracene
Daya Bay | 0.3% PPO, 0.0015% bis-MSB | 8700 | Relative to anthracene
Stereo | 0.3% PPO, 0.0020% bis-MSB | 8400 | Quantum efficiency of PMT
14

## Slide 15
Synthesis of tellurium-containing additives
15