## Slide 1: Recent progress of aerogel Cherenkov radiators production in Novosibirsk
Aleksandr A. Kattsina (A.A.Kattsin@inp.nsk.su)
A.Yu. Barnyakova, E.A. Kravchenkoa, A.F. Danilyukb, A.Yu. Predeinb.
aBudker Institute of Nuclear Physics of SB RAS
bBoreskov Institute of Catalysis SB RAS

## Slide 2: Silica aerogel
Silica aerogel - porous material with pore dimension less than visible light wavelength. 3D network of SiO2 nanometer sized pellets and 50-100 nm pores.
Aerogel is a light, fragile material with strong Rayleigh scattering of light which easily absorb gases and vapours.
SiO2
50-60 nm
Hole diameter
Particle diameter
2-3 nm
quartz
Lightest solids. Close the nature’s gap in refractive index between gases (n-1≲10-3) and liquids/solids (n≳1.3).

## Slide 3: Aerogel primary annealing protocol
In 2023, the procedure for primary annealing aerogel in an air atmosphere was changed so that the blocks would not crack. The process of heating to the organic burnout temperature (approximately 170 ℃) has become smoother (taking longer), and the aerogel annealing stage is also included in this cycle without raising the temperature for several hours at 170 ℃, so that the organic matter contained in the aerogel burns out without destroying the source block.
aerogel mass lost
Up to about 120 ℃, the annealing process involves heat absorption (desorption of water and organic matter).
Starting from 170 ℃, heat generation begins to increase and mass decreases – organic matter burns out.
Heat release at 417 ℃ is presumably the afterburning of organic matter.
heat flow
Thermogravimetric and differential scanning calorimetry analysis
derivative mass
After changing
the primary annealing procedure, its efficiency was almost 100%: 100% of the large aerogel blocks do not crack.

## Slide 4: Focusing Aerogel RICH - FARICH
n=1,030 6,0 мм
n=1,027 6,3 мм
n=1,024 6,7 мм
n=1,022 7,0 мм
first four-layer monolithic sample
2004
19 years of R&Ds
n=1,046 8,5 mm
n=1,043 8,5 mm
n=1,040 9,0 mm
n=1,039 9,0 mm
230 mm
230 mm
2023
50 mm
50 mm
The four-layer focusing aerogel sample with 230x230x35 mm size and with correct parameters for refractive index and transparency.
Refractive index profile is measured by means of X-ray setup at the BINP
Photon Detector
Cherenkov light
Thicknesses and refractive indexes in each layer are adjusted in such way that Cherenkov rings from each layer overlap in the same region of the position-sensitive photon detector.
The number of detected Cherenkov photons increases due to increase of the thickness without degradation of Cherenkov angle resolution due to uncertainties of photon emission point.
first four-layer monolithic sample
T.Iijima et al., NIM A548 (2005) 383 and A.Yu.Barnyakov et al., NIM A553 (2005) 70
35 mm

## Slide 5: Aerogel optimization for 66 mm pixels according SPD FARICH concept and status of production
four-layer aerogel with nmax=1.04 and ttot=40 mm
• PDE for H12700 and pixel 66 mm
• Npe≈34
• mrad
• π/K–separation at 6 GeV/c –
• “New4”
• Material budget ~ 2.7%X0
three-layer aerogel with nmax=1.04 and ttot=40 mm
• PDE for H12700 and pixel 66 mm
• Npe≈35
• mrad
• π/K–separation at 6 GeV/c –
• “New3”
• Material budget ~ 2.7%X0
at 6 GeV/c –
for all aerogel tiles
at 6 GeV/c –
Material budget ~ 2.7%X0
for all aerogel tiles

## Slide 6: Thick aerogel radiator made of large single-layer tiles for threshold counters or for focusing with lenses
Considered as an option!
New samples of transparent thick large single-layer tiles aerogel radiators were manufactured in Novosibirsk for ASHIPH prototype.
Cutting of aerogel
n=1.027

## Slide 7: Thick aerogel radiator made of large single-layer tiles for threshold counters or for focusing with lenses
Photon Detector
Fresnel Lens
BINP sim
May 2025
240 mm
240 mm
40 mm
n=1.03
Aerogel RICH with Fresnel Lens: Ring image is shifted toward the central region on the photon detector
BINP test beam hitmap
BINP test beam (pixel 66 mm):8 mrad for track
can expect π/K–separation at 5 GeV/c –

## Slide 8: Ultralight aerogel
R&D on aerogel with n=1.008 is carrying out for high-momenta separation:
n=1.0036
50 mm
50 mm
22 mm
22 mm
50 mm
May 2025
produced
Aerogel
2005
2025
FARICH based: aerogel n1=1.0068 (20 mm) +
aerogel n2=1.008 (20 mm)
  pixel 66 mm: π/K–separation at 10 GeV/c;
𝜇/π–separation at 2 GeV/c.
  pixel 33 mm: π/K–separation at 13 GeV/c;
𝜇/π–separation at 2.6 GeV/c.
can think about
50 mm

## Slide 9: Summary
The primary annealing procedure was changed. Its efficiency is almost 100%. 100% of the large thick aerogel blocks remain intact.
Refractive index of multilayer focusing aerogel Cherenkov radiators were optimized for pixel 6×6 mm.
In Novosibirsk three-layer and four-layer aerogel optimized for pixel 6×6 mm was produced in 2025.
Large and highly transparent aerogel tiles with n=1.03 (230x230x40 & 50mm size) were produced for ASHIPH prototype options.
Ultralight aerogels (nmax=1.008) were produced for R&D on high-momenta separation () by FARICH method.

## Slide 10: FARICH motivation
~
~
T. Iijima et al., NIM A548 (2005) 383 and A.Yu. Barnyakov et al., NIM A553 (2005) 70
Thicknesses and refractive indexes in each layer are adjusted in such way that Cherenkov rings from each layer overlap in the same region of the position-sensitive photon detector.
The number of detected Cherenkov photons increases due to increase of the thickness without degradation of Cherenkov angle resolution due to uncertainties of photon emission point.
To get from aerogel with n=1.05 & thickness 1 cm is too hard practice task!!!

## Slide 11
Pixel 6x6 mm
Geom.Eff. ~ 80%
Pixel 3x3 mm
Geom.Eff. ~ 20%
Main results:
• Npe 16 (~ 0.8 of Ring)
• ( 6mm)
• ( 3mm)
Focusing Aerogel RICH beam test results

## Slide 12: History of aerogel radiators in Novosibirsk
SND ASHIPH system (VEPP-2000 – BINP):
  𝜋/K-separation in the momentum range 300÷870 MeV/с.
  Aerogel (V~9 L).
KEDR ASHIPH system (VEPP-4М – BINP):
  𝜋/K-separation in the momentum range 0,6÷1,5 GeV/с.
  Aerogel (V~1000 L).
DIRAC-II (PS – CERN):
  𝜋/K-separation in the momentum range 5,5÷8,0 GeV/с.
  Aerogel (V~9 L).
LHCb aerogel RICH (LHC – CERN):
  𝜋/K-separation in the momentum range 5,5÷8,0 GeV/с.
  Aerogel (S~0,5 m2), aerogel tile 20х20х5 см3.
CLAS-12 aerogel RICH (J-Lab):
  𝜋/K- & K/p-separation at level 4𝜎 with several momentum GeV/с.
  Aerogel (S~6 m2), aerogel tile 20х20х2-3 см3.
AMS-02 aerogel RICH (ISS):
  Search for antimatter, study of cosmic rays.
  Aerogel (S~1 m2).
Aerogel RICH for CLAS12
The history of the Novosibirsk aerogel begins in 1986.