## Slide 1: The Budker Institute of Nuclear Physics

## Slide 2: SPD magnet
Status of the SPD superconductive solenoid design development

## Slide 3
SPD yoke and solenoid
The cryostat of the magnet with the coils, cold mass and thermal shields is located inside the yoke.
Outside diameter of the cryostat is 4008 mm and a gap between the yoke and the cryostat about 20 mm. Radially a free diameter of 3468 mm is left for the SPD detectors. The length of the magnet is 4220 mm and the magnet should be installed symmetrically inside the yoke.

## Slide 4
SPD solenoid
The magnetic field along the solenoid axis should be 1.0 T.
BINP presents our participation in SPD project with the following items:
Magnetic and engineering design of the magnet including tools and support;
Production and delivery of the magnet (consisting of the cryostat with cold mass, alignment components, proximity cryogenics, supports);
Power converter, energy extraction system, quench protection and instrumentation.
Control Dewar
Cryostat
Instrumentation
Power converter
and EES
Transfer line

## Slide 5
SPD Magnet
The main characteristics of the magnet:
Magnetic field along the axis - 1.0T with uniformity ± 2%;
The current is 5200 A.
Coils: (2 pieces): Number of layers - 2; Number of turns 2x156=312.
(1 piece): Number of layers - 2; Number of turns 2x78=156
Total number of turns - 780
Conductor type: Rutherford type cable consists of 8 strands with a diameter of 1.4 mm and a Cu / NbTi ratio of one, extruded into a matrix of high purity aluminum Al996, the conductor cross-section at a temperature of 4.5K is 7.90mm in width and 10.90mm in height;
Switching box
Cryostat
Coil
Shield

## Slide 6: Cryostat: Material: St. Steel. Outer diameter is 4008 mm, Inner diameter is 3468 mm, length is 4220 mm. The thickness of the outer shell is 12 mm, the inner shell is 20 mm, the thickness of the flanges is 45 mm. The thickness at the ends of the shells is 40 mm. The weight of Cryostat is ~16.7 t
Cryostat. Thermal shield. Cold mass.
(The design of the magnet was presented at the VIII SPD Collaboration Meeting in Dubna)
Shield: Material - aluminum alloy AMg-5. Outer diameter - 3898 mm, inner diameter - 3568 mm, length - 3720 mm. Wall thickness - 4 mm, Shield weight ~1 t
Cold mass: Material - aluminum alloy AMg-5. Outer diameter -3756 mm; Inner diameter - 3662 mm; Length 3416 mm; The weight 5.4 t.

## Slide 7: Cold Mass (design)
The coil consists of 3 parts.
2 coils x 2 layers - 312 turns
1 coil x 2 layers - 156 turns
10.95 мм x 7.93 мм,
NbTi / Cu d=1.4 мм
Magnetic field - 1 T
Current - 5.2 kA
36 x M12
64 x M12
Conductor mechanical and electrical parameters.
Rutherford cable, 8 strands, extruded in Al matrix
Thickness (after cold work) at 300 K | mm | 7.93 | ± 0.03
Width (after cold work) at 300 K | mm | 10.95 | ± 0.03
Critical current (at 4.2 K, 5 T) | A | > 14690 | 
Critical current (at 4.5 K, 3 T) | A | > 16750 | 
Overall Al/Cu/sc ratio |  | 10.5/1.0/1.0 | 
Aluminum RRR (at 4.2 K, 0 T) |  | > 600 | 
Al 0.2% yield strength at 300 K | MPa | > 30 | 
Rutherford cable is used to wind the coils. The cold mass consists of three coils, The coils are fixed together using bolts. If necessary, we will use special shims between the sections of the coils.

## Slide 8
It is planned to use the thermosiphon method of cooling the superconducting coil due to the natural convection of two-phase helium.
The volume of liquid helium is 10 - 20 liters
Helium mass flow SPD - 9-10 g/sec.
Cooling Shield of Magnet
Cooling Magnet
Cooling Shield of Control Dewar
SPD solenoid. Cold mass cooling design.
Volume for liquid helium

## Slide 9
Flow Scheme Magnet-Control Dewar.
Control Dewar
Transfer line
Magnet

## Slide 10
Control Dewar with Transfer Line.
Spacer
Transfer line
Conductive
Bus Bars
Shield of TL
Pipelines
Reverse flow
Bus Bars
Insulator (СТЭФ)
Shell (Al)
The transfer line connects the vacuum volumes of the cryostat and the control Dewar.
The transfer line has an outer diameter of 219.1 mm and the length of 2240 mm. It contains the superconducting bus bars, direct and return pipes for gaseous and liquid helium flows.
The superconducting bus bars in the transfer line is cooled by a reverse flow of helium.
Shell of TL

## Slide 11
Control Dewar.
Current leads
Top and bottom Shields
Pipelines
Valves
Safety
Valves
The volume of liquid helium in the vessel is 800 litres. The maximum LHe level must be less than 594 mm from the bottom of the vessel.The minimum LHe level must be more than 230 mm.
Ø1600
2780
230
594
20%
70%
The Сontrol Dewar consists of a lower cryostat with a shield and an upper part with a volume for liquid helium, valves, pipelines and current leads.
Volume for liquid helium

## Slide 12: Position of equipment on the Platform.
Flexible Copper Connector
Diagnostic connectors
Capillaries for pressure sensors
Power converter and Energy Extraction System
Control Sensors System
Supporting Frame
Control Dewar
Platform
Current Leads
Bus Bar

## Slide 13: SPD Магнит with Control Dewar
Connection of current leads with Bas-bars coils.
The connection of the coil with the current leads is carried out in a special box located outside the cryostat. For testing the magnet, an additional length of bass bars is provided, which is removed after testing.
Switching box
Current leads
Working position
Test position
200
Part to remove

## Slide 14: SPD Magnet (fixation)
Adjustable support
The cryostat is fixed in an iron yoke by means of special adjustable supports fixed on octants .
The wedge surface of the support allows you to fix the cryostat after positioning the magnet using hydraulic jacks.
Hydraulic jack
Removable
Support

## Slide 15
To assemble the magnet, a special Stand with an I-beam - 700 GOST 26020-83, 10 meters long, with a guide rail and a roller system (Roller skate Boerkey model AM-H) for rolling up the magnet elements, is used.
The stand design is shown on the slide. 3D model of the stand is ready.
Magnet assembly Stand
Assembly Stand
Roller skate Boerkey

## Slide 16: SPD Магнит (Container)
Dimensions: length –5200 мм;
width – 4750 мм;
height – 4960 мм;
Weight : Container– 15 т
4960
4750
5520
The Container for sea transportation has been designed to deliver the Magnet to Dubna.

## Slide 17: The location of the Magnet inside the Container
Weight : - Container – 15 т
- Magnet – 24 т
Total: ~39 т
The maximum equivalent stress is 47 MPa. The maximum deformation is 0,3 mm.

## Slide 18
Drawings of the SPD Magnet

## Slide 19
Drawings of the Cryostat

## Slide 20
Drawings of the Shield

## Slide 21
Drawings of the Cold Mass

## Slide 22
Status of SPD solenoid design
• Magnetic design of the magnet, including calculations of magnetic forces. Magnetic map is ready.
• Engineering design of the magnet, including calculations of all loads and forces is ready.
• 3D model of the magnet including cryostat, cold mass, shield, suspension system is ready.
• Prototype of suspension - triangle is manufactured and tested. Selection of material for suspensions with the best characteristics is in progress.
• The procedure for assembling the magnet has been developed. 3D model of the assembly stand is ready.
• The design of the container for delivering the magnet to Dubna has been developed. The 3D model of the container is ready.
• Assembly drawings of the magnet and main assemblies are ready.

## Slide 23: Thank you for your attention!