## Slide 1
Zel I.Yu.,
Neutron tomography for structural analysis of cement materials, rocks and meteorites
S.E. Kichanov, D.P. Kozlenko, K. Nazarov, M. Kenessarin, M. Petružálek, T. Lokajíček, I. Porosnicu, P. Schnabl, P. Pruner, T.I. Ivankina, M. Balasoiu, M. Nicu, L. Ionascu, A.C. Dragolici, F. Dragolici, B. A. Abdurakhimov, A. K. Kirillov, I. K. Lapina, Y. L. Mentsin, O. Lis, E. Myrzabekova, M. Tashmetov, K. Ishbaev, K. Kosbergenov, O.G. Duliu
JINR, Frank Laboratory of Neutron Physics, Russia
State University “Dubna”, Russia
Museum of the History of Astronomy, Sternberg Astronomical Institute, Russia
Institute of Physics, Kazan Federal University, Russia
Institute of Geology of the Czech Academy of Sciences, Czech Republic
Institute of Nuclear Physics, Ministry of Energy of the Republic of Kazakhstan, Kazakhstan
“Horia Hulubei” National Institute of Physics and Engineering, Romania
National Institute for Laser, Plasma and Radiation Physics, Romania
University of Bucharest, Faculty of Physics, Romania
Institute of Nuclear Physics, Academy of Sciences of the Republic of Uzbekistan, Uzbekistan
Institute of Geology and Geophysics Named after Kh.M. Abdullaev, State Committee for Geology of the Republic of Uzbekistan, Uzbekistan

## Slide 2
Key parameters:
neutron spectra: 0,2-8 Å
neutron flux: 5.5x106 m/cm2/s
max. field of view: 20x20 cm
(optional) rotation step: 0,5о
(optional) projections number: 360
(optional) exposition: 20 s
(optional) mean meas. time: 4 h
min. voxel size: 52x52x52 µm3
spatial resolution > 140 µm
1. Neutron tomography at IBR-2
Principal scheme
First experiments in 2014
2

## Slide 3
2. Cement materials for radioactive graphite conditioning
2.1 Experimental data
Sample Composition
G1 CEM V + D2O + 50 wt% graphite
G2 CEM V + D2O + 50 wt% graphite +0.5 wt % additive (Sika ®)
G3 CEM V + D2O + 75 wt% graphite
G4 CEM V + D2O + 75 wt% graphite + 0.5 wt% additive (Sika ®)
Neutron tomography results
Neutron diffraction results
3

## Slide 4
2. Cement materials for radioactive graphite conditioning
2.2 Particle analysis
4

## Slide 5
3. Structure and anisotropy in biotite gneisses
3.1 Experimental data
OKU2
Biotite gneiss
quartz – 39,6 %
plagioclase – 36,9 %
biotite – 23,4 %
Content:
Neutron attenuation:
Pl367
quartz – 27,6 %
plagioclase – 26,4 %
biotite – 31,8 %
muscovite – 14,2 %
Biotite gneiss
Content:
Neutron attenuation:
Tomography results
5

## Slide 6
3.1 Experimental data
MFK1 Kappabridge (Agico Ltd., Brno)
OKU2
Pl367
magnetic field: 200 А/m
frequency: 976 Hz
Measured magnetic anisotropy:
Pair of transducers with 2 MHz ,
Sample diameter 49,99 mm,
Number of measurement directions – 150,
High hydrostatic pressure up to 400 MPa,
Velocity error ~ 1%.
Measurements of P-waves on spheres:
P-wave velocities at 200 MPa:
OKU2
3. Structure and anisotropy in gneisses
Pl367
Institute of Geology of the Czech Academy of Sciences
6

## Slide 7
3.2 Particle analysis
3. Structure and anisotropy in gneisses
7

## Slide 8
3.3 Anisotropy modeling
3. Structure and anisotropy in gneisses
OKU2
Pl367
OKU2
Pl367
Magnetic susceptibility anisotropy
P-wave velocity anisotropy
8

## Slide 9
4. Lamprophyre Dike
4.1 Samples description
Koytash
dikes
Lamprophyre dikes:
Rock matrix (opaque):
amphibole (30-70%)
plagioclase (70-30)%
Spheroidal inclusions:
quartz
feldspars
calcite
wrinkles
amygdules
ocelli
xenocrysts
(vesicles)
Locality:
Uzbekistan
9

## Slide 10
4. Lamprophyre Dike
4.2 Neutron tomography
x
y
z
3D models of dike samples
Dike’s wall model
position of the walls in the stereoplot
granodiorite
dike
10

## Slide 11
4. Lamprophyre Dike
4.3 Particle analysis
I max
mean
I min
I int
data
walls
Black lines contour the 95% confidence regions
Sample no. 8
Sample no. 7
Isolated gas or liquid filled vesicle undergoing simple shear flow
Estimation of magma flow direction &
conduit walls orientation
?
11

## Slide 12
5.1 Sample description
5. Kunya-Urgench chondrite
Kunya-Urgench
Dashkhowus Velayat, Turkmenistan
Fell 1998 June 20, 17:25 local time
Ordinary chondrite
Sample
Neutron diffraction (DN-12)
Major phases:
Pyroxene – Enstatite
Olivine – Fa92Fo08
Kamacite – Fe97Ni03
12

## Slide 13
5.1 Experimental data
5. Kunya-Urgench chondrite
Neutron tomography results
longitudinal slice
transverse slice
transverse slice
iron-rich phase
iron-rich phase
13

## Slide 14
5.2 Particle analysis
5. Kunya-Urgench chondrite
Kamacite spatial distribution
Kamacite particle’s principal inertia axis (min)
Kamacite particle’s principal inertia axis (max)
Foliation fabric is due to shock loading?
Friedrich, J. M. et al. (2008)
Friedrich, J. M. et al. (2017)
14

## Slide 15
Thank you !