## Slide 1: Possibilities of producing medically relevant Auger electron emitter 195mPt
Alexander S. Madumarov
Flerov Laboratory of Nuclear Reactions, JINR
60th meeting of the PAC for Nuclear Physics

## Slide 2: Radiation ‘in service’ to Nuclear medicine
Nuclear medicine
therapy
diagnostics
high LET
low LET
-alpha
-conversion
electrons
-Auger
electrons
-beta
-gamma SPECT
-positron PET
(half life 0.125 ps)
particle radiation
electromagnetic
Theranostics

## Slide 3: Auger Emitters in Medicine
High LET
(about 104-107 Grey/decay/nm3)
Available radionuclides:
67Ga, 111In, 123,125I, 99mTc, 201Tl
Taken from Web site of Department of Nuclear Physics Research School of Physics & Engineering ANU College of Physical & Mathematical Sciences

## Slide 4: Nuclear properties of 195mPt
Theranostics (personalised medicine)
Nuclide | T1/2, d | E, keV | Yield per 100 decays | Decay type | Auger electrons per decay
195mPt | 4.02 | 98.9 | 11.4 | IT | 36.6
 |  | 129.8 | 2.83 |  | 

## Slide 5: Platinum complexes
Carboplatin
Cisplatin
Oxaliplatin
Miboplatin
Pt→*Pt same efficacy, smaller toxic effect!

## Slide 6: 195mPt Production
Reactions | Cross section, <> | Specific activity (SA)
Reactor |  | 
194Pt(n,γ)195mPt | 0.09 | Max SA = 44 MBq/mg Pt
Accelerator |  | 
199Hg(γ,α)195mPt | (Max yield  1.1 GBq) | High SA  370 GBq/mg
197Au(γ,np)195mPt |  210-3 | SA  37 GBq/mg
192Os(α,n)195mPt | 3.710-3 (Max yield: 1 MBq) | No carrier added, high SA
196Pt(γ,n)195mPt 195Pt(γ, γ’)195mPt | (Yield  1 MBq/mg Pt) | Max SA  259 MBq/mg Pt
Method to produce with high specific activity and yield is needed!
Hoeschele,
1982
Dikiy,
2007
Dikiy, 2005
Qaim, 2008

## Slide 7: Photonuclear method
Reactions involved:
192Pt(,n)191Pt
196Pt(,n)195mPt
195Pt(,)195mPt
E, MeV | Radionuclide | Specific activity A, MBq/mg | Yield, kBq/(μАmgh) | Radionuclide ratio [Ym/Yx]
23 | 195mPt | 0.20 | 8.55 | 0.15
 | 191Pt | 1.30 | 57.0 | 
Irradiation parameters:
W = 0.57 kW
Ie = 12 μA
Ee = 23 MeV.

## Slide 8: Photonuclear cross sections
196Pt(γ,n)195mPt

## Slide 9: Target composition
Target: {cis-[Pt(NH3)2Cl2], KMn8O16}. m(cis-[Pt(NH3)2Cl2]) ≈ 20 mg.
m(cis-[Pt(NH3)2Cl2]):m(KMn8O16) = 1:b, where b = 1, 2, 5, 8, 10.
Szillard-Chalmers technique for specific activity elevation:
1. Cisplatinum – recoil nuclei emitter
2. Cryptomelane K2(Mn4+,Mn2+)8(0,OH)16 (KMn8O16) – recoils acceptor
3. Initial Pt compound and released atoms of Pt* show different chemical properties
Target assembly
Irradiation

## Slide 10: Radioactive platinum separation
Decantation
KMn8O16
10 ml H2O (80-90 С)
10 ml H2O (80-90 С)
cisPt
Dissolution in
1 М HCl + 1.5 % H2O2
Target cisPt+KMn8O16
Evaporation
0.5 ml 0.1 M HCl
Separation
Dowex 50Wx8
Platinum elution

## Slide 11: Isolation of Pt out of cryptomelane
Chart: Eluate, ml
| 0.5 | 1 | 1.5 | 2 | 2.5 | 3 | 3.5 | 4 | 4.5 | 5 | 5.5 | 6 | 6.5 | 7
Pt | 837.8656 | 887.75 | 2249.8154 | 1232.5784 | 182.8765 | 47.6149 | 10.7276 | 0 | 9.1264 | 11.5024 | 16.421 | 0 | 12.3526 | 0
Mn-54 | 0 | 6.6699 | 154.8408 | 419.7105 | 537.5457 | 529.3935 | 413.2876 | 332.0135 | 254.4449 | 200.8385 | 176.3822 | 115.3648 | 65.958 | 49.1597 | 26.4326 | 18.2805 | 9.6343 | 6.1264
0.1 M HCl
3 M HCl
Resin Dowex50Wx8 (200 mesh), H+
h = 4.3 cm
Ø10-11.3 cm

## Slide 12: Ratio impact on yield and SA of 195mPt

## Slide 13: Conclusions
Photonuclear approach:
Maximum yield and carrier discard are found for platinum to be 81% and 90% respectively, further improvements of the technique are being explored.

## Slide 14
Thank you for your kind attention!