## Slide 1
Bulat Bakirov1,2
1Frank Laboratory of Neutron Physics, Joint Institute for Nuclear Research
2Institute of Archaeology, Russian Academy of Sciences
Research capabilities of the Frank Laboratory of Neutron Physics in the field of materials science and cultural heritage

## Slide 3
IBR-2M high-flux pulsed reactor
240 s
3

## Slide 4
IBR-2M Spectrometers Complex
Diffractometers:
HRFD, DN-6, RTD, DN-12, FSD, SKAT, Epsilon, FSS
Small Angle Scattering Spectrometer:
YuMO
Reflectometers:
REMUR, REFLEX, GRAINS
Inelastic Neutron Scattering Spectrometers:
NERA
New Instruments:
SANSARA (in development)
INS spectrometer in inverted geometry BJN (new project)
Radiography and Tomography:
NRT
4

## Slide 5
Condensed Matter Physics and Materials Science;
Physics of Nanosystems and Nanoscale Phenomena;
Physics of Complex Liquids and Polymers;
Biophysics and Pharmacology;
Applied Materials and Engineering Sciences.
The priority research directions at the IBR-2 instruments:
5

## Slide 6
Neutrons are weakly interacting neutral particles that penetrate deep into most materials, so they can be used for non-destructive interior imaging of large objects.
The scattering or absorption of neutrons by atomic nuclei varies randomly in the periodic table. This makes neutron imaging highly complementary to X-ray imaging.
The scattering or absorption can also vary significantly between isotopes of the same chemical element. The contrast of particular materials in an image can therefore be enhanced by substituting one isotope for another.
Properties of neutrons
6

## Slide 7
Neutron tomography
Spatial resolution
I ‒ transmitted neutron intensity
I0 ‒ incident neutron intensity
x ‒ thickness
μ ‒ attenuation coefficient
L ‒ distance between input aperture and sample
D ‒ aperture diameter
7
‒ the Radon transform of the function
Conventional Reconstruction Methods:
Fourier transformation (FBP, DFR)
Solving a system of equations (SIRT, SART etc.)
AI

## Slide 8
Neutron tomography at the IBR-2 reactor
8

## Slide 9
Neutron radiography and tomography (NRT) experimental station
14th beamline
9
Neutron tomography at the IBR-2 reactor
Neutron beam flux ‒ 5.5×106 n/cm2/s
L/D ratio ‒ 200-2000
Field of view ‒ 20x20 cm2

## Slide 10
Time of flight method (TOF)
Neutron momentum (wave-particle behavior):
Velocity from experimental setup:
Thus, the neutron wavelength is:
Bragg's law:
Putting all the ratios together, we get:
1) Pulsed neutron source
2) Moderator
3) Flight path of the primary beam
4) Sample
5) Detector
6) Time analyzer
7) RW memory
10

## Slide 11
Rietveld refinement
The Rietveld method fits a calculated profile to experimental data.
It employs the non-linear least squares method.
11

## Slide 12
Parameters | DN-6 | DN-12
Neutron flux at sample position | ~3107 n/cm2/s | ~1.5106 n/cm2/s
Distance: Moderator-sample Sample-detector | 30.5 m 0.5 m | 26.0 m 0.4 m
Resolution d/d (d=2 Å) | 2=90: 0.025 | 2=90: 0.022
Exposition time per pressure point | 2-48 h | 12-36 h
Sample volume | 0.01-2 mm3 | 2 mm3
Pressure range | 50 Gpa (diamond anvils) 8 Gpa (sapphire anvils) | 8 Gpa (sapphire anvils)
DN-6 and DN-12
DN-12
DN-6

## Slide 13
Cultural Heritage Studies
Production Technology
Economic Development
Restoration and Preservation
13

## Slide 14
14

## Slide 15
Antique Bronze Coins from the Necropolis Volna-1 in Krasnodar Region
20 mm
6
2
3
4
5
1
7
8
9
Photos of coins.
‒ Necropolis Volna-1
15

## Slide 16
Neutron Diffraction Studies of Antique Copper Coins
Neutron diffraction spectra of coins and pure copper.
Tin content in coins calculated from the bias of the unit cell parameters.
16

## Slide 17
Surface Reconstruction
Bakirov, B., Saprykina, I., Kichanov, S. et al. Phase Composition and Its Spatial Distribution in Antique Copper Coins: Neutron Tomography and Diffraction Studies. J. Imaging. 2021, 7, 129.
17

## Slide 18
Roman mosaic (IV century AD)
in Constanta (Romania)

## Slide 19
10 mm
Roman mosaic
Ion, R.M., Bakirov, B.A., Kichanov, S.E. et al. Non-Destructive and Micro-Invasive Techniques for Characterizing the Ancient Roman Mosaic Fragments. Appl. Sci. 2020, 10, 3781.
19

## Slide 20
General view of the Bulgar hillfort

## Slide 21
21
Coins of Volga Bulgaria
Copper content: ~10 %
No copper phase
Copper content: ~50 %

## Slide 22
Copper phase localization
I don’t have enough silver!
Medieval king
22

## Slide 23
Ancient pottery of Kazakhstan
23
Sample photos

## Slide 24
Neutron tomography of pottery
Bakirov, B.A., Zhomartova A.Zh., Kichanov, S.E. et al. Non-Destructive Neutron Structural Studies of Ancient Ceramic Fragments of the Cultural Heritage of the Republic of Kazakhstan. J. Phys. Funct. Mater. 2022, 6(1), 56–70.
Medieval
Iron Age
Bronze Age
Bronze Age
Iron Age
Medieval
24
cm-1
0.7
0.3

## Slide 25
The required number of projections for reconstruction
Shepp-Logan phantom – a standard test image
Shepp-Logan phantom reconstructed from:
9 projections
72 projections
360 projections
The number of radiographic projections satisfying the Nyquist–Shannon theorem
25

## Slide 26
Computations were held on the basis of the HybriLIT heterogeneous computing platform (LIT, JINR).
Implementation of the convolutional neural network
Visualization of convolution and deconvolution layers.
Building blocks of the convolution neural network.
Convolution
Normalization
Activation
Input
Output
+
Skip Connection
26

## Slide 27
Implementation of the convolutional neural network
U-net
architecture
Data from 40 experiments
56000 input images
56000 target images
Training dataset
27

## Slide 28
Determination of the required number of projections
Structural similarity index measure (SSIM)
– U-net trained on 36 projections
– U-net trained on 72 projections
– U-net trained on 144 projections
– unexpected number of projections is fed to the input of U-net trained on 72 projections
28

## Slide 29
The results of training a CNN
72 + U-net
72
360
360
projections
72
72
U-net
difference
Bakirov B., Kichanov S. E., Kozlenko D. P. (2025). Convolutional neural networks for reconstruction of neutron tomography from incomplete data. Nuclear Instruments and Methods in Physics Research Section B: Beam Interactions with Materials and Atoms, 563, 165682.
29

## Slide 30
30